CHAPTER FIVE

5.0	CONCLUSION AND RECOMMENDATION

5.1	CONCLUSION

From the results obtained during this study, the following conclusion were made:

- Specimen density increased with PKOS content, rising from an average of 1 830 kg/m³ at 0% PKOS to 2 120 kg/m³ at 3.0% PKOS after 7 days, with similar trends at 14 and 28 days.

- The compressive strength of the foam concrete for the different samples after 28 days of curing for samples at 0.8 water/cement ratio varies from 3.3 N/mm2 to 4.0 N/mm2. Which falls within 5-20 N/mm2 specified for light weight concrete.

- Increasing PKOS reduced water uptake, with absorption falling from 1.88% at 0% to 1.34% at 3.0% PKOS, indicating improved pore structure and durability potential.

- Adopting a PKOS concentration of 1.5% in hybrid foam concrete for applications requiring moderate structural performance and improved durability, using a 60:40 stone dust: laterite blend improves optimal strength of foam concrete.

- The results demonstrate that PKOS enhances foam stability and densification, though excessive concentrations (3.0%) may marginally impair strength. A PKOS content of 1.5% offers the best balance between density, strength, and permeability.

5.2	RECOMMENDATION

From the result obtained and conclusions made

- Recommend that foam concretes made with PKOS and Laterite Soil at a nominal mix of 1:2 and w/c ratio of 0.8 is suitable for light weight concrete.

- Investigation into combined effects of nano-additives (e.g., silica fume, nano-silica) and fibers (synthetic or natural) alongside PKOS and LS can be used to further enhance mechanical and durability properties.

- Since sourcing for PKOS and LS is very affordable, the use of PKOS and LS should be encouraged in the making of foamed concrete.

- Further studies need to be carried out to improve the compressive strength of Foam concrete either through adding of additives or aggregates.