CHAPTER FIVE

5.0	CONCLUSION AND RECOMMENDATION

5.1	CONCLUSION

From the results obtained during this study, the following conclusion were made:

- Palm kernel oil-based surfactant (PKO-S) successfully reduces the density of hybrid foam concrete, achieving densities as low as 1828 kg/m³ (cubes) and 1717 kg/m³ (cylinders), making it suitable for lightweight construction applications.

- While PKO-S stabilizes foam effectively, the material exhibits variable compressive strength, peaking at 2.2 N/m² (cubes) and 2.1 N/m² (cylinders) before declining, highlighting the need for further material optimization to enhance long-term strength and durability.

- Adopting a PKOS concentration of 0.5% and above in hybrid foam concrete for applications requiring moderate structural performance and will improves optimal strength of foam concrete.

- The use of palm kernel oil-based surfactant (PKO-S) as a biodegradable additive in foam concrete promotes eco-friendly construction practices, supporting global sustainability goals and showcasing the potential of agro-waste utilization in building materials.

5.2	RECOMMENDATION

From the result obtained and conclusions made

- Recommend that foam concretes made with PKOS and Laterite Soil at a nominal mix of 1:2 and w/c ratio of 0.8 is suitable for light weight concrete.

- Enhance strength retention in concrete by adjusting the water-to-cement ratio and utilizing controlled curing conditions, such as steam curing

- Investigation into combined effects of nano-additives (e.g., silica fume, nano-silica) and fibers (synthetic or natural) alongside PKOS and LS can be used to further enhance mechanical and durability properties.

- Since sourcing for PKOS and Stone dust is very affordable, the use of PKOS and st should be encouraged in the making of foamed concrete.

- Further studies need to be carried out to improve the compressive strength of Foam concrete either through adding of additives or aggregates.