# 4.	RESULTS AND DISCUSSIONS

# 4.1.	Properties of Hybrid Foam Concrete

### 4.1.1	Slump Test (Workability Test)

The slump test is carried out to evaluate the consistency and workability of freshly mixed concrete. The outcomes of this test serve as a reference for quality control during the proportioning and mixing, as well as for verifying conformity with specified requirements. In this project, concrete was batched by weight, and different proportions of PKO (0%, 1%, and 1.5%) were incorporated into the mix. A nominal mix ratio of 1:1:2 was used with a water-to-cement ratio of 0.8. The corresponding test results are presented in Table 4.1.

Table 4.1.	Slump test

| PKO Surfactant, % | Water Absorption, % | Slump Value, mm |
| --- | --- | --- |
| 0 | 12 | 120 |
| 1.0 | 10 | 112 |
| 1.5 | 8 | 90 |

### 4.1.2.	Thermal Insulation Performance

The thermal insulation property test is conducted on foam concrete to determine its ability to resist heat flow, which is a critical aspect of its performance in building applications. For this project, various cured concrete ages are tested which are incorporated with 1.5% of PKO and compared with conventional concrete.

The thermal insulation test was conducted under the following environmental conditions:

- Date of Test: 22th April 2025.

- Time of Exposure: 12:00 PM to 2:00 PM

- Location: I.O.T yard, Kwara State Polytechnic, Ilorin, Nigeria.

- Weather Condition: Clear skies with direct sunlight.

- Ambient Temperature: Ranged between 38°C and 42°C during the test.

The corresponding test results for the curing ages are presented in Tab1e 4.1.2,

Table 4.1.2.	7th, 14th and 28th Days Thermal Insulation Properties

| Curing age (day) | Time (minutes) | Surface Temperature (oC) | Backside Temperature (oC) | Temperature Difference (oC) |
| --- | --- | --- | --- | --- |
|  | 0 | 27.00 | 27.00 | 0.00 |
|  | 30 | 36.70 | 28.90 | 7.80 |
| 7 | 60 | 37.20 | 29.10 | 8.10 |
|  | 90 | 40.20 | 30.50 | 9.70 |
|  | 120 | 44.10 | 34.10 | 10.00 |
|  | 0 | 27.00 | 27.00 | 0.00 |
|  | 30 | 35.70 | 29.00 | 6.70 |
| 14 | 60 | 36.20 | 29.50 | 6.70 |
|  | 90 | 38.80 | 31.20 | 7.60 |
|  | 120 | 42.00 | 33.20 | 8.80 |
|  | 0 | 27.00 | 27.00 | 0.00 |
|  | 30 | 34.70 | 28.20 | 6.50 |
| 28 | 60 | 35.40 | 28.80 | 6.60 |
|  | 90 | 38.20 | 31.10 | 7.10 |
|  | 120 | 40.50 | 32.70 | 7.80 |

The corresponding test results obtain for Thermal properties of conventional concrete is presented in Table 4.1.3.

Table 4.1.3.

| Curing age (day) | Time (minutes) | Surface Temperature (oC) | Backside Temperature (oC) | Temperature Difference (oC) |
| --- | --- | --- | --- | --- |
|  | 0 | 27.00 | 27.00 | 0.00 |
|  | 30 | 37.40 | 30.00 | 7.40 |
| 28 | 60 | 40.60 | 32.50 | 8.10 |
|  | 90 | 45.30 | 36.70 | 8.60 |
|  | 120 | 52.00 | 42.20 | 9.80 |

Thermal insulation results obtained from the practical are given in the chart at Fig. 4.1.1. The higher the day increases, the temperature value decreases.

Fig. 4.1.2.

The specimen containing foaming agent present a high thermal insulation performance. The temperature difference of hybrid foam concrete and conventional concrete is compared (Both cured for 28 days) In Fig. 4.1.2.

Fig. 4.1.2.

### 4.1.3.	Compressive Strength Test

The compressive strength test is the most common test carried out on hardened concrete, because most of the desirable characteristics properties of concrete are qualitatively related to its compressive strength. The result of this test are used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification. For this practical 150mmx150mmx150mm cube was use and the results are presented in Table 4.1.3.

Table 4.1.3.	Compressive strength of HFC cube at 7, 14 and 28days

| Curing Age (Days) | Percentage of PKO (%) | Weight (g) | Failure Load (KN) | Compressive Strength (N/mm2) | Average Compressive Strength (N/mm2) |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 6801 | 40 | 1.778 |  |
|  | 1 | 6853 | 42 | 1.867 | 1.8223 |
| 7 |  |  |  |  |  |
|  | 0.5 | 6977 | 47 | 2.089 | 2.045 |
|  | 0.5 | 6970 | 45 | 2.000 |  |
|  | 1 | 7015 | 50 | 2.222 |  |
|  | 1 | 7075 | 54 | 2.400 | 2.311 |
| 14 |  |  |  |  |  |
|  | 0.5 | 7094 | 55 | 2.444 | 2.556 |
|  | 0.5 | 7008 | 60 | 2.667 |  |
|  | 1 | 7281 | 70 | 3.111 |  |
|  | 1 | 7352 | 65 | 2.889 | 3.000 |
| 28 |  |  |  |  |  |
|  | 0.5 | 7377 | 72 | 3.200 | 3.134 |
|  | 0.5 | 7293 | 69 | 3.067 |  |