CHAPTER FOUR

4.0	RESULTS AND DISCUSSIONS

4.1	Properties of Materials

The table below shows the properties and number of materials used in this research project.

Table 4.1	Properties and Number of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Laterite Soil | 1800 |
| Cement | 1440 |
| SLS |  |
| Water/Cement | 0.8 |
| PKO | 0%, 1.5%, 3.0% of cement |

4.2	Density

The tables below show the weight of each specimen cubes in 7, 14 and 28 days

Table 4.2	Weight of Specimen Cubes in 7 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 7 | 0% | 6117 |
|  | 0% | 6227 |
|  | 1.5% | 6664 |
|  | 1.5% | 6852 |
|  | 3.0% | 7134 |
|  | 3.0% | 7183 |

Table 4.3	Weight of Specimen Cubes in 14 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 14 | 0% | 6196 |
|  | 0% | 6247 |
|  | 1.5% | 6704 |
|  | 1.5% | 7003 |
|  | 3.0% | 7212 |
|  | 3.0% | 7214 |

Table 4.4	Weight of Specimen Cubes in 28 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 28 | 0% | 6281 |
|  | 0% | 6413 |
|  | 1.5% | 6794 |
|  | 1.5% | 7042 |
|  | 3.0% | 7662 |
|  | 3.0% | 7580 |

Table 4.5	Average Weight of Specimens for 7, 14 and 28 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 7 | 0% | 6172 |
|  | 1.5% | 6758 |
|  | 3.0% | 7159 |
| 14 | 0% | 6222 |
|  | 1.5% | 6854 |
|  | 3.0% | 7213 |
| 28 | 0% | 6347 |
|  | 1.5% | 6918 |
|  | 3.0% | 7621 |

Table 4.6	Density of The Specimens

| Days | % of PKO | Average weight (g) | Density (Kg/m3) |
| --- | --- | --- | --- |
| 7 | 0% | 6172 | 1830 |
|  | 1.5% | 6758 | 2000 |
|  | 3.0% | 7159 | 2120 |
| 14 | 0% | 6222 | 1840 |
|  | 1.5% | 6854 | 2030 |
|  | 3.0% | 7213 | 2140 |
| 28 | 0% | 6347 | 1880 |
|  | 1.5% | 6918 | 2050 |
|  | 3.0% | 7621 | 2260 |

Fig 4.1: Density Chart

4.3	Compressive Strength Test

The compressive strength test is the most common test carried out on hardened concrete, because most of the desirable characteristics properties of concrete are qualitatively related to its compressive strength. The result of this test is used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification.

For this project, batching by weight was adopted and the 7th, 14th and 28th day compressive strength of foam concrete using laterite soil and palm kernel oil as surfactant, for a nominal mix ratio of 1:2 (60% Stone Dust and 40% Laterite Soil), at water/cement ratio of 0.8. The results are as shown below

Table 4.7:	Compressive strength of sample at 7, 14 and 28 days of curing.

| Days | % of PKO | Average weight (g) | Average Failure Load (KN) | Compressive Strength (N/mm2) |
| --- | --- | --- | --- | --- |
| 7 | 0% | 6172 | 70 | 3.1 |
|  | 1.5% | 6758 | 35 | 1.5 |
|  | 3.0% | 7159 | 40 | 1.8 |
| 14 | 0% | 6222 | 75 | 3.3 |
|  | 1.5% | 6854 | 45 | 2.0 |
|  | 3.0% | 7213 | 25 | 1.1 |
| 28 | 0% | 6347 | 90 | 4.0 |
|  | 1.5% | 6918 | 75 | 3.3 |
|  | 3.0% | 7621 | 75 | 3.3 |

Fig 4.2: Compressive Strength Chart

4. 4.	Water Absorption Test

Table 4.8	Water Absorption test results

| Description | Value |  |  |
| --- | --- | --- | --- |
|  | 0% | 1.5% | 3.0% |
| Weight of the Sun-dried Sample (g) | 6068 | 6024 | 5842 |
| Weight of the submerged sample after 24hrs (g) | 6182 | 6106 | 5920 |
| Water Absorption capacity | 1.88% | 1.36% | 1.34% |