CHAPTER FOUR

# RESULT AND DISCUSSION

## 4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

### Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Cement | 1440 |
| SLS | 400 |
| Water | 1000 |
| PKO | 940 |

## 4.2	Fresh Properties

### 4.2.1.	Workability

The slump test was conducted to evaluate the workability of the fresh concrete mix. The values indicate the ease with which the mix flows, measured using a standard slump cone.

| % of P.K.O. | Slump Value (mm) | Workability |
| --- | --- | --- |
| 0 | 120 | Very High Flowable |
| 1.5 | 110 | High Flowable |
| 3 | 90 | Low Flowable |

Table 4.2.	Workability of Hybrid Foam Concrete

Observation: As PKO concentration increases, slump values decrease, indicating reduced workability likely due to air entrainment and altered mix consistency. The recorded slump value shows that the lower the percentage of P.K.O the higher it flowable, with 0% give 120mm and 3% give 90mm. Which is within the range of 90mm – 120mm. Therefore, the results of the slump are a partially shear.

### 4.2.2.	Fresh Density of The Foam Concrete

Fresh density refers to the mass per unit volume of the concrete immediately after mixing, including entrained air. It was measured in kgm-³ using the weight-to-volume method.

Table 4.3.	 Fresh Density of The Foam Concrete

| Sample Id | % of P.K.O. | Mass m1 (g) |  | Volume V1 (m3) | Density P = m1/V1 (kgm-3) |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6482 6417 | 0.003375 | 1921 |  |
|  |  | 6547 |  |  |  |
| B | 1.5 | 7058 6864 | 0.003375 | 2091 |  |
|  |  | 7252 |  |  |  |
| C | 3.0 | 7424 7514 | 0.003375 | 2200 |  |
|  |  | 7333 |  |  |  |

Observation: The density increases with higher PKO concentrations, showing the effectiveness of PKO as a lightweight surfactant.

## 4.3	Dry Properties

### 4.3.1.	Water Absorption

Water absorption was measured as the percentage increase in specimen weight after 24-hour immersion. It reflects the porosity of the hardened concrete and affects durability.

Table 4.4.	Water Absorption of Hybrid Foam Concrete

| Sample ID | % of P.K.O. | Initial Dry Weight m1 (g) | Final Weight (24hrs) m2 (g) | Value of Water Absorption Wo | % of Wo |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6172 | 6310 | 0.0224 | 2.24 |
| B | 1.5 | 6758 | 6887 | 0.0191 | 1.91 |
| C | 3.0 | 7159 | 7295 | 0.0189 | 1.89 |

Formula: Water Absorption (%) = ((Wet - Dry) / Dry) × 100

Observation: Percentage of water absorption decrease with PKO, reflecting decrease in porosity. Optimal performance was observed around 1.5%–3.0% PKO concentration.

### 4.3.2.	Dry Density

Dry density was measured after 28 days of curing to assess the hardened structure of the concrete. Lower dry density indicates more entrained air and a lighter concrete.

Table 4.4.	Dry Density of Hybrid Foam Concrete

| Sample ID | % of P.K.O. | Mass m1 (g) |  | Volume V1 (m3) | Density P = m1/V1 (kgm-3) |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6117 | 6172 | 0.003375 | 1829 |
|  |  | 6227 |  |  |  |
| B | 1.5 | 6664 | 6758 | 0.003375 | 2002 |
|  |  | 6852 |  |  |  |
| C | 3.0 | 7134 | 7159 | 0.003375 | 2121 |
|  |  | 7183 |  |  |  |

Observation: Increasing PKO reduces the final density of the concrete. However, excessive reduction may compromise strength.