CHAPTER FOUR

# RESULT AND DISCUSSION

## 4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

# Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Cement | 1440 |
| SLS | 400 |
| Water | 1000 |
| PKO | 940 |

## 4.2	Fresh Properties

### 4.2.1.	Workability

The slump test was conducted to evaluate the workability of the fresh concrete mix. The values indicate the ease with which the mix flows, measured using a standard slump cone.

| % of P.K.O. | Slump Value (mm) | Workability |
| --- | --- | --- |
| 0 | 120 | Very High Flowable |
| 1.5 | 110 | High Flowable |
| 3 | 90 | Low Flowable |

Table 4.2.	Workability of Hybrid Foam Concrete

Observation: As PKO concentration increases, slump values decrease, indicating reduced workability likely due to air entrainment and altered mix consistency. The recorded slump value shows that the lower the percentage of P.K.O the higher it flowable, with 0% give 120mm and 3% give 90mm. Which is within the range of 90mm – 120mm. Therefore, the results of the slump are a partially shear.

### 4.2.2.	Fresh Density of The Foam Concrete

Fresh density refers to the mass per unit volume of the concrete immediately after mixing, including entrained air. It was measured in kgm-³ using the weight-to-volume method.

Table 4.3.	 Fresh Density of The Foam Concrete

| Sample Id | % of P.K.O. | Mass m1 (g) |  | Volume V1 (m3) | Density P = m1/V1 (kgm-3) |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6482 6417 | 0.003375 | 1921 |  |
|  |  | 6547 |  |  |  |
| B | 1.5 | 7058 6864 | 0.003375 | 2091 |  |
|  |  | 7252 |  |  |  |
| C | 3.0 | 7424 7514 | 0.003375 | 2200 |  |
|  |  | 7333 |  |  |  |

Observation: The density increases with higher PKO concentrations, showing the effectiveness of PKO as a lightweight surfactant.

## 4.3	Dry Properties

### 4.3.1.	Water Absorption

Water absorption was measured as the percentage increase in specimen weight after 24-hour immersion. It reflects the porosity of the hardened concrete and affects durability.

Table 4.4.	Water Absorption of Hybrid Foam Concrete

| Sample ID | % of P.K.O. | Initial Dry Weight m1 (g) | Final Weight (24hrs) m2 (g) | Value of Water Absorption Wo | % of Wo |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6172 | 6310 | 0.0224 | 2.24 |
| B | 1.5 | 6758 | 6887 | 0.0191 | 1.91 |
| C | 3.0 | 7159 | 7295 | 0.0189 | 1.89 |

Formula: Water Absorption (%) = ((Wet - Dry) / Dry) × 100

Observation: Percentage of water absorption decrease with PKO, reflecting decrease in porosity. Optimal performance was observed around 1.5%–3.0% PKO concentration.

### 4.3.2.	Dry Density

Dry density was measured after 28 days of curing to assess the hardened structure of the concrete. Lower dry density indicates more entrained air and a lighter concrete.

Table 4.4.	Dry Density of Hybrid Foam Concrete

| Sample ID | % of P.K.O. | Mass m1 (g) |  | Volume V1 (m3) | Density P = m1/V1 (kgm-3) |
| --- | --- | --- | --- | --- | --- |
| A | 0 | 6117 | 6172 | 0.003375 | 1829 |
|  |  | 6227 |  |  |  |
| B | 1.5 | 6664 | 6758 | 0.003375 | 2002 |
|  |  | 6852 |  |  |  |
| C | 3.0 | 7134 | 7159 | 0.003375 | 2121 |
|  |  | 7183 |  |  |  |

Observation: Increasing PKO reduces the final density of the concrete. However, excessive reduction may compromise strength.

CHAPTER FIVE

# 5.0.	CONCLUSION AND RECOMMENDATION

## 5.1.	Conclusion

This study successfully evaluated the effects of palm kernel oil surfactant (PKOS) on the water absorption and density of hybrid foam concrete. Results demonstrated that PKOS significantly influences the physical and mechanical properties of foam concrete. Specifically, as the PKO concentration increased, water absorption decreased due to reduced porosity, while dry density showed a proportional increase. The study confirms that PKOS enhances foam stability, improves workability, and contributes to the production of lightweight, durable concrete suitable for construction applications. The findings support PKOS as a sustainable alternative for improving foam concrete performance.

Beyond academic significance, this study contributes to global efforts in sustainable construction by promoting bio-based alternatives that enhance energy efficiency. Hybrid foam concrete incorporating PKOS could be particularly beneficial for thermal insulation in buildings, reducing heating and cooling energy demands. The research also aligns with the broader goal of reducing carbon footprints by integrating natural, locally available materials into construction.

## 5.2.	Recommendations

- Optimal PKOS Dosage: Based on experimental results, a PKOS concentration range of 1.5–3.0% is recommended for achieving balanced properties of strength, durability, and lightweight construction.

- Further Research: Additional studies should explore long-term durability, structural integrity, and resistance to environmental factors such as temperature variations and chemical exposure.

- Practical Applications: Field applications should be conducted to assess the real-world performance of PKOS-based foam concrete in construction, particularly for insulation, partitioning, and lightweight structural elements.

- Economic Feasibility Analysis: A comparative cost-benefit assessment should be conducted to evaluate the affordability and scalability of PKOS-enhanced foam concrete compared to conventional foaming agents.

- Comparative Analysis: Future research should compare PKOS-based foam concrete with other eco-friendly foaming agents to determine its superiority in sustainability and cost-effectiveness.

- Regulatory Considerations: Standardization efforts should be initiated to establish industry guidelines for PKOS-based foam concrete, ensuring its widespread adoption in sustainable building practices.

- Innovation in Hybrid Mixes: Researchers can explore combining PKOS with other natural surfactants or supplementary materials like recycled aggregates to further optimize foam concrete properties.