CHAPTER FOUR

4.0	RESULTS AND DISCUSSIONS

4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Sharp sand | 1400 |
| Cement | 1440 |
| SLS |  |
| Water |  |
| PKO | 1% |

4.2	Density

The tables below show the weight of each specimen cubes in 7, 14 and 28 days

Table 4.3 Weight of Specimen Cubes In 7 Days

| Days | Curing Method | % Of PKO | Weight(g) |
| --- | --- | --- | --- |
| 7 | Air | 1% | 7023 |
|  |  |  | 6560 |
|  | Water | 1% | 7101 |
|  |  |  | 7253 |
|  | Steam | 1% | 6800 |
|  |  |  | 6680 |

Table 4.4	Weight of Specimen Cubes in 14 days

| Days | Curing Method | % Of PKO | Weight(g) |
| --- | --- | --- | --- |
| 14 | Air | 1% | 7083 |
|  |  |  | 6508 |
|  | Water | 1% | 7215 |
|  |  |  | 7375 |
|  | Steam | 1% | 6640 |
|  |  |  | 6809 |

Table 4.5	Weight of Specimen Cubes in 28 days

| Days | Curing Method | % Of PKO | Weight(g) |
| --- | --- | --- | --- |
| 28 | Air | 1% | 6870 |
|  |  |  | 5995 |
|  | Water | 1% | 7377 |
|  |  |  | 6893 |
|  | Steam | 1% | 6101 |
|  |  |  | 6498 |

Table 4.5	Average Weight of Specimens for 7, 14 and 28 days

| Days | Curing Method | % of PKO | Average Weight(G) |
| --- | --- | --- | --- |
| 7 | Air | 1% | 6791 |
|  | Water |  | 7177 |
|  | Steam |  | 6740 |
| 14 | Air | 1% | 6796 |
|  | Water |  | 7295 |
|  | Steam |  | 6725 |
| 28 | Air | 1% | 6433 |
|  | Water |  | 7135 |
|  | Steam |  | 6300 |

Table 4.6	Density of The Specimens i.e Density= weight/volume of cubes

| Days | % of PKO | Average weight (g) | Density (Kg/m3) |
| --- | --- | --- | --- |
| 7 | 1% | 6791 | 2012 |
|  |  | 7177 | 2127 |
|  |  | 6740 | 1997 |
| 14 | 1% | 6796 | 2014 |
|  |  | 7295 | 2161 |
|  |  | 6725 | 1993 |
| 28 | 1% | 6433 | 1906 |
|  |  | 7135 | 2114 |
|  |  | 6300 | 1867 |

Density chart fig 4.1

4.3	Compressive Strength

Compressive strength is the capacity of a material or structure to withstand loads tending to reduce size. It is defined as the maximum compressive stress a material can bear before it fractures or deforms permanently. The result of this test is used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification.

For this project, batching by weight was adopted and the 7th, 14th and 28th day compressive strength of foam concrete using palm kernel oil as surfactant, for a nominal mix ratio of 1:2 (50% Stone Dust and 50% sharp sand), at water/cement ratio of 0. .75.The results are as shown below

Table 4.7:	Compressive strength of sample at 7, 14 and 28 days of curing.

| Days | % of PKO | Average weight (g) | Average Crushing load(KN) | Compressive strength (KN/ m2 ) |
| --- | --- | --- | --- | --- |
| 7 | 1% | 6791 | 50 | 2222 |
|  |  | 7177 | 45 | 2000 |
|  |  | 6740 | 40 | 1778 |
| 14 | 1% | 6796 | 60 | 2668 |
|  |  | 7295 | 80 | 3556 |
|  |  | 6725 | 60 | 2667 |
| 28 | 1% | 6433 | 80 | 3556 |
|  |  | 7135 | 100 | 4444 |
|  |  | 6300 | 93 | 4133 |

Compressive strength chart fig