CHAPTER FIVE

CONCLUSION AND RECOMMENDATION

The following conclusion and recommendation which are drawn includes:

- The average moisture content and water absorption of the crushed coconut shell were found to be 4.20 % and 24.00 % respectively. The CS aggregates have higher water absorption because of higher porosity in its’ shell structure.

- The aggregate impact value and aggregate crushing value of CS aggregates were much lower compared to the crushed stone aggregate, which indicates that these aggregates have good absorbance to shock.

- The specific gravity under SSD condition of CS and crushed granite was found to be 1.05 and 2.82 respectively.

The 28-day compressive strength of the concrete using coconut shell aggregate was found to be 29.3 N/mm2 under full water curing and it satisfies the requirement for structural lightweight concrete. It should, however, further investigations are required before it can be used as a building material.