CHAPTER FOUR

RESULTS AND DISCUSSIONS

4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Sawdust | 400 |
| Cement | 1440 |
| SLS |  |
| Water | 0.6 |
| PKO | 1.5% of cement |

4.2	Slump Test (Workability Test)

The slump test is carried out to evaluate the consistency and workability of freshly mixed concrete. The outcomes of this test serve as a reference for quality control during the proportioning and mixing, as well as for verifying conformity with specified requirements. In this project, concrete was batched by weight, and different proportions of PKO (1.5%) were incorporated into the mix. A nominal mix ratio of 1:2 was used with a water-to-cement ratio of 0.6. The corresponding test results are presented in Table 4.1.

Table 4.2.	Slump test

| PKO Surfactant, % | Water Absorption, % | Slump Value, mm |
| --- | --- | --- |
| 1.5 | 8 | 90 |

4.2	Density

The tables below show the weight of each specimen cubes in 7, 14 and 28 days

Table 4.2	Weight of Specimen Cubes in 7 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 7 | 1.5% | 6821 |
|  | 1.5% | 6888 |
|  | 1.5% | 6793 |

Table 4.3	Weight of Specimen Cubes in 14 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 14 | 1.5% | 7166 |
|  | 1.5% | 7046 |
|  | 1.5% | 6918 |

Table 4.4	Weight of Specimen Cubes in 28 days

| Days | % of PKO | Weight (Kg) |
| --- | --- | --- |
| 28 | 1.5% | 6562 |
|  | 1.5% | 6055 |
|  | 1.5% | 6251 |

Table 4.5	Density of The Specimens

| Days | % of PKO | Average weight (g) | Density (Kg/m3) |
| --- | --- | --- | --- |
| 7 | 1.5% | 6834 | 2024.89 |
| 14 | 1.5% | 7043 | 2086.91 |
| 28 | 1.5% | 6289 | 1863.50 |

Fig 4.1: Density Chart

4.3	Compressive Strength

The compressive strength test is the most common test carried out on hardened concrete, because most of the desirable characteristics properties of concrete are qualitatively related to its compressive strength. The result of this test is used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification.

For this project, batching by weight was adopted and the 7th, 14th and 28th day compressive strength of foam concrete using laterite soil and palm kernel oil as surfactant, for a nominal mix ratio of 1:2, at water/cement ratio of 0.6. The results are as shown below

Table 4.6:	Compressive strength of sample at 7, 14 and 28 days of curing.

| Days | % of PKO | Average weight (g) | Average Failure Load (KN) | Compressive Strength (N/mm2) |
| --- | --- | --- | --- | --- |
| 7 | 1.5% | 6834 | 47 | 1.93 |
| 14 | 1.5% | 7043 | 87 | 2.85 |
| 28 | 1.5% | 6289 | 43 | 3.77 |

Fig 4.2: Compressive Strength Chart