CHAPTER FIVE

# Conclusion

- Palm kernel oil-based surfactant (PKO-S) successfully reduces the density of hybrid foam concrete, achieving densities as low as 1828 kg/m³ cubes, making it suitable for lightweight construction applications.

- While PKO-S stabilizes foam effectively, the material exhibits variable compressive strength, peaking at 4444 KN/m2 having being the highest, highlighting the need for further material optimization to enhance long-term strength and durability.

- The curing stage plays a significant role in foam concrete production, and steam curing emerges as the most effective method, yielding greater strength compared to air or water curing.

- The use of 1% palm kernel oil significantly enhanced concrete strength, particularly with steam curing. However, the decline in strength observed in water and air-cured samples after 14 days suggests that further increasing the palm kernel oil concentration may lead to even greater strength gains, warranting further investigation

# Recommendations

- Based on the observed strength enhancements, it is recommended to explore higher concentrations of palm kernel oil beyond 1% to determine the optimal dosage for maximum strength gains in concrete, particularly with steam curing

- Conduct pilot tests in non-load-bearing applications (e.g., partition walls) to validate practical performance.

- Since sourcing for PKOS and stone dust is very affordable, the use of PKOS and stone dust should be encouraged in the making of foamed concrete.

- Further studies need to be carried out to improve the compressive strength of Foam concrete either through adding of additives or aggregates.