CHAPTER FOUR

4.0 Result and Discussions

4.1 Flexural Test Strength

4.1.1 Flexural Strength Test on Copal wood Reinforced Concrete Slab

Table 4.1 shows experimental load results of the central point flexural test on the copal wood reinforced concrete slabs. The flexural strength of the teak reinforced slabs (CRS) at 28 days strength was from 2.39 N/mm2 to 2.46 N/mm2 with increase in the percentage of teak rebar from 1% to 2%.

Table 4.1 Flexural Strength (Experimental Load) Result of Copal Wood Rebar Slab

|  |  | 1st crack load Pcr (N) | Failure load Pult (N) | Deflection at peak (mm) | Flexural Strength (N/mm2) |  |
| --- | --- | --- | --- | --- | --- | --- |
| Label |  |  |  |  |  | Mode of failure |
| 1TTTS | Minimum | 3250 | 5804 | 5.64 | 2.35 | Two number of cracks and failure is in Tension |
|  | Maximum | 4675 | 5993 | 5.62 | 2.43 |  |
|  | Mean | 3963 | 5899 | 5.63 | 2.39 |  |
| 2TTTS | Minimum | 3851 | 5663 | 6.76 | 2.62 | Two number of cracks and failure is in Tension |
|  | Maximum | 5551 | 6455 | 7.92 | 2.3 |  |
|  | Mean | 4701 | 6059 | 7.34 | 2.46 |  |

4.2 Flexural Strength on Steel Reinforced Concrete Slab

Table 4.2 shows experimental load results of the central point flexural test on the steel reinforced concrete slabs. The failure stress of the steel reinforce slabs at 28 days strength is 5.28 N/mm2

Table 4.2: Flexural Strength Test (Experimental Load) Result of Steel Reinf. Slab

| Label | 1st Crack Load | Failure Load (N/mm2 ) | Deflection at Peak (mm ) | Flexural Strength (N/mm2 ) | Mode of Failure |
| --- | --- | --- | --- | --- | --- |
| SRS | 9647 | 12863 | 4.12 | 5.28 | visible cracks and failure is in tension |

4.3 Mechanical Properties Test Results

4.3.1 Tensile Parallel to Grain

Tensile strength parallel to grain results of copal wood  are presented in Table 4.3. The studies shows that the average tensile strength of the copal wood timber parallel to the grain at the top parts of stem heartwood  is 15.79 N/mm2 with a coefficient of variation of 22.35%. The average tensile strain is 1.08% and the youngs modulus (modulus of elasticity) is 2276.17 N/mm2.

Table 4.3: Tensile Strength Test Results of  Copal wood

|  | Stress (σ) at Yield (N/mm2) | Strain (ε) at Yield (%) | Youngs Modulus (N/mm2) | Energy to Yield (N.m) |
| --- | --- | --- | --- | --- |
| Minimum | 13.29 | 0.99 | 1925.78 | 4.66 |
| Maximum | 18.28 | 1.16 | 2626.56 | 7.31 |
| Mean | 15.79 | 1.08 | 2276.17 | 5.99 |
| S.D | 3.53 | 0.12 | 495.52 | 1.87 |
| C. of V. | 22.35% | 11.11 | 21.77 | 31.22 |
| L.C.L | ± 30.98% | ±15.50% | ± 30.17% | ± 43,39% |
| U.C.L | ± 40.72% | ± 20.37% | ± 39.65% | ± 57.03% |

Source (Abdulraheem, etal., 2024)

4.3.2 Bending Strength Parallel to Grain

Bending strength parallel to grain results of copal wood are presented in Table 4.4. The studies shows that the average bending strength of the copal wood timber parallel to the grain at the top parts of stem heartwood  is 63.36 N/mm2 with a coefficient of variation of 25.66%. The average strain is 2.24% and the bending modulus (modulus of elasticity) is 6423.71 N/mm2.

Table 4.4: Bending Strength Test Results of Copal Wood

|  | Stress (σ) at Yield (N/mm2) | Strain (ε) at Yield (%) | Deflection at yield (mm) | Youngs Modulus (N/mm2) | Energy to Yield (N.m) |
| --- | --- | --- | --- | --- | --- |
| Minimum | 60.16 | 1.48 | 7.77 | 5460.85 | 8.25 |
| Maximum | 74.86 | 3.00 | 17.86 | 7386.57 | 23.55 |
| Mean | 63.36 | 2.24 | 12.82 | 6423.71 | 15.9 |
| S.D | 16.26 | 1.07 | 7.13 | 1361.69 | 10.82 |
| C. of V. | 25.66 | 47.76 | 55.61 | 21.19 | 68.05 |
| L.C.L | ± 35.57% | ± 66.50% | ± 77.16% | ± 29.38% | ± 94.30% |
| U.C.L | ± 46.76% | ± 87.40% | ± 101.41% | ± 38.61% | ± 123.94% |

Source (Abdulraheem, etal., 2024)

4.3.3 Local Modulus of Elasticity

Local MOE results of copal wood are presented in Table 4.5. The studies shows that the average local MOE in bending of the copal wood at the top parts of stem heartwood is 60.55 N/mm2 with a coefficient of variation of 19.42%. The average strain is 2.45% and the bending modulus (modulus of elasticity) is 5965.71 N/mm2.

Table 4.5: Local MOE Test Results of Copal Wood

| Local MOE |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parts |  | Stress (σ) at Yield (N/mm2) | Strain (ε) at Yield (%) | Deflection at yield (mm) | Youngs Modulus (N/mm2) | Energy to Yield (N.m) |
| Top | Minimum | 52.23 | 2.23 | 12.48 | 5060.34 | 15.71 |
|  | Maximum | 68.86 | 6.26 | 31.04 | 6871.08 | 75.20 |
|  | Mean | 60.55 | 4.25 | 21.76 | 5965.71 | 45.46 |
|  | S.D | 11.76 | 2.85 | 13.12 | 1280.39 | 42.07 |
|  | C. of V. | 19.42 | 67.05 | 60.29 | 21.46 | 92.54 |
|  | L.C.L | ± 26.92% | ± 93.04% | ± 83.59% | ± 29.75% | ± 128.26% |

Source (Abdulraheem, etal., 2024)