CHAPTER FOUR

4.0	RESULTS, OBSERVATION AND DISCUSSION

4.1	Results

Table 4.1 shows the corrosion rate in cassava fluid without inhibitor.

Table 4.2a, b, c, d, and e show the weight loss in cassava fluid in the presence of 0.05m, 0.10m, 0.20m, 0.30m and 0.40m concentration of leucine inhibitor.

Table 4.3a, b, c, d, and e show the weight loss in cassava fluid in the presence 0.05m, 0.10m, 0.20m, 0.30m and 0.40m concentration of alanine inhibitor.

Table 4.4a, b, c, d and e show the weight loss in cassava fluid in the presence 0.05m, 0.10m, 0.20m, 0.30m and 0.40m concentration of methionine inhibitor.

Figure 4.1 shows the effect of leucine inhibitor of mild steel corrosion in cassava fluid.

Figure 4.2 shows the effect alanine of inhibitor of mild steel corrosion in cassava fluid.

Figure 4.3 show the effect of methionine inhibitor of mild steel corrosion in cassava fluid.

4.2	Observation

The experimental procedures employed weight loss analysis to investigate the corrosion behavior of mild steel in cassava fluid, both in the absence and presence of various concentrations of amino acid inhibitors—specifically leucine, alanine, and methionine. The test specimens were exposed to the cassava fluid for a period of 10 days, with weight measurements taken at 2-day intervals to determine the extent of material degradation.

    - Baseline Observation (Cassava Fluid without Inhibitor): Mild steel specimens exposed to cassava fluid without any inhibitor showed a steady and significant loss in weight over the 10-day period. The corrosion rate (in mpy) was highest in the early exposure days and gradually reduced over time. This reduction is attributed to the formation of corrosion products on the steel surface, which may have partially hindered further metal dissolution.

    - Leucine as Inhibitor: The inclusion of leucine at various molar concentrations (0.05 M to 0.40 M) resulted in a noticeable reduction in corrosion rate compared to the uninhibited system. At lower concentrations (0.05 M and 0.10 M), the inhibition was moderate. The inhibition efficiency increased significantly at concentrations between 0.20 M and 0.30 M. Beyond 0.30 M (i.e., at 0.40 M), the corrosion rate did not decrease appreciably, suggesting a saturation point where additional leucine had no further protective effect.

    - Alanine as Inhibitor: Similar to leucine, alanine inhibited corrosion progressively with increasing concentration. A substantial decrease in corrosion rate was observed between 0.05 M and 0.20 M. However, beyond 0.20 M, the rate of inhibition plateaued, indicating that alanine’s adsorption on the metal surface reached its maximum effective coverage at this point.

    - Methionine as Inhibitor: Methionine displayed behavior similar to leucine: A consistent decrease in corrosion rate was recorded from 0.05 M up to 0.30 M. Beyond 0.30 M (at 0.40 M), the rate of corrosion reduction was minimal, pointing again to a saturation point in the adsorption of the inhibitor on the steel surface.

Table 4.1: Corrosion rate in Cassava Fluid Without Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 17.3562 | 17.3243 | 0.0319 | 29.0272 |
| 4 | 17.1923 | 17.1322 | 0.0601 | 27.4807 |
| 6 | 16.9033 | 16.8220 | 0.0813 | 24.6615 |
| 8 | 17.4520 | 17.3640 | 0.0880 | 20.0599 |
| 10 | 16.6254 | 16.5316 | 0.0938 | 17.0713 |

Table 4.2a: Weight Loss in Cassava Fluid in the Presence of 0.05M Concentration of Leucine Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.6470 | 16.6213 | 0.0257 | 23.3736 |
| 4 | 16.7000 | 16.6616 | 0.0384 | 17.4593 |
| 6 | 17.1098 | 17.0571 | 0.0527 | 15.9871 |
| 8 | 16.5426 | 16.4625 | 0.0801 | 18.2205 |
| 10 | 16.6948 | 16.6139 | 0.0809 | 14.6865 |

Table 4.2b: Weight Loss in Cassava Fluid in the Presence of 0.10M Concentration of Leucine Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 17.2350 | 17.2099 | 0.0251 | 22.8404 |
| 4 | 16.4080 | 16.3724 | 0.0356 | 16.2001 |
| 6 | 17.0337 | 16.9821 | 0.0516 | 15.6489 |
| 8 | 17.2542 | 17.1807 | 0.0735 | 16.7180 |
| 10 | 16.9707 | 16.8966 | 0.0741 | 13.4735 |

Table 4.2c: Weight Loss in Cassava Fluid in the Presence of 0.20M Concentration of Leucine Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.4840 | 16.4600 | 0.0240 | 21.8421 |
| 4 | 17.2650 | 17.2300 | 0.0350 | 15.9226 |
| 6 | 16.5463 | 16.4991 | 0.0472 | 14.2822 |
| 8 | 16.5009 | 16.4393 | 0.0616 | 14.0122 |
| 10 | 16.7959 | 16.7330 | 0.0629 | 11.4454 |

Table 4.2d: Weight Loss in Cassava Fluid in the Presence of 0.30M Concentration of Leucine Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.4251 | 16.4044 | 0.0207 | 18.8385 |
| 4 | 16.5578 | 16.5268 | 0.0310 | 14.1057 |
| 6 | 16.4291 | 16.3880 | 0.0411 | 12.4674 |
| 8 | 16.9341 | 16.8839 | 0.0502 | 11.4173 |
| 10 | 16.4922 | 16.4405 | 0.0517 | 9.4043 |

Table 4.2e: Weight Loss in Cassava Fluid in the Presence of 0.40M Concentration of Leucine Inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.4524 | 16.4322 | 0.0202 | 18.3791 |
| 4 | 16.4500 | 16.4200 | 0.0300 | 13.6494 |
| 6 | 17.0413 | 17.0010 | 0.0403 | 12.2251 |
| 8 | 17.0779 | 17.0284 | 0.0495 | 11.2632 |
| 10 | 16.8033 | 16.7527 | 0.0506 | 9.2094 |

Table 4.3a: Weight Loss in Cassava Fluid in the Presence 0.05M Concentration of Alanine inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.9224 | 16.8975 | 0.0248 | 22.5717 |
| 4 | 16.7619 | 16.7229 | 0.0390 | 17.7420 |
| 6 | 16.8523 | 16.7989 | 0.0534 | 16.2002 |
| 8 | 17.3310 | 17.2500 | 0.0810 | 18.4220 |
| 10 | 17.2236 | 17.1404 | 0.0832 | 15.1395 |

Table 4.3b: Weight Loss in Cassava Fluid in the Presence of 0.10M Concentration of Alanine inhibitor. Area 2rl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 17.1238 | 17.1010 | 0.0228 | 20.7520 |
| 4 | 17.2145 | 17.1782 | 0.0363 | 16.4992 |
| 6 | 17.2088 | 17.1586 | 0.0502 | 15.2233 |
| 8 | 17.0984 | 17.0317 | 0.0667 | 15.1745 |
| 10 | 16.5858 | 16.5160 | 0.0698 | 12.6827 |

Table 4.3c: Weight Loss in Cassava Fluid in the Presence of 0.20M Concentration of Alanine inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.5561 | 16.5378 | 0.0183 | 16.6375 |
| 4 | 17.1736 | 17.3477 | 0.0259 | 11.7963 |
| 6 | 17.3902 | 17.3500 | 0.0402 | 12.1929 |
| 8 | 16.6504 | 16.6022 | 0.0482 | 10.9654 |
| 10 | 17.3149 | 17.2659 | 0.0490 | 8.9196 |

Table 4.3d: Weight Loss in Cassava Fluid in the Presence of 0.30M Concentration of Alanine inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.8627 | 16.8450 | 0.0177 | 16.0911 |
| 4 | 17.3377 | 17.3127 | 0.0250 | 11.3763 |
| 6 | 16.8266 | 16.7875 | 0.0391 | 11.8616 |
| 8 | 17.3129 | 17.2650 | 0.0479 | 10.8889 |
| 10 | 16.9024 | 16.8549 | 0.0475 | 8.6447 |

Table 4.3e: Weight Loss in Cassava Fluid in the Presence of 0.40M Concentration of Alanine inhibitor. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.7419 | 16.7244 | 0.0175 | 15.9582 |
| 4 | 17.1984 | 17.1739 | 0.0245 | 11.1717 |
| 6 | 16.6326 | 16.5937 | 0.0389 | 11.8236 |
| 8 | 17.0712 | 17.0248 | 0.0464 | 10.5778 |
| 10 | 17.2010 | 17.1548 | 0.0462 | 8.4267 |

Table 4.4a: Weight Loss in Cassava Fluid in the Presence of 0.05M Concentration Inhibitor of Methionine. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.8565 | 16.8300 | 0.0265 | 24.1209 |
| 4 | 17.2865 | 17.2474 | 0.0391 | 17.7852 |
| 6 | 16.9576 | 16.8834 | 0.0742 | 22.4485 |
| 8 | 17.1519 | 17.0723 | 0.0796 | 18.0806 |
| 10 | 16.5100 | 16.4298 | 0.0802 | 14.5966 |

Table 4.4b: Weight Loss in Cassava Fluid in the Presence of 0.10M Concentration Inhibitor of Methionine. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 17.3474 | 17.3215 | 0.0259 | 23.5354 |
| 4 | 17.2916 | 17.2538 | 0.0378 | 17.1829 |
| 6 | 17.0811 | 17.0300 | 0.0511 | 15.4857 |
| 8 | 16.4869 | 16.4247 | 0.0722 | 16.4048 |
| 10 | 16.4878 | 16.4128 | 0.0750 | 13.6389 |

Table 4.4c: Weight Loss in Cassava Fluid in the Presence of 0.20M Concentration Inhibitor of Methionine. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.6221 | 16.5969 | 0.0252 | 22.9777 |
| 4 | 16.4615 | 16.4250 | 0.0365 | 16.6447 |
| 6 | 17.2271 | 17.1773 | 0.0498 | 15.1376 |
| 8 | 17.1931 | 17.1300 | 0.0631 | 14.3867 |
| 10 | 16.7105 | 16.6465 | 0.0640 | 11.6729 |

Table 4.4d: Weight Loss in Cassava Fluid in the Presence of 0.30M Concentration Inhibitor of Methionine. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 17.2808 | 17.2575 | 0.0233 | 21.2477 |
| 4 | 16.5244 | 16.4943 | 0.0301 | 13.7239 |
| 6 | 16.7904 | 16.7462 | 0.0442 | 13.4354 |
| 8 | 17.2635 | 17.2111 | 0.0524 | 11.9433 |
| 10 | 17.3900 | 17.3368 | 0.0532 | 9.7023 |

Table 4.4e: Weight Loss in Cassava Fluid in the Presence of 0.40M Concentration Inhibitor of Methionine. Area = 2πrl = 10.05cm²

| Days of Exposure | Original Weight (gm) | New Weight (gm) | Weight Loss (gm) | Mils Per Year (mpy) |
| --- | --- | --- | --- | --- |
| 2 | 16.6058 | 16.5828 | 0.0230 | 20.9401 |
| 4 | 16.7802 | 16.7500 | 0.0302 | 13.7346 |
| 6 | 16.6246 | 16.5817 | 0.0429 | 13.0637 |
| 8 | 16.6697 | 16.6188 | 0.0509 | 11.5776 |
| 10 | 16.7983 | 16.7470 | 0.0513 | 9.3376 |

Figure 4.1 Effect of Leucine Inhibitor of mild steel corrosion in Cassava fluid

Figure 4.2 Effect of Alanine Inhibitor of Mild Steel Corrosion in Cassava Fluid

Figure 4.3 Effect of Methionine Inhibitor of Mild Steel Corrosion in Cassava fluid

4.3	Discussion of Result

This research has demonstrated that the corrosion of mild steel in cassava fluid—a highly aggressive environment due to the presence of cyanic acid—can be effectively inhibited using amino acid derivatives. Through a systematic weight loss analysis over a 10-day exposure period, it was established that leucine, alanine, and methionine serve as efficient corrosion inhibitors, significantly reducing material degradation compared to uninhibited conditions.

The relationships between corrosion rate in mill per year (mpy) and duration of exposure of mild steel in cassava fluid with different concentrations of inhibitors are shown in Figures 4.1 to 4.3. Figures 4.1 and 4.3 show that leucine and methionine caused a continuous decrease in corrosion rate with increase in their molar concentration over the concentration ranges of 0.05-0.30 M. Beyond 0.30 M concentration, no appreciable decrease in corrosion rate occurred. Figure 4.2 shows that alanine caused a significant occurred. Figure 4.2 shows that alanine caused a significant decrease in corrosion rate with increase in the concentration of the inhibitor in cassava fluid over the range 0.05 to 0.20 Μ. However, above 0.20 M, no significant decrease in corrosion rate was observed. In other words, the effectiveness of the inhibitors varied with their concentrations, while each of them had a peak concentration for optimal inhibition in the cassava fluid.