CHAPTER FOUR

TESTING OF THE CREEP MEASUREMENT APPARATUS

The aim for constructing the creep measurement apparatus is to determine and show the creep time curve of an aluminium specimen for the purpose of knowing it mechanical property and how it will operate to an agreement level of performance under the condition specified for it use.

4.1 	PROCEDURES FOR OPERATING THE APPARATUS

1. 	The specimen is placed between the stirrups through a hole at the top and bottom end of the heating chamber

2. 	The dial indicator is set to zero

3. 	The thermostat is set to the elevated temperature required.

4. 	The stop watch is also set to zero.

5. 	The apparatus is plug to the power supply with the switch off.

6. 	The power supply is switch on and the test specimen loaded in tension by suspending the load from the weight hanger.

7. 	The lever arm is gently lowered until the specimen takes up the full load.

8. 	The stop watch is start.

9. 	The extension of the specimen during heating is recoded at suitable interval of time say 30 seconds.

10. 	The time for heating is taken and recorded using the timer.

11. 	The steps are repeated for another temperature value.

12. 	The extension of the specimen during heating at the same interval of time are also recorded.

4.2 	RESULTS AND DISCUSSION

The apparatus tested and the reading is tabulated as shown below.

The graph of strain against time at the two temperature was plotted and shown below.

Table 4.1 Table of extension and time at a temperature of 200°C and constant of 20N

Extension during loading = 0.30mm

| Load (N) | Extension (mm) | Time (Secs) |
| --- | --- | --- |
| 20 | 0.30 | 0.0 |
| 20 | 0.35 | 30 |
| 20 | 0.37 | 60 |
| 20 | 0.39 | 90 |
| 20 | 0.42 | 120 |
| 20 | 0.44 | 150 |
| 20 | 0.47 | 180 |

Table 4.2 Table of extension and time at a temperature of 250°C and constant load of 20N.

Extension during loading = 0.35mm

| Load (N) | Extension (mm) | Time (Secs) |
| --- | --- | --- |
| 20 | 0.35 | 0.0 |
| 20 | 0.42 | 30 |
| 20 | 0.45 | 60 |
| 20 | 0.48 | 90 |
| 20 | 0.52 | 120 |
| 20 | 0.54 | 150 |
| 20 | 0.56 | 180 |

To determine the creep rate

Creep rate = change in strainChange in time

Strain=Extension Oiginal length

And the original length of the specimen = 110mm.

Strain and creep at 200°C

At 0 sec

Stain = 0.30/110         =0.0027

Creep = 0.0027/0        = 0/ sec

At 60 sec.

Strain = 0.37/110        = 0.0033

Creep = 0.0033/60       = 0.00005/ sec.

At 90 sec

Stain = 0.39/110        =0.0035

Creep = 0.0035/90    =0.000038/sec

At 120 sec.

Strain = 0.42/110      = 0.0038

Creep  = 0.0038/120 = 0.000032 / sec.

At 150 sec.

Strain = 0.44/110       = 0.0040

Creep  = 0.0040/130 = 0.000027 / sec.

At 180 sec.

Strain = 0.47 / 110   = 0.0043

Creep = 0.0043/180 = 0.000023/ sec

Strain and creep at 250°C.

At 0 sec.

Strain = extension/ original length

Strain = 0.35/110  = 0.0032

Creep = Strain/time 0.0032/0  = 0.sec

At 30 sec.

Strain = extension/ original length

Strain = 0.42/110  = 0.0038

Creep = 0.0038/30 = 0.00013/ sec

At 60 sec.

Strain = 0.45/110  = 0.0041

Creep = 0.0041/60 = 0.000068/ sec

At 90 sec.

Strain = 0.48/110  = 0.0044

Creep = 0.0044/90 = 0.000049/ sec.

At 120 sec.

Strain = 0.52/110 = 0.0047

Creep = 0.0047/120 = 0.000039/ sec

At 150 sec.

Strain = 0.54/110      = 0.0049

Creep  = 0.0049/150 = 0.000033/ sec

At 180 sec.

Strain = 0.56/110      = 0.0051

Creep  = 0.0051/180 = 0.000028/ sec

Stress = Force/Area. Force = 20N, Area = Area of Specimen =   110 x 10 = 1100mm2, stress = 20/1100 = 1.8 MN/m2

Table 4.3 Table of Strain and Time at 2000c

| TIME (SECS) | STRAIN |
| --- | --- |
| 0.0 | 0.0027 |
| 30 | 0.0031 |
| 60 | 0.0033 |
| 90 | 0.0035 |
| 120 | 0.0038 |
| 150 | 0.0040 |
| 180 | 0.0043 |

Table 4.4 Table Strain and Time at 2500c

| TIME (SECS) | STRAIN |
| --- | --- |
| 0.0 | 0.0032 |
| 30 | 0.0038 |
| 60 | 0.0041 |
| 90 | 0.0044 |
| 120 | 0.0047 |
| 150 | 0.0049 |
| 180 | 0.0051 |