CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATION

5.1	Conclusion

The main conclusions drawn from this investigation were:

The corrosion of carbon steel in cassava fluid can be inhibited by the amino acid derivatives alanine, methionine and leucine to varying degrees of molar concentration

Alanine was observed to be ore efficient than leucine and methionine by providing corrosion inhibition at molar concentration of 0.20M, 0.30M and 0.30M respectively.

The Inhibitive power of these inhibitors increased with increase in concentration but there was a peak concentration beyond which inhibition efficiency decreased

The inhibitive power of amino-acid derivative in cassava fluid decreased in the following ranking order: alanine > leucine > and methionine.

5.2	Recommendation

Depending on the specific agro-processing conditions (pH, temperature, fluid composition), the choice of amino acid inhibitor may be optimized. For example, alanine may be preferred in environments requiring quick inhibition at lower concentrations.

Since the amino-acid used are proteinous derivatives, more inhibitors in plant-based extracts should be used in order to a good comparison.

REFERENCES

Alagbe, O. A. (2012). Corrosion Inhibition: An Overview of Principles and Practices.

Ogunniyi, D. S., et al. (2001). Corrosion of Materials in Agro-Industries.

Montagnac, J. A., Davis, C. R., & Tanumihardjo, S. A. (2009). Nutritional Value of Cassava for Use as a Staple Food and Recent Advances for Improvement. Comprehensive Reviews in Food Science and Food Safety.

Obot, I. B., & Obi-Egbedi, N. O. (2010). Adsorption and corrosion inhibitive properties of clotrimazole for aluminum corrosion in hydrochloric acid. International Journal of Electrochemical Science, 5(7), 994-1007.

Sanya, M., Raja, P. B., et al. (2014). Review on Eco-Friendly Corrosion Inhibitors Based on Organic Compounds.

Revie, R. W., & Uhlig, H. H. (2008). Corrosion and Corrosion Control: An Introduction to Corrosion Science and Engineering. John Wiley & Sons.

Onuchukwu, A. I. (1995). Corrosion of Mild Steel in Agro Fluids.

Okafor, P. C., et al. (2008). Inhibitive Action of Carica Papaya Extracts on the Corrosion of Mild Steel in Acidic Medium.

Odoemelam, S. A., et al. (2009). Corrosion Behavior of Mild Steel in Cassava Juice and its Inhibition using Extracts from Natural Sources.

Bundy, F. P., & Luedemann, H. D. (1989). Effect of High Pressure and Temperature on Corrosion Rate.

Llewelyn, D. (1958). Oxide Film Formation and Corrosion of Metals.

White, R. A. (1992). Atmospheric Corrosion of Iron and Steel.

Mardhiah, S., et al. (2014). Corrosion Behavior of Mild Steel in Different pH Media.

Fouda, A. S., et al. (2009). Corrosion Inhibition of Mild Steel Using Some Organic Compounds as Corrosion Inhibitors.

Umoren, S. A., et al. (2006). Corrosion Inhibition of Mild Steel by Gum Arabic in Alkaline Medium.

Schmuki, P., et al. (1993). Inhibition Mechanisms of Organic Substances in Metal Corrosion.

Quraishi, M. A., & Sardar, R. (2002). Amino Acids as Corrosion Inhibitors for Mild Steel in Acidic Medium.

Patel, N. S., & Jauhari, P. (2011). Inhibitive Action of Natural Amino Acids on Corrosion of Mild Steel.

Singh, A., et al. (2021). Advances in Organic Corrosion Inhibitors: Molecular Design and Electrochemical Techniques.

Khaled, K. F. (2008). New Insights into the Inhibition Mechanism of Mild Steel Corrosion by Organic Inhibitors in Neutral Solutions.

Hamadi, L., et al. (2018). Corrosion Inhibition of Steel in Acidic Media by Organic Compounds: A Review.

Ebenso, E. E., et al. (2010). Corrosion Inhibition by Eco-Friendly Organic Compounds: A Review.

McGraw-Hill. (2000). Corrosion Engineering Handbook.

Popoola, L. T., Grema, A. S., Latinwo, G. K., Gutti, B., & Balogun, A. S. (2013). Corrosion problems during oil and gas production and its mitigation. International Journal of Industrial Chemistry, 4(1), 1,15.

Verma, C., Quraishi, M. A., & Mukherjee, A. K. (2015). A review on green corrosion inhibitors for mild steel in hydrochloric acid. Journal of Materials and Environmental Science, 6(3), 775,790.

Solomon, M. M., Umoren, S. A., & Ebenso, E. E. (2018). Eco-friendly corrosion inhibitors: Adsorption and thermodynamic characteristics of amino acids on mild steel in acidic media. Journal of Molecular Liquids, 254, 72,88.

Loto, C. A. (2017). Inhibition effect of amino acids on the corrosion behavior of mild steel in acid media – A review. Cogent Engineering, 4(1), 1,17.

Rani, B. E. A., & Basu, B. B. J. (2012). Green inhibitors for corrosion protection of metals and alloys: An overview. International Journal of Corrosion, 2012.

Zhang, D. Q., Gao, L. X., & Zhou, G. D. (2004). Effect of methionine on the corrosion inhibition of mild steel in sulfuric acid solution. Materials Chemistry and Physics, 93(2-3), 217-223.

ASTM G1-03 (2011). Standard Practice for Preparing, Cleaning, and Evaluating Corrosion Test Specimens. ASTM International.