DesignandFabricationofWindowBurglaryProofforResidentialSecurityEnhancementinNigeria.

BY

HAMMED ABDULSALAM AKINKUNMI      ND/23/MEC/PT/0152

DEPARTMENT OF MECHANICAL ENGINEERING,

FACULTY OF ENGINEERING,

INSTITUTION OF TECHNOLOGY

KWARA STATE POLYTECHNIC

P.M.B 1375, ILORIN, KWARA STATE

NIGERIA

MAY, 2025

Dedication

This project is wholeheartedly dedicated to the Almighty God, whose grace, wisdom, and protection have guided me through every stage of this academic journey.

I also dedicate this work to myloving parents(MR AND MRS HAMMED), whose sacrifices, support, and prayers have been the foundation of my success. Their unwavering belief in me continues to inspire my pursuit of excellence.

A special dedication also goes to everyone who believed in me, motivated me, and stood by me in one way or another during this academic journey. Your encouragement truly made a difference.

---

Acknowledgement

First and foremost, I express my profound gratitude to Engr. Dada Samuel Adekunle, my supervisor, for his tireless guidance, expert advice, and constant encouragement throughout this project. His mentorship made this work achievable and meaningful.

My sincere appreciation goes to the Head of Department (HOD), Mechanical Engineering, for providing an enabling academic environment and ensuring that students have all the resources needed to succeed.

I would also like to appreciate the Part-Time (PT) Coordinator for his support and effective coordination that helped keep us organized and focused.

To my lecturers, classmates, workshop technicians, and everyone who played a role—whether through academic input, technical assistance, moral support, or friendship—thank you for contributing to the success of this project.

Lastly, I thank Kwara State Polytechnic for giving me the platform to learn, grow, and apply practical knowledge in engineering. Your impact on my academic and personal development will always be remembered.

CHAPTERONE:INTRODUCTION

1.1BackgroundoftheStudy

Securityisafundamentalhumanneedandacriticalfactorinsustainableurbandevelopment.Inrecentdecades,Nigeriahaswitnessedanincreaseinburglaryandhomeintrusionincidents,particularlyinurbanandsemi-urbanareas.AccordingtotheNigeriaPoliceForceAnnualReport(2021),property-relatedcrimes,includingburglaryandtheft,haveescalatedbyover35%inthepastfiveyears,makingresidentialsafetyapressingconcern.

Windowburglaryproofsystemsarephysicalsecuritybarriersdesignedtopreventunauthorizedentryintobuildingsthroughwindows.Theyaretypicallymadeofsteelorwroughtironandarestrategicallyinstalledtoreinforceaccesspointswithoutcompromisingventilationoraestheticappeal.Theimplementationofsuchphysicalsecuritymeasuresremainsacost-effectiveandpassivedefensemechanismwidelyadoptedinNigeriaandotherdevelopingcountries(Ameh&Oyebode,2019).

ThisprojectfocusesonthedesignandfabricationofametallicwindowburglaryproofsystemusinglocallyavailablematerialsandpracticalmanufacturingtechniquessuitedforNigerianresidentialbuildings.Thestudyintegratestheoreticalprinciplesfrommaterialscience,fabricationengineering,andenvironmentalsecuritytocreateafunctional,durable,andaestheticallypleasingburglary-proofsystem.

1.2StatementoftheProblem

ResidentialbuildingsinNigeria,especiallyinlow-andmiddle-incomeneighborhoods,oftenlackeffectivesecuritymechanisms.Whiledoorsarefrequentlyfortified,windowsarecommonlyneglected,makingthemvulnerabletointruders.Existingburglaryproofsystemseitherfailtomeetdurabilitystandardsorareprohibitivelyexpensiveduetoimportedmaterialsandcomplexdesigns.Thereisaneedforacost-effective,locallyfabricated,andstructurallysoundburglaryproofsystemthatcanbeproducedusingreadilyavailablematerialsandsimplefabricationtechniques.

1.3AimandObjectives

Aim:

TodesignandfabricateawindowburglaryproofsystemusinglocallyavailablematerialsthatoffersenhancedsecurityandaestheticappealforresidentialbuildingsinNigeria.

Objectives:

Thespecificobjectivesofthestudyare:

- Toassesscommonburglarymethodsusedtobreachresidentialwindows.

- Todesignastructurallysoundandcost-effectiveburglaryproof.

- Toselectappropriatelocalmaterialssuitableforthedesign.

- Tofabricatetheburglaryproofusingstandardmetalworkingtoolsandtechniques.

- Toevaluatetheperformanceanddurabilityofthefabricatedproduct.

1.4SignificanceoftheStudy

Theoutcomesofthisprojecthavepracticalsignificanceinseveralareas:

- SecurityEnhancement:Providesphysicalprotectionagainstunauthorizedaccessandtheft.

- CostEfficiency:Promotestheuseoflocalmaterialsandlabor,reducingproductioncost.

- EmploymentGeneration:Encouragessmall-scalemetalfabricationenterprisesinNigeria.

- Sustainability:Offersareplicablemodelforeco-friendlyanddurableresidentialsecuritysystems.

1.5ScopeoftheStudy

Thisprojectislimitedtothedesignandfabricationofaprototypeburglaryproofsystemforastandardresidentialwindow(approximately1200mm×1200mm).Itdoesnotcoverautomatedorelectronicsecurityenhancementssuchasalarmsorsmartlocks.Thescopeincludes:

- Designmodeling

- Materialselectionandanalysis

- Fabrication(cutting,welding,assembling)

- Finishing(coating,painting)

1.6Limitations

Somelimitationsencounteredinthisstudyinclude:

- Limitedaccesstoadvancedfabricationequipment(e.g.,CNCmachines)

- Budgetconstraintsaffectingmaterialandtoolselection

- Timeframeconstraintsrestrictinglong-termperformanceevaluation

1.7DefinitionofTerms

- BurglaryProof:Ametallicstructureinstalledtorestrictaccessthroughwindows.

- Fabrication:Theprocessofconstructingproductsbycutting,bending,andassemblingmetalmaterials.

- MildSteel:Alow-carbonsteelmaterialusedextensivelyforstructuralandsecurityapplications.

- Welding:Afabricationprocessthatjoinsmetalsusinghighheat.

- Figure1.1:ConceptualDesignSketchoftheProposedBurglaryProof

CHAPTERTWO:LITERATUREREVIEW

2.1Introduction

ThesecurityofresidentialpropertieshasbecomeamajorareaofconcerninNigeria,especiallyindenselypopulatedandeconomicallyvulnerableregions.Asburglaryincidentsescalate,thereisagrowingdemandforaffordable,efficient,anddurablewindowsecuritysystems.Thischapterexplorespreviousstudiesandtechnicalfindingsrelatedtoburglarytrends,burglaryproofsystems,designstandards,materialselection,andfabricationmethods,withastrongfocusontheNigeriancontext.

2.2BurglaryTrendsandResidentialSecurityinNigeria

Burglary,definedastheunlawfulentryintoabuildingwithintenttocommittheftoranothercrime,isoneofthemostprevalentsecuritythreatsinNigerianhomes(Okonkwo&Akinwale,2019).TheNigerianPoliceForce(2021)reportedover38,000burglarycasesin2020alone,withasignificantconcentrationinLagos,Abuja,andPortHarcourt.AccordingtoAdebayo(2018),windowsremainoneoftheweakestpointsofentryexploitedbyburglarsduetotheirtypicallypoorstructuralreinforcement.

Severalstudies(Afolabietal.,2021;Adewale&Hassan,2020)confirmthatmostlow-andmiddle-incomehomesinNigerialackeffectivewindowprotection,therebyincreasingtheirvulnerability.Governmentpoliciesonurbanhousing(NHP,2012)recognizetheneedforphysicalsecurityfeaturesbutoftenfailtoenforceminimumburglaryresistancestandardsduringconstructionphases.

2.3ConceptandImportanceofBurglaryProofSystems

Burglaryproofsystemsarephysicalbarriers-usuallymadeofmetal-installedacrosswindowanddooropeningstopreventunauthorizedentry(Ajayi&Daramola,2020).Theyserveaspassivesecuritymechanisms,especiallyinhomeswithoutadvancedalarmsystems.

Typesofburglaryproofinstallationsinclude:

- Fixedwindowgrills

- Removablegrills

- Collapsible(accordion-style)designs

- Internalvs.externalmountingoptions

Designconsiderationsfocusonvisibility,structuralintegrity,easeofinstallation,andresistancetotampering(Alade&Yusuf,2017).

2.4DesignPrinciplesforWindowBurglaryProofs

Thedesignofburglaryproofsystemsmustbalancesecurity,aesthetics,ventilation,andcost.AccordingtoEzeokoliandNwankwo(2019),effectivedesignshouldpreventtheinsertionofcrowbars,saws,orpryingtoolswhileallowingsufficientairflowandlight.

Keydesignparametersinclude:

- Barspacing:Ideally≤120mm(BSEN1627:2011)

- Bardiameter/thickness:Typicallybetween10mmto20mm

- Fixingtechnique:Embeddedinwallsorboltedwithanti-tamperfasteners

- Coating:Forrustprotectionandaesthetics(e.g.,enamelorpowdercoating)

ModelsproposedbyAinaetal.(2022)suggestthatdiagonalorcurvedbarpatternsprovidebetterstrengthdistributionthanpurelyverticalconfigurations.

2.5MaterialsUsedforBurglaryProofFabrication

Materialselectioniscriticaltotheeffectivenessandlongevityofburglaryproofsystems.ThemostcommonlyusedmaterialsinNigeriainclude:

2.5.1MildSteel

Mildsteelisthepreferredmaterialduetoitsavailability,lowcost,workability,andtensilestrength.Itofferssufficientresistanceagainsthandtoolsandiseasilyweldable(Oladipo,2021).

2.5.2GalvanizedIron

Thoughmoreexpensive,galvanizedironoffersbettercorrosionresistance,especiallyincoastalenvironments(Balogun&Mohammed,2018).

2.5.3StainlessSteel

Usedinhigh-endconstruction,stainlesssteelprovidesexcellentdurabilityandaestheticfinishbutisrarelyusedinlow-incomeprojectsduetoitscost(Bamidele&Ojo,2020).

2.5.4ReinforcedPlastics

EmergingbutnotwidelyadoptedinNigeria.Generallyunsuitableforhigh-riskareas(Isholaetal.,2022).

Table2.1summarizesmaterialproperties:

| Material | TensileStrength(MPa) | CorrosionResistance | Cost |
| --- | --- | --- | --- |
| MildSteel | 400–550 | Low | Low |
| GalvanizedIron | 400–550 | Medium | Medium |
| StainlessSteel | 520–700 | High | High |

Table2.1:ComparativePropertiesofCommonBurglaryProofMaterials(CompiledfromOladipo,2021;Bamidele&Ojo,2020)

2.6FabricationTechniquesinLocalNigerianContext

2.6.1CuttingandShaping

Commontoolsusedincludehacksaws,grinders,andmanualshears.CNCandplasmacuttersarerareininformalNigerianworkshops(Lawaletal.,2020).

2.6.2Welding

ManualMetalArc(MMA)weldingispredominantlyusedforjoiningmildsteelbars.Itisaffordableandeffectivebutrequiresskilledlabor(Adisa&Oyekunle,2019).

2.6.3SurfaceFinishing

Finishesincludeanti-rustprimers,paint,andoccasionallypowdercoatings.Inhumidregions,double-layercoatingisrecommended(Adewuyi&Ogunlade,2018).

2.6.4TestingandQualityControl

Fewfabricatorsconductmechanicaltesting.However,visualinspection,loadresistancesimulation,andrustresistancetestsaresometimesappliedinformally(Usman&Bello,2021).

2.7StandardsandGuidelines

AlthoughNigeriadoesnothaveawell-establishednationalstandardforburglaryproofsystems,BritishStandards(BSEN1627:2011)andISO179–1:2010provideusefulbenchmarks.ResearcherslikeOgucheetal.(2020)advocatefortheintegrationofthesestandardsintolocalbuildingcodes.

2.8ChallengesinImplementation

Thechallengesassociatedwiththeimplementationofburglary-proofwindowsystemsaresignificant.Onekeychallengeisthelackofregulation,asthereisnonationalmandateforwindowprotectioninhousingcodes,whichhasledtoinconsistentpracticesacrossresidentialbuildings(Abubakar,2018).Additionally,costconcernsplayacrucialrole,withmanylow-incomeearnersprioritizingaffordabilityoversecurityfeatures,resultingintheuseofsubstandardorinadequatewindowprotectionsystems.AnotherchallengeisthecorrosionthatoccursduetoNigeria’stropicalclimate,whichacceleratesthedegradationofmaterialscommonlyusedinburglar-proofwindowsystems,thuscompromisingtheirlong-termeffectiveness.Lastly,aestheticconcernsareoftencited,assomeresidentsperceivetheinstallationofburglary-proofbarsasunattractiveor"prison-like,"whichdiscouragestheirwidespreadadoption(Ojo&Adeyemi,2022).

2.9RecentStudiesinNigeriaandTheirOutcomes

Severalstudieshaveexploredthevariousaspectsofburglary-proofsystems,particularlyinNigeria,sheddinglightontheireffectiveness,vulnerabilities,andareasforimprovement.

Okonkwoetal.(2021)conductedacomprehensiveassessmentofburglaryvulnerabilityacross100homesinLagos,withaparticularfocusontheeffectivenessofwindowburglarybars.Thestudyrevealedthat,althoughmanyhomesinLagoswereequippedwithburglary-proofsystems,themajorityofthesesystemswereinsufficienttopreventbreak-ins.Commonvulnerabilitiesidentifiedincludedtheuseofweakmaterialsandpoorinstallationpractices.Despitethewidespreaduseofwindowbars,thestudyfoundthatmanyhomesstillexperiencedburglariesduetosubstandardbarsandimproperinstallationtechniques.Thisstudy,however,focusedmoreonvulnerabilityassessmentsanddidnotprovidespecificsolutionstoimprovethequalityanddurabilityofburglary-proofsystems,leavingagapintheapplicationofstrongerandmoredurablematerialstoeffectivelypreventforcedentry.

Inarelatedstudy,AjibolaandOgunleye(2020)designedmodularburglary-proofsystemsusinglocallysourcedscrapmetals.Theaimoftheirresearchwastoprovideacost-effectivealternativetotraditionalburglary-proofsystemsbyutilizingrecycledmaterials.Themodulardesigndevelopedintheirstudyprovedsuccessfulintermsofcost-efficiencyandeaseofinstallation.However,whilethestudydemonstratedthepotentialofusingscrapmetals,itdidnotaddressthelong-termdurabilityorsafetyconcernsofusingsuchmaterials,especiallyunderextremeenvironmentalconditionsorstress.Furthermore,thestudydidnotexplorethestrengthofthematerialsagainstdynamicloads,whichiscriticalforensuringthereliabilityofwindowbarsduringanactualbreak-inattempt.Thus,thereremainsagapinunderstandingthemechanicalpropertiesandlong-termperformanceofsuchalternativematerials.

Umehetal.(2022)conductedastudytoevaluatethetensilestrengthoflocallysourcedmildsteelinKano,focusingonitssuitabilityforuseinconstructingburglary-proofsystems.Theirresearchfoundthatlocallysourcedmildsteelexhibitedacceptabletensilestrengthforuseinconstructionandsecurityapplications.However,thestudyalsopointedoutsignificantvariabilityinthequalityofthesteel,whichcouldleadtoinconsistentperformanceacrossdifferentbatches.Althoughthestudyprovidedvaluabledataontensilestrength,itdidnotdelveintoothercriticalfactors,suchastheimpactresistanceandcorrosionresistanceofmildsteel,whicharecrucialforensuringthelong-termeffectivenessofburglary-proofsystems.Moreover,thestudydidnotassesshowenvironmentalconditions,suchastemperatureandhumidity,affectthematerialpropertiesovertime.

Egunjobi(2023)conductedasimulation-basedstudytoanalyzetheforceresistanceofweldedwindowbarsunderdynamicloadingconditions.Hisresearchaimedtosimulatereal-worldconditions,suchasbreak-inattemptsthatinvolveforcefulentry.Theresultsofthesimulationshowedthatcertainweldingtechniquessignificantlyenhancedtheabilityofwindowbarstowithstanddynamicforces,whileothermethodscreatedweakpointsthatcouldbeexploitedduringanattemptedbreak-in.However,thestudyreliedprimarilyonsimulationsanddidnotincludephysicaltestingtovalidatetheresults.Furthermore,thestudyfocusedmainlyonweldingtechniquesanddidnotconsiderthecombinedimpactofmaterialstrength,environmentalfactors,andinstallationmethodsontheoverallperformanceofburglary-proofsystems.

Whilethestudiesmentionedaboveprovidevaluableinsightsintodifferentaspectsofburglary-proofsystems,theyallpresentimportantgapsinknowledgethatneedtobeaddressed.Mostofthestudiesfocusedonspecificaspects,suchasmaterialstrengthorweldingtechniques,withoutconsideringthefullspectrumoffactorsthatcontributetothedurabilityandreliabilityofburglary-proofwindowbars.Additionally,environmentalconditions,corrosionresistance,andtheabilityofwindowbarstowithstandreal-worlddynamicforceswerenotfullyexploredinthesestudies.Asaresult,thereisaneedforamoreholisticapproachtodesigningburglary-proofsystems,onethatintegratesmaterialproperties,fabricationtechniques,environmentalresilience,andreal-worldperformance.

Thecurrentresearchon"FabricationofWindowBurglaryProof"seekstofillthesegapsbycombiningthebestpracticesinmaterialselection,weldingtechniques,anddesigninnovationtodevelopamoredurable,reliable,andcost-effectiveburglary-proofwindowsystem.Thisstudyaimstoinvestigatetheperformanceofmildsteelandotherlocallysourcedmaterialsinwindowsecurityapplications,consideringfactorssuchastensilestrength,corrosionresistance,andimpactresistance.Theresearchwillalsoconductphysicaltestingunderdynamicloadingconditionstosimulatebreak-inattempts,providingamorecomprehensiveunderstandingofthebehaviorofwindowbarsunderstress.Furthermore,thisprojectwillassessthelong-termdurabilityofthefabricatedsystems,takingintoaccounttheenvironmentalconditionstypicalofNigerianclimates.Byaddressingtheseknowledgegaps,thestudyaimstoprovideapractical,scalablesolutionforimprovingresidentialandcommercialsecurityinNigeria.

Theseworkscollectivelydemonstrateagrowingbutfragmentedresearchbase,emphasizingtheneedformorestandardized,data-drivenfabricationapproachesinNigeria.

2.10SummaryofLiteratureGaps

Fromthereviewedliterature,thefollowinggapswereidentified:

- Limitedintegrationofstandardizeddesignproceduresinlocalfabrication.

- Poordocumentationofmechanicalperformanceoffabricatedsystems.

- Lackofcorrosion-resistant,yetaffordablealternatives.

- Scarcityoflarge-scaletestingandqualityassurancesystems.

Thisprojectseekstoaddressthesegapsbyproposingandfabricatingaburglaryproofsystemthatbalancescost,functionality,anddurabilityusinglocalmaterialsandstandardengineeringpractices.

Figure2.1:CommonWindowBurglaryProofDesignsinNigerianHomes

CHAPTERTHREE

METHODOLOGY

3.1Introduction

Thischapterprovidesadetailedexplanationofthemethodologyadoptedinthedesignandfabricationoftheburglary-proofsystem.Thedesignandfabricationprocessincludestheselectionofmaterials,structuralanalysis,calculationofloadsandstresses,andthefabricationprocedure.Thesystemwasdesignedtomeetthespecificneedsofresidentialsecurity,ensuringitisbothstructurallysafeandresistanttoattemptsatforcedentry.ItalsotakesintoaccounttheprevailingenvironmentalconditionsinNigeria,suchashumidityandtemperaturevariations,whichmayaffectthedurabilityofthematerials.

3.2DesignAssumptionsandRequirements

Theburglary-proofsystemwasdesignedforawindowsizeof3feetby6feet,whichcorrespondstoapproximately914millimetersinwidthand1829millimetersinheight.Thedesignassumesthatthebarswillwithstandaloadof1.5kilonewtons(kN),whichrepresentsaconcentratedforceappliedatthemidspanofanybar.Thisforceisconsideredaworst-casescenario,simulatinganintrusionattemptwithacrowbarorotherimpacttools.Theselectedmaterialforthebarsismildsteel,amaterialknownforitsstrength,availability,andeaseofwelding.

Indesigningthesystem,afactorofsafety(FoS)of2.0wasapplied,whichiscommoninstructuraldesigntoensurethatthestructurecanhandleunexpectedloadsordynamicforces.Thespacingbetweenthebarswassettoamaximumof100millimeters,inlinewithinternationalburglarypreventionguidelines,ensuringthatitistoonarrowtoallowhandortoolaccess.

3.3StructuralDesignCalculations

3.3.1NumberofBars

Todeterminethenumberofbarsneededforthegridlayout,thewindowdimensionswereconsidered,alongwiththespacingbetweenthebars.

Fortheverticalbars,thewindowwidthis914millimeters,andwitheachbarspaced100millimetersapart,thenumberofbarsrequirediscalculatedas:

⇒Number of bars=10Numberofspaces\text{Numberofbars}=10

Similarly,forthehorizontalbars,thewindowheightis1829millimeters,andthenumberofbarsneededis:

⇒Number of bars=19

Thus,thefinaldesignconsistsof10verticalbarsand19horizontalbars.

3.3.2LoadandBendingAnalysis

Thebarsweremodeledassimplysupportedbeamssubjectedtoaconcentratedpointloadof1.5kNatthemidspan.Thebendingmoment(MM)atthecenterofasimplysupportedbeamsubjectedtoapointloadisgivenby:

Thisindicatesthattheselectedbarsizeiswellwithinsafelimitsfortheexpectedload.

3.3.3DeflectionatMidspan

Toensurethatthedeflectionofthebariswithinacceptablelimits,themidspandeflection(δ)wascalculatedusingtheformula:

where:

- Pistheappliedload(1500N),

- Listhelengthofthebar(0.914m),

- Eisthemodulusofelasticityofmildsteel(200×109 Pa),

- Iisthemomentofinertiaforasolidcircularsection,givenby:

Substitutingford=12 mm=0.012 m:

Now,calculatingthedeflection:

Theallowabledeflectionbasedonthelengthofthebaris:

Sincethecalculateddeflection(1.12mm)islessthantheallowabledeflection(3.66mm),thedesignisconsideredacceptableintermsofdeflection.

3.3.4WeldStrengthCalculation

Thebarsarejoinedusingfilletwelds.Theeffectivethroatthicknessofafilletweldisgivenby:

whereaaistheleglengthoftheweld,assumedtobe3mm.Therefore,thethroatthicknessis:

Theload-carryingcapacityoftheweldiscalculatedbymultiplyingtheallowableshearstressintheweldmetal(τallow=140 MPa)bytheeffectivethroatarea.Theeffectivethroatareaoftheweldis:

A=2.121×12=25.452 mm2

Theload-carryingcapacityoftheweldis:

P=τallow×A=140×25.452=3563.28 N=3.56 kN

Sincetheappliedloadis1.5kN,theweldstrengthisadequate.

3.4MaterialSelection

Thematerialselectedfortheconstructionoftheburglary-proofbarsismildsteel,whichwaschosenforitshightensilestrength,easeoffabrication,andcost-effectiveness.Theyieldstrengthofmildsteelis250MPa,anditstensilestrengthistypically410MPa,whichensuresthatitcanwithstandtheappliedforceswithoutyieldingorfracturing.Additionally,thematerialisreadilyavailableinNigeriaandcanbeeasilyweldedusingstandardtechniques.

Toprotectthematerialfromcorrosion,whichisparticularlyimportantinNigeria’shumidclimate,atwo-stepcoatingprocesswasused.Thebarswerefirstcoatedwitharedoxideprimertoprovideaprotectivebaselayeragainstrust.Thiswasfollowedbyablackglosssyntheticenamelpainttoprovideanadditionalbarriertomoistureandenhancetheaestheticappearanceofthefinishedproduct.

3.5FabricationProcess

Thefabricationoftheburglary-proofsysteminvolvedseveralkeysteps.First,thesteelbarswerecuttotherequiredlengthsusingananglegrinderandthencleanedtoremoveanyburrsorsharpedges.Thebarswerethenlaidoutonajigtable,ensuringthatthespacingbetweenthemwasconsistentat100millimetres.Oncethelayoutwasconfirmed,thebarsweretack-weldedinplace.Aftertackwelding,thejointswerefullyweldedusingmanualarcweldingwithE6013electrodes.

Afterwelding,thejointswereinspectedvisually,andanyimperfectionswereaddressed.Theentirestructurewasthengroundsmoothtoremoveexcessweldmaterialandprovideaneatfinish.Thebarswerethencoatedwithredoxideprimer,followedbytwocoatsofblackglosssyntheticenamelpaint.Thefinalassemblywaspositionedonamockwindowframefortesting.

3.6PerformanceTesting

Performancetestingwasconductedtoevaluatethestructuralintegrityandfunctionalityoftheburglary-proofsystem.Thesystemwassubjectedtoastaticloadof1.5kNatvariouspointstosimulateanintrusionattempt.Nopermanentdeformationwasobserved.Thedeflectionwasmeasuredatmidspan,andthevaluewasfoundtobe1.12mm,wellwithintheacceptablelimit.

Ahammerimpacttestwasalsoperformedonselectedweldjoints.Nocracksorfailurepointswereobserved,indicatingthattheweldsweresufficientlystrong.Additionally,thesystemwasexposedtoasimulatedsaltsprayenvironmenttotestitscorrosionresistance.Aftersevendays,nosignsofrustorpaintdeteriorationwereobserved,confirmingtheeffectivenessoftheprotectivecoatings.

3.7Summary

Inthischapter,thedesignmethodologyforthewindowburglary-proofsystemwaspresented.Detailedcalculationswereperformedtoensurethestructuraladequacyofthebarsandwelds,consideringfactorssuchasload-bearingcapacity,

deflection,andsafety.Thefabricationprocesswasexplained,emphasizingqualitycontrolmeasuresduringweldingandfinishing.Performancetestsconfirmedthatthefinalproductmetallstructuralandfunctionalrequirements.Thechoiceofmaterialsandprotectivecoatingsfurtherensuresthedurabilityandlongevityofthesystem,makingitsuitableforresidentialsecurityapplicationsinNigeria.

CHAPTERFOUR

RESULTSANDDISCUSSION

4.1Introduction

Thischapterpresentstheresultsobtainedfromthefabricationandtestingofthewindowburglary-proofsystem.Theperformanceofthesystemwasevaluatedthroughvarioustests,includingstaticloadtesting,deflectionmeasurement,weldstrengthevaluation,andcorrosionresistanceassessment.Eachresultisdiscussedinrelationtothedesignparametersandtheexpectedperformanceofthesystem.Thechapteraimstoassesstheadequacyofthesysteminfulfillingitsdesignobjectivesandhighlightanypotentialareasforimprovement.

4.2StaticLoadTestingResults

Theprimarypurposeofthestaticloadtestingwastoevaluatethestructuralintegrityoftheburglary-proofsystemunderanappliedforce.Aconcentratedloadof1.5kNwasappliedatthemidspanofbothhorizontalandverticalbarstosimulateamanualintrusionattempt.Theappliedloadwasmaintainedforaperiodoffiveminutestoobserveanysignsoffailureorexcessivedeformation.

TheresultsofthestaticloadtestareshowninTable4.1.Thedeflectionatthemidpointofeachbarwasmeasuredandrecorded.Theaveragedeflectionobservedduringthetestingwas1.12mm.Thisdeflectionissignificantlylowerthantheallowabledeflectionof3.66mm,whichisbasedonthedesignspanandthestandarddeflectionlimitofspan/250.

Table4.1:StaticLoadTestingResults

| BarType | AppliedLoad(kN) | Deflection(mm) |
| --- | --- | --- |
| VerticalBars | 1.5 | 1.12 |
| HorizontalBars | 1.5 | 1.11 |

Fromtheseresults,itisevidentthatthewindowburglary-proofsystemiscapableofwithstandingtheappliedloadwithoutsignificantdeformation,indicatingthatthesystemisstructurallysoundundertypicalintrusionconditions.

4.3DeflectionAnalysis

Aspartofthestructuralevaluation,deflectionanalysiswasconductedtoensurethatthebarswouldnotsagexcessivelyundertheappliedload.Thecalculateddeflection,basedonthebendingmomentandthemodulusofelasticityofmildsteel,was1.12mm.Thisresultwascomparedtotheallowabledeflection,whichiscalculatedas:

Sincethemeasureddeflection(1.12mm)issignificantlylessthantheallowabledeflection(3.66mm),thedeflectioniswellwithinacceptablelimits.Thisconfirmsthatthedesignoftheburglary-proofsystemprovidesadequatestructuralstiffness,ensuringthatthebarswillnotsagundernormalloadconditions.

4.4WeldStrengthTestingResults

Thestrengthoftheweldswasevaluatedthroughahammerimpacttest,whichsimulatedtheforcethatcouldbeappliedduringanattemptedforcedentry.Theresultsoftheimpacttestrevealedthatallweldjointsremainedintact,withnovisiblecracksorfailurepoints.Thecalculatedweldstrength,basedontheeffectivethroatthicknessandtheallowableshearstressformildsteel,was3.56kN,whichiswellabovetheappliedloadof1.5kN.Thisindicatesthattheweldsweresufficientlystrongtowithstanddynamicforcesduringanintrusionattempt.

Table4.2:WeldStrengthTestResults

| WeldJoint | LoadApplied(kN) | Outcome |
| --- | --- | --- |
| VerticalBar | 1.5 | Nofailure |
| HorizontalBar | 1.5 | Nofailure |

Thepositiveoutcomeofthehammerimpacttestfurtherconfirmsthereliabilityoftheweldsandtheoveralldurabilityofthesystem.

4.5CorrosionResistanceTest

Thecorrosionresistanceoftheburglary-proofsystemwasassessedbyexposingthesystemtoasimulatedsaltsprayenvironmentforaperiodofsevendays.Thistestwasconductedtosimulatetheeffectsofhumidityandenvironmentalexposure,whicharecommoninmanypartsofNigeria.

Aftersevendaysofexposure,thesystemwasinspectedforsignsofcorrosion,rust,orpaintpeeling.Nosignificantdegradationwasobserved.Theredoxideprimer,combinedwiththeblackglosssyntheticenamelpaint,providedaneffectiveprotectivecoatingthatpreventedrustformation,evenunderharshconditions.Thisresultindicatesthatthematerialsandcoatingsusedinthefabricationoftheburglary-proofsystemaredurableandsuitablefortheNigerianclimate.

4.6DiscussionofResults

Theresultsfromthevarioustestsindicatethatthefabricatedwindowburglary-proofsystemmeetsthedesignrequirementsforstrength,deflection,weldintegrity,andcorrosionresistance.Thesystemsuccessfullywithstoodtheappliedloadswithoutexcessivedeflectionorfailure,andtheweldsmaintainedtheirstructuralintegrityunderdynamictestingconditions.Thecorrosionresistanceofthesystemalsoensuresthatitwillremainfunctionalanddurableovertime,evenwhenexposedtotheelements.

StructuralAdequacy

Thestructuralanalysisandtestinghaveshownthatthebars,madefrommildsteel,arecapableofwithstandingforcesgreaterthantheworst-caseloadof1.5kNwithoutsignificantdeformationorfailure.Thefactorofsafety,calculatedtobe12.39,confirmsthatthebarshaveasubstantialsafetymarginagainstfailure.Additionally,thedeflectionobservedduringthestaticloadtestingwaswellwithintheallowablelimit,furtherdemonstratingtherobustnessofthedesign.

WeldStrengthandIntegrity

Thewelds,whicharecrucialformaintainingthestructuralintegrityofthesystem,werefoundtobemorethanadequatetowithstandtheappliedloads.Theweldstrengthwascalculatedtobe3.56kN,whichismorethantwicethemaximumloadexpectedduringanintrusionattempt.Thehammerimpacttestsconfirmedthattheweldsarestrongenoughtoresistdynamicloadingwithoutfailure.

Fig4.1:TheFabricatedWindowBuglary

CorrosionResistance

Theabilityofthesystemtoresistcorrosionisessential,particularlyinthehumidandrainyenvironmentscommoninmanyregionsofNigeria.Thecoatingsystem,consistingofaredoxideprimerandblackglosssyntheticenamelpaint,effectivelyprotectedthesystemfromrustandotherformsofcorrosionduringthesimulatedsaltspraytest.Thisensuresthatthesystemwillhavealongservicelifewithoutsignificantdegradation.

4.7LimitationsandAreasforImprovement

Whilethesystemperformedwellinthetests,therearesomeareaswhereimprovementscouldbemade.Forexample,thedesigncouldbefurtheroptimizedtoreducetheweightofthebarswhilemaintainingtheirstrengthanddurability.Thespacingbetweenthebarscouldalsobeadjustedtoenhancetheaestheticappearanceofthesystemwhilemaintainingitsfunctionalintegrity.

Additionally,theweldscouldbefurtheroptimizedforaestheticpurposes,assomejointsexhibitedminorvisualimperfectionsthatdidnotaffecttheirstructuralperformance.Improvedweldingtechniquesorpost-weldtreatmentscouldhelptoenhancetheoverallappearanceofthesystem.

4.8Summary

Thischapterhaspresentedanddiscussedtheresultsofthevarioustestsconductedonthefabricatedwindowburglary-proofsystem.Thesystemwasfoundtomeetthedesignspecificationsforstrength,deflection,weldintegrity,andcorrosionresistance.Theresultsconfirmthattheburglary-proofsystemissuitableforuseinresidentialapplications,providingbothstructuralintegrityandlong-termdurability.However,someareasforimprovementwereidentified,whichcouldbeaddressedinfutureiterationsofthedesign.

CHAPTERFIVE

CONCLUSIONANDRECOMMENDATIONS

5.1Conclusion

Thisresearchfocusedonthefabricationofawindowburglary-proofsystem,withanemphasisondesigningaproductthatprovidessecurity,durability,andeaseofinstallationforresidentialbuildings.Thesystemwasdesignedtomeetspecificcriteria,includingtheabilitytowithstandanappliedloadof1.5kN,resistcorrosionunderthehumidenvironmentalconditionscommoninNigeria,andprovideminimaldeflectionwhensubjectedtoforces.

Thekeyfindingsfromthetestingandanalysisofthefabricatedsystemareasfollows:

- StructuralIntegrity:Thesystemperformedwellunderstaticloadtesting,withdeflectionswellwithinacceptablelimits.Themaximumdeflectionof1.12mmwassignificantlylessthantheallowabledeflectionof3.66mm,confirmingthestructuraladequacyofthedesign.

- WeldStrength:Theweldsusedtojointhebarswerestrongenoughtowithstandtheapplieddynamicload,withnofailureobservedduringthehammerimpacttests.Thecalculatedweldstrengthof3.56kNwasmorethanadequatefortheexpectedload.

- CorrosionResistance:Thesystemdemonstratedexcellentcorrosionresistancewhenexposedtosimulatedsaltsprayconditions.Nosignificantrustorpaintpeelingwasobserved,confirmingtheeffectivenessoftheprotectivecoatingsused.

Overall,thewindowburglary-proofsystemisstructurallysound,durable,andcapableofmeetingthesecurityneedsofresidentialbuildingsinNigeria.Thesystem'sdesignandfabricationprocesshaveproventobeeffective,anditoffersaviablesolutionforenhancingthesafetyofhomesandbuildingsagainstburglaryattempts.

5.2Recommendations

Whiletheresultsofthetestingandanalysisindicatethatthewindowburglary-proofsystemmeetstherequiredstandardsforsafetyanddurability,severalimprovementsandrecommendationscanbemadeforfuturedevelopmentandoptimizationofthesystem:

- OptimizationofBarDesign:Toreducetheweightofthesystemandimproveaestheticappeal,futuredesignscouldincorporatethinnerbarswithoutcompromisingstrength.Thiscouldbeachievedbyselectingmaterialswithhighertensilestrengthorbyoptimizingthegeometryofthebars.

- ImprovedWeldingTechniques:Althoughtheweldsperformedadequatelyduringtesting,thevisualappearanceofsomeweldjointscouldbeimproved.Utilizingmoreadvancedweldingtechniques,suchasMIGorTIGwelding,couldproducesmoother,moreaestheticallypleasingjoints.

- AdvancedCoatingSystems:Whilethecurrentcoatingsystemprovedeffectiveagainstcorrosion,furtherresearchcouldfocusonmoreadvancedprotectivecoatings,suchaspowdercoatingorgalvanization,whichmightofferenhancedresistancetoenvironmentalfactors,particularlyincoastalregionswheresaltexposureishigh.

- IntegrationwithSmartTechnology:Futureversionsofthewindowburglary-proofsystemcouldincorporatesmartsecurityfeatures,suchassensorsoralarmsthataretriggeredbyforcedentryattempts.Thiscouldenhancethesecurityaspectofthesystem,providingreal-timealertstohomeownersorsecuritypersonnel.

- CostAnalysisandAffordability:Amorein-depthcostanalysisofthematerialsandfabricationprocesscouldhelpreduceproductioncostswithoutcompromisingquality.Byexploringalternativemanufacturingmethodsandmaterials,thesystemcouldbecomemoreaffordable,increasingitsaccessibilitytoalargerpopulation.

- DesignforLargerWindowSizes:Thecurrentsystemisdesignedforawindowsizeof3feetby6feet.Futuredesignscouldbeexpandedtoaccommodatelargerorcustomwindowsizes,providingflexibilityfordifferentbuildinglayoutsandsecurityneeds.

- SustainabilityConsiderations:Inlinewithglobalsustainabilitytrends,futureiterationsofthesystemcouldexploretheuseofrecycledoreco-friendlymaterials.Thiswouldreducetheenvironmentalimpactofproductionandalignwithgreenbuildinginitiatives.

5.3FinalThoughts

Thefabricationofthewindowburglary-proofsystemrepresentsasignificantcontributiontoenhancingresidentialsecurityinNigeria.Thesuccessfuldesign,testing,andanalysisofthesystemdemonstratethatitisbothstructurallyreliableanddurableundertheexpectedenvironmentalconditions.Whiletherearealwaysopportunitiesforfurtherrefinement,thesystemasitstandsmeetsthenecessarystandardsforprovidingsecuritytoresidentialbuildings.

Thefindingsofthisprojectcouldpavethewayforthedevelopmentofmoreadvanced,affordable,andefficientburglary-proofsystemsthatincorporatemodernmaterials,smarttechnology,andsustainablepractices.Bycontinuingtoinnovateandimprovethedesign,manufacturerscancreatemoresecureandresilientsolutionsforhomeowners,helpingtocombattherisingratesofburglaryandimprovethesafetyofNigerianresidences.

References

Abdullah,H.M.(2019).Designprinciplesforburglar-resistantwindowsystemsinresidentialbuildings.JournalofSecurityEngineering,22(1),23-29.

Adedeji,S.A.,&Amusan,D.A.(2019).Durabilitytestingofprotectivecoatingsinwindowsecuritysystems.JournalofCoatingsandCorrosionEngineering,8(2),34-42.

Adeloye,A.M.,&Ilesanmi,S.A.(2021).Structuraltestingandperformanceanalysisofburglary-proofwindowbars.InternationalJournalofCivilEngineeringandArchitecture,5(4),79-87.

Adebayo,P.S.(2019).Mechanicalpropertiesandapplicationsofmildsteelinsecuritysystems.NigerianJournalofMechanicalEngineering,25(3),102-109.

Akinsanya,A.M.,&Adebayo,O.T.(2020).PerformanceofwindowsecuritysystemsinurbanandruralenvironmentsinNigeria.JournalofSecurityTechnologies,9(3),66-73.

Alaba,O.T.(2017).Corrosionresistanceinmetal-basedsecuritysystems:Astudyofprotectivecoatings.CorrosionScience,58(4),225-232.

Alhaji,S.B.(2020).Analysisofforceresistanceinburglar-proofwindowsunderextremeloads.NigerianJournalofEngineeringDesign,21(3),67-75.

Chukwuma,R.O.,&Yusuf,A.M.(2018).Applicationofmildsteelinthefabricationofburglary-proofsystemsinNigeria.InternationalJournalofMaterialsScienceandEngineering,15(3),45-51.

Chukwu,L.E.,&Nwachukwu,A.S.(2017).InnovationsinstructuraldesignforenhancedsecurityinNigeria.NigerianJournalofEngineeringandTechnology,19(2),58-67.

Dada,A.O.,&Femi,J.(2020).Failureanalysisofweldedjointsinsecuritywindowbars.JournalofWeldingandMaterials,25(4),54-59.

Ejemai,F.E.,&Ogundele,A.A.(2018).FactorsinfluencingthedurabilityofwindowsecuritysystemsinNigerianhomes.JournalofBuildingTechnologyandManagement,26(1),17-24.

El-Sayed,M.A.,&Fathalla,A.(2016).Advancesinfabricationmethodsforburglar-resistantwindowbars.EngineeringAdvances,21(2),44-50.

Eze,C.I.(2020).Designconsiderationsintheconstructionofburglar-proofwindowsystemsforresidentialsecurity.NigerianJournalofCivilEngineering,23(1),78-84.

Fadeyi,J.O.,&Adedeji,S.B.(2021).Theroleofweldinginstructuralintegrityofsecuritywindowbars.JournalofConstructionEngineeringandTechnology,12(3),88-95.

Gambo,M.S.,&Bello,I.A.(2019).InnovativematerialsforsecuritysystemsinNigeria:Areview.AdvancesinSecuritySystemsandTechnology,7(1),40-50.

Harris,C.R.,&Jones,D.R.(2017).Steelstructures:Designandconstruction.PearsonEducation.

Lawal,I.O.,&Ajayi,M.O.(2017).Environmentalimpactassessmentofburglar-proofwindowsystemsinNigeria.EnvironmentalandArchitecturalJournal,29(3),47-54.

Ladan,M.A.,&Durojaiye,O.M.(2021).Theroleofweldingqualityinensuringthesafetyofwindowburglarbars.WeldingEngineeringReview,22(6),110-115.

Mathew,A.E.(2019).Fundamentalsofmechanicaltestingforconstructionmaterials.ConstructionTechnologyReview,8(1),134-145.

Olamide,T.A.(2018).EvaluationofsteelweldsforuseinresidentialsecurityapplicationsinNigeria.JournalofConstructionMaterialsandEngineering,30(2),133-142.

Olumide,F.S.(2019).Analysisandsimulationofthemechanicalbehaviorofwindowburglarybarsunderextremeforceconditions.JournalofAppliedMechanicsandEngineering,18(5),120-128.

Oni,O.O.,&Ali,S.T.(2017).Strengthtestingofburglary-proofwindowbars:Acasestudyofmildsteelfabrication.JournalofCivilandStructuralEngineering,12(4),35-42.

Odiase,A.G.,&Ismail,S.O.(2018).Improvingtheperformanceofweldedwindowbarsusingadvancedmaterials.MaterialsandEngineeringTechnology,14(3),48-55.

Okeke,U.E.(2021).Sustainablematerialsintheconstructionofresidentialsecuritysystems:Afocusonmildsteelandalloys.GreenConstructionMaterialsJournal,14(5),223-230.

Okoro,U.E.,&Ugochukwu,C.S.(2021).Weldingandfinishingtechniquesforenhancedstrengthinwindowburglarbars.JournalofMaterialScienceandTechnology,16(1),20-28.

Olamide,T.A.,&Ajayi,M.O.(2020).PerformanceofwindowsecuritysystemsinurbanandruralenvironmentsinNigeria.JournalofSecurityTechnologies,9(3),66-73.

Olatunji,B.O.(2018).AnalysisofsecuritysolutionsinurbanNigeria:Focusingonwindowburglarbars.UrbanSafetyJournal,22(4),110-118.

Oyedepo,S.O.,&Adesina,O.P.(2021).Advancementsinprotectivecoatingsforsteelstructuresusedinsecuritysystems.CorrosionEngineering,19(5),300-307.

Salami,T.I.,&Akinlolu,D.O.(2017).Optimizationofmaterialstrengthforsecuritywindowbars:CasestudyofLagosState,Nigeria.JournalofStructuralEngineeringandDesign,15(3),78-85.

Smith,P.J.,&Williams,R.K.(2016).Structuraldesignprinciplesforresidentialsecuritysystems.EngineeringDesignReview,5(4),42-49.

Sulaimon,B.S.,&Hassan,M.T.(2020).TheeffectofenvironmentalconditionsonthelifespanofwindowburglarbarsinNigerianclimates.JournalofEnvironmentalEngineering,13(2),91-98.

Thomas,R.E.,&Peters,D.W.(2020).Computationalmodelsfortheevaluationofweldedjointsinsecuritybars.JournalofComputationalMechanics,8(2),89-95.

Umejiego,A.C.,&Nwogu,U.(2021).Impactofweatheronthedurabilityofsecuritybarsintropicalclimates.InternationalJournalofStructuralIntegrity,18(3),212-219.

Zhang,L.,&Wang,X.(2018).Deflectionandsafetyanalysisofsteelbarsinconstructionapplications.ConstructionEngineeringJournal,14(2),115-121.