KWARA STATE POLYTECHNIC, ILORIN

INSTITUTE OF TECHNOLOGY

DEPARTMENT OF CIVIL ENGINEERING TECHNOLOGY

ON

INVESTIGATION ON THE DURABILITY OF HYBRID FOAM CONCRETE USING PALM KERNEL OIL SURFACTANT UNDER DIFFERENT CURING CONDITION.

PREPARE BY

HAMMED HABIBULLAHI TAIYE

HND/23/CEC/FT/0285

SUPERVISED BY

ENGR. R. O. SANNI

CHAPTER ONE

# Introduction

## Background of study

With the development of society and the increase of population, the problem of energy shortage has become increasingly prominent, and countries all over the world have attached great importance to energy conservation and environmental protection in the construction industry(Huang et al 2013)The Chinese government proposed the development of “applicable, economical and green buildings” in the “13th Five-Year Plan” ( fan et al 2019)As an important part of the building, the design of the enclosure structure is closely related to the building energy consumption (liu et al. 2014). In recent years, with the continuous enhancement of China’s scientific research and economic strength, relevant functional departments have put forward higher requirements on building environmental protection, and have successively introduced various policies and measures. With the strong support of these favorable policies, reforms in the construction sector have been deepened, and significant progress has been made in the research of building energy-saving technologies and building energy-saving materials (Chang et al 2016) From the chemical composition, building insulation materials can be divided into organic materials (Silvestre et al 2016). inorganic materials (wang et al 2020)and organic-inorganic composite materials(Yang et al 2018) In China’s building materials market, organic building materials such as polystyrene foam and polyurethane foam are common(Hou et al 2016, He 2017)Compared with inorganic materials, organic materials have the advantages of light weight and low thermal conductivity, which made them favored by the market. Apart from the above advantages, the problems of low ignition point and easy aging of organic building materials can’t be ignored (Vuong at al 2016). On the morning of March 9, 2021, an indoor fire in the Zhongxin Building in Shijiazhuang City, Hebei Province caused serious casualties and property losses because the fire spread to the insulation layer of the building’s external walls. The intensification of fires caused by the inflammable insulation of the exterior wall of buildings such as this occurs many times a year, seriously endangering national health and economic construction. In order to reduce the fire threat caused by organic building materials, the Ministry of Housing and Urban-Rural Development of the People’s Republic of China has issued a series of announcements to limit the excessive use of organic building materials (Xiao and Ding 2013). Therefore, inorganic materials represented by foamed concrete have gradually become a research hotspot in the field of building materials (Yang et 2021).

Foamed concrete is a kind of lightweight and porous concrete that receives considerable attention from builders worldwide. The irregular voids inside are derived from the foaming agent mixture in the mortar (Amran et al 2015).The urgent need for energy-saving and environmentally-friendly building technology has promoted the rapid promotion of foam concrete. Pure cement mixed with fine sand is commonly used for preparing foamed concrete with light weight and uniformly distributed discrete bubbles (Rammamuty et al 2009). In different countries such as the United Kingdom, Germany, Turkey, the Philippines and Thailand, foam concrete has become a common material required for construction (mydin and wang 2011). In history, the Romans first realized that by adding blood to a mixture of small gravel, coarse sand and hot lime and stirring it with water, the resulting block containing small bubbles was more durable and practical (hill 2013) In 1923, Axel Eriksson was granted a patent for Portland cement-based foam concrete (valore 1954). After that, major improvements in production equipment and better superplasticizer and foaming agents have allowed foamed concrete to be used on a large scale, and a lot of efforts have been made to comprehensively study the characteristics and behavior of foamed concrete to simplify its usage in building structure application. Foamed concrete can be prepared by two techniques, which are called pre-foaming method and hybrid foaming method. For the former, it is necessary to prepare stable foam with the help of an air compressor, and then mix it with the basic mixture (consisting of cement, sand and water). For the latter, the foaming agent solution is mixed with the base mixture in a high-speed mixer. Since Davidovits introduced geopolymers, the concept of cement-free concrete has been formally put forward (liu et al 2016). The concrete can be prepared by a reaction between an alkaline solution and a raw material rich in silica and alumina, followed by curing and drying (hadjito et al 2004)The use of geopolymers to replace the ordinary Portland cement (OPC) to make concrete not only significantly reduces the CO2 emissions of the cement industry, but also realizes the reuse of industrial waste residues such as fly ash. In addition, geopolymer concrete also exhibits lower absorptivity than OPC concrete. As a relatively new material, the preparation process, proportion of doped components and material properties of foamed concrete are yet to be studied.

## 1.1 Problem statement

The construction industry is increasingly seeking sustainable alternatives to traditional concrete materials due to their high environmental impact. Foam concrete, which is lightweight and has good thermal insulation properties, presents a promising solution. However, its production still faces challenges in achieving the desired performance while maintaining environmental sustainability. One potential solution is to incorporate a natural surfactant, such as palm kernel oil, to improve the properties of foam concrete. Despite the benefits of palm kernel oil in other industrial applications, its role in enhancing the performance of foam concrete has not been widely explored. Furthermore, the influence of different curing conditions on the properties of hybrid foam concrete remains under-researched. This study aims to investigate the effect of palm kernel oil-based surfactant on foam concrete's properties under various curing conditions, contributing to the development of more sustainable and efficient construction materials.

## 1.2 Justification of study

The environmental impact of traditional concrete production is a growing concern due to the high carbon emissions associated with cement production. Foam concrete, made using lightweight aggregates and air-entrained bubbles, offers a viable alternative by reducing the density of the concrete and improving its thermal and acoustic properties. Incorporating natural surfactants like palm kernel oil could not only enhance the performance of foam concrete by stabilizing the foam but also make the production process more sustainable.

The study will help determine the viability of palm kernel oil as a sustainable surfactant in foam concrete, providing insights into its effects on compressive strength, density, thermal conductivity, and durability. The research will also explore the impact of different curing conditions (e.g., ambient curing, water curing, and heat curing) on the mechanical properties and longevity of the foam concrete. These findings will be valuable for the construction industry, as they can lead to the development of greener, more cost-effective building materials that are suitable for a variety of applications, including residential buildings, infrastructure projects, and insulation systems.

Additionally, palm kernel oil is widely available in tropical regions and is considered a renewable resource, making it an economically viable alternative to synthetic surfactants, which are often expensive and less sustainable. This aligns with the global push for green building materials and the reduction of carbon footprints in construction.

## 1.3 Aim of the Study

Investigation of the durability of hybrid foam concrete with palm kernel oil surfactant under different curing conditions.

## 1.4 Objectives of the Study

The specific objectives of this research are to:

- Determine the optimal concentration of palm kernel oil surfactant that enhances the durability of foam concrete.

- Evaluate the impact of palm kernel oil surfactant on the compressive strength and water absorption of foam concrete under various curing methods (water curing, air curing, and steam curing).

- Assess freeze-thaw resistance of foam concrete with palm kernel oil surfactant when exposed to different curing techniques.

- Compare the performance of foam concrete with and without palm kernel oil surfactant under identical curing conditions to understand the effects of the surfactant on long-term durability.

## 1.5 Scope of study

This study will focus on the following key aspects:

- Preparation of Foam Concrete: Various mixes of foam concrete will be prepared using different dosages of palm kernel oil-based surfactant to observe the effects on foam stability and concrete properties.

- Curing Conditions: The study will examine the effect of three curing conditions—ambient curing, water curing, and heat curing—on the mechanical properties of foam concrete, including compressive strength, density, and thermal conductivity.

- Performance Evaluation: The concrete’s performance will be evaluated through standard tests such as compressive strength, density, water absorption, and thermal insulation. Additionally, the long-term durability of the foam concrete will be assessed under various environmental conditions.

- Environmental Impact Assessment: A comparative analysis of foam concrete with palm kernel oil surfactant versus conventional foam concrete will be conducted, focusing on the reduction of the carbon footprint and resource utilization.

CHAPTER TWO

# Literature review

## Preamble

Marcin Kozłowski (2018) The targeted density denoted is 400-1400 kg/m3. Fly ash is used. The commercial foaming agent is used. Density of FC is 20% higher than FCA. The strength of specimen to freezethaw cycles is 15% lower values. The Compressive Strength, Modulus of elasticity and Flexural Strength get decreased when the density of the foamed concrete decreased. 5% addition of fly ash causes the decrease of the Compressive Strength, Flexural Strength and Modulus of Elasticity of foamed concrete. Yanbin Fu (2020) This paper describes manufacturing and material properties like drying shrinkage, compressive strength, stability and pore structure. The experimental results implies that the compressive strength of FC increases with density and confining pressure. Synthetic and Protein based Surfactants are used. The usage of fibers such as Polypropylene, glass and polypropylene and palm oil, Steel, coconut, waste paper cellulose, carbon used in 0.2% and 1.5 of mixture volume. Finally it is concluded that foam concrete with uniformly distributed closed circular airpores, it shows good thermal and mechanical properties. Devid Falliano(2019) The protein based foaming agent called Foamin C was used. Three dry densities are targeted, they are 400 kg/m3, 600 kg/m3, 800 kg/m3. Three different fiber content were analysed like 0.7%, 2%, 5%.When we are adding 2 and 5% of fiber, it results in the increase of flexural strength.

A study by Lee et al 2023. emphasises geopolymer binders in foamed concrete production for sustainability. The study thoroughly compares geopolymer-based foamed concrete to Portland cement-based concrete in mechanical qualities, durability, and environmental impact. This research shows how to improve performance and reduce carbon emissions. Martinez et al. study foamed concrete's response to fly ash nanoparticles. The study carefully examines microstructural changes, porosity, permeability, and chemical resistance to determine the material's endurance in harsh environments. Chen et al 2021. examine foamed concrete's compressive strength development and curing conditions. The study explores how temperature and moisture during curing affect mechanical qualities, providing insights for practise optimisation. Wang et al. study lightweight foamed concrete's thermal conductivity and insulation. Their detailed examination of density, porosity, and thermal performance illuminates foamed concrete's thermal insulation potential. Garcia et al 2017. conduct a long-term performance evaluation of foamed concrete structures under real-world situations. This research reveals the material's mechanical qualities, durability, and microstructure over its lifespan. These numerous research endeavours improve foamed concrete knowledge, advancing construction practises, sustainability, and creative building solutions. The several chemical additives (such as stabilizers or Superplasticizers) can be added to foam concrete to enhance its properties. Depending on project specifications, these additives enhance the mixture's durability, workability, and strength. The foam concrete can be produced using a process of continuous production. This method mixes a continuous stream of cementitious mixture with the foaming compound. This approach is frequently used in high-production settings and streamlines the manufacturing process.

CHAPTER THREE

# METHODOLOGY

## Introduction

This study adopts an experimental method to refine the hybrid foam concrete mix design by using palm kernel oil-based surfactants. The approach focuses on developing, testing, and analysing various mix compositions to achieve an optimal balance between density and compressive strength, considering different curing conditions (air, water, and steam) and also the splitting tensile strength.

## The research was carried out in several stages: initially, materials were sourced and prepared; next, trial mixes were performed to establish the final concrete mix design; then, concrete cubes measuring 150 mm by 150 mm by 150 mm were cast; and finally, these cubes were crushed to measure their crushing load and compressive strength, using a 1:2 nominal mix composed of 50% stone dust and 50% sharp sand with a water-to-cement ratio of 0.75.

## Materials Needed

The materials utilized in this study comprised cement, water, aggregates (stone dust and sharp sand), palm kernel oil, and foaming agents (SLS). These materials were used to cast concrete cubes measuring 150 mm × 150 mm × 150 mm. The batching was done using a 1:2 mix ratio, and the concrete was poured into molds of the same dimensions. After casting, the molds were removed after 24 hours, and the samples were then placed in a curing container. Curing was carried out for periods of 7, 14, and 28 days, during which tests for crushing strength, density, and compressive strength were performed

Below is a brief overview of the materials:

Portland Limestone Cement: Portland Limestone Cement Typically Grade 42.5R, as specified in ASTM C150-20 and BS EN 197-1:2011 was used during this research. The cement serves as the primary binder in foam concrete. The cement is gotten from a cement store around the school area in Ilorin, Kwara State. Each bag of PLC is 50kg in size.

    - Sharp sand: as it is one of the most important components in the mix, Sharp sand, also known as coarse sand, is typically obtained from quarries, riverbeds, or other natural sources. It is essential to source the sharp sand from reputable suppliers to ensure it is clean, free from impurities, and properly graded

Fig3.2 sharp sand from nearby quarry

    - Hybridized Stone Dust (Coarse Aggregate): Stone dust is been introduced as a hybridized coarse aggregate in the mix. Since, there is no need for coarse aggregate in foam concrete to reduce its weight and density. Stone dust is collected from quarry sites and sieved using a 1.7mm sieve to remove particles. The gradation is verified as per ASTM C33/C33M.

fig 3.3: stone dust from a nearby quarry

    - Palm kernel oil-based surfactants: Palm kernel oil-based surfactants are derived from the oil extracted from the seeds of the palm kernel through processes such as polyesterification or amidopropylation. PKO-S is been gotten from a nearby market aroundIlorin metropolis.

    - Water: Water is essential for hydration and foam generation. Potable water is been used for mixing and curing, conforming to ASTM C1602. The water used for this work was obtained from the nearby water source at Institute of Technology, Kwara State Polytechnic, Ilorin. The water was free from injurious amount of oil, acid, organic matter, alkali and other deleterious substances

    - Foaming agent: Sodium Lauryl Sulfate (SLS) is a commonly used foaming agent in foamed concrete. The SLS is sourced for in OJA TUNTUN market, Ilorin.

## Methods

Six samples of foamed concrete were produced for optimization, two for each curing conditions Optimization will be between a sample with PKO-S and another without PKO-S. The mix ratio used for both samples is 1:2:0.75 where 1 is the ratio for the binder (PLC), 2 is the ratio divided between the aggregates (sharp sand 50% and Stone dust 50%), and the water/cement ratio used is 0.75, The foaming agent varies in response to the water cement ratio.

Mixing Procedure:

- Weigh the Portland Limestone Cement (PLC), sharp sand, stone dust, SLS, and palm kernel oil.

- Mix the cement with part of the water from the water/cement ratio to form a cement paste.

- In a separate container, dissolve the SLS in a small amount of water to prepare a foam solution.

- Add the sharp sand and stone dust in their respective proportions, stirring continuously until the mixture is uniform. The remaining water is added gradually to achieve a smooth consistency.

- Incorporate the generated foam into the wet mix and blend thoroughly.

- Add the palm kernel oil to the mixture.

- Continue mixing the combined foam concrete for an additional 3 to 4 minutes before pouring it into cleaned molds.

- After 24 hours, remove the cube molds and immerse the samples in a water tank for curing.

Mix Proportioning:

- PKO-S concentrations is definite 1%

- The water-to-binder ratio follows the required water-to-cement ratio (0.75 was incorporated)

- The Foaming agents also is in concentration with the water – cement ratio.

- Specimens (150 mm x 150 mm x 150 mm cubes) were casted, compacted, and cured in water for 7, 14, and 28 days.

Various types of tests were carried out on the sample to check for the compressive strength and density of the Foam Concrete, and to know the effect of Palm Kernel Oil Based Surfactant on the sample. The following test was carried out by following the code of practice:

Compressive Strength: The compressive strength test is a standard method for determining the strength of concrete. The compressive strength test was conducted using the ASTM C39/C39M standard. During this research, 18 cubes of 150 mm x 150 mm x 150 mm of concrete were been casted and cured for 7, 14 and 28 days (2 cubes for each curing conditions) in water of average room temperature after 24 hours of casting. The specimens were tested for compressive strength by applying compressive load to the specimen until it crushes. Therefore, the maximum load is recorded which is given by N/mm2. The compressive strength is then calculated using the formula:

Compressive Strength= Maximum LoadCross-sectional Area

Where:

Maximum load (N) = The maximum load from the machine until failure

Cross – sectional Area (mm2) = The area of the cube

CHAPTER FOUR		RESULTS AND DISCUSSIONS

4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Sharp sand | 1400 |
| Cement | 1440 |
| SLS |  |
| Water | 0.75 |
| PKO | 1% |

4.2	Density

The tables below show the weight of each specimen cubes in 7, 14 and 28 days

Table 4.2 Weight of Specimen Cubes In 7 Days

| Days | Curing Method | % Of PKO | Weight(g) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7 | Air | 1% | 7023 |  |  |  |  |
|  |  |  | 6560 |  |  |  |  |
|  | Water | 1% | 7101 |  |  |  |  |
|  |  |  | 7253 |  |  |  |  |
|  | Steam | 1% | 6800 |  |  |  |  |
|  |  |  | 6680 |  |  |  |  |

Table 4.3	Weight of Specimen Cubes in 14 days

| Days | Curing Method | % Of PKO | Weight(g) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 14 | Air | 1% | 7083 |  |  |  |  |
|  |  |  | 6508 |  |  |  |  |
|  | Water | 1% | 7215 |  |  |  |  |
|  |  |  | 7375 |  |  |  |  |
|  | Steam | 1% | 6640 |  |  |  |  |
|  |  |  | 6809 |  |  |  |  |

Table 4.4	Weight of Specimen Cubes in 28 days

| Days | Curing Method | % Of PKO | Weight(g) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 28 | Air | 1% | 6870 |  |  |  |  |
|  |  |  | 5995 |  |  |  |  |
|  | Water | 1% | 7377 |  |  |  |  |
|  |  |  | 6893 |  |  |  |  |
|  | Steam | 1% | 6101 |  |  |  |  |
|  |  |  | 6498 |  |  |  |  |

Table 4.5	Average Weight of Specimens for 7, 14 and 28 days

| Days | Curing Method | % of PKO | Average Weight(G) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7 | Air | 1% | 6791 |  |  |  |  |
|  | Water |  | 7177 |  |  |  |  |
|  | Steam |  | 6740 |  |  |  |  |
| 14 | Air | 1% | 6796 |  |  |  |  |
|  | Water |  | 7295 |  |  |  |  |
|  | Steam |  | 6725 |  |  |  |  |
| 28 | Air |  | 6433 |  |  |  |  |
|  | Water | 1% | 7135 |  |  |  |  |
|  | Steam |  | 6300 |  |  |  |  |

Table 4.6	Density of The Specimens i.e Density= weight/volume of cubes

| Days | % of PKO | Average weight (g) | Density (Kg/m3) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7 | 1% | 6791 | 2012 |  |  |  |  |
|  |  | 7177 | 2127 |  |  |  |  |
|  |  | 6740 | 1997 |  |  |  |  |
| 14 | 1% | 6796 | 2014 |  |  |  |  |
|  |  | 7295 | 2161 |  |  |  |  |
|  |  | 6725 | 1993 |  |  |  |  |
| 28 | 1% | 6433 | 1906 |  |  |  |  |
|  |  | 7135 | 2114 |  |  |  |  |
|  |  | 6300 | 1867 |  |  |  |  |

Density chart fig 4.1

From the chat and table, it was derived that the density of hybrid foam concrete increases alongside the curing conditions (air and steam) in relation with the number of curing days, and also it varies for water curing condition it tends to decrease after 14days.

4.3	Compressive Strength

Compressive strength is the capacity of a material or structure to withstand loads tending to reduce size. It is defined as the maximum compressive stress a material can bear before it fractures or deforms permanently. The result of this test is used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification.

For this project, batching by weight was adopted and the 7th, 14th and 28th day compressive strength of foam concrete using palm kernel oil as surfactant, for a nominal mix ratio of 1:2 (50% Stone Dust and 50% sharp sand), at water/cement ratio of 0. .75.The results are as shown below

Table 4.7:	Compressive strength of sample at 7, 14 and 28 days of curing.

| Days | % of PKO | Average weight (g) | Average Crushing load(KN) | Compressive strength (KN/m2 ) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7 |  | 6791 | 50 | 2222 |  |  |  |  |  |
|  | 1% | 7177 | 45 | 2000 |  |  |  |  |  |
|  |  | 6740 | 40 | 1778 |  |  |  |  |  |
| 14 |  | 6796 | 60 | 2668 |  |  |  |  |  |
|  | 1% | 7295 | 80 | 3556 |  |  |  |  |  |
|  |  | 6725 | 60 | 2667 |  |  |  |  |  |
| 28 |  | 6433 | 80 | 3556 |  |  |  |  |  |
|  | 1% | 7135 | 100 | 4444 |  |  |  |  |  |
|  |  | 6300 | 93 | 4133 |  |  |  |  |  |

Fig: 4.2 Compressive strength chart

The compressive strength from the chat and table, signifies that water curing has the highest compressive strength followed by the steam curing, there is an increase in the compressive strength of hybrid foam concrete in respect to the curing days and conditions.

CHAPTER FIVE

# Conclusion

- Palm kernel oil-based surfactant (PKO-S) successfully reduces the density of hybrid foam concrete, achieving densities as low as 1828 kg/m³ cubes, making it suitable for lightweight construction applications.

- While PKO-S stabilizes foam effectively, the material exhibits variable compressive strength, peaking at 4444 KN/m2 having being the highest, highlighting the need for further material optimization to enhance long-term strength and durability.

- The curing stage plays a significant role in foam concrete production, and steam curing emerges as the most effective method, yielding greater strength compared to air or water curing.

- The use of 1% palm kernel oil significantly enhanced concrete strength, particularly with steam curing. However, the decline in strength observed in water and air-cured samples after 14 days suggests that further increasing the palm kernel oil concentration may lead to even greater strength gains, warranting further investigation

# Recommendations

- Based on the observed strength enhancements, it is recommended to explore higher concentrations of palm kernel oil beyond 1% to determine the optimal dosage for maximum strength gains in concrete, particularly with steam curing

- Conduct pilot tests in non-load-bearing applications (e.g., partition walls) to validate practical performance.

- Since sourcing for PKOS and stone dust is very affordable, the use of PKOS and stone dust should be encouraged in the making of foamed concrete.

- Further studies need to be carried out to improve the compressive strength of Foam concrete either through adding of additives or aggregates.

REFERENCES

  - Liu, P.; Gong, Y.F.; Tian, G.H.; Miao, Z.K. Preparation and experimental study on the thermal characteristics of lightweight prefabricated nano-silica aerogel foam concrete wallboards. Constr. Build. Mater. 2021, 272, 121895. [https://doi.org/10.1016/j.conbuildmat.2020.121895]

- Marcin Kozlowski and Marta Kadela (2018) on ‘Mechanical Characterization of Lightweight Foamed Concrete’, Journal of Advances in Materials Science and Engineering, Vol.2018.

- Yanbin Fu et.al., (2020) ‘Foam Concrete: A State-of-the-Art and State-of-the-Practice Review’, Journal of Advances in Materials Science and Engineering, Vol.2020.

- Devid Falliano et.al., (2019) ‘Compressive and Flexural Strength of Fiber-Reinforced Foamed Concrete: Effect of fiber content, curing conditions and dry density’, Journal of Construction and Building Materials, Vol.198.

- Bindiganavile, V.; Hoseini, M. Foamed Concrete; Elsevier: Amsterdam, The Netherlands, 2019.

- Panesar, D. Cellular concrete properties and the effect of synthetic and protein foaming agents. Constr. Build. Mater. 2013, 44, 575–584. [https://doi.org/10.1016/j.conbuildmat.2013.03.024]

- Li, T.; Huang, F.; Zhu, J.; Tang, J.; Liu, J. Effect of foaming gas and cement type on the thermal conductivity of foamed concrete. Constr. Build. Mater. 2020, 231, 117197. [https://doi.org/10.1016/j.conbuildmat.2019.117197]

- Falliano, D.; de Domenico, D.; Ricciardi, G.; Gugliandolo, E. Experimental investigation on the compressive strength of foamed concrete: Effect of curing conditions, cement type, foaming agent and dry density. Constr. Build. Mater. 2018, 165, 735–749. [https://doi.org/10.1016/j.conbuildmat.2017.12.241]

- Li, T.; Huang, F.; Li, L.; Zhu, J.; Jiang, X.; Huang, Y. Preparation and properties of sulphoaluminate cement-based foamed concrete with high performance. Constr. Build. Mater. 2020, 263, 120945. [https://doi.org/10.1016/j.conbuildmat.2020.120945]

- Li, T.; Wang, Z.; Zhou, T.; He, Y.; Huang, F. Preparation and properties of magnesium phosphate cement foam concrete with H2O2 as foaming agent. Constr. Build. Mater. 2019, 205, 566–573. [https://doi.org/10.1016/j.conbuildmat.2019.02.022]

- Khan, Q.S.; Sheikh, M.N.; McCarthy, T.; Robati, M.; Allen, M. Experimental investigation on foam concrete without and with recycled glass powder: A sustainable solution for future construction. Constr. Build. Mater. 2019, 201, 369–379. [https://doi.org/10.1016/j.conbuildmat.2018.12.178]

- Ma, C.; Chen, B. Experimental study on the preparation and properties of a novel foamed concrete based on magnesium phosphate cement. Constr. Build. Mater. 2017, 137, 160–168. [https://doi.org/10.1016/j.conbuildmat.2017.01.092]

- Lesovik, V.; Voronov, V.; Glagolev, E.; Fediuk, R.; Alaskhanov, A.; Amran, Y.M.; Murali, G.; Baranov, A. Improving the behaviors of foam concrete through the use of composite binder. J. Build. Eng. 2020, 31, 101414. [https://doi.org/10.1016/j.jobe.2020.101414]

- Kearsley, E.P.; Wainwright, P. The Effect of fly ash content on the compressive strength development of concrete. Cem. Concr. Res. 2001, 31, 105–112. [https://doi.org/10.1016/S0008-8846(00)00430-0]

- Jones, M.; McCarthy, A. Heat of hydration in foamed concrete: Effect of mix constituents and plastic density. Cem. Concr. Res. 2006, 36, 1032–1041. [https://doi.org/10.1016/j.cemconres.2006.01.011] SSSSS

- Raj, A.; Sathyan, D.; Mini, K. Physical and functional characteristics of foam concrete: A review. Constr. Build. Mater. 2019, 221, 787–799. [https://doi.org/10.1016/j.conbuildmat.2019.06.052]

- She, W.; Du, Y.; Zhao, G.; Feng, P.; Zhang, Y.; Cao, X. Influence of coarse fly ash on the performance of foam concrete and its application in high-speed railway roadbeds. Constr. Build. Mater. 2018, 170, 153–166. [https://doi.org/10.1016/j.conbuildmat.2018.02.207]

- Krishna, A.S.; Siempu, R.; Kumar, G.S. Study on the fresh and hardened properties of foam concrete incorporating fly ash. Mater. Today Proc. 2021, 46, 8639–8644. [https://doi.org/10.1016/j.matpr.2021.03.599]

- Pan, Z.; Li, H.; Liu, W. Preparation and characterization of super low-density foamed concrete from Portland cement and admixtures. Constr. Build. Mater. 2014, 72, 256–261. [CrossRef]

- Amran, Y.H.M.; Alyousef, R.; Alabduljabbar, H.; Khudhair, M.H.R.; Hejazi, F.; Alaskar, A.; Alrshoudi, F.; Siddika, A. Performance properties of structural fibred-foamed concrete. Results Eng. 2020, 5, 100092. [CrossRef]

- Gökçe, H.S.; Hatungimana, D.; Ramyar, K. Effect of fly ash and silica fume on hardened properties of foam concrete. Constr. Build. Mater. 2019, 194, 1–11. [CrossRef]

- Bing, C.; Zhen, W.; Ning, L. Experimental Research on Properties of High-Strength Foamed Concrete. J. Mater. Civ. Eng. 2012, 24, 113–118. [CrossRef]

- Bindiganavile, V.; Hoseini, M. Foamed Concrete, 1st ed.; Woodhead Publishing Limited: Sawston, UK, 2008.

- Gencel, O.; Oguz, M.; Gholampour, A.; Ozbakkaloglu, T. Recycling waste concretes as fine aggregate and fly ash as binder in production of thermal insulating foam concretes. J. Build. Eng. 2021, 38, 102232. [CrossRef]

- Ibrahim, N.M.; Salehuddin, S.; Amat, R.C.; Rahim, N.L.; Izhar, T.N.T. Performance of Lightweight Foamed Concrete with Waste Clay Brick as Coarse Aggregate. APCBEE Procedia 2013, 5, 497–501. [CrossRef]

- Amran, Y.M.; Farzadnia, N.; Ali, A.A. Properties and applications of foamed concrete, A review. Constr. Build. Mater. 2015, 101, 990–1005. [CrossRef]

- Ranjani, G.I.S.; Ramamurthy, K. Analysis of the Foam Generated Using Surfactant Sodium Lauryl Sulfate. Int. J. Concr. Struct. Mater. 2010, 4, 55–62. [CrossRef]

- . Mastali, M.; Kinnunen, P.; Isomoisio, H.; Karhu, M.; Illikainen, M. Mechanical and acoustic properties of fiber-reinforced alkali-activated slag foam concretes containing lightweight structural aggregates. Constr. Build. Mater. 2018, 187, 371–381. [CrossRef]

- Raj, B.; Sathyan, D.; Madhavan, M.K.; Raj, A. Mechanical and durability properties of hybrid fiber reinforced foam concrete. Constr. Build. Mater. 2020, 245, 118373. [CrossRef]

- Chang, R.-d., Soebarto, V., Zhao, Z.-y., and Zillante, G. (2016). Facilitating the Transition to Sustainable Construction: China's Policies. J. Clean. Prod. 131, 534–544. doi:10.1016/j.jclepro.2016.04.147

- Fan, J.-L., Wang, J.-X., Hu, J.-W., Wang, Y., and Zhang, X. (2019). Optimization of China's Provincial Renewable Energy Installation Plan for the 13th Five-Year Plan Based on Renewable Portfolio Standards. Appl. Energ. 254, 113757. doi:10.1016/j.apenergy.2019.113757

- Hardjito, D., Wallah, S. E., Sumajouw, D. M. J., and Rangan, B. V. (2004). Factors Influencing the Compressive Strength of Fly Ash-Based Geopolymer concrete. Civil Eng. Dimension. 6 (2), 88–93. doi:10.9744/ced.6.2

- He, M. (2017). Polyurethane Foam Technology in Green Building Eco-Efficiency Design (In Chinese). Bull. Sci. Technol. 33 (1), 174–177. doi:10.13774/j.cnki.kjtb.2017.01.037

- Hill, D. (2013). Ancient Roman Concrete Could Hold Secrets to Improving Modern Construction. Civ. Eng. Mag. Arch. 83 (9), 44–45. doi:10.1061/ciegag.0000655

- Hou, M., Wang, Y., Zhao, H., Zhang, Q., Xie, Q., Zhang, X., et al. (2018). Halogenated Flame Retardants in Building and Decoration Materials in China: Implications for Human Exposure via Inhalation and Dust Ingestion. Chemosphere 203, 291–299. doi:10.1016/j.chemosphere.2018.03.182

- Huang, Y. (2013). Development of Foreign Building Saving-Energy Technology. Adv. Mater. Res. 671–674 (2), 2126–2128. doi:10.4028/www.scientific.net/AMR.671-674.2126

- Liu, M. Y. J., Alengaram, U. J., Santhanam, M., Jumaat, M. Z., and Mo, K. H. (2016). Microstructural Investigations of palm Oil Fuel Ash and Fly Ash Based Binders in Lightweight Aggregate Foamed Geopolymer concrete. Construction Building Mater. 120, 112–122. doi:10.1016/j.conbuildmat.2016.05.076

- Liu, Y., Yan, H., and Lam, J. C. (2014). Thermal comfort and Building Energy Consumption Implications – A Review. Appl. Energ. 115 (4), 164–173. doi:10.1016/j.apenergy.2013.10.062

- Mydin, M. A. O., and Wang, Y. C. (2011). Structural Performance of Lightweight Steel-Foamed concrete-steel Composite walling System under Compression. Thin-Walled Structures 49 (1), 66–76. doi:10.1016/j.tws.2010.08.007

- Ramamurthy, K., Kunhanandan Nambiar, E. K., and Indu Siva Ranjani, G. (2009). A Classification of Studies on Properties of Foam concrete. Cement and Concrete Composites 31 (6), 388–396. doi:10.1016/j.cemconcomp.2009.04.006

- Silvestre, J., Pargana, N., de Brito, J., Pinheiro, M., and Durão, V. (2016). Insulation Cork Boards-Environmental Life Cycle Assessment of an Organic Construction Material. Materials 9 (5), 394. doi:10.3390/ma9050394

- Tang, S., Xu, Y., Zhu, G., and Fang, W. (2011). Orthogonal experiment Optimum Design in the Power of the Rotor on Straight-Bladed Vawt. Energ. Proced. 12, 856–861. doi:10.1016/j.egypro.2011.10.113

- Valore, R. C. (1954). Cellular Concretes Part 1 Composition and Methods of Preparation. ACI J. Proc. 50 (5), 773–796. doi:10.14359/11794

- Vuong, X. T., Prietzel, J., and Heitkamp, F. (2016). Measurement of Organic and Inorganic Carbon in Dolomite-Containing Samples. Soil Use Manage 32 (1), 53–59. doi:10.1111/sum.12233

- Wang, Z., Gao, H., Liu, H., Liao, L., Mei, L., Lv, G., et al. (2020). Inorganic thermal Insulation Material Prepared from Pitchstone. J. Building Eng. 32 (2), 101745. doi:10.1016/j.jobe.2020.101745

- Xiao, J., and Ding, T. (2013). Research on Recycled concrete and its Utilization in Building Structures in china. Front. Struct. Civ. Eng. 7 (3), 215–226. doi:10.1007/s11709-013-0212-z

- Xuan, W., and Leung, D. (2011). Optimization of Biodiesel Production from Camelina Oil Using Orthogonal experiment. Appl. Energ. 88 (11), 3615–3624. doi:10.1016/j.apenergy.2011.04.041

- Yang, H., Jiang, Y., Liu, H., Xie, D., Wan, C., Pan, H., et al. (2018). Mechanical, thermal and Fire Performance of an Inorganic-Organic Insulation Material Composed of Hollow Glass Microspheres and Phenolic Resin. J. Colloid Interf. Sci. 530, 163–170. doi:10.1016/j.jcis.2018.06.075

- Yang, S., Yao, X., Li, J., Wang, X., Zhang, C., Wu, S., et al. (2021). Preparation and Properties of Ready-To-Use Low-Density Foamed concrete Derived from Industrial Solid Wastes. Construction Building Mater. 287 (1), 122946. doi:10.1016/j.conbuildmat.2021.122946