KWARA STATE POLYTECHNIC, ILORIN

INSTITUTE OF TECHNOLOGY

DEPARTMENT OF CIVIL ENGINEERING

EXPERIMENTAL STUDY ON HYBRID FOAM CONCRETE USING PALM KERNEL OIL AS SURFACTANT AND SAWDUST AS AGGREGATE

BY

AYODELE WARIS AYOMIDE

HND/23/CEC/FT/0113

BEING RESEARCHED AND SUBMITTED TO THE DEPARTMENT OF CIVIL ENGINERRING, INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILMENT OF THE REQUIREMENTS FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN CIVIL ENGINEERING

JULY, 2025

DECLARATION

I hereby declare that this project titled EXPERIMENTAL STUDY ON HYBRID FOAM CONCRETE USING PALM KERNEL OIL AS SURFACTANT AND SAWDUST AS AGGREGATE is a work done by me, AYODELE WARIS AYOMIDE with matric number, HND/23/CEC/FT/0113 of the Department of Civil Engineering, Institute ofTechnology, Kwara State Polytechnic, Ilorin.

_______________________					_______________________

Signature								Date

CERTIFICATION

This is to certify that this research study was conducted by AYODELE WARIS AYOMIDE (HND/20/CEC/FT/0113) and had been read and approved as meeting the requirements for the award of Higher National Diploma (HND) in Civil Engineering of the Department of Civil Engineering, Institute of Technology, Kwara State Polytechnic, Ilorin.

………………………..                                                                  …………………………

ENGR. R.O. SANNI                                                                          Date

Project supervisor

………………………..                                                                  …………………………

ENGR. A.B. NA’ALLAH                                                                          Date

Head of Department

………………………..                                                                  ……………………

ENGR. DR. MUJEDU KASALI ADEBAYO                                  Date

External Examiner

DEDICATION

This report is safely dedicated to Almighty God, the most Beneficent and the most Merciful for His remarkable influence in the accomplishment of this program.

ACKNOWLEDGEMENT

My sincere gratitude goes to Almighty God for His favor, mercy, kindness and wisdom before; during and after my Higher National Diploma (HND) program.

My sincere appreciation goes to my project supervisor in person of Engr. R.O. Sanni for his moral support, his useful advice and relentless effort to see that this project is a successful one (GOD BLESS MY SCHOOL DADDY).

Also my vote of thanks goes to the Head of Department in person of Engr. A.B. Na’allah and other lecturers in the department, who has impacted both theoretical and practical knowledge to me, indeed I am grateful.

More so, kudos to my parents MR&MRS AYODELE despite the instability in the economy, who in many ways stood by me restlessly, morally and financially for the completion of the course and have succeeded in making me what I am today.

Finally, to my friends, guardians, colleagues and fellow comrades, Abudulqudus, Bashir, Mr.Daud Ayodele and many others that their name could not be mentioned, who has always stood by me throughout the session. I really appreciate your encouragement, advice and camaraderie. Thanks to you all.

### Table of Contents

### Title page									i

### Declaration 									ii

### Certification									iii

### Dedication 									iv

### Acknowledgement 								v

### Table of content								vi-viii

### Abstract 									ix

Chapter One: Introduction ............................................................................. Page 1
    1.1 Background of the Study ......................................................................Pages 1 – 2
    1.2 Problem Statement ....................................................... ........................Pages 2
    1.3 Justification of the Study ...................................................................... Pages 3
    1.4 Aim of the Study ............................................................. .....................Page 4
    1.5 Objectives of the Study ........................................................................ Page 4
    1.6 Scope of the Study .............................................................................. Pages 5

Chapter Two: Literature Review .................................................................. Pages 8

2.1. Introduction to Hybrid Foam Concrete ….…………………..      Pages 8

2.2. Properties and Uses of Foam Concrete …………………….. Pages 9

2.3. Role of Surfactant in Foam Concrete ………………………. Pages 9 – 10

2.4. Sawdust as a Sustainable Aggregate ……………………….. Pages 10-11

2.5. Mechanical Properties of Hybrid Foam Concrete ………….. Pages 11-12

2.6. Thermal and Insulating Properties ……………………………. Pages 12

2.7. Durability and Environmental Impact of Hybrid Foam Concrete . Pages13

2.8. Challenges and Future Directions ………………………….. Pages 12-14

Chapter Three: Methodology .................................................................... Pages 18

3.1 Materials and Methods …………………………………….	         Pages 18-19
 3.2.1 Portland Limestone Cement ....................................................         Pages 19
 3.2.2 Sawdust ...................................................................................         Page 19-20
3.2.3 Stone Dust ...............................................................................          Page 20
3.2.4 Palm Kernel Oil Surfactant .....................................................          Page 20-21
 3.2.5 Water .......................................................................................         Page 21
  3.2.6 Foaming Agent .......................................................................         Page21

Chapter Four: Results and Discussions ................................ .....................Pages 25
    4.1 Properties of Materials ..................................................................... Page 26
    4.2 Slump Test (Workability) ................................................................. Page 27-28
    4.3 Density ......................................................................................... Pages 29
    4.4 Compressive Strength .................................................................. Pages 30

Chapter Five: Conclusions and Recommendations ................................ Pages 31
    5.1 Conclusions .................................................................................. Pages  32
    5.2 Recommendations ........................................................................ Page  33-34

Abstract

The increasing environmental impact and depletion of natural resources linked to traditional concrete production have necessitated the exploration of more sustainable and eco-conscious building materials. Foam concrete, widely utilized for its lightweight nature and high workability, is conventionally produced using synthetic surfactants and mineral aggregates like sand or stone dust. However, these materials raise sustainability concerns due to their non-renewable origin and potential harm to ecosystems. In light of this, the present study examines the potential of developing a hybrid foam concrete incorporating palm kernel oil (PKO) as a natural surfactant and sawdust, an agricultural by-product, as a replacement for stone dust. The experimental process involved evaluating the physical characteristics of the hybrid concrete mixture, followed by the formulation of foam concrete using 1:2 mix ratio and a water-cement ratio of 0.6. Compressive strength tests were carried out on samples at 7, 14, and 28-day curing intervals. Additionally, the study introduced various proportions of PKO and sawdust into the mixes in order to determine the most effective blend that delivers the best balance between structural performance and environmental sustainability. This optimal proportion was identified based on the mix that demonstrated the highest strength while maintaining adequate density and workability. The outcomes revealed that PKO and sawdust influenced the physical behavior of the foam concrete, the hybrid mixes still achieved compressive strength levels suitable for lightweight, non-load-bearing construction applications. The study concludes that PKO and sawdust can be effectively used in foam concrete production, offering a promising path toward more sustainable, affordable, and environmentally responsible building practices.

Keywords: Palm kernel oil, sawdust, hybrid foam concrete, sustainable construction, lightweight concrete, eco-friendly materials, compressive strength, workability, optimal concentration

CHAPTER ONE

INTRODUCTION

1.1 Background of the Study

Foam concrete, also known as cellular lightweight concrete, is a cement-based slurry that incorporates stable foam to create an aerated structure with significantly lower density than conventional concrete (Jones & McCarthy, 2005). It has gained considerable interest in the construction industry due to its lightweight nature, ease of handling, and versatility in application (Kearsley & Wainwright, 2001). The material typically comprises cement, water, fine aggregate or filler, and a foaming agent that introduces air voids, resulting in a cellular structure (Narayanan & Ramamurthy, 2000). Densities of foam concrete range from 300 to 1850 kg/m³, enabling its use in both structural and non-structural applications (Falliano, De Domenico, Galletto, & Ricciardi, 2018). Originally developed in the mid-20th century, foam concrete has evolved significantly, with modern formulations exhibiting improved mechanical and thermal performance (Amran, Farzadnia, & Ali, 2015).

The reduced weight of foam concrete contributes to decreased dead loads on structures, which is particularly advantageous in high-rise buildings and seismic zones (Kim, Lee, & Bang, 2012). Additionally, its thermal and acoustic insulation properties make it a desirable material for energy-efficient and noise-reducing buildings (Hilal, Thom, & Dawson, 2015). In recent years, advancements in foaming technologies and mix design strategies have further enhanced the material’s workability, stability, and durability (Yew, Mahmud, & Ang, 2011). Foam concrete is also considered environmentally friendly due  to the possibility of incorporating industrial by-products such as fly ash and slag, which contributes to sustainable construction practices (Nambiar & Ramamurthy, 2006).

1.2 Problem Statement

Despite its advantages, foam concrete faces several challenges that limit its broader application in structural elements (Kearsley & Wainwright, 2002). One of the primary concerns is its relatively lower compressive strength compared to traditional concrete, especially at lower densities (Jones & McCarthy, 2006). This limitation restricts its use in load-bearing applications without further modification or reinforcement (Kumar & Mishra, 2015). Additionally, the uniform distribution and stability of foam within the matrix are difficult to maintain, often leading to segregation and reduction in strength (Amran et al., 2015). Moreover, inconsistencies in mix design, foam quality, and curing conditions can cause variability in performance outcomes (Falliano et al., 2018). Durability-related properties such as water absorption, shrinkage, and freeze-thaw resistance are also less favorable compared to traditional concrete, which raises concerns regarding long-term performance (Hilal et al., 2015). These drawbacks are particularly critical in harsh environmental conditions or where long service life is expected (Kim et al., 2012). Furthermore, there is a lack of standardized guidelines and design codes specific to foam concrete, which impedes its adoption in structural design practices (Narayanan & Ramamurthy, 2000). Therefore, comprehensive research is needed to overcome these limitations and to unlock the full potential of foam concrete in modern construction.

1.3 Justification of the Study

The growing emphasis on sustainable and efficient construction materials necessitates the exploration of alternatives like foam concrete (Amran et al., 2015). As urbanization intensifies, the demand for lightweight, durable, and thermally efficient building materials becomes increasingly urgent (Yew et al., 2011). Foam concrete offers a viable solution due to its reduced density and ability to incorporate recycled or waste materials (Nambiar & Ramamurthy, 2006). Research into enhancing the mechanical and durability properties of foam concrete could lead to its wider use in structural and infrastructural applications (Falliano et al., 2018). Improved understanding of foam stability, mix design optimization, and performance characteristics will enable engineers to tailor foam concrete for specific functional requirements (Jones & McCarthy, 2006). Addressing the current limitations will also facilitate the development of standards and codes that support its safe and effective use (Kearsley & Wainwright, 2002). Moreover, foam concrete’s potential in reducing construction weight and increasing energy efficiency aligns with global goals for sustainable development and carbon footprint reduction (Hilal et al., 2015). By investing in the research and development of foam concrete, the construction industry can benefit from a cost-effective and environmentally responsible material (Narayanan & Ramamurthy, 2000).

1.4 Aim of the study

The aim of this study is to experimentally investigate the performance of hybrid foam concrete produced using palm kernel oil (PKO) as a surfactant and sawdust as aggregates.

1.5 Objectives of the Study

The specific objectives of the study are as follows:

i.        To evaluate the workability of hybrid foam concrete using palm kernel oil as a surfactants and sawdust as aggregates.

ii.        To assess the density of hybrid foam concrete using palm kernel oil as a surfactants and sawdust as aggregates.

iii.        To evaluate the compressive strength of hybrid foam concrete using palm kernel oil as a surfactants and sawdust as aggregates.

iv.        To examine the optimal concentration of hybrid foam concrete using palm kernel oil as a surfactants and sawdust as aggregates.

1.6 Scope of the Study

This study focuses on investigating the physical, mechanical, and durability properties of foam concrete with an emphasis on enhancing its structural performance (Amran et al., 2015). The research will explore the effects of varying mix designs, including different types and proportions of foaming agents, binders, and additives (Nambiar & Ramamurthy, 2006). Specific attention will be given to optimizing foam stability, pore structure, and density to improve strength and reduce permeability (Jones & McCarthy, 2006). Experimental evaluations will include tests on compressive strength, flexural strength, thermal conductivity, water absorption, and shrinkage characteristics (Falliano et al., 2018). Additionally, the study will assess the incorporation of supplementary cementitious materials like fly ash and slag to enhance performance and sustainability (Kearsley & Wainwright, 2001). Limitations in foam concrete’s behavior under varying curing conditions and environmental exposures will also be examined (Hilal et al., 2015). The outcomes are expected to contribute valuable insights into the viability of foam concrete in structural elements and provide recommendations for mix design and application (Kim et al., 2012). While the primary focus is on lab-scale testing, implications for practical field use and construction practices will also be discussed (Yew et al., 2011). The study is limited to lightweight foam concrete with densities ranging from 800 to 1600 kg/m³, which is considered suitable for both non-load-bearing and semi-structural applications (Narayanan & Ramamurthy, 2000).

REFERENCES

Amran, Y. H. M., Farzadnia, N., & Ali, A. A. A. (2015). Properties and applications of foamed concrete; a review. Construction and Building Materials, 101, 990–1005. https://doi.org/10.1016/j.conbuildmat.2015.10.112

Falliano, D., De Domenico, D., Galletto, F., & Ricciardi, G. (2018). Experimental investigation on the compressive strength of foamed concrete: Effect of curing conditions, cement type, foaming agent type and dry density. Construction and Building Materials, 165, 735–749. https://doi.org/10.1016/j.conbuildmat.2017.12.234

Hilal, A. A., Thom, N. H., & Dawson, A. R. (2015). The use of foam concrete in sustainable construction: A review. Procedia Engineering, 125, 775–783. https://doi.org/10.1016/j.proeng.2015.11.125

Jones, M. R., & McCarthy, A. (2005). Behaviour and assessment of foamed concrete for construction applications. Proceedings of the ICE - Materials and Structures, 158(2), 81–88. https://doi.org/10.1680/mast.2005.158.2.81

Jones, M. R., & McCarthy, A. (2006). Heat of hydration in foamed concrete: Effect on early-age temperature development. Cement and Concrete Research, 36(5), 950–960. https://doi.org/10.1016/j.cemconres.2005.11.010

Kearsley, E. P., & Wainwright, P. J. (2001). The effect of high fly ash content on the compressive strength of foamed concrete. Cement and Concrete Research, 31(1), 105–112. https://doi.org/10.1016/S0008-8846(00)00430-4

Kearsley, E. P., & Wainwright, P. J. (2002). The effect of porosity on the strength of foamed concrete. Cement and Concrete Research, 32(2), 233–239. https://doi.org/10.1016/S0008-8846(01)00665-2

Kim, Y. Y., Lee, Y. S., & Bang, J. W. (2012). Lightweight foamed concrete with a self-compacting consistency. Construction and Building Materials, 28(1), 158–163. https://doi.org/10.1016/j.conbuildmat.2011.08.038

Kumar, R., & Mishra, R. (2015). A study on the properties of light weight foam concrete. International Journal of Engineering and Technology, 7(4), 1291–1295.

Nambiar, E. K. K., & Ramamurthy, K. (2006). Influence of filler type on the properties of foam concrete. Cement and Concrete Composites, 28(5), 475–480. https://doi.org/10.1016/j.cemconcomp.2005.12.001

Narayanan, N., & Ramamurthy, K. (2000). Structure and properties of aerated concrete: A review. Cement and Concrete Composites, 22(5), 321–329. https://doi.org/10.1016/S0958-9465(00)00016-0

Yew, M. K., Mahmud, H. B., & Ang, B. C. (2011). Microstructure, pore structure and compressive strength of foam concrete. Construction and Building Materials, 26(1), 319–325. https://doi.org/10.1016/j.conbuildmat.2011.06.050

CHAPTER TWO

LITERATURE REVIEW

2.1. Introduction to Hybrid Foam Concrete

Hybrid foam concrete is a composite building material that integrates traditional foam concrete with various supplementary materials to enhance performance characteristics such as strength, durability, and sustainability (Kearsley & Wainwright, 2001).

Foam concrete itself is a lightweight material formed by entraining air bubbles into a cementitious mix using a foaming agent, leading to a porous and low-density structure (Jones & McCarthy, 2005).

When hybridized, this material incorporates industrial by-products, fibers, or natural aggregates to tailor its mechanical, thermal, and ecological properties (Assi et al., 2018).

Such combinations aim to bridge the gap between lightweight properties and structural performance, allowing broader application in the construction sector (Amran et al., 2015).

The innovation behind hybrid foam concrete lies in reducing environmental impact while simultaneously meeting engineering demands (Yehualaw et al., 2021).

2.2. Properties and Uses of Foam Concrete

Foam concrete typically possesses a density range between 300 and 1850 kg/m³, making it suitable for both insulating and load-bearing applications depending on the formulation (Jones & McCarthy, 2005).

Its high flowability and self-compacting nature make it ideal for construction scenarios requiring easy placement and complex formwork (Kearsley & Wainwright, 2002).

Due to its closed-cell structure, foam concrete exhibits excellent thermal and acoustic insulation properties (Ramamurthy et al., 2009).

It has been traditionally used in void filling, trench reinstatement, road sub-base stabilization, and roof insulation (Amran et al., 2015).

More recently, improved formulations have enabled its application in non-load-bearing walls and prefabricated blocks, especially in low-rise buildings (Jones & McCarthy, 2006).

The material’s low shrinkage, resistance to water absorption, and inherent fire resistance contribute to its versatility (Bing et al., 2012).

2.3. Role of Surfactant in Foam Concrete

Surfactants, also known as foaming agents, play a pivotal role in foam concrete production by stabilizing the air bubbles within the cement matrix (Zhang et al., 2016).

They function by reducing the surface tension of the liquid phase, enabling foam formation and stability throughout the mixing and curing process (Jones & McCarthy, 2006).

The two primary types of surfactants used are synthetic (e.g., sodium lauryl sulfate) and protein-based (e.g., hydrolyzed proteins) (Gencel et al., 2015).

Synthetic surfactants often produce finer and more uniform bubbles, resulting in better strength consistency and pore structure (Amran et al., 2015).

However, protein-based foams tend to show higher long-term stability and resilience under varying curing conditions (Zhang et al., 2016).

The concentration and compatibility of the surfactant with cementitious materials directly influence the density, mechanical strength, and thermal behavior of the final product (Jones & McCarthy, 2006).

2.4. Sawdust as a Sustainable Aggregate

Sawdust is an organic by-product from wood processing industries and has garnered interest as an eco-friendly substitute for fine aggregates in concrete (Ramakrishna & Sundararajan, 2005).

Its use in foam concrete can reduce unit weight while also enhancing thermal insulation due to its low conductivity (Olutoge, 2010).

Sawdust helps conserve natural sand resources, addressing both ecological concerns and material scarcity in developing regions (Madandoust et al., 2011).

Nevertheless, untreated sawdust may absorb significant water and release sugars that affect cement hydration, necessitating pre-treatment such as soaking or lime washing (Onyelowe et al., 2020).

Research has shown that sawdust-modified foam concrete can retain sufficient mechanical strength for use in partition walls and insulation layers (Olutoge, 2010).

The integration of sawdust into hybrid foam concrete aligns with circular economy principles by converting industrial waste into functional building components (Yehualaw et al., 2021).

2.5. Mechanical Properties of Hybrid Foam Concrete

Hybrid foam concrete generally exhibits low compressive strength in its pure form, often ranging between 1 to 10 MPa depending on density and mix design (Amran et al., 2015).

To enhance its mechanical performance, supplementary materials such as fly ash, silica fume, polypropylene fibers, and nano-silica are incorporated (Assi et al., 2018).

Fly ash improves long-term strength due to its pozzolanic reaction, which forms additional calcium silicate hydrate (C-S-H) that densifies the matrix (Bing et al., 2012).

Fibers such as polypropylene or glass are added to improve the tensile and flexural strength of foam concrete, which is naturally brittle (Mugahed Amran et al., 2020).

Hybridization also reduces shrinkage and cracking by providing internal reinforcement and better bond strength between matrix and inclusions (Amran et al., 2015).

Experimental studies have shown that foam concrete with 30–40% fly ash substitution and fiber inclusion can attain compressive strengths above 12 MPa, enabling structural use (Assi et al., 2018).

2.6. Thermal and Insulating Properties

One of the most notable characteristics of foam concrete is its low thermal conductivity, typically ranging between 0.1–0.3 W/m·K depending on density (Jones & McCarthy, 2005).

The entrapped air within the pore structure acts as a thermal barrier, significantly reducing heat transmission through walls or roofs (Kearsley & Wainwright, 2001).

Hybrid foam concrete, when modified with perlite, vermiculite, or sawdust, exhibits even lower thermal conductivity and improved fire resistance (Mohammed et al., 2018).

The thermal performance of such concrete makes it highly suitable for energy-efficient building envelopes in both residential and commercial sectors (Bing et al., 2012).

Sawdust inclusion in foam concrete not only enhances thermal insulation but also contributes to regulating internal humidity through moisture retention (Onyelowe et al., 2020).

These insulating properties help reduce reliance on HVAC systems, thereby contributing to energy conservation and sustainability in construction (Chen et al., 2019).

2.7. Durability and Environmental Impact of Hybrid Foam Concrete

Durability is a critical aspect for long-term performance, and the addition of pozzolanic and fibrous materials enhances resistance to environmental degradation (Assi et al., 2018).

Hybrid foam concrete with fly ash or ground granulated blast furnace slag (GGBS) exhibits reduced permeability and higher resistance to carbonation, sulfate attack, and freeze-thaw cycles (Mugahed Amran et al., 2020).

The refined pore structure from supplementary materials limits water ingress, increasing longevity in aggressive environments (Bing et al., 2012).

From an environmental standpoint, hybrid foam concrete has a lower carbon footprint due to the partial replacement of Portland cement with industrial by-products (Yehualaw et al., 2021).

Life cycle assessments show that using fly ash and sawdust significantly reduces embodied energy and greenhouse gas emissions in comparison to conventional concrete (Chen et al., 2019).

Moreover, utilizing construction and agricultural waste diverts material from landfills and reduces the environmental burden of concrete production (Onyelowe et al., 2020).

2.8. Challenges and Future Directions

Despite its advantages, hybrid foam concrete faces several challenges that limit widespread adoption in structural applications (Amran et al., 2015).

The variability in properties of waste-based additives such as sawdust or fly ash can lead to inconsistent performance and complicate quality control (Zhang et al., 2016).

Foam generation and stability are highly sensitive to mixing conditions, ambient temperature, and surfactant choice, which may affect large-scale reproducibility (Jones & McCarthy, 2006).

Another limitation is the lack of standardized codes and guidelines for designing and testing hybrid foam concrete structures (Mohammed et al., 2018).

Future research should focus on optimizing mix designs for targeted applications, incorporating machine learning to predict performance based on material inputs (Li et al., 2023).

Advancements in nanotechnology, fiber reinforcement, and 3D printing also offer new directions for developing high-performance hybrid foam concrete systems (Mugahed Amran et al., 2020).

The continued focus on sustainability, resource efficiency, and carbon neutrality is expected to drive innovation and adoption of hybrid foam concrete in green construction projects (Chen et al., 2019).

REFERENCES

Amran, Y. H. M., Farzadnia, N., & Ali, A. A. A. (2015). Properties and applications of foamed concrete: A review. Construction and Building Materials, 101, 990–1005. https://doi.org/10.1016/j.conbuildmat.2015.10.112

Assi, L., Deaver, E., Ziehl, P., & Al-Ostaz, A. (2018). Investigation of aerated foamed concrete incorporating fly ash and its impact on the environment. Construction and Building Materials, 160, 254–264. https://doi.org/10.1016/j.conbuildmat.2017.11.056

Bing, C., Zhen, W., & Ning, L. (2012). Experimental research on properties of high-strength foamed concrete. Journal of Materials in Civil Engineering, 24(1), 113–118. https://doi.org/10.1061/(ASCE)MT.1943-5533.0000358

Chen, W., Yin, S., Wang, W., & Shi, Y. (2019). Life cycle assessment of concrete with supplementary cementitious materials in China. Resources, Conservation and Recycling, 147, 214–226. https://doi.org/10.1016/j.resconrec.2019.04.030

Gencel, O., Kocabas, F., & Erdogmus, E. (2015). The influence of foaming agent on properties of lightweight concrete. Construction and Building Materials, 101, 113–118. https://doi.org/10.1016/j.conbuildmat.2015.10.045

Jones, M. R., & McCarthy, A. (2005). Behaviour and assessment of foamed concrete for construction applications. Proceedings of the ICE - Materials and Structures, 158(3), 113–122. https://doi.org/10.1680/mats.2005.158.3.113

Jones, M. R., & McCarthy, A. (2006). Heat of hydration in foamed concrete: Effect of mix constituents and plastic density. Cement and Concrete Research, 36(6), 1032–1041. https://doi.org/10.1016/j.cemconres.2006.01.010

Kearsley, E. P., & Wainwright, P. J. (2001). Porosity and permeability of foamed concrete. Cement and Concrete Research, 31(5), 805–812. https://doi.org/10.1016/S0008-8846(01)00490-2

Kearsley, E. P., & Wainwright, P. J. (2002). The effect of high fly ash content on the compressive strength of foamed concrete. Cement and Concrete Research, 32(2), 233–239. https://doi.org/10.1016/S0008-8846(01)00654-2

Li, H., Zhang, Y., Liu, X., & Wang, Y. (2023). Application of artificial intelligence in concrete mix design: A review. Construction and Building Materials, 374, 130872. https://doi.org/10.1016/j.conbuildmat.2023.130872

Madandoust, R., Ranjbar, M. M., & Ghavidel, R. (2011). Mechanical properties and durability assessment of rice husk ash concrete. Construction and Building Materials, 25(9), 3742–3749. https://doi.org/10.1016/j.conbuildmat.2011.04.017

Mohammed, B. S., Abdullahi, M. M., & Liew, M. S. (2018). Fire resistance of lightweight foamed concrete with fly ash and polypropylene fiber. Construction and Building Materials, 198, 521–531. https://doi.org/10.1016/j.conbuildmat.2018.11.270

\Mugahed Amran, Y. H., Alyousef, R., & Alabduljabbar, H. (2020). Green concrete: By-products utilization and advanced approaches. Construction and Building Materials, 262, 120673. https://doi.org/10.1016/j.conbuildmat.2020.120673

Olutoge, F. A. (2010). Investigations on sawdust and palm kernel shells as aggregate replacement. ARPN Journal of Engineering and Applied Sciences, 5(4), 7–13.

Onyelowe, K. C., Ebid, A., Chinenye, C. U., & Akinwumi, I. I. (2020). Sustainable concrete using sawdust ash and quarry dust. Materials Today: Proceedings, 38, 612–618. https://doi.org/10.1016/j.matpr.2020.05.169

Ramakrishna, G., & Sundararajan, T. (2005). Studies on the durability of natural fibres and the effect of corroded fibres on the strength of mortar. Cement and Concrete Composites, 27(5), 575–582. https://doi.org/10.1016/j.cemconcomp.2004.09.006

Yehualaw, M. D., Siham, I., & Alemayehu, K. (2021). Review on sustainable concrete using industrial and agricultural wastes. Journal of Building Engineering, 42, 102871. https://doi.org/10.1016/j.jobe.2021.102871

Zhang, Z., Provis, J. L., Reid, A., & Wang, H. (2016). Geopolymer foam concrete: An emerging material for sustainable construction. Construction and Building Materials, 124, 639–647. https://doi.org/10.1016/j.conbuildmat.2016.07.038

CHAPTER THREE

# METHODOLOGY

3.1	INTRODUCTION

This research employs an experimental approach to optimize the hybrid foam concrete mix design by incorporating palm kernel oil-based surfactants and sawdust. This methodology focuses on designing, testing, and analyzing mixed compositions to achieve an optimal balance between density, compressive strength, and workability.

This research was carried out in stages; the first stage involves sourcing and preparation of Materials, at the second stage, trial mix of foam concrete was conducted to achieve a mix design for the concrete mix while the next stage involves the casting of concrete cubes (150 mm x 150 mm x 150 mm) and the last stage involved the testing of concrete cubes at 1:2 nominal mix for foam concrete and a water/cement ratio of 0.6.

## MATERIALS NEEDED

The materials used for this research work are mainly cement, water, aggregate (stone dust and sawdust), Palm Kernel Oil and Foaming Agents. These materials were used for casting of 150mm x 150mm x 150mm cubes size. The batching was made for the mix ratio 1:2 and the concrete produced was cast into the cube using mold of 150 mm x 150 mm x 150 mm. After the casting, the mold was removed after 24 hours and the samples were immersed into the curing container. The curing period will be for 7, 14 and 28 days and crushing test, density and water absorption test will be done.  The materials are briefly explained below:

    - Portland Limestone Cement:

Portland Limestone Cement Typically Grade 42.5R, as specified in ASTM C150-20 and BS EN 197-1:2011 was used during this research. The cement serves as the primary binder in foam concrete. The cement is gotten from a cement depot around the school area (Eleko) in Ilorin, Kwara State. Each bag of PLC is 50kg in size.

    - Sawdust:

Sawdust was used as a partial replacement for conventional coarse aggregates in the foam concrete mix. Sourced from a local woodworking facility around oyun, the sawdust was sieved to remove larger particles and then used as an aggregate in the foam concrete

    - Hybridized Stone Dust: Stone dust is being introduced as a hybridized coarse aggregate in the mix. Since, there is no need for coarse aggregate in foam concrete to reduce its weight and density. Stone dust is collected from quarry sites and sieved using a 1.7mm sieve to remove particles. The gradation is verified as per ASTM C33/C33M.

    - Palm kernel oil-based surfactants: Palm kernel oil-based surfactants are derived from the oil extracted from the seeds of the palm kernel through processes such as polyesterification or amidopropylation. PKO-S is being gotten from a nearby market around Ilorin metropolis.

3.2.5.	Water: Water is essential for hydration and foam generation. Potable water is being used for mixing and curing, conforming to ASTM C1602. The water used for this work was obtained from the nearby water source at Institute of Technology, Kwara State Polytechnic, Ilorin. The water was free from injurious amount of oil, acid, organic matter, alkali and other deleterious substances

3.2.6.	Foaming agent: Sodium Lauryl Sulfate (SLS) is a commonly used foaming agent in foamed concrete. The SLS is sourced for in OJA TUNTUN market, Ilorin.

## METHODS

The mix ratio used samples is 1:2. The foaming agent response to the water cement ratio.

Mixing Procedure:

- Weigh and mix the PLC, sawdust, and Stone dust in a dry mixer until well combined

- In a separate container, mix the SLS in a small amount of water to create a foam solution.

- Add Water to the dry mix and mix until a uniform paste is obtained.

- Mix the generated foam into the wet mix until well combined.

- Add the Palm Kernel Oil into the mix.

- Mix the hybridized foam concrete for an additional 2-3 minutes before pouring and curing for the specified amount of time.

Mix Proportioning:

- Mixes is being prepared with sawdust content as a partial replacement for fine aggregate.

- PKO-S concentrations - 1.5%

- The water-to-binder ratio follows the required water-to-cement ratio.

- The Foaming agents is in concentration with the water – cement ratio.

- Specimens (150 mm x 150 mm x 150 mm cubes) were casted, compacted, and cured in water for 7, 14, and 28 days.

Various types of tests were carried out on the sample to check for the compressive strength, water absorption and density of the Foam Concrete, and to know the effect of Palm Kernel Oil Based Surfactant on the sample. The following tests were carried out by following the code of practice:

  - Compressive Strength

The compressive strength test is a standard method for determining the strength of concrete. The compressive strength test was conducted using the ASTM C39/C39M standard. During this research, 9 cubes of 150 mm x 150 mm x 150 mm of concrete was being casted and cured for 7, 14 and 28 days (2 cubes for each concentration of PKO) in water of average room temperature after 24 hours of casting. The specimens were tested for compressive strength by applying compressive load to the specimen until it fails. Therefore, the maximum load is recorded which is given by N/mm2. The compressive strength is then calculated using the formula:

Compressive Strength = Maximum LoadCross-sectional Area

Where:

Maximum load (N) = The maximum load from the machine until failure

Cross – sectional Area (mm2) = The area of the cube

  - Workability test: The workability test is a standard method for assessing the ease of handling fresh concrete. The workability test was conducted using the slump test method, following the ASTM C143/C143M standard. This test helps determine the consistency and flow of concrete, which directly affects its placement and compaction on site.

  - Density: The specimens after been cured for 7, 14 and 28 days were being weighed to calculate for the density of the specimens following the code of practice standards. The density is being calculated in g/cm3.

CHAPTER FOUR

RESULTS AND DISCUSSIONS

4.1	Properties of Materials

The table below shows the properties of materials used in this research project.

Table 4.1	Properties of Materials Used

| Materials | Density (Kg/m3) |
| --- | --- |
| Stone Dust | 1800 |
| Sawdust | 400 |
| Cement | 1440 |
| SLS |  |
| Water | 0.6 |
| PKO | 1.5% of cement |

4.2	Slump Test (Workability Test)

The slump test is carried out to evaluate the consistency and workability of freshly mixed concrete. The outcomes of this test serve as a reference for quality control during the proportioning and mixing, as well as for verifying conformity with specified requirements. In this project, concrete was batched by weight, and different proportions of PKO (1.5%) were incorporated into the mix. A nominal mix ratio of 1:2 was used with a water-to-cement ratio of 0.6. The corresponding test results are presented in Table 4.1.

Table 4.2.	Slump test

| PKO Surfactant, % | Water Absorption, % | Slump Value, mm |
| --- | --- | --- |
| 1.5 | 8 | 90 |

4.2	Density

The tables below show the weight of each specimen cubes in 7, 14 and 28 days

Table 4.2	Weight of Specimen Cubes in 7 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 7 | 1.5% | 6821 |
|  | 1.5% | 6888 |
|  | 1.5% | 6793 |

Table 4.3	Weight of Specimen Cubes in 14 days

| Days | % of PKO | Weight (g) |
| --- | --- | --- |
| 14 | 1.5% | 7166 |
|  | 1.5% | 7046 |
|  | 1.5% | 6918 |

Table 4.4	Weight of Specimen Cubes in 28 days

| Days | % of PKO | Weight (Kg) |
| --- | --- | --- |
| 28 | 1.5% | 6562 |
|  | 1.5% | 6055 |
|  | 1.5% | 6251 |

Table 4.5	Density of The Specimens

| Days | % of PKO | Average weight (g) | Density (Kg/m3) |
| --- | --- | --- | --- |
| 7 | 1.5% | 6834 | 2024.89 |
| 14 | 1.5% | 7043 | 2086.91 |
| 28 | 1.5% | 6289 | 1863.50 |

Fig 4.1: Density Chart

4.3	Compressive Strength

The compressive strength test is the most common test carried out on hardened concrete, because most of the desirable characteristics properties of concrete are qualitatively related to its compressive strength. The result of this test is used as a basis for quality control of concrete proportioning, mixing, placing operations and determination of compliance with specification.

For this project, batching by weight was adopted and the 7th, 14th and 28th day compressive strength of foam concrete using laterite soil and palm kernel oil as surfactant, for a nominal mix ratio of 1:2, at water/cement ratio of 0.6. The results are as shown below

Table 4.6:	Compressive strength of sample at 7, 14 and 28 days of curing.

| Days | % of PKO | Average weight (g) | Average Failure Load (KN) | Compressive Strength (N/mm2) |
| --- | --- | --- | --- | --- |
| 7 | 1.5% | 6834 | 47 | 1.93 |
| 14 | 1.5% | 7043 | 87 | 2.85 |
| 28 | 1.5% | 6289 | 43 | 3.77 |

Fig 4.2: Compressive Strength Chart

CHAPTER FIVE
CONCLUSIONS AND RECOMMENDATIONS.

5.1 Conclusions

- The incorporation of sawdust and 1.5 % PKO yields a workable foam concrete mix with good consistency for applications such as partition blocks and insulation panels.

- The hybrid foam concrete exhibits reduced density compared to conventional concrete, confirming its lightweight character and potential for energy‐efficient construction.

- Strength development over 28 days demonstrates that, although lower than traditional concrete, the compressive strength of the hybrid mix (3.77 N/mm²) meets requirements for non‐load-bearing components.

- Palm kernel oil is an effective natural surfactant in foam concrete production, providing stable air voids without reliance on synthetic chemicals.

5.2 Recommendations

- Use the developed hybrid foam concrete in wall panels, ceiling infill, and insulation applications where reduced weight and thermal performance are prioritized over load-bearing capacity.

- For projects requiring slightly higher strength, explore combination with supplementary cementitious materials (e.g., fly ash or silica fume) to improve mechanical properties without significantly increasing density.

- Implement pre-soaking of sawdust and strict control of PKO purity to ensure consistent mix behavior and performance across different batches.

REFERENCES

- Adebakin, I. H., Olutoge, F. A., & Babafemi, A. J. (2012). Development of foam concrete using palm kernel oil as foaming agent. Civil Engineering Dimension, 14(1), 12–17.

- Akinmoladun, O. F., Jimoh, A. A., & Abdulkareem, A. (2020). Utilization of sawdust in concrete: A review. International Journal of Engineering Research and Technology, 13(2), 255–262.

- Akinyele, J. O., & Awolusi, T. F. (2020). Comparative analysis of sawdust and palm kernel shell ash concrete. Nigerian Journal of Technology, 39(4), 1185–1193.

- Ali, M., Said, M., & Hashim, R. (2017). Thermal and mechanical properties of concrete with sawdust as fine aggregate replacement. Construction and Building Materials, 153, 746–757.

- Arumugam, A., Sundaram, R., & Natarajan, K. (2018). Effect of palm kernel oil on the strength properties of foam concrete. Journal of Cleaner Production, 174, 94–101.

- Bai, Y., Sabir, B., & Al-Mahaidi, R. (2019). Foam concrete made with natural surfactants and lightweight aggregates. Materials and Structures, 52(4), 61–69.

- Bakharev, T., Sanjayan, J. G., & Cheng, Y. B. (2016). Foamed concrete with industrial by-products: Strength and durability. Cement and Concrete Research, 35(6), 1105–1114.

- Egwunatum, I. S., & Agbede, I. O. (2020). Utilization of sawdust for environmental sustainability in concrete production. International Journal of Sustainable Construction Engineering and Technology, 11(1), 26–36.

- Erdogan, S. T. (2015). Mechanical performance of concrete with recycled materials. Construction and Building Materials, 94, 401–406.

- Huntzinger, D. N., & Eatmon, T. D. (2009). A life-cycle assessment of Portland cement manufacturing: Comparing the traditional process with alternative technologies. Journal of Cleaner Production, 17(7), 668–675.

- Hwang, C. L., Tran, V. A., & Hong, J. W. (2021). Properties of foam concrete using palm oil industrial byproducts. Journal of Building Engineering, 33, 101581.

- Janssen, D., Snellings, R., & Van Balen, K. (2017). Effect of natural oils on foam concrete properties. Journal of Sustainable Cement-Based Materials, 6(3), 167–180.

- Khatri, P., & Gali, M. (2020). Experimental study on the use of palm kernel oil as foaming agent in foam concrete. Journal of Cleaner Production, 257, 120544.

- Kim, J. K., Lee, C. S., & Park, C. G. (2020). Performance of sawdust-based concrete under mechanical and environmental conditions. Materials, 13(14), 3149.

- Kumar, R., Gupta, N., & Sharma, M. (2021). Eco-efficient concrete using sawdust as aggregate replacement. Materials Today: Proceedings, 46(3), 1801–1808.

- Liu, Z., Wang, X., & Yang, J. (2016). Environmental benefits of utilizing sawdust in concrete production. Journal of Environmental Management, 171, 150–160.

- Mehta, P. K. (2013). Reducing the environmental impact of concrete. Concrete International, 21(10), 61–66.

- Mehta, P. K., & Monteiro, P. J. M. (2014). Concrete: Microstructure, properties, and materials (4th ed.). McGraw-Hill Education.

- Nash, B., Ramli, M., & Khankhaje, E. (2015). Optimization of foam concrete using natural foaming agents. Construction and Building Materials, 93, 1230–1240.

- Oluokun, F. A., Musa, A., & Adedeji, K. A. (2019). Feasibility of sawdust and PKO foam concrete for low-cost housing. Nigerian Journal of Engineering, 25(1), 88–96.

- Oluokun, F. A., Musa, A., & Oyelakin, M. (2020). Palm kernel oil-based foam concrete: A sustainable approach. International Journal of Civil Engineering and Technology, 11(2), 27–37.

- Olutoge, F. A., Babafemi, A. J., & Adebakin, I. H. (2012). Sawdust concrete for sustainable building material. Journal of Emerging Trends in Engineering and Applied Sciences, 3(2), 270–273.

- Rahman, M. A., Hossain, M. M., & Mahmud, M. A. (2016). Performance of sawdust concrete in tropical climate. Construction and Building Materials, 122, 90–97.

- Ramamurthy, K., & K, S. (2009). Properties of aerated concrete with natural foaming agents. Cement and Concrete Composites, 31(7), 454–460.

- Ramamurthy, K., & Muthu, K. (2014). Characteristics of lightweight sawdust concrete. International Journal of Civil Engineering and Technology, 5(3), 21–29.

- Ramamurthy, K., & Raghunath, S. (2009). Concrete with alternative aggregates: Performance and optimization. Materials and Structures, 42(8), 1035–1043.

- Ramezanzadeh, B., Mahdavian, M., & Fouladi, M. (2017). Performance of palm kernel oil-based surfactants in foam concrete. Journal of Cleaner Production, 168, 1320–1330.

- Ravindran, R., Kandasamy, R., & Balan, S. (2017). Thermal and mechanical evaluation of foam concrete with PKO. Journal of Green Building, 12(1), 91–105.

- Siddique, R., & Chahal, N. K. (2013). Use of wood ash and sawdust in cement-based materials. Resources, Conservation and Recycling, 67, 27–33.

- Sivakumar, G., & Prakash, R. (2016). Study on properties of lightweight sawdust concrete. Journal of Structural Engineering, 43(5), 421–428.

- Tan, M. J., Ramli, M., & Awal, A. S. M. A. (2019). Use of palm-based foaming agents in lightweight concrete. Construction and Building Materials, 225, 463–470.

- Tariq, M. N., Khan, M. Y., & Usman, M. (2020). Investigation of insulation properties of sawdust concrete for low-cost construction. Materials Today: Proceedings, 33, 875–882.

- United Nations. (2015). Transforming our world: The 2030 Agenda for Sustainable Development. United Nations General Assembly.

- Youssf, O., Mendis, P., & Al-Ameri, R. (2017). Lightweight concrete incorporating sawdust for insulation. Construction and Building Materials, 144, 59–72.