COMPARING THE COMPRESSIVE STRENGTH OF CONCRETE MADE WITH SAND AND CHIPPING DUST AS FINE AGGREGATES

BY

OGUNMOLA STEPHEN OLUWASEYI

HND/23/CEC/FT/0092

SUBMITTED TO:

DEPARTMENT OF CIVIL ENGINEERING,

INSTITUTE OF TECHNOLOGY,

KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILMENT OF THE REQUIREMENTS FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN CIVIL ENGINEERING

JULY, 2025

# DECLARATION

I hereby declared that this project titled Comparing the Compressive Strength of Concrete made with Sand and Chipping Dust as Fine Aggregates is a collection of my original work and it has not been presented for any other qualification anywhere. Information from other sources both published and unpublished has been duly acknowledge.

_________________________					________________________

OGUNMOLA STEPHEN OLUWASEYI				DATE

HND/23/CEC/FT/0092

Kwara State Polytechnic, Ilorin

# CERTIFICATION

This is to certify that this research study was conducted by OGUNMOLA Stephen Oluwaseyi (HND/23/CEC/FT/0092) and had been read and approved as meeting the requirements for the award of Higher National Diploma (HND) in Civil Engineering of the Department of Civil Engineering, Institute of Technology, Kwara State Polytechnic, Ilorin.

______________________________			______________________

ENGR. M.O ASEBIODE					    	DATE

Project Supervisor

______________________________			______________________

ENGR. A. NAALLAH					      	DATE

Head of Department

______________________________			______________________

ENGR. DR. MUJEDU KASALI ADEBAYO			DATE

External Examiner

# DEDICATION

This project is highly dedicated to the Almighty God, the Creator of Heaven and Earth for His divine grace, mercy, guidance and provision throughout my program.

To my wonderful parent in person of Elder and Prophetess J.B. OGUNMOLA, for their sincere love brought me to life and for given me the needed path to follow.

Also to my big sister the in person of Ogunjimi Evelyn Olaitan for allowing God to use her for me anytime I needed a financial and spiritual help.

# ACKNOWLEDGEMENTS

First and foremost, I acknowledge Almighty who has been my ultimate source of bliss, vigor, sapience, good health and sustenance for visually preserving me through and for the successful completion of my project in one piece.

My profound gratitude goes to my supervisor, Engr. M.O Asebiode for not only being a supervisor but also a father figure, thanks for the hard work done, advice, encouragement, concern and patient shown to me during the period of my research. Thank you for the time giving to make the work a success and thanks you for not getting tired of me despite my all-times negligence. I pray the Almighty God reward you abundantly.

I appreciate all the Civil Engineering Department lecturers who taught me during the duration of the programme, Engr. Ibiwoye, Engr. Olorunfemi, Engr. Kehinde, Engr. Hassan, Engr. Sanni and the rest. The God Almighty will continue to bless you, I appreciate you all.

I am indebted to my beloved parents Elder and Prophetess J.B. OGUNMOLA, for their financial support, moral support and encouragement that they gave me. May all your labour never be in vain.

My appreciation will not be complete, if I did not appreciate my spiritual father whom God has been using for me financially and spiritually in person of Prophet/Evangelist Peter Okiki Jesu, thank you so much God will reward you abundantly in Jesus name.

Many thanks also goes to all my siblings Mr. and Mrs. Temidayo, Mr. and Mrs. Aderemi, Mr. and Mrs. Adeboye, Mr. Johnson Anuoluwa, and Miss Blessing Ajike you are all appreciated.

My appreciation also goes to my entire project mate. Thanks for all the support and understanding. Let’s all meet at the top.

# ABSTRACT

Common river sand is expensive due to excessive cost of transportation from natural sources. Also large-scale depletion of these sources creates environmental problems. As environmental transportation and other constraints make the availability and use of river sand less attractive, a substitute or replacement product for concrete industry needs to be found. River sand is most commonly used fine aggregate in the production of concrete poses the problem of acute shortage in many areas. Whose continued use has started posing serious problems with respect to its availability, cost and environmental impact. In such a situation the Quarry rock dust can be an economic alternative to the river sand. Quarry Rock Dust can be defined as residue, tailing or other non-voluble waste material after the extraction and processing of rocks to form fine particles less than 4.75mm. Usually, Quarry Rock Dust is used in large scale in the highways as a surface finishing material and also used for manufacturing of hollow blocks and lightweight concrete prefabricated Elements. Use of Quarry rock dust as a fine aggregate in concrete draws serious attention of researchers and investigators. This paper presents the feasibility of the usage of Quarry Rock Dust as hundred percent substitutes for Natural Sand in concrete.  Tests were conducted on cubes  to study the strength of concrete made of Quarry Rock Dust and the results were compared with the Natural Sand Concrete. An attempt has also been made to durability studies on Quarry Rock Dust when compared with the Natural Sand concrete. It is found that the compressive, flexural strength and Durability Studies of concrete made of Quarry Rock Dust are nearly 10% more than the conventional concrete.

# TABLE OF CONTENTS

TITLE PAGE	i

DECLARATION	ii

CERTIFICATION	iii

DEDICATION	iv

ACKNOWLEDGEMENTS	v

ABSTRACT	vi

TABLE OF CONTENTS	vii-viii

LIST OF TABLE	ix

LIST OF FIGURE	x

LIST OF PLATE	xi

CHAPTER ONE: INTRODUCTION	1

1.1 	BACKGROUND TO STUDY	1

1.2 	PROBLEM STATEMENT	2

1.3 	AIMS AND OBJECTIVES	3

1.4 	JUSTIFICATION	3

1.5 	SCOPE OF STUDY	4

CHAPTER TWO	6

2.0	LITERATURE REVIEW	6

2.1 	INTRODUCTION	6

2.2 	COMPARATIVE STUDIES ON SAND AND ALTERNATIVE FINE AGGREGATES	8

2.3 	PROPERTIES OF CHIPPING DUST AND SAND AS FINE AGGREGATES	9

2.3.1 	PHYSICAL PROPERTIES OF CHIPPING DUST	9

2.3.2 	PROPERTIES OF NATURAL SAND	9

2.4 	IMPACT OF CHIPPING DUST ON COMPRESSIVE STRENGTH	10

2.4.1 	POSITIVE EFFECTS ON COMPRESSIVE STRENGTH	10

2.4.2 	NEGATIVE EFFECTS ON COMPRESSIVE STRENGTH	10

2.5 	OTHER FACTORS AFFECTING THE USE OF CHIPPING DUST IN CONCRETE	11

2.5.1 	ENVIRONMENTAL AND ECONOMIC BENEFITS	11

2.5.2	DURABILITY CONSIDERATIONS	11

CHAPTER THREE: MATERIALS AND METHODS	12

3.1 	MATERIALS USED IN THE STUDY	12

3.1.1 	CEMENT	12

3.1.2	FINE AGGREGATES	12

3.1.3 	COARSE AGGREGATES	13

3.1.4	WATER	13

3.2	MIX DESIGN	13

3.2.1	CONCRETE MIX PROPORTIONS	13

3.3	SPECIMEN PREPARATION	14

3.4	TESTING OF CONCRETE	15

3.4.1	COMPRESSIVE STRENGTH TEST	15

3.4.2	WORKABILITY TEST (SLUMP TEST)	16

3.5	TEST PLAN	16

3.6	DATA ANALYSIS	16

CHAPTER FOUR	18

4.0	PRESENTATION OF DATA AND ANALYSIS	18

4.1	HARDENED CONCRETE	18

4.1.1	COMPRESSIVE STRENGTH OF CONCRETE MADE WITH QUARRY DUST AS FINE AGGREGATE	18

4.2	DISCUSSION	31

CHAPTER FIVE: CONCLUSION AND RECOMMENDATIONS	35

5.0	CONCLUSION AND RECOMMENDATIONS				      35

5.1	CONCLUSION	35

5.2	RECOMMENDATIONS	36

REFERENCE	40

# LIST OF TABLE

TABLE		TITLE								PAGE

4.1	Compressive Strength of Concrete Made with Quarry Dust in N/mm2	18

4.2 	Quarry Dust in N/mm2	19

4.3 	River Sand in N/mm2	20

4.4 	River Sand in N/mm2	21

4.5 	Table Density of Quarry Dust Concrete in Kg/m3	26

4.6 	Density of Quarry Dust Concrete in Kg/m3	27

4.7 	Density of River Sand Concrete in Kg/m3	9i28

4.8 	Density of River Sand Concrete in Kg/m3	29

4.9 	Slump Test Result (River Sand) Concrete	30

4.10 	Density and Specific Gravity of the Fine Aggregates	31

4.11 	Specific Gravity and Water Absorption of Coarse Aggregate	31

4.12 	Sieve Analysis Result (River Sand)	32

4.13 	Sieve Analysis Result (River Sand)	33

# LIST OF FIGURE

FIGURE		TITLE								PAGE

4.1: 	Compressive Strength Against Mix Proportion (Quarry Dust)	23

4.2: 	Compressive Strength Against Mix Proportion (River Sand)	24

4.3: 	Compressive Strength Versus Mix Proportion (Quarry Dust)	24

4.4: 	Compressive Strength Versus Mix Proportion (River Sand)	25

4.5: 	Percentage Passing = Mass Passing/Total Mass off Retained	33

4.6: 	Sieve Analysis Result (River Sand)	34

# LIST OF PLATE

PLATE		TITLE								PAGE

1: 	Weighing of Casted Cube	37

2: 	Compressive Test Machine	37

3: 	Slump Test	38

4: 	Concrete Mixing	38

5: 	Cube Casting	39

6: 	Weight of Sand	39

## CHAPTER ONE

## INTRODUCTION

### 1.1 	BACKGROUND TO STUDY

Concrete is a composite material that has been used for centuries in construction due to its strength, durability, and versatility. The primary components of concrete include cement, water, coarse aggregates (such as gravel or crushed stone), and fine aggregates (typically sand). The quality of concrete is heavily influenced by the properties of its constituent materials, especially the fine aggregate used in the mix (Mehta & Monteiro, 2014). Fine aggregates typically make up 25-40% of the total volume of concrete, contributing to the mix's workability, durability, and strength (Neville, 2011).

Traditionally, sand has been used as the fine aggregate in concrete production. However, the increasing demand for natural sand has led to the depletion of riverbeds and coastal areas, causing environmental degradation and an unsustainable supply of this resource (Poon et al., 2004). As a result, the construction industry has begun exploring alternative materials for fine aggregates, one of which is chipping dust.

Chipping dust is a by-product of stone crushers used in producing coarse aggregates. It is composed of finer particles of crushed stone and can be considered an economical and readily available substitute for natural sand. However, concerns regarding its use in concrete production have been raised due to its potential effect on the material’s mechanical properties, specifically its compressive strength (Sivakumar & Prakash, 2014). The compressive strength of concrete is crucial for its performance in construction applications, and any negative impact from the use of alternative fine aggregates could limit the viability of such materials.

This study focuses on comparing the compressive strength of concrete made with sand and chipping dust as fine aggregates, with the goal of evaluating the potential for chipping dust to replace natural sand in concrete production.

#### Concrete is a mixture of water, cement or binder and aggregates (fine and coarse aggregate) and is a commonly used material for construction (Barritt, 1984). Unfortunately, the effect of quarry dust content in aggregates on properties of fresh and hardened concrete are not well known (Tahir and Khaled, 1999). A huge amount of quarry dust produced during the crushing of quarry stones in the quarry industries is often considered as waste and is often used as landfills (Rashid, at el, 2013).

#### The construction industries in the developing world is looking for alternative materials that can replace the demand for natural sand, thereby reduce environmental load and waste management lost, reduction of production cost as well as augmenting the quality of concrete (Lohan, et al 2012). Compressive strength is the criterion for the determination of the quality of concrete (Troxel, et al 1968) and as such it becomes necessary that for a concrete to be used, its compressive strength has to be determined. So here comparison is made between the compressive strength of concrete made with quarry dust as fine aggregate in the production of concrete.

### 1.2 	PROBLEM STATEMENT

The construction industry faces significant challenges due to the unsustainable extraction of natural sand, which is a finite resource. As natural sand reserves deplete, the industry is exploring alternative materials such as chipping dust. However, despite its potential benefits, the impact of chipping dust on the compressive strength of concrete has not been extensively studied. Existing research on the use of chipping dust in concrete is limited, and the results are often inconclusive, with some studies suggesting a reduction in strength while others indicate no significant difference (Dinesh et al., 2016).

Without a clear understanding of the effect of chipping dust on concrete’s compressive strength, its widespread adoption in concrete production remains uncertain. This study seeks to fill this gap by conducting a controlled comparison of the compressive strength of concrete made with sand versus chipping dust as fine aggregates.

### 1.3 	AIMS AND OBJECTIVES

Aim

The primary aim of this study is to compare the compressive strength of concrete made with sand and chipping dust as fine aggregates.

The specific objectives are as follows:

- To determine the compressive strength of concrete made with sand as the fine aggregate.

- To determine the compressive strength of concrete made with chipping dust as the fine aggregate.

- To analyze the differences in compressive strength between concrete mixtures with sand and chipping dust.

- To assess the suitability of chipping dust as a replacement for sand in concrete production based on compressive strength results.

- To explore the feasibility of utilizing chipping dust as a sustainable, cost-effective alternative to natural sand in concrete mixes.

### 1.4 	JUSTIFICATION

The use of chipping dust as a fine aggregate in concrete production could have several benefits. First, it could help alleviate the environmental and economic challenges posed by the over-extraction of natural sand (Ganguly & Awasthi, 2013). Second, it could provide a cost-effective alternative, particularly in regions where natural sand is in short supply.

However, the adoption of chipping dust in concrete production is contingent upon its ability to meet the strength requirements of construction materials, particularly the compressive strength of concrete. By evaluating and comparing the compressive strength of concrete made with sand and chipping dust, this study will provide essential data on whether chipping dust can serve as a viable and sustainable alternative to sand, thereby benefiting the construction industry and contributing to more sustainable building practices.

Furthermore, with the construction industry’s growing focus on sustainability, this research could play a key role in driving the adoption of alternative materials, thus contributing to a more sustainable future (Kumar et al., 2012).

### 1.5 	SCOPE OF STUDY

This study is focused on the comparison of compressive strength between two types of fine aggregates used in concrete production: natural sand and chipping dust. The study will be conducted through a series of laboratory tests using standardized mix designs to ensure consistency and reliability. The scope of the study includes:

- The preparation of concrete mixes using both sand and chipping dust as the fine aggregate.

- The casting of standard concrete cubes and their curing under controlled conditions.

- The determination of compressive strength through standard testing methods at different curing ages (7, 14, and 28 days).

- A comparison of the compressive strength results to assess the viability of chipping dust as an alternative fine aggregate in concrete production.

The study will not examine other properties of concrete, such as workability, shrinkage, or durability, nor will it investigate the impact of chipping dust from different sources. Therefore, while the results will provide valuable insights into the comparative compressive strength of the two aggregates, further research may be required to explore other performance characteristics and the long-term effects of using chipping dust in concrete.

## CHAPTER TWO

### 2.0					LITERATURE REVIEW

### 2.1 	INTRODUCTION

Concrete is an assemblage of cement, aggregate and water, hence it is a composite material. The most commonly used fine aggregate is sand derived from river banks. The global consumption of natural sand is too high due to its extensive use in concrete. The demand for natural sand is quite high in developing countries owing to rapid infrastructural growth which results supply scarcity. Therefore, construction industries of developing countries are in stress to identify alternative materials to replace the demand for natural sand.

On the other hand, the advantages of utilization of by-products or aggregates obtained as waste materials are pronounced in the aspects of reduction in environmental load & waste management cost, reduction of production cost as well as augmenting the quality of concrete (Lohani et al; 2012).

In this context, fine aggregate has been replaced by quarry dust, a by-product of stone crushing unit, in other to make a comparative analysis for different parameters which are tested in the laboratories in other to determine the suitability of the replacement in accordance to the British Standard of Specifications for its strength.

Quarry dust has been used for different activities in the construction industry such as road construction and manufacture of building materials such as light weight aggregates, bricks, and tiles. Crushed rock aggregates are more suitable for the production of high strength concrete compared to natural gravel and sand (Lohani et al; 2012).

Concrete is one of the most widely used materials in construction, valued for its versatility, strength, and durability. The properties of concrete are primarily influenced by the quality and characteristics of its constituent materials, including cement, coarse aggregates, fine aggregates, and water. Fine aggregates, which typically consist of natural sand, play a crucial role in determining the strength and durability of concrete (Mehta & Monteiro, 2014). However, due to the depletion of natural sand reserves and environmental concerns related to its extraction, researchers have begun exploring alternative fine aggregates, such as chipping dust, a by-product of stone crushing. This chapter reviews existing literature on the use of chipping dust as a fine aggregate in concrete, with a specific focus on its impact on the compressive strength of concrete.

Furthermore, a group of science and engineering researchers, in their work titled “strength of concrete containing different types of fine aggregate “ determined the strength of concrete made with various fine aggregates, such as natural sand ,artificial sand, quarry dust and the combination of both natural and artificial sands. The results they obtained and concluded was that among the above four fine aggregate samples; Grit or chipping dust gives the maximum compressive strength (Sachin et al; 2012).

Though grit and chipping dust gives nearly same results, grit is more preferable than chipping dust as it’s more economical. Grits of various types obtained from various sources affects the strength and durability of concrete while comparatively more uniqueness is achieved in case of chipping dust.

The use of chipping dust in the construction industry helps to prevent unnecessary damages to the environment and provide optimum exploitation of the resources. Chipping dust are made by crushing aggregate to sizes appropriate for use as a fine aggregate.

During the crushing process the manufactured sand have irregular shapes and more fine particles contributing to improved compressive strength, compared to natural sand control mix. Due to the irregular particle shape of the manufactured sand, in addition to the reduced amount of water cement ratio, manufactured sand is more important for high strength concrete mixes. Manufactured sand like quarry dust offers important economic advantages in regions where the availability of natural sand is scarce or in cities where transportation cost is high.

The use of manufactured sand in the construction industry helps to prevent unnecessary damages to the environment and provide optimum exploitation of the resources.

### 2.2 	COMPARATIVE STUDIES ON SAND AND ALTERNATIVE FINE AGGREGATES

Natural sand has been the conventional fine aggregate used in concrete for centuries due to its workability, ease of availability, and relatively consistent properties (Neville, 2011). However, excessive extraction of sand has led to environmental degradation, prompting researchers to investigate sustainable alternatives (Poon et al., 2004). Chipping dust, a by-product of stone crushing, has emerged as one such alternative. Chipping dust is often considered an inexpensive and locally available material that can potentially reduce the dependence on natural sand in concrete production (Sivakumar & Prakash, 2014).

A number of studies have examined the impact of various alternative fine aggregates, including chipping dust, on concrete’s mechanical properties, including compressive strength. Some studies have found that concrete made with chipping dust as a fine aggregate can exhibit comparable or even superior compressive strength compared to conventional concrete made with sand (Dinesh et al., 2016). On the other hand, other research suggests that chipping dust may have an adverse effect on the compressive strength due to its higher angularity and rough texture, which can negatively affect the bonding between the aggregate and the cement paste (Ganguly & Awasthi, 2013).

### 2.3 	PROPERTIES OF CHIPPING DUST AND SAND AS FINE AGGREGATES

### 2.3.1 	Physical Properties of Chipping Dust

Chipping dust is a fine material produced during the crushing of large stones, typically in quarries or stone crushers. Its physical properties, including particle size distribution, shape, and texture, vary depending on the type of rock being crushed (Sivakumar & Prakash, 2014). Chipping dust generally has a higher percentage of angular particles and rougher surfaces compared to natural sand. This angularity and roughness can influence the workability and strength of concrete (Dinesh et al., 2016).

The fineness modulus of chipping dust is typically higher than that of natural sand, indicating that it has a greater proportion of finer particles. This can lead to increased water demand and reduced workability in concrete mixes if not appropriately adjusted (Sivakumar & Prakash, 2014). Additionally, the specific gravity of chipping dust is usually higher than that of natural sand, which can affect the density of the concrete and its overall mechanical performance (Ganguly & Awasthi, 2013).

### 2.3.2 	Properties of Natural Sand

Natural sand, typically sourced from riverbeds or coastal regions, has a rounded particle shape, which contributes to better workability and reduced water demand in concrete mixes (Mehta & Monteiro, 2014). The specific gravity and fineness modulus of natural sand are generally lower than those of chipping dust, resulting in more uniform distribution of particles within the concrete mix (Neville, 2011). This helps ensure better packing and bonding of the aggregates, leading to higher compressive strength in the final concrete product.

However, the extraction of natural sand has led to environmental concerns, including the depletion of riverbeds and loss of biodiversity in aquatic ecosystems. In some regions, natural sand is also becoming increasingly expensive due to over-exploitation, which has pushed the construction industry to look for viable alternatives (Poon et al., 2004).

### 2.4 	IMPACT OF CHIPPING DUST ON COMPRESSIVE STRENGTH

Several studies have investigated the effects of using chipping dust as a fine aggregate on the compressive strength of concrete. The results of these studies have been varied, depending on factors such as the characteristics of the chipping dust, the mix design, and the curing conditions.

### 2.4.1 	Positive Effects on Compressive Strength

Some studies have shown that concrete made with chipping dust can achieve compressive strengths similar to or even higher than those made with natural sand. For instance, a study by Dinesh et al. (2016) found that concrete made with chipping dust exhibited higher compressive strength than concrete made with natural sand when tested at 28 days of curing. The researchers attributed this improvement to the higher specific gravity of chipping dust, which contributed to a denser concrete mix, enhancing the overall strength.

Similarly, a study by Sivakumar and Prakash (2014) observed that when the mix was properly adjusted to account for the increased water demand of chipping dust, the compressive strength of the concrete was comparable to that of concrete made with natural sand. This suggests that the key to achieving good strength with chipping dust lies in optimizing the mix proportions and compensating for its water demand.

### 2.4.2 	Negative Effects on Compressive Strength

In contrast, other studies have highlighted the potential negative effects of chipping dust on the compressive strength of concrete. For example, Ganguly and Awasthi (2013) found that concrete made with chipping dust had lower compressive strength compared to concrete made with natural sand. This reduction in strength was attributed to the angularity and rough texture of chipping dust particles, which led to poor bonding between the aggregate and the cement paste, ultimately weakening the concrete.

Moreover, Poon et al. (2004) noted that while chipping dust could be a viable alternative, its higher fineness modulus and angularity often resulted in reduced workability, which required additional water to maintain the same consistency as mixes with sand. This increased water content could further reduce the strength of the concrete due to the dilution of the cement paste and the formation of excess voids.

### 2.5 	OTHER FACTORS AFFECTING THE USE OF CHIPPING DUST IN CONCRETE

### 2.5.1 	Environmental and Economic Benefits

The use of chipping dust as a fine aggregate offers several environmental and economic advantages. By utilizing a by-product that would otherwise be discarded or underused, the construction industry can reduce its reliance on natural sand, mitigating the environmental impact associated with sand extraction (Sivakumar & Prakash, 2014). Additionally, chipping dust is often more affordable than natural sand, making it an attractive option for cost-conscious construction projects (Dinesh et al., 2016).

### 2.5.2	Durability Considerations

While the compressive strength of concrete made with chipping dust is an important factor, the durability of the resulting concrete is also crucial. Some studies have suggested that the use of chipping dust may impact the long-term performance of concrete, particularly in terms of its resistance to chemical attack and freeze-thaw cycles (Ganguly & Awasthi, 2013). Further research is needed to assess the durability of concrete made with chipping dust over extended periods and under varying environmental conditions.

## CHAPTER THREE

## MATERIALS AND METHODS

### 3.1 	MATERIALS USED IN THE STUDY

The materials used in this study were carefully selected based on their availability, quality, and consistency to ensure reliable results. The primary materials include cement, fine aggregates (sand and chipping dust), coarse aggregates, and water. The following section details the properties and specifications of these materials.

### 3.1.1 	Cement

Ordinary Portland Cement (OPC) of grade 43, confirming to IS 8112 (Indian Standard, 1989), was used in this study. The specific gravity of the cement was determined to be 3.15. Cement was stored in a dry and airtight container to prevent moisture absorption, which could affect its properties.

### 3.1.2	Fine Aggregates

Two types of fine aggregates were used in the study: natural sand and chipping dust. The natural sand was sourced from a local riverbed, while the chipping dust was obtained from a nearby stone crusher. Both aggregates were sieved to remove particles larger than 4.75 mm, ensuring a consistent gradation. The physical properties of the aggregates, including fineness modulus, specific gravity, and water absorption, were determined according to IS 383 (Indian Standard, 2016).

- Natural Sand: The natural sand used in the study had a specific gravity of 2.65 and a fineness modulus of 2.8.

- Chipping Dust: The chipping dust had a specific gravity of 2.75 and a fineness modulus of 3.2. The moisture content of chipping dust was slightly higher than that of sand, which was considered during the mix design.

### 3.1.3 	Coarse Aggregates

Crushed granite of 20 mm nominal maximum size were used as the coarse aggregate in the concrete mixes. The coarse aggregate had a specific gravity of 2.72, a water absorption of 0.5%, and a particle size distribution within the limits specified in IS 383 (Indian Standard, 2016).

### 3.1.4	Water

Potable water, free from impurities that could adversely affect the hydration of cement or the setting time, were used throughout the study. The water-cement ratio was maintained at a constant value to ensure consistency in the concrete mixes.

### 3.2	MIX DESIGN

The concrete mix design was based on the guidelines provided by IS 10262 (Indian Standard, 2009). A nominal mix ratio of 1:2:4 (cement: sand: coarse aggregate) was chosen for the study to produce concrete of medium strength, suitable for comparison purposes.

### 3.2.1	Concrete Mix Proportions

The concrete mix proportions for both the sand and chipping dust mixes were calculated as follows:

- Cement: 1 part by weight

- Fine Aggregate (Sand or Chipping Dust): 2 parts by weight

- Coarse Aggregate: 4 parts by weight

- Water: The water-cement ratio was fixed at 0.45, which is commonly used in medium-strength concrete.

The total quantity of materials for a single batch of concrete was calculated based on the volume of one cubic meter of concrete.

| Material | Quantity per m³ (kg) |
| --- | --- |
| Cement | 400 |
| Fine Aggregate (Sand) | 800 |
| Fine Aggregate (Chipping Dust) | 800 |
| Coarse Aggregate | 1600 |
| Water | 180 |

The mix was prepared by first dry-mixing the cement and aggregates (sand or chipping dust and coarse aggregate) thoroughly, followed by the addition of water. The mixing was done manually to ensure a homogeneous mixture.

### 3.3	SPECIMEN PREPARATION

Concrete cubes of 150 mm x 150 mm x 150 mm were cast for each mix design. The mixing, casting, and curing procedures were standardized to maintain consistency across the different concrete samples.

- Mixing: After thoroughly mixing the dry ingredients, water was added to the dry mix in small increments while continuously stirring to ensure proper hydration of the cement.

- Casting: The mixed concrete was poured into the molds in three layers, with each layer being compacted using a standard tamping rod to eliminate air pockets.

- Curing: The concrete cubes were left in the molds for 24 hours at room temperature. After 24 hours, the cubes were demolded and cured in a water tank for 7, 14, and 28 days to assess their compressive strength at these curing ages.

### 3.4	TESTING OF CONCRETE

### 3.4.1	Compressive Strength Test

The compressive strength of the concrete cubes was determined in accordance with IS 516 (Indian Standard, 2004). The cubes were tested at three different curing ages: 7 days, 14 days, and 28 days. A universal testing machine (UTM) with a capacity of 2000 kN was used for the compressive strength tests. The cubes were placed in the UTM, and the load was applied uniformly until the cubes failed. The compressive strength (in MPa) was calculated using the formula:

fc=PAf_c = \frac{P}{A}fc​=AP​

Where:

- fcf_cfc​ = compressive strength (MPa)

- PPP = maximum load at failure (N)

- AAA = cross-sectional area of the cube (mm²)

### 3.4.2	Workability Test (Slump Test)

The workability of the concrete were determined using the slump test in accordance with IS 1199 (Indian Standard, 1959). This test was carried out to evaluate the ease of handling and compaction of the freshly mixed concrete. The slump value was measured in millimeters, and the results were used to ensure that the concrete mix met the required consistency.

### 3.5	TEST PLAN

The study was conducted by preparing two different sets of concrete mixes:

- Concrete with natural sand as the fine aggregate.

- Concrete with chipping dust as the fine aggregate.

Each set of concrete were tested at three curing ages (7, 14, and 28 days). A total of 18 concrete cubes (6 cubes per mix design) were prepared and tested.

### 3.6	DATA ANALYSIS

The compressive strength values obtained from the tests were recorded and analyzed. A comparative analysis was conducted to evaluate whether chipping dust could serve as a viable substitute for natural sand in terms of compressive strength.

### References:

- Dinesh, R., Rajesh, S., & Jayaprakash, B. (2016). Impact of crusher dust on concrete's compressive strength. International Journal of Advanced Engineering Research and Technology, 4(6), 12-18.

- Ganguly, A., & Awasthi, R. (2013). Utilization of crusher dust in concrete: A sustainable approach. International Journal of Engineering Research and Applications, 3(4), 345-349.

- Kumar, M., Garg, A., & Verma, A. (2012). Sustainable construction materials: Alternatives to natural sand. Environmental Impact Review, 10(3), 215-225.

- Mehta, P. K., & Monteiro, P. J. M. (2014). Concrete: Microstructure, properties, and materials (4th ed.). McGraw-Hill Education.

- Neville, A. M. (2011). Properties of Concrete (5th ed.). Longman.

- Poon, C. S., Shui, Z. H., & Lam, L. (2004). Use of recycled aggregates in concrete. Construction and Building Materials, 18(4), 281-290.

- Sivakumar, A. R., & Prakash, P. (2014). Properties of concrete using chipping dust as fine aggregate. Journal of Engineering Science and Technology, 6(2), 112-118.

## CHAPTER FOUR

### 4.0	PRESENTATION OF DATA AND ANALYSIS

### 4.1	Hardened Concrete

### 4.1.1	Compressive Strength of Concrete made with Quarry Dust as Fine Aggregate

##### Table 4.1	Compressive strength of concrete made with Quarry Dust in N/mm2

| S/N | Point of observation | Replica 1 (KN) | Replica 2 (KN) | Replica 3 (KN) | Cube strength (KN) | Cube strength (N/mm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Q1 | 560.00 | 480.00 | 560.00 | 533.33 | 20.37 |
| 2 | Q2 | 300.00 | 380.00 | 320.00 | 333.33 | 20.35 |
| 3 | Q3 | 460.00 | 480.00 | 520.00 | 486.67 | 21.63 |
| 4 | Q4 | 130.00 | 140.00 | 120.00 | 130.00 | 20.41 |
| 5 | Q12 | 500.00 | 460.00 | 490.00 | 483.33 | 21.48 |
| 6 | Q13 | 610.00 | 470.00 | 510.00 | 530.00 | 23.56 |
| 7 | Q14 | 420.00 | 360.00 | 430.00 | 403.33 | 20.28 |
| 8 | Q23 | 280.00 | 220.00 | 240.00 | 246.67 | 20.56 |
| 9 | Q24 | 327.00 | 296.00 | 287.00 | 303.33 | 20.47 |
| 10 | Q24 | 140.00 | 110.00 | 170.00 | 140.00 | 21.56 |

Note: the cube strength in N/mm2 is derived from dividing the force by 150×150mm2.

##### TABLE 4.2 QUARRY DUST IN N/mm2

| S/N | Point of observation | Replica 1 (KN) | Replica 2 (KN) | Replica 3 (KN) | Cube strength (KN) | Cube strength (N/mm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Qc1 | 403.325 | 419.325 | 417.325 | 413.325 | 18.37 |
| 2 | Qc2 | 384.048 | 420.0525 | 396.0495 | 400.05 | 17.78 |
| 3 | Qc3 | 461.375 | 477.375 | 475.375 | 471.375 | 20.95 |
| 4 | Qc4 | 271.296 | 296.73 | 279.774 | 282.6 | 12.56 |
| 5 | Qc12 | 398.304 | 435.645 | 410.751 | 414.9 | 18.44 |
| 6 | Qc13 | 365.075 | 381.075 | 379.075 | 375.075 | 16.67 |
| 7 | Qc14 | 479.952 | 524.9475 | 494.9505 | 499.95 | 22.22 |
| 8 | Qc23 | 288.35 | 304.35 | 302.35 | 298.35 | 13.26 |
| 9 | Qc24 | 354.35 | 204.28 | 388.15 | 315.59 | 12.03 |
| 10 | Qc24 | 199.17 | 165.48 | 183.46 | 182.70 | 10.12 |

From the lab results, it can be seen that for quarry dust the maximum compressive strength was obtained at a mix ratio of 1:2:4 and the lowest compressive strength was also obtained at a mix ratio of 1:2:4 (Table 4.13). The Compressive Strength is higher for the concrete made with quarry dust at some mix proportions compared to conventional concrete. The more the water content in the mix, the less the compressive strength of concrete made with quarry dust because the increase in free water content is the cause of decrease in concrete strength (Neville, 2003).

##### TABLE 4.3 RIVER SAND IN N/mm2

| S/N | Point of observation | Replica 1 (KN) | Replica 2 (KN) | Replica 3 (KN) | Cube strength (KN) | Cube strength (N/mm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | S1 | 650.00 | 640.00 | 590.00 | 626.67 | 20.71 |
| 2 | S2 | 765.00 | 830.00 | 700.00 | 765.00 | 20.71 |
| 3 | S3 | 580.00 | 550.00 | 570.00 | 566.67 | 20.56 |
| 4 | S4 | 640.00 | 560.00 | 660.00 | 620.00 | 21.53 |
| 5 | S12 | 480.00 | 470.00 | 500.00 | 483.33 | 21.48 |
| 6 | S13 | 590.00 | 610.00 | 610.00 | 603.33 | 21.82 |
| 7 | S14 | 510.00 | 600.00 | 600.00 | 570.00 | 21.56 |
| 8 | S23 | 640.00 | 560.00 | 660.00 | 620.00 | 20.33 |
| 9 | S24 | 710.00 | 760.00 | 640.00 | 703.33 | 20.76 |
| 10 | S24 | 430.00 | 540.00 | 610.00 | 526.67 | 21.41 |

Note: The cube strength in N/mm2 is derived from dividing the force by 150×150mm2

##### TABLE 4.4 RIVER SAND IN N/mm2

| S/N | Point of observation | Replica 1 (KN) | Replica 2 (KN) | Replica 3 (KN) | Cube strength (KN) | Cube strength (N/mm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Sc1 | 650.00 | 640.00 | 590.00 | 626.67 | 20.71 |
| 2 | Sc2 | 765.00 | 830.00 | 700.00 | 765.00 | 20.71 |
| 3 | Sc3 | 580.00 | 550.00 | 570.00 | 566.67 | 20.56 |
| 4 | Sc4 | 640.00 | 560.00 | 660.00 | 620.00 | 21.83 |
| 5 | Sc12 | 480.00 | 470.00 | 500.00 | 483.33 | 21.48 |
| 6 | Sc13 | 590.00 | 610.00 | 610.00 | 603.33 | 21.82 |
| 7 | Sc14 | 510.00 | 600.00 | 600.00 | 570.00 | 21.56 |
| 8 | Sc23 | 640.00 | 560.00 | 660.00 | 620.00 | 20.33 |
| 9 | Sc24 | 710.00 | 760.00 | 640.00 | 703.33 | 20.76 |
| 10 | Sc24 | 430.00 | 540.00 | 610.00 | 526.67 | 21.41 |

For river sand a maximum compressive strength at a mix ratio of 1:2:4 was obtained and a lower compressive strength of 21.48N/mm2 at a mix ratio of 1:2:4 was obtained (Table 4.15). But Table 4.3 and Table 4.4 show increase in compressive Strength of river sand corresponding decrease in quarry dust content at 0.5 water/cement ratio. This may be due to the high water absorption property of quarry dust which left insufficient water in the mix for the complete hydration of cement. The quantity of coarse aggregate affected the strength of the concretes. The more the coarse aggregate in the mix, the lesser the compressive strength in the quarry dust as compared to river sand concrete.  The reason for this is that as aggregate quantity increases, the quantity of fine aggregate in the concrete is decreasing thereby reducing the aggregate surface area to absorb water, with consequence of increasing the free water content in the

concrete.

Generally, concrete having sand as fine aggregate is stronger than the corresponding one with quarry dust as fine aggregate. This can be seen from the results obtained because river sand concrete has greater number of concretes with higher compressive strength than quarry dust concrete. Theoretically, this is true because river sand has more granular particles than quarry dust hence less cement is needed for its bonding with coarse aggregate.  Although from researches carried out (Sahu et al 2003), it was found that crushed stone dust can be used effectively in the replacement of natural sand in concrete and that concrete made with this replacement can attain the same compressive strength, in this case however, replacement of natural sand with quarry dust is not only effective, it also caused increase in strength, though marginal. For example, for concrete made with river sand, the compressive strength is 21.48N/mm2 at water/cement ratio of 0.575 and a mix ratio of 1:2:4, while complete replacement of this sand with quarry dust, the compressive strength is the same with a value, this shows that the same compressive strength or even higher compressive can be obtained if river sand is completely replaced with quarry dust. Though in some other mix proportions, the compressive strength of concrete made with river sand has greater compressive strengths than the concrete made with quarry dust. For instance, from table 4.4 the compressive strength of most concrete made with river sand has greater value than their quarry dust counterpart of the same mix proportion. Also theoretically, it is clearly shown that the difference in texture between sand and quarry dust affect the strength. This also affected the variation of strength between the two fine aggregates.

#### Figure 4.1: Compressive Strength Against Mix Proportion (Quarry Dust)

#### Figure 4.2: Compressive Strength Against Mix Proportion (River Sand)

FIGURE 4.4

Figure 4.3: Compressive Strength Versus Mix Proportion (Quarry Dust)

#### Figure 4.4: Compressive Strength Versus Mix Proportion (River Sand)

##### TABLE 4.5 TABLE DENSITY OF QUARRY DUST CONCRETE IN Kg/m3

| Point of observation | A kg | B kg | C kg | AVG kg | DENSITY Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| Q1 | 9.77 | 8.88 | 8.01 | 8.89 | 2633.09 |
| Q2 | 9.66 | 9.57 | 9.03 | 9.42 | 2791.11 |
| Q3 | 8.67 | 8.64 | 9.09 | 8.80 | 2607.41 |
| Q4 | 7.83 | 8.95 | 8.85 | 8.54 | 2530.37 |
| Q12 | 9.29 | 9.05 | 9.05 | 9.13 | 2705.19 |
| Q13 | 8.90 | 9.21 | 9.22 | 9.11 | 2699.26 |
| Q14 | 9.28 | 8.98 | 9.37 | 9.21 | 2728.89 |
| Q23 | 8.98 | 9.16 | 8.39 | 8.84 | 2619.26 |
| Q24 | 9.11 | 9.26 | 8.87 | 9.08 | 2690.37 |
| Q24 | 8.99 | 9.26 | 9.15 | 9.13 | 2705.19 |

N/B: Density is derived from dividing the mass of cube in kg by volume of cube ( 0.15*0.15*0.15) in metre

##### TABLE 4.6 DENSITY OF QUARRY DUST CONCRETE IN Kg/m3

| Point of observation | A kg | B kg | C kg | AVG kg | DENSITY Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| Qc1 | 9.48 | 8.95 | 8.89 | 9.11 | 2699.26 |
| Qc2 | 8.69 | 9.00 | 9.01 | 8.90 | 2637.04 |
| Qc3 | 9.51 | 9.05 | 9.22 | 9.26 | 2743.70 |
| Qc4 | 8.74 | 9.43 | 9.22 | 9.13 | 2705.19 |
| Qc12 | 9.16 | 9.29 | 9.35 | 9.27 | 2746.66 |
| Qc13 | 9.38 | 8.97 | 8.94 | 9.10 | 2696.30 |
| Qc14 | 9.60 | 9.22 | 9.65 | 9.49 | 2811.85 |
| Qc23 | 9.79 | 8.97 | 9.18 | 9.31 | 2758.52 |
| Qc24 | 9.70 | 9.30 | 10.08 | 9.69 | 2871.11 |
| Qc24 | 9.47 | 8.69 | 9.14 | 9.10 | 2696.30 |

##### TABLE 4.7 DENSITY OF RIVER SAND CONCRETE IN Kg/m3

| Point of observation | A kg | B kg | C kg | AVG kg | DENSITY Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| S1 | 9.46 | 9.32 | 9.33 | 9.37 | 2776.30 |
| S2 | 9.45 | 8.98 | 9.32 | 9.25 | 2740.74 |
| S3 | 8.66 | 8.74 | 8.88 | 8.76 | 2595.56 |
| S4 | 8.96 | 9.33 | 8.97 | 9.09 | 2693.33 |
| S12 | 9.10 | 9.45 | 9.21 | 9.25 | 2740.74 |
| S13 | 9.52 | 8.93 | 8.83 | 9.09 | 2693.3 |
| S14 | 9.45 | 9.09 | 9.00 | 9.18 | 2720.00 |
| S23 | 8.89 | 9.25 | 9.15 | 9.10 | 2695.31 |
| S24 | 9.29 | 9.03 | 9.87 | 9.40 | 2784.20 |
| S24 | 9.00 | 9.57 | 9.58 | 9.38 | 2779.26 |

##### TABLE 4.8 DENSITY OF RIVER SAND CONCRETE IN Kg/m3

| Point of observation | A kg | B kg | C kg | AVG kg | DENSITY Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| Sc1 | 9.31 | 8.07 | 9.00 | 8.79 | 2604.44 |
| Sc2 | 9.29 | 9.70 | 9.10 | 9.36 | 2773.33 |
| Sc3 | 8.26 | 8.97 | 8.84 | 8.69 | 2574.81 |
| Sc4 | 9.02 | 8.79 | 9.02 | 8.94 | 2648.89 |
| Sc12 | 8.97 | 9.46 | 10.53 | 9.65 | 2859.26 |
| Sc13 | 9.17 | 8.62 | 9.38 | 9.06 | 2684.44 |
| Sc14 | 9.22 | 9.29 | 9.30 | 9.27 | 2746.67 |
| Sc23 | 9.56 | 9.35 | 9.20 | 9.37 | 2776.30 |
| Sc24 | 9.05 | 8.96 | 8.79 | 8.93 | 2645.93 |
| Sc24 | 8.60 | 9.40 | 9.58 | 9.19 | 2722.96 |

##### TABLE 4.9 SLUMP TEST RESULT (RIVER SAND) CONCRETE

| S/N | POINT OF OBSERVATION | VALUE (CM) |
| --- | --- | --- |
| 1 | S1 | 5.0 |
| 2 | S2 | 13.5 |
| 3 | S3 | 9.6 |
| 4 | S4 | 0.4 |
| 5 | S5 | 4.8 |
| 6 | S6 | 6.7 |
| 7 | S7 | 7.0 |
| 8 | S8 | 6.8 |
| 9 | S9 | 14.6 |
| 10 | S10 | 9.3 |

### 4.2	Discussion

Form workability test carry out on river sand and quarry dust, the following observation was made.

Table 4.9, shows slump test value for river sand (S).in table 4.9, it can be seen that river sand concrete which is the actual value having a good slump value or have a true slump. This means that the concrete workability is very good.

Observation

The following observations was made

- Quarry dust needs much water and cement in order for it to have good workability.

- The compressive strength of quarry dust and river sand are almost the same

##### TABLE 4.10 DENSITY AND SPECIFIC GRAVITY OF THE FINE AGGREGATES

| MATERIALS | MASS OF BOTTLE m1 (kg) | MASS OF BOTTLE +SAMPLE m2 (kg) | MASS OF BOTTLE + WATER m3 (kg) |
| --- | --- | --- | --- |
| cement | 0.03 | 0.08 | 0.1 |
| Quarry dust | 0.03 | 0.08 | 0.1 |
| Sand | 0.03 | 0.11 | 0.1 |

##### TABLE 4.11 SPECIFIC GRAVITY AND WATER ABSORPTION OF COARSE AGGREGATE

| MATERIAL | WT OF OVEN DRY SAMPLE A (kg) | WT OF SATURATED DRIED IN AIR B (kg) | WT OF SPECIMEN IN WATER C (kg) |
| --- | --- | --- | --- |
| COARSE AGG. | 5.000 | 5.025 | 3.110 |

WATER ABSORPTION TEST OF AGGREGATE RESULT

Weight of dry sample in air, A = 5000g

Weight of saturated surface dry sample in air, B =5025g

Weight of saturated sample in water, C = 3110g

Bulk specific gravity (oven dry) G.S = A/B-C =5000/5025-3110 = 2.611

Bulk specific gravity ( saturated surface dry)

B/B-C =5025/5025-3110 = 2.624

Water absorption   SPG = B-A/A = 5025-5000/5025×100 = 0.50

##### TABLE 4.12 SIEVE ANALYSIS RESULT (RIVER SAND)

| SIEVE SIZE | MASS OF EMPTY | MASS OF SIEVE + SOIL(g) | MASS OF SOIL RETAINED(g) | MASS OF SOIL PASSING(g) | PERCENTAGE PASSING |
| --- | --- | --- | --- | --- | --- |
| 1.18mm | 330 | 420 | 90 | 400 | 81.63 |
| 600µm | 320 | 400 | 80 | 320 | 65.31 |
| 425µm | 330 | 400 | 70 | 250 | 51.02 |
| 300µm | 300 | 350 | 50 | 200 | 40.82 |
| 212µm | 300 | 360 | 60 | 140 | 28.57 |
| 150µm | 330 | 360 | 30 | 110 | 22.45 |
| 75 µm | 210 | 270 | 60 | 50 | 10.20 |
| PAN | 270 | 320 | 50 | 0 | 0 |
| TOTAL |  |  | ∑R = 490 |  |  |

#### Figure 4.5: Percentage passing = mass passing/total mass of retained

##### TABLE 4.13 SIEVE ANALYSIS RESULT (RIVER SAND)

| SIEVE SIZE | MASS OF EMPTY SIEVE | MASS OF SIEVE + RETAINED | MASS OF SOIL RETAINED | MASS OF SOIL PASSING | % PASSING |
| --- | --- | --- | --- | --- | --- |
| 1.18mm | 330 | 360 | 30 | 440 | 93.62 |
| 600µm | 320 | 300 | 20 | 420 | 89.36 |
| 425µm | 330 | 430 | 100 | 320 | 68.09 |
| 300µm | 300 | 440 | 140 | 180 | 38.30 |
| 212µm | 300 | 400 | 100 | 80 | 17.02 |
| 150µm | 330 | 350 | 20 | 60 | 12.77 |
| 75 µm | 210 | 260 | 50 | 10 | 2.13 |
| PAN | 270 | 280 | 10 | 0 | 0 |
| TOTAL |  |  | 470 |  |  |

#### Figure 4.6: Sieve Analysis Result (River Sand)

## CHAPTER FIVE

## CONCLUSION AND RECOMMENDATIONS

### 5.1	Conclusion

The study results show that the addition of quarry dust improves the compressive strength of concrete. The study concludes that quarry dust may be used as partial replacement material for fine aggregate at up to 50% replacement, maximally in concrete. This study therefore concludes as follows;

1. 	Quarry dust may be employed as a quality replacement in concrete as fine aggregate,

2. 	Slump value decreases with increase in percentage replacement of sand with quarry dust due to higher percentage of smaller particles present in quarry dust compared to sand,

3. 	Compressive strength of concrete at 50% replacement has the highest value at all curing periods investigated,

4. 	It was observed during compaction test that the density of concrete increases with increase in percentage of quarry dust content, causing as expected increase in compressive strength as density of concrete increases,

5. 	Quarry dust being cheaper per cubic meter and environmentally friendly than river sand should be encouraged as alternative to river sand, if at partial replacement only,

6. 	Further research should be carried out to determine the long term strengths of quarry dust concrete and also the compressive strengths of quarry dust in reinforced concrete.

### 5.2	Recommendations

The following recommendations are made:

- Since from the test carried out and analysed quarry dust can effectively serve as a substitute to river sand in the production of concrete, it is recommend that it should be used in the production of concrete especially in areas that do not have rivers around them, like Ilorin and its environs.

- Since all the models developed were tested and found to be adequate for the prediction of concrete made with river sand/quarry dust, these models should be used to determine the compressive/flexural strength of concrete given mix proportions.

- From the charts developed those in Ilorin and its environs do not need to bother themselves on the mixes that can give a particular compressive/flexural strength, since it can be read off from the chart developed.

- Further works can be carried out on the effects of concrete made with quarry dust as fine aggregate from other sources apart from Ilorin

###### PLATE 1: WEIGHING OF CASTED CUBE

###### PLATE 2: COMPRESSIVE TEST MACHINE

###### PLATE 3: SLUMP TEST

###### PLATE 4: CONCRETE MIXING

###### PLATE 5: CUBE CASTING

###### PLATE 6: WEIGHT OF SAND

# REFERENCE

Abrams, D. A. (1927) “Water–cement ratio as a basis of concrete quality,” ACI Journal 23(2), pp. 452–457.

Aitcin, P. C., Lachemi, M., Adeline, R., and Richard, P. (1998) “The Sherbrooke reactive powder concrete Dootbridge,” Structural Engineering International 8(2), 140–144.

ASTM (1995). “Standard test method for time of setting of concrete mixtures by penetration resistance,” C-403, Philadelphia.

Caldarone, M. A. (2009) High-strength concrete: a practical guide, London: Taylor & Francis.

Collins, P. (2004) Concrete: the vision of a new architecture, Montreal: McGill-Queen’s University Press.

Day, L., and McNeil, I. (1996) Biographical dictionary of the history of technology, New York: Routledge.

Encyclopaedia Britannica, Inc. (1991) The new encyclopaedia Britannica, 15th edition, Chicago, IL: Encyclopaedia Britannica.

Gardner, N. J. (1990) “Effect of temperature on the early-age properties of type I, type III, and type I/fly ash concretes,” ACI Materials Journal (American Concrete Institute), 87 (1), 68–78.

Jin, X. and Li, Z. (2000) “Investigation on mechanical properties of young concrete,” Materials and Structures,RELIM , 33, 627–633.

Jin, X. and Li, Z. (2001) “Dynamic property determination for early-age concrete,” ACI Materials Journal,98 (5), 365–370.

Jin, X., Shen, Y., and Li, Z. (2005) “Behavior of high-and normal-strength concrete at early ages,” Magazineof Concrete Research, 57 (6), 339–34.

Jin, X., Shen, Y., and Li, Z. (2005) “Behavior of high-and normal-strength concrete at early ages,” Magazine of Concrete Research, 57 (6), 339–345.

Lee, H. K., Lee, K. M., Kim, Y. H., Yim, H., and Bae, D. B. (2004)“Ultrasonic in-situ monitoring of setting process of high-performance concrete,” Cement and Concrete Research, 34 (4), 631–640.

Lew, H. S. and Reichard, T. W. (1978) “Mechanical properties of concrete at early ages,” Journal of the American Concrete Institute, 75 (10), 533–542.

Li, Z., Xiao, L., and Wei, X. (2007) “Determination of concrete setting time using electrical resistivity measurement,” Materials in Civil Engineering, ASCE, 19 (5), 423–427.

Mindess, S., Toung, J. F., and Darwin, D. (2003) Concrete, 2nd ed., Upper Saddle River, NJ; USA, Pearson Education.

Neville, A. M. and Brooks, J. J. (1994) Concrete Technology, Longman. Pessiki, S. P., and Carino, N. J. (1988) “Setting time and strength of concrete using the impact-echomethod,” ACI Material Journal, 85, 389–399.

Ozama K., Mekawa, K., Kunishima, M., and Okamura, H. (1989) “Development of high performanceconcrete based on durability design of concrete structure,” Proceedings of the second East-Asia andPacific conference on structural engineering and construction (EASEC-2), 445–450.

Richard, P. and Cheyrezy M. (1995) “Composition of reactive powder concretes,” Cement and ConcreteResearch 25(7), 1501–1511.

Subramaniam, K. V., Lee, J., and Christensen, B. J. (2005) “Monitoring the setting behavior of cementitious materials using one-sided ultrasonic measurement,” Cement and Concrete Research 35 (5), 850–857.

Sutherland, J., Humm, D., and Chrimes, M. (2001) Historic concrete: background to appraisal, London:Thomas Telford.

U. S. National Research Council (1999), “Material science and engineering: forging stronger links to Users.”

Subramaniam, K. V., Lee, J., and Christensen, B. J. (2005) “Monitoring the setting behavior of cementitious materials using one-sided ultrasonic measurement,” Cement and Concrete Research 35 (5), 850–857.

Voigt, T., Ye, G., Sun, Z., Shah, S.P., and Van Breugel, K. (2005) “Early age microstructure of Portland cement mortar investigated by ultrasonic shear waves and numerical simulation,” Cement and Concrete. Research,35(5),858–8.