COMPRESSIVE STRENGTH OF CONCRETE WITH PALM KERNEL SHELL AS A PARTIAL REPLACEMENT FOR COARSE AGGREGATE

ABDULMALIK ADAM

ND/23/CEC/FT/0022

BEING A RESEARCH PROJECT SUBMITTED TO THE DEPARTMENT OF CIVIL ENGINEERING, INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILLMENT OF THE REQUIREMENTS

FOR THE AWARD OF NATIONAL DIPLOMA (ND)

IN CIVIL ENGINEERING, KWARA STATE POLYTECHNIC, ILORIN.

JULY, 2025

CERTIFICATION

This is to satisfy that this research study was conducted by Abdulmalik Adam (ND/23/CEC/FT/0022) and had been read and approved as meeting the requirement for the award of National Diploma (ND) in Civil engineering Department, Institute of Technology, Kwara State Polytechnic, Ilorin.

______________________						________________

ENGR. M. GARUBA						DATE

Project Supervisor

______________________						________________

ENGR. A NAALLAH							DATE

Head of Department

_____________________						________________

ENGR. DR. MUJEDU KASALI ADEBAYO				DATE

External Examiner

_____________________						________________

External Examiner								DATE

DEDICATION

This project is dedicated to Almighty Allah for the strength and power given to me to able to meet up the level and also spared my life, protect me and leading me to the right path throughout the duration of my course in Kwara State polytechnic, Ilorin. Glory be to Allah.

ACKNOWLEDGEMENT

Glory be to God for the meteoric metamorphosis of my seemingly inordinate and unattainable dreams, he sent loads of angel my ways, whose assistance are quite unquestionable. (Alhamdulilahi Robil Alamin).

I will like to take this opportunity to express my profound gratitude to my supervisor, ENGR. M. GARUBA Department of Civil Engineering, who provided insight and expertise that greatly assisted the research. He gave valuable feedback and constant encouragement, throughout the duration of the project, working under him was an extremely knowledgeable experience for me, I say a big thank you sir.

I also want to acknowledge the effort of my one and only parents,( MR AND MRS ABDULMALIK), I say a very big thank you, and I pray you would surely live to reap the fruit of your labour (Ameen).

I acknowledge the H.O.D and other staff member  of my department for creating the enabling atmosphere for this research work, many thanks to my lecturers for sharing their pearls of wisdom with me while I was studying for my National Diploma Programme and during this research.

I also appreciate my brother Abdulmalik  Kasim, and also my friend Mohammed Sanni for their love and support, you really mean a lot to me.

TABLE OF CONTENTS

Title page

Certification

Dedication

Acknowledgement

Table of content

CHAPTER ONE

1.0	Introduction									1

1.1	Statement of the Problem							3

1.2 	Aim and Objectives								4

1.3	Justification of the Study							5

1.4	The Scope of the Project							5

CHAPTER TWO: LITERATURE REVIEW

2.1	General Introduction								6

2.2 	Concrete									6

2.3 	The Palm Kernel Shell							11

2.4	 Properties of Palm Kernel Shell						12

2.5	Physical Properties Tests on Course Aggregate Grading Test		14

2.6	Result Of Slump Test slump 							21

CHAPTER THREE

3.1	Methodology									25

3.2	Material Procurement.								25

3.3	Material Treatment								26

3.4	Preparation of Material and Equipment					26

3.5	Procedure of the Concrete Cube.						26

CHAPTER FOUR

4.0 	Data Analysis									31

4.1	 Result as Collected								31

4.2 	Analysis and Discussion							31

CHAPTER FIVE

5.1 	Conclusion									38

5.2 	Recommendations								38

REFERENCE

CHAPTER ONE

1.0	INTRODUCTION

Many materials are used in construction industry. Concrete is one of such material, very widely used in many instances of most structural element. This is because the constituents material of concrete are easily obtained. Concrete is the world most consumed man made material (Naik, 2018).

Its great versality and relative economy in filling wide range of need has made it a competitive building material. Concrete production is not only a valuable source of societal development but it is also significant source of employment.

Production of concrete relies to a large extent on the availability of cement sand and coarse aggregate such as granite. The cost of which have risen astronomically over the past few year. Despite the rising cost of production, the demand for concrete is increasing. The negative consequences of the increasing demand for concrete includes depletion of aggregate deposited environmental degradation and ecological imbalance.

The possibility of complete depletion of aggregate resources in the near future can therefore not be over emphasized.

Rising construction costs and the need to reduce environmental stress to make construction sustainable, has necessitated research into the use of alternative materials, especially locally available one which can replace conventional one used in concrete production.

The use of such replacement materials should not only contribute to construction cost reduction and drive infrastructural development but should be able to contribute to reduce stress on the environment and make engineering construction sustainable to help transform the building and construction sectors of national economics and contribute towards the realization of national and global poverty reduction strategies such materials should be cheap and readily available. The cheaper building materials without loss of performance is very crucial to growth of developing countries (Zemke & Wood, 2019).

Historically, agriculture and industrial wastes have created waste management and pollution problems. Complement other traditional materials in construction provide both practical and economical advantages the waste generally have no commercial value and beinglocally available transportation cost in minimal (Chandra & Berntsson, 2022).

Agricultural wastes have advantages over conventional materials in low costconstruction. The use of waste materials in construction contribute to conservation of naturalresources and the protection of the environment (Ramezanian, Mahdikhani & Ahma Dibeni,2019). Investigating the use of coconut husk ash, com cob ash and peanut shell ash as cement replacement in concrete production.

The palm oil industry produces wastes such as palm kernel shell. Palm oil fibres which are usually dumped in the open thereby impacting the environment negatively without any economic benefits. Palm kernel shell (PKS) are hard, carbonaceous, organic by products of the processing of the palm oil fruit. Palm kernel shell consists of small size practices, medium size particles and large size particles in the range 0 - 5mm, 5 - 10mm and 10 - 15 the shell have no commercial value, but create disposal and waste management problem. In Ghana palm kernel shell are generally not used in construction they are used as fuel by local blacksmiths and as fill materials or as palliatives.

Investigating the comparative strength of concrete with palm kernel shell as a partial replacement for coarse aggregate in asphalt concrete.

As part of effort to make efficient use of locally available materials, this study was conducted to investigate and compare the influence of weight replacement and volume replacement of conventional aggregate by palm kernel shell on the workability, density and compressive strength of concrete as well as to assess the suitability of palm kernel shell concrete as a structural materials.

1.1	STATEMENT OF THE PROBLEM

The materials in construction can be defined as an item that can be permanently fixed in position as a component of the final products. Labour, equipment, management and finance are other major construction inputs, to facilitate and bring in the materials shape.

There is no doubt that there is now a high demand for various substitute materials in the construction industry in Nigeria due to ever increasing price of the conventional construction materials because materials input supersede all other input in building activities.

The following points are given so as to justify the uses of palm kernel shell as a partial substitute in concrete.

a. Availability: Palm kernel shell is readily available unlike gravel and granite, which involves a bit of bureaucracy at quarries.

b. The cost of acquiring natural coarse aggregate in the market is very high unlike the cost of palm kernel shell.

C. Possession of favourable chemical and physical properties by palm kernel shell is also added to its advantages.

d. Cost of production: Since palm kernel shell is a waste product, it requires little or no cost or production unlike high sum of capital involved in the production of gravel and granite.

1.2 AIM AND OBJECTIVES

The aim of this project is to test and compare the strength of concrete with concrete produce with palm kernel shell as a partial replacement for coarse aggregate.

The objective of this project is

- To determine the compressive strength of the concrete by the used of cube testing

processes at the curing ages of 7, 14, 21, and 28 days.

- To determine how to reduce the environmental waste.

- To determine the strength or palm kernel shell as a partial replacement of concrete.

1.3	JUSTIFICATION OF THE STUDY

This research work will help us to know if palm kernel shell can be used instead of granite and identifying the effect of palm kernel concrete with respect to the strength attained also the rate at which it is attained. As a result of increasing in the price of granite and gravel in concrete. It is important to look towards finding alternative building materials that could be substituted for granite and gravel in concrete.

1.4	THE SCOPE OF THE PROJECT

The scope of study is limited to determine the compressive strength of concrete produced with palm kernel shell as a partial replacement for coarse aggregate. which includes the compressive strength of concrete cubes at 7, 14 and 28days.

CHAPTER TWO

LITERATURE REVIEW

2.1	General introduction

Various research have been under taken to confirm the feasibility of using natural aggregate such as palm kernel shell as a partial substitute for coarse aggregate and light weight aggregate in concrete.

The research also based on how the substitution of this Agricultural waste materials will conserve dwindling resources and will avoid the environmental factors or problems and ecological damages caused by quarrying and exploitation of the raw materials for making cement. (Jackson 1999).

In this review of literature a concise approach shall be employed to give explanation on this project work with respect to the research materials, concrete, its properties, design and practical situations. Previous studies have shown that palm kernel shell posses similar properties with coarse aggregate and light weight.

2.2 Concrete

Concrete is a composite inert materials comprising of a binder course e.g cement, mineral filter (body) in aggregate and water. Aggregate on the other hand are two categories of fine (Sand) and Coarse (gravel or crushed stone) aggregate. The aggregate are usually graded from fine sand to stones of about 20rmm in diameter depending on the project to be executed.

Concrete is a man-made composite materials made up of natural aggregate like gravel, crushed rock and sand. Such aggregate particles are bound together using a binding medium made up of cement and water. It is reported that good concrete is that which is dense and non-porous and as such the proportion of fine aggregate present in any given mix ratio should not fall short or exceed that proportion that would fill the spaces present in the coarse aggregate. (Neville A.M.2001).

The amount of water added to any concrete mix should be that which would allow for proper workability and this amount of water is usually determined considering the water cement ration and aggregate cement ratio. The mathematical equation of the water-cement ratio and aggregate cement ratio are show below:

Water-Cement Ratio 			=	Mass of water.....(1)

Mass of Cement

Aggregate Cement ration		= 	Mass of aggregate (ii)

Mass of cement

Combing equation 1 and 2

Mass of cement			=	Mass of water

Water cement		=	 mass agg.

Agg-cement ration

Fresh concrete exist in a plastic state and due to its fluidity can take the shape of any mould or formwork it is poured into.

Table 2.1				Properties of concrete

Strength in tension			concrete

Strength in compression		good

Strength in shear			fair

Durability				Good

Dire					Good

Source: Mosley and Bunger (1992).

Typical concrete mixes are proportioned by absolute weights.

Table 2.2

Satish Chandra. waste materials used in concrete manufacturing

Concrete can also be classified based on place and for type of production i.e.

1. in-situ

2. Pre-cast

3. Ready mix

4. Un-rein forced

5. Light weigh concrete

Definitions

- In-situ concrete: This is concrete produced on site, poured and cured at its final positions as a beam, slab, and column etc.

- Pre-cast: This describes a variety of concrete unit produced, cast and cured in moulds in factory or site other than their final position. These types of concrete are used usually when there is need for tensioning.

The structure either pre-tensioning or pos-tensioning pre-cast concrete is used as roof quitters. Lintels, stair case unit, Kerbs, brick etc.

(c)Ready-mix Concrete: This is used to describe concrete mixed at one location usually a batching plant and transported to site via a rotating drum mounted on a truck.It is used mostly when large volumes of concrete are required

(d)Un-reinforced Concrete: This is sometime referred to as mass concrete. The resulting concrete here has considerable compressive strength but low tensile stresses due to bending, shear, and torsion. These types of concrete can be used for thick spread foundation and also in a mass retain wall.

(e) Reinforced concrete : This is a concrete in which steel is embedded in such a manner that the two material act together in resisting force, the reinforcing steel rods, bans or mesh absorb the tensile, shear, and sometimes  compressive stress in a concrete structure.

Generally speaking any concrete when subjected to a loading is stronger on compression  than in tension (British cement association 2001)

2.3 The Palm Kernel Shell

The kernel seed of oil palm is covered by the shell. A single gene controls, the shell thickness. Oil palm is now a major produce in some tropical countries of the world, the major producers in the world today include Malaysia (higher producer), Nigeria.

Table 2.33 World Production of Oil Palm

Oil palm shell is the hard endocarp that surrounds the palm kernel fruit used in the production oil palm oil. The oil palm industry in Malaysia account for over half of the worlds total palm oil output problem contributing as much 2.6 million tones of solid waste in form of oil palm shell annually (Basriet AL 1998). Oil palm shell is light and naturally sized and ideals for substitution as aggregate in light weight concrete construction. Due to their hardness and organic virgin, they will not contaminate or leach to produce toxic substances once they are bound in concrete matrix.

Oil palm shell concrete is the best suited for light weight concrete application that require low to moderate strength such as pavement and infilling panels for floorings and Well and foot bridge. Currently. There is also an increasing demand for low-cost houses in Malaysia and therefore palm kernel shell can be used as alternative to the conventional aggregate in fulfilling this demand.

The shells are lack and surface textures are fairly smooth for both concave and convex laces while the broken edges are rough and spiky.

Table 2.4 Physical Properties of Oil Palm Shell and Crushed stories

2.4 Properties of Palm Kernel Shell

The properties of palm kernel shell that are considered of importance in this work includes the shape, size the void ratio, crushing strength durability water absorption rate thermal conductivity and moisture content.

- Shape and Size: Palm kernel shell after cracking the nut is remove. The kernel inside assume an irregular shape and size. the cracking 1s done manually with aid of a stone or using mechanical by using a palm null cracker.

As a light weight aggregate, it has the advantages of being able to insulate the walls to prevent excessive exchange of heat between the inside and the outside Of  the structure

- Void ratio: As a result of the irregular shape and Sizes of the shell a lot of voids will be created inside the concrete. The pores will be created within the concrete makes it permeable to water, which can lead to frost action. Frost weakens the structure and reduced its life span.

- Water Absorption Rate: A good coarse aggregate and light weight  aggregate should be stabled in mature. The affinity rate should be stabled immature. The affinity for water must be very if  the materials absorb water at a high rate, it will lead to an increase in us bulk density when Subjected to a continuous wetting and drying the collapse of the structure may soon be imminent. Palm kernel shell has a relatively to absorption rate when it immersed in water.

- Moisture Content: In its natural state, Palm Kernel shell contain very low moisture. If the moisture content is high, it will affect the workability of the concrete paste and difficult will be faced in determining the water Cement ratio. Before being used as a light weight aggregate the moisture content in dry bores must first be in a weathering chemical action and wear. The internal Coarse are the effect on interaction between the materi1als and other constituent materials to make up the concrete. These includes alkali aggregate reaction, volume change, absorption and permeability. Palm kernel shell has been found to be chemically inactive either in alkali or acidic conditions, hence it could be stable when used as a lightweight aggregate.

- Thermal Conductivity: Thermal conductivity is a measure of flow of heat through a material. It is measured in walls per unit meter, Per unit meter in temperature. A research carried out by Folayan (1988), on the measurement of thermal conductivities of oil palm kernel shell and fiber shows that about 0.12 wrn-1 at 70°c. This is a good property of aggregate for a light weight concrete as it is resistance to heat flow is low.

2.5	Physical Properties Tests on Course Aggregate Grading Test

Grading Test is carried out in materials to know the population of different sizes of particles in making up. The materials BS 410 gives the guideline for carrying out the test. In the test carried out in he coarse aggregate, a known weight of a sample was allowed to pass through a set ofsieves o progressively smaller openings by the use of mechanical shaker.

- Unit weight: Unit weight of a sample is the ratio of a given weight of the sample to the volume it occupies. The volume comprises of the voids between and within the particles. To determine the bulk density of palm kernelshell. It is the weight of aggregate that will fill the container of unit volume and this depends on the grading distribution, aggregate shape and degree of compaction.

The difference in the volume of the container and that of water used to fill up the void in sample was noted and actual volume occupied by palm kernel shell in the container estimated. The bulk density for loose aggregate and test method would also different. The un-compacted bulk density determined for palm kernel shell sample is given below.

Weight of empty container			=	w i

Weight container plus sample		=	w2

Volume of empty container			=	V

The unit weight of the sample is the ratio betweenthe weight of the sample to the actual volume it occupieddivided by the volume.

Therefore, Bulk density 		=	W2 WL

V

For the given palm kernel shell sample weight of sample

filling mould 			=	0.582kg

Volume of mould used 		= 	9.423x 10-3m3

Bulk density	 = 0.582			=	61.76m3

9.423x10-3

Comparing the bulk density value of palm kernel shell withthat of their light weight aggregate like

- Expanded shale and day made by sin star standprocess.

- Expanded blast furnace slag. it was concluded thatpalm kernel shell can be used as light relatively low.(Okpala 1990).

2.Moisture Content: This is the amount of moisture present with and  on the surface aggregate materials (treemoisture)The absorbed moisture and free moisturetogether gives the total moisture content of the aggregate.For give sample of palm kernel shell. The moisture contentwas determined using drying method and the resultexpressed either as a percentage of the sample dry weight oras a percentage of it weight.

Moisture content is given as Mc =Ww--Wd x100

Wd

It should be noted that palm kernel shall whencompared to normalweightaggregate have higherabsorption rate and this range between 21.7% 24% acorresponding moisture content between 14.90%-15.6%(Akomolafe, 1998).

Laboratory Test conducted on two samples of palmkernel shell gives the following result.

Table 2.5Moisture Content of palm kernel shell

Adeyemi 1998.Use of palm kernel shell as partialreplacement in concrete.

In order not to exceed the water cement ratio for anygiven concrete mix. The water absorption rate and moisturecontent of the palm kernel shell should be known. Knowingthat moisture content of palm kernel shell has a greatinfluence on the workability and strength of the hardenedconcrete.

- Void Ratio: for any given aggregate, the ratio of volumeoccupied by void to that volume occupied by solid is calledvoid ratio. Aggregate with small volume of ratio produce concrete  with low drying shrinkage and thermal movement.With the apparent specific gravity(s) and the bulk densknown as void ratio is calculated from the expression.

Void ratio =	1 - bulk density

5 x [unit weight of water)

For palm kernel shell,

Void ratio = 1-617.64

1.307x 10o		=	0.528

Thus, it can be concluded that for palm kernel the ratio isalmost one (1). therefore palm kernel shell can be predictedto produced concrete of moderate drying shrinkage andthermal movement.

- Grading Analysis: T his is a process of defined sizedistribution within any given aggregate sample usingstandard test sieve determined by the diameter of itsopenings. the sieve are arranged in the order of  reducing mesh diameter i.e. sieve with large openings are placed ontop sieve with smaller hereby given a progressivelyreducing mesh diameter which would only allow very lineparticles to pass through.The sieves are usually mounted in a frame and materials, retained in each sieve after shaking a sample through isweight and record. Result of a mechanical sieve analysisis usually represented graphically on grading curves with aWell defined range of upper and lower limits.

The dividing line between the fine and coarse aggregate isthe mm sieve size. It should however be noted thataggregate size are affected by the action of water thataccompanies the production of such aggregate and theirhandling on any job site.

Grading requirement of Bs 88:2 1973 allows between 5and 15 percent were size and between 5 and 10 percentunder size material for any concrete mix.

- Workability Test: Workability is a physical properties ofconcrete. which describe the case with  (ASTM andBritish code of practice)from a point of mixing to it final compacted stage. The workability of a given concrete lendto affect the quality of the fresh concrete and the hardened concrete

The test already  reported f or determining workability ofconcrete s given below.

- Slump test

- V-B consistometre test

- Compaction factor test

These tests usually do not give a fill physical assessmenton the concrete consistency. compatibility or mobilityinstead act as practical guide on the workability of a mix inaccordance with standards such as the British standards.Slump test described in BS 1881: Part 2.

Apparatus

- Mould (slump cone 300mm high)

- Tapping rod

- Flat base plate

- steel ruler

- trowel

Aims

To measure consistency of fresh concrete and detect andchanges in workability.

Also to control the waste content in various mix batches

Procedure

- Place cone on the flat base plate with the larger diameteropening of the cone resisting firmly onthe plate.

- Fill the cone in lour layer in which each layer receiving25 tamping with the aid of a standard 16mmdiameter steelrod rounded a the end.

- Level the top of the cone using bricklayer trowel.

- Live cone vertically and solely in order to allow theunsupported concrete to slump

- Place empty cone beside the slumped concrete. Placethe rod across it and cone  beside the slump from the top ofthe slump concrete to the botton of the rod. This heightdifferences is regarded as the slump for a particular batchfornormal weight concretesamplea slump of 25-100 is regarded of medium workability  10-50mm as 1owworkability and less than 10mm as very low workability(Neville, 1987). it has been reported that are increased in water content is required where palm kernel shells arepartially introduced in to the lightweight aggregate concreteis reported to have a lower slump than normal weightconcrete due to a reduced gravitational force in lightweightcoaggregate concrete (Neville, 2001).

Thus. For a light weight aggregate concrete using Pksa slump of 50-75mm represent a high workability and aslump in excess of 75-100 may cause particle segregation

Basri et al 1998).Table

2.6 Result of slump testSlump

Precaution

- The thickness of layers were kept fairly constant

- The cone and base were properly oiled avoid honeycombing.

- Carefully removal of cone was ensured avoiddissertation during concrete pouring and tamping. V.B Consistometer Test

Apparatus

- V-B consistometer consisting of slump cone

- Shell metal container

- Vibrating table

- Funnel and transparent disc

- Scope

- Ramping rod

- Stop clock

Aim

Is  to measure workability of concrete in terms of vibration.

Procedure.

- Fill concrete sample into the slump cone using the scoop

- Place the transparent disc on the concrete

- Switch vibration t able on.

- Measure the time taking for the concrete to completelycover the underside of  he transparent disc starting fromwhen the table was switch on.

Observation

It is reported that rich mixes almost immediately remoldinto a cylindrical from when the slump cone is removed.

Precautions

- Adequate accuracy was ensure during the timingprocess

- Vibration was done under a three phase power supply.So as not to reduce the time  of a  total remolding

7.	Compressive Strength Test

The strength of concrete is define on the maximum loadit can carry.

The strength of  hardened concrete change with age andenvironment in an increase manner. Concrete compressiveis Commonly used for the purpose of specification  quality control as started in  the British standard of codes.

Compressive strength is defined as the maximumcompressive 1oad an element of hardened concrete cancarry per area. t is reported that specimens forcompressive Strength test can be cast in three (3) shapewhich are cubes, cylinder and prisms but the cubes aremost widely used.

The cube moulds are usually 150mm x 150mm x 150mmand they are cost with the same concrete for structuralelements. The inner surface of the mould is coated thinlywith mould oil in order to avoid bond between concrete andmould. Concrete is poured into the mould in three 3)layers with each layer being compacted with 35shokes oftamping road.

Scrape off excess concrete On the mould and smoothenSurface. The mould is removed after 24hr and the cubeskept  in a water bath unit their age is ripe for testing(Crushing). The crushing ages are 28 days each cubes isremoved from the water bath and placed in a concrete cubecrushing machine to crush under increasing load. Loadsat final failure of  the cube are recorded as crushing load.

The compressive Strength of the cubes is calculated usingthe expression below.

Compressive strength 		= 	Crushing load (w)

Cube area ( mm2)

The reading is then recorded against the cube. Three (3)readings Were obtained from each percentage constituent ofpalm kernel shell and the average determined.

CHAPTER THREE

3.0	Methodology

3.1	It 1s very important to give details of the procedureto be adopted in this research work and this would includethe sourcing of  materials, step invalid in their conversion,experimental test carried out toknow the physicalproperties etc.

The procedure to be adopted in carrying out this research work is divided into three [3). Stage

- The design of mix proportion

- the procurement and preparation of materials

- The mixing of concrete casting and curing.

3.2	Material Procurement.

- Ordinary Portland cement. Confirming to BS 12 (1996)was used in the concrete and production

- Fine aggregate (sharp sand)

- Coarse aggregate (Granite size 20mm)

- Water

- Painting brush

- Palm kernel shell

- Lubrication oil

- The tools involved during the cube concreteproduction stage are shovel, head pan.

3.3	Material Treatment

The palm kernel shell was washed thoroughly withdetergent, to further remove palm oil form the shell andother impurities that could be detrimental to concrete, andthen rinsed with water thrice to remove the detergent usedin washing the palm kernel shell.

3.4	Preparation of Material and Equipment

The palm kernel shell was thoroughly cleaned to removeddirt and was later spread on the floor for proper drying. TheSand after transporting was sieved to remove stones andOther unwanted materials that might have been transportedalong with it.

The sand was allowed to dry appreciable so that when feltwith hand does not contain a great amount of moist. black oil was used as a primer to the surface of the mould, So that when removing the mould the concrete will not behaving  cracks.

3.5	Procedure of the concrete cube.

The steps involved in the production of the concrete for this research work are outline below

- Mould acquisition

- Mix design

- Hand mixing procedure

- Concrete production and pouring

- curing of the cube

- Crushing test

3.5.1	Mould acquisition

The mould used for this research work was collected fromKwara State Polytechnic Laboratory of Civil EngineeringDepartment and the mould dimension is 150x150x150mm,the formwork is made of metal. The mould coated with usedof black oil to facilitate mould removal and avoid honeycomb in the cube. The specimens were made in accordancewith Bs 1881 (1996).

Diagram

150mm x 150mm x 150mm

Figure 3.1 Shows the diagrammatic representation of themould for the experiment.

3.5.2 	Mix Design

Numerous method of mix design are in use but all can becategorized either by weight or volume. Batching weight bymaking use of weighing spring balance to carried out thequality of different constituents.

Mixing by weight of concrete is more specific than byvolume because of the avoid ratio of the aggregate. Themass of each constituent was determined relatively to the mass of cement required in the mix.

3.5.3	Hand Mixing Procedure

The aggregate s spread in a uniform layer on hard clears and non-porous base.Cement is then uniformlySpread over the aggregate and the dry materials are mixedby turning over from one end to the other and cuttingwith a shovel until the mix appears uniform.

Water is then gradually added so that neither water norwater with cement can escape.

The mix is then mixed again until it appears uniform incolor and consistency. It is important to note inmodern days, Concrete is mixed using mechanical mixersand when large quantities are needed, the batching plant isput to use. When using mixers, it is important to note theminimum mixing time necessary to produce a concretemixing. it is not actually the time, but the total number ofrevolutions done by the mixer and this depends on the typeof mixer. Since there is an optimum speed of rotationrecommended by the manufacture of mixer. The number ofrevolutions and time of mixing are interdependent for smallquantitiesof concrete like the quantity of this experiment,hand mixing method is employed.

3.5.4	Concrete Production and Pouring

This study utilized two control mixes ratio of 1:2:4,batched by volume and 1:2:4, batched by weight. Thepercentage replacements of the aggregate by palm kernelshell are 0%. 30%. 60% ,90%, 100% by volume and byweight respectively.

Concrete pouring is the process of transferring the freshconcrete from the point to mixing to its final compactedstate with the mould. Neat polythene was placed on levelground and the mould was placed on it. Steady compactionwas maintained during the process of concrete pouring.

3.5.5	Curing the Cube

Curing is the process that describes the gradualattainment of strength due to transformation of freshconcrete to hardened concrete.After 24hours, theformworks were strike and concrete cube were immediatelyfully immersed in a ready made. Long period of moist curing reduces the incidence of cracking (Kong and Evans 1994 )

Concrete are Cured Under Moist Condition

Ensure that moisture is available to hydrate the cement.Reduce the rate at which initial drying shrinkageOccur in order to minimize cracking

-Reduce the permeability and increase the durability ofconcrete.

-Curing period of  7,14, 28 days are reported here.

The compaction factor apparatus was used to assessworkability of the fresh concrete. The concrete cubes werecrushed using Matest Digital Compression Machine, whichautomatically evaluate both the compression load and thecompressive stresses at failure and displays the results onLCD screen. The cubes were removed from the curing tankand let in the open air for about two hours before crushing.

All tests were conducted at the material laboratory of theDepartment of Civil Engineering of the Kwara StatePolytechnic.

CHAPTER FOUR

4.0 DATA ANALYSIS

This chapter shows the result of the investigation how variation in a comparatives study on the compressive strength of concrete produced from palm kernel shell concrete and granite with conventional Aggregate.

4.1 RESULT AS COLLECTED

The table below shows the result obtained from the compressive testing of the concrete cubes.

Compressive strength result for palm kernel shell concrete and granite at 0% for control Normal ratio 1:2:4.

4.2 ANALYSIS AND DISCUSSION

The following are the fact drawn out based on the best result collected from the laboratory

1. The weight of each cubes differs even through 150mm' mould was used throughout in this study

2. The compressive strength of the concrete cubes decreases as the percentage of palm kernel shell is increase than that of granite

3. It was noticed that in the process of using palm kernel shell only as coarse aggregate, the weight of the cube is low compared to other cubes

4. The concrete made of palm kernel shell only also have lowest compressive strength at 7, 14, 28 days.

5. The crushing lead of the concrete cube decrease as the percentage of palm kernel shell increase.

Table 4.1	compressive strength result for palm shell concrete and granite at 0% for control.

| Date of cast | Identification mark | Age of cube | Cube size (mm2) | Dry weight to cube (kg/m3) | Dry density (kg/m3) | Failure load | Compressive strength (N/mm3) | Average comp strength (N/mm3) | Average dry density (kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 08-03-2025 | 1 | 7days | 150×150× 150 | 8.036 | 2381.40 | 380 | 16.9 | 14.45 | 2379.95 |
|  | 2 |  |  | 8.032 | 2378.25 | 270 | 12.0 |  |  |
| 08-03-2025 | 1 | 14days | 150×150× 150 | 8.250 | 244.44 | 470 | 20.9 | 18.90 | 2439.26 |
|  | 2 |  |  | 8.215 | 2434.07 | 380 | 16.89 |  |  |
| 08-03-2025 | 1 | 28days | 150×150× 150 | 8.108 | 2402.3 | 520 | 24.4 | 25.3 | 2408.55 |
|  | 2 |  |  | 8.150 | 2414.8 | 590 | 26.2 |  |  |

Table 4.2: compressive strength result for palm shell concrete and granite at 5% for control

| Date of cast | Identification mark | Age of cube | Cube size (mm2) | Dry weight to cube (kg/m3) | Dry density (kg/m3) | Failure load | Compressive strength (N/mm3) | Average comp strength (N/mm3) | Average dry density (kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 08-03-2025 | 1 | 7days | 150×150× 150 | 7.723 | 2288.30 | 260 | 11.56 | 11.23 | 2263.71 |
|  | 2 |  |  | 7.557 | 2239.0 | 245 | 10.89 |  |  |
| 08-03-2025 | 1 | 14days | 150×150× 150 | 7.350 | 2177.778 | 290 | 12.89 | 12.23 | 2148.149 |
|  | 2 |  |  | 7.15 | 2118.519 | 260 | 11.56 |  |  |
| 08-03-2025 | 1 | 21days | 150×150× 150 | 6.546 | 1937.7 | 320 | 14.22 | 14.33 | 1917.0 |
|  | 2 |  |  | 6.400 | 1896.30 | 325 | 14.44 |  |  |

Table 4.3:	compressive strength result for palm shell concrete and granite at 10% for control.

| Date of cast | Identification mark | Age of cube | Cube size (mm2) | Dry weight to cube (kg/m3) | Dry density (kg/m3) | Failure load | Compressive strength (N/mm3) | Average comp strength (N/mm3) | Average dry density (kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 08-03-2025 | 1 | 7days | 150×150× 150 | 7.765 | 2300.74 | 230 | 10.22 | 9.82 | 2228.74 |
|  | 2 |  |  | 7.279 | 2156.75 | 212 | 9.42 |  |  |
| 08-03-2025 | 1 | 14days | 150×150× 150 | 7.330 | 1272.15 | 267 | 11.87 | 11.83 | 2160.5 |
|  | 2 |  |  | 7.250 | 2148.15 | 225 | 11.78 |  |  |
| 08-03-2025 | 1 | 28days | 150×150× 150 | 6.560 | 1943.7 | 320 | 14.22 | 14.11 | 1922.95 |
|  | 2 |  |  | 6.420 | 1902.2 | 295 | 14.00 |  |  |

Table 4.4:	compressive strength result for palm shell concrete and granite at 15% for control

| Date of cast | Identification mark | Age of cube | Cube size (mm2) | Dry weight to cube (kg/m3) | Dry density (kg/m3) | Failure load | Compressive strength (N/mm3) | Average comp strength (N/mm3) | Average dry density (kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 08-03-2025 | 1 | 7days | 150×150× 150 | 7.01 | 2077.33 | 192 | 8.53 | 8.05 | 2025.48 |
|  | 2 |  |  | 6.66 | 1973.63 | 170 | 7.56 |  |  |
| 08-03-2025 | 1 | 14days | 150×150× 150 | 6.76 | 2002.07 | 270 | 12.0 | 11.6 | 2016.29 |
|  | 2 |  |  | 6.85 | 2030.52 | 252 | 11.2 |  |  |
| 08-03-2025 | 1 | 28days | 150×150× 150 | 6.510 | 1929.0 | 322 | 14.31 | 13.94 | 1899.32 |
|  | 2 |  |  | 6.360 | 1869.63 | 305 | 13.56 |  |  |

Table 4.5	compressive strength result for palm shell concrete and granite at 20% for control.

| Date of cast | Identification mark | Age of cube | Cube size (mm2) | Dry weight to cube (kg/m3) | Dry density (kg/m3) | Failure load | Compressive strength (N/mm3) | Average comp strength (N/mm3) | Average dry density (kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 08-03-2025 | 1 | 7days | 150×150× 150 | 6.912 | 2048.00 | 144 | 6.40 | 6.14 | 2047.71 |
|  | 2 |  |  | 6.910 | 2047.41 | 132 | 5.87 |  |  |
| 08-03-2025 | 1 | 14days | 150×150× 150 | 6.694 | 1983.41 | 175 | 7.78 | 8.73 | 1980.44 |
|  | 2 |  |  | 6.674 | 1977.48 | 167 | 7.42 |  |  |
| 08-03-2025 | 1 | 28days | 150×150× 150 | 6.35 | 1881.48 | 336 | 14.9 | 14.5 | 1866.64 |
|  | 2 |  |  | 6.26 | 1854.8 | 256 | 12.71 |  |  |

Table 4.6	comparisons of compressive strength of normal concrete with concrete mix of palm kernel shell.

| Days | Compressive strength of normal concrete (N/mm2) | Compressive strength of 5% replacement of palm kernel (N/mm2) | Compressive strength of 10% replacement of palm kernel (N/mm2) | Compressive strength of 15% replacement of palm kernel (N/mm2) | Compressive strength of 20% replacement of palm kernel (N/mm2) |
| --- | --- | --- | --- | --- | --- |
| 7 | 14.45 | 11.23 | 39.82 | 8.05 | 6.14 |
| 14 | 18.90 | 12.25 | 11.83 | 11.06 | 18.73 |
| 28 | 25.3 | 14.33 | 14.11 | 13.94 | 13.8 |

CHAPTER FIVE

5.1 CONCLUSION AND RECOMMENDATION, CONCLUSION

From the result obtained the following conclusion were arrived at.

- The density of concrete cube decrease quite significantly as the percentage by constituted of palm kernel shell is increases from 1620.5kg/m3 to 1036.14kg/m3 at 0% to 20%.

- The crushing strength of the concrete cube slightly decreases as the percentage of palm kernel shell increases.

- Palm kernel shell produced light weight concrete with optimum level of workability.

- The decrease of concrete cube is affected due to partial replacement of palm kernel shellinstead of granite.

5.2 RECOMMENDATION

The test and studies carried out are limited to some extent though improvement have beenmade over past works and as such, for the purpose of future works, the following recommendation are made.

• The effect of age on the physical properties of palm kernel shell should be studied. This means that to find out if there is any variation in the physical properties due to age and also to pre determine the behaviour of palm kernel shell under loading as the age increases.

• A study in to the physical properties and compatibility of palm kemel shell with other agricultural and product liker rice husk, coconut shell, and oil palm clinker should be under taken.

• Through the result indicate the possible use of palm kernel shell as a structure material.

So it is recommended that long term behavior should be investigated to evaluate thispossibility.

• Plasticizer should be used in work involve palm kernels shell concrete.

• Based on the result obtained replacement of 15% crushed granite by palm kernel shell involume batched concrete can be used in reinforcement.

REFERENCE

A.A Rame Zanian Pour, Mahdikhani and M. Ahmadebeni (2019). The Effect of Rice Husk Ash on mechanical properties and Durability of Sustainable. concrete International Journal of Civil Engineer. 7 (2) 83-9

A.P Adewuyi and B.F ola (2021). Application for water works Sludge as Partial Replacement for Cement in concrete Production. Science Focus.

C. Sashider and His. Rao (2018). durability studies on Concrete with wood Ash Additive. 35 th conference on our World in concrete August 2010, Sign apore.

NZamke and Ewoods (2019) Rice husk Ash California Polytechnic State University.

F.A Olutoge (2020). Investigation on Saw dust palm kernel shell as aggregate replacement.

APRN Journal of Engineering and Applied Science. 5(4), 7-13

T. R Naik (2017) Sustainability of Concrete construction. Practice Periodical on Structural

Design and Construction 13(2), 98-128.