SUITABILITY OF SELECTED SILICA SANDS IN KWARA STATE FOR FOUNDRY APPLICATIONS

BY

CHUKWU EZRA CHIJIDEM

HND/23/MET/FT/007

SUBMITTED TO THE

DEPARTMENT OF METALLURGICAL ENGINEERING, INSTITUTE OF TECHNOLOGY,

KWARA STATE POLYTECHNIC, ILORIN, NIGERIA.

IN PARTIAL FULFILMENT OF THE REQUIREMENT FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN METALLURGICAL ENGINEERING TECHNOLOGY

JULY, 2025

CERTIFICATION

This is to certify that this project work was carried out by Chukwu Ezra Chijidem with Matric Number: HND/23/MET/FT/007 has met the requirement and regulations governing the award of Higher National Diploma (HND) in Metallurgical Engineering Technology, Kwara State Polytechnic, Ilorin and under the supervision of the project supervisor.

_________________________				_________________

ENGR. A. S. ADESINA						DATE

Supervisor

_______________________				_________________

ENGR. D. A. ADEGBITE					DATE

Head of Department

_______________________				_________________

EXTERNAL EXAMINER 					DATE

DEDICATION

This project is dedicated to Almighty God for sparing my life, for his mercy, divine protection, for being my guidance and shining of his light on my pathways from the beginning of my Diploma till the end.

ACKNOWLEDGEMENT

Firstly, I wish to express my profound gratitude to Almighty God who has been the source of my strength, for sparing my life all these years. Also, my sincere gratitude goes to my project supervisor; Engr. A. S. Adesina for creating time out of his tight schedule to go through my project, I say a big thank you. I also appreciate all my lecturers in the department.

My in-depth and immeasurable thanks goes to my loving, caring and courageous parents, who are structural designers and the pillar I rely on for making my dream a reality through their support financially, physically, morally and spiritually.

Finally, I appreciate the efforts of my beloved family and friends. May Almighty God bless you all you.

ABSTRACT

The suitability of selected silica sands in Kwara State for foundry applications were carried out in the three regions of Kwara State viz: Kwara central (Oloje), Kwara South (Ajase-Ipo) and Kwara North (Tsaragi). It is an established fact that silica sand is one of the many important variables that dictates or determines the quality and soundness of casting. In view of this, it becomes expedient to know the inherent properties of the silica sand that makes it more suitable for a specific application. Three out of important properties of silica sand that are required during casting processes are carried out in this study. These properties are green compressive strength, green shear strength and moisture content. The results showed average mechanical properties of the natural moulding sands’ samples to include grain finess number for Oloje silica sand to be 66.45, Ajase-Ipo silica sand to be 68.03 and Tsaragi silica sand to be 67.81. Also, their green compressive strength, green shear strength and moisture content were all within the required standards for casting of non-ferrous metals. In the foregoing of all these, it was concluded that the silica sands at Oloje, Ajase-Ipo and Tsaragi are relatively fine and can be used for zinc casting, or any non-ferrous metals e.g. aluminum, copper etc. It can also be employed for small and medium light weight iron castings.

TABLE OF CONTENTS

Title page										i

Certification										ii

Dedication										iii

Acknowledgement									iv

Abstract										v

Table of contents									vi

List of Tables										ix

List of Figures										x

CHAPTER ONE

1.0	INTRODUCTION								1

1.1	Background of the Study							3

1.2	Statement of the Problem							4

1.3	Significant of the Study							4

1.4	Aim and Objectives of the Project						5

1.5	Scope of the Study								6

CHAPTER TWO

2.0	LITERATURE REVIEW							7

2.1	Moulding Sands								8

2.2	Principal Ingredient of Moulding Sand					9

2.2.1	Silica sand grains							9

2.2.1.1 Rounded grains						9

2.2.1.2 Sub angular grains						10

2.2.1.3 Angular grains							10

2.2.1.4 Compounded grains						10

2.2.1.5 Sands								10

2.2.2 Bonding clay								12

2.2.3 Moisture 								13

CHAPTER THREE

3.0	MATERIALS AND METHOD

3.1	Collections and Preparation of Materials					14

3.1.1 	Silica Sand								14

3.1.2	Preparation of the standard test specimens				14

3.2	Method									15

3.2.1	Green compressive and green shear strength 				15

3.2.2 Permeability 								15

3.2.3 Moisture content							16

3.2.4 Sieve analysis								16

CHAPTER FOUR

4.0	RESULTS AND DISCUSSION

4.1	Data and Results								17

4.2	Discussion of Results								26

4.2.1 Green compressive strength						26

4.2.2	Green Shear Strength 							26

4.2.3 Moisture content							27

4.2.4 Grain size								27

4.2.5 Surface finish of the casting						27

4.2.5.1 Surface finish of the casting using Oloje sand		28

4.2.5.2 Surface finish of the casting using Ajase-Ipo sand		28

4.2.5.3 Surface finish of the casting using Tsaragi sand		28

4.2.5.4 Surface finish of the casting using all the moulding sands	29

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATIONS

5.1	Conclusions									30

5.2	Recommendations								31

REFERENCES								32

LIST OF TABLES

Table 4.1:	Sieve Analysis of Oloje Silica sand					17

Table 4.2:	Sieve Analysis of Ajase-Ipo Silica sand				18

Table 4.3:	Sieve Analysis of Tsaragi Silica sand					19

Table 4.4:	Moulding properties of prepared Oloje moulding sand

(8% bentonite, 6% coal dust)						20

Table 4.5:	Moulding properties of prepared Ajase-Ipo moulding sand

(8% bentonite, 6% coal dust)						20

Table 4.6:	Moulding properties of prepared Tsaragi moulding sand

(8% bentonite, 6% coal dust)						21

Table 4.7:	Moulding properties of prepared Oloje moulding sand

(8.5% bentonite, 6.5% coal dust)					21

Table 4.8:	Moulding properties of prepared Ajase-Ipo moulding sand

(8.5% bentonite, 6.5% coal dust)					22

Table 4.9:	Moulding properties of prepared Tsaragi moulding sand

(8.5% bentonite, 6.5% coal dust)					22

Table 4.10:	Moulding properties of prepared Oloje moulding sand

(9% bentonite, 7% coal dust)						23

Table 4.11:	Moulding properties of prepared Ajase-Ipo moulding sand

(9% bentonite, 7% coal dust)						23

Table 4.12:	Moulding properties of prepared Tsaragi moulding sand

(9% bentonite, 7% coal dust)						24

LIST OF FIGURES

Figure 4.1:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (8% bentonite and 6% coal dust)		24

Figure 4.2:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (8.5% bentonite and 6.5% coal dust)		25

Figure 4.3:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (9% bentonite and 7% coal dust)		25