SUITABILITY OF SELECTED SILICA SANDS IN KWARA STATE FOR FOUNDRY APPLICATIONS

BY

ADESOJI YUSUF OLALEKAN

HND/23/MET/FT/027

SUBMITTED TO THE

DEPARTMENT OF METALLURGICAL ENGINEERING, INSTITUTE OF TECHNOLOGY,

KWARA STATE POLYTECHNIC, ILORIN, NIGERIA.

IN PARTIAL FULFILMENT OF THE REQUIREMENT FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN METALLURGICAL ENGINEERING TECHNOLOGY

JULY, 2025

CERTIFICATION

This is to certify that this project work was carried out by Adesoji Yusuf Olalekan with Matric Number: HND/23/MET/FT/027 has met the requirement and regulations governing the award of Higher National Diploma (HND) in Metallurgical Engineering Technology, Kwara State Polytechnic, Ilorin and under the supervision of the project supervisor.

_________________________				_________________

ENGR. A. S. ADESINA						DATE

Supervisor

_______________________				_________________

ENGR. D. A. ADEGBITE					DATE

Head of Department

_______________________				_________________

EXTERNAL EXAMINER 					DATE

DEDICATION

This project is dedicated to Almighty Allah, whose guidance has been my constant companion throughout my academic journey.

# ACKNOWLEDGEMENT

I am profoundly grateful to Almighty Allah for His grace in enabling me to successfully complete this project.

My sincere appreciation goes to my supervisor, Engr. A. S. Adesina, for his invaluable guidance and support. I also extend my heartfelt thanks to every member of the Team for their contributions and collaboration.

I owe my deepest gratitude to my Late Dad, whose great efforts laid the foundation for my education, and to my mom, who has been by my side ever since. I also wish to thank Mr. Edunjobi Raheem, Lawal Sodiq, Adesoji Aminat, Olukotun Abdulrahmon, and Adebayo Muminat for their invaluable support during this journey. Finally, I am grateful to all my friends who have contributed to my growth.

ABSTRACT

The suitability of selected silica sands in Kwara State for foundry applications were carried out in the three regions of Kwara State viz: Kwara central (Oloje), Kwara South (Ajase-Ipo) and Kwara North (Tsaragi). It is an established fact that silica sand is one of the many important variables that dictates or determines the quality and soundness of casting. In view of this, it becomes expedient to know the inherent properties of the silica sand that makes it more suitable for a specific application. Three out of important properties of silica sand that are required during casting processes are carried out in this study. These properties are green compressive strength, green shear strength and moisture content. The results showed average mechanical properties of the natural moulding sands’ samples to include grain finess number for Oloje silica sand to be 66.45, Ajase-Ipo silica sand to be 68.03 and Tsaragi silica sand to be 67.81. Also, their green compressive strength, green shear strength and moisture content were all within the required standards for casting of non-ferrous metals. In the foregoing of all these, it was concluded that the silica sands at Oloje, Ajase-Ipo and Tsaragi are relatively fine and can be used for zinc casting, or any non-ferrous metals e.g. aluminum, copper etc. It can also be employed for small and medium light weight iron castings.

TABLE OF CONTENTS

Title page										i

Certification										ii

Dedication										iii

Acknowledgement									iv

Abstract										v

Table of contents									vi

List of Tables										ix

List of Figures										x

CHAPTER ONE

1.0	INTRODUCTION								1

1.1	Background of the Study							3

1.2	Statement of the Problem							4

1.3	Significant of the Study							4

1.4	Aim and Objectives of the Project						5

1.5	Scope of the Study								6

CHAPTER TWO

2.0	LITERATURE REVIEW							7

2.1	Moulding Sands								8

2.2	Principal Ingredient of Moulding Sand					9

2.2.1	Silica sand grains							9

2.2.1.1 Rounded grains						9

2.2.1.2 Sub angular grains						10

2.2.1.3 Angular grains							10

2.2.1.4 Compounded grains						10

2.2.1.5 Sands								10

2.2.2 Bonding clay								12

2.2.3 Moisture 								13

CHAPTER THREE

3.0	MATERIALS AND METHOD

3.1	Collections and Preparation of Materials					14

3.1.1 	Silica Sand								14

3.1.2	Preparation of the standard test specimens				14

3.2	Method									15

3.2.1	Green compressive and green shear strength 				15

3.2.2 Permeability 								15

3.2.3 Moisture content							16

3.2.4 Sieve analysis								16

CHAPTER FOUR

4.0	RESULTS AND DISCUSSION

4.1	Data and Results								17

4.2	Discussion of Results								26

4.2.1 Green compressive strength						26

4.2.2	Green Shear Strength 							26

4.2.3 Moisture content							27

4.2.4 Grain size								27

4.2.5 Surface finish of the casting						27

4.2.5.1 Surface finish of the casting using Oloje sand		28

4.2.5.2 Surface finish of the casting using Ajase-Ipo sand		28

4.2.5.3 Surface finish of the casting using Tsaragi sand		28

4.2.5.4 Surface finish of the casting using all the moulding sands	29

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATIONS

5.1	Conclusions									30

5.2	Recommendations								31

REFERENCES								32

LIST OF TABLES

Table 4.1:	Sieve Analysis of Oloje Silica sand					17

Table 4.2:	Sieve Analysis of Ajase-Ipo Silica sand				18

Table 4.3:	Sieve Analysis of Tsaragi Silica sand					19

Table 4.4:	Moulding properties of prepared Oloje moulding sand

(8% bentonite, 6% coal dust)						20

Table 4.5:	Moulding properties of prepared Ajase-Ipo moulding sand

(8% bentonite, 6% coal dust)						20

Table 4.6:	Moulding properties of prepared Tsaragi moulding sand

(8% bentonite, 6% coal dust)						21

Table 4.7:	Moulding properties of prepared Oloje moulding sand

(8.5% bentonite, 6.5% coal dust)					21

Table 4.8:	Moulding properties of prepared Ajase-Ipo moulding sand

(8.5% bentonite, 6.5% coal dust)					22

Table 4.9:	Moulding properties of prepared Tsaragi moulding sand

(8.5% bentonite, 6.5% coal dust)					22

Table 4.10:	Moulding properties of prepared Oloje moulding sand

(9% bentonite, 7% coal dust)						23

Table 4.11:	Moulding properties of prepared Ajase-Ipo moulding sand

(9% bentonite, 7% coal dust)						23

Table 4.12:	Moulding properties of prepared Tsaragi moulding sand

(9% bentonite, 7% coal dust)						24

LIST OF FIGURES

Figure 4.1:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (8% bentonite and 6% coal dust)		24

Figure 4.2:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (8.5% bentonite and 6.5% coal dust)		25

Figure 4.3:	Variation in moulding properties of prepared Oloje, Ajase-Ipo and

Tsaragi moulding sand (9% bentonite and 7% coal dust)		25

CHAPTER ONE

1.0	INTRODUCTION

Over the past years, many new moulding and core-making processes have been introduced in the foundry industries, and in particular ones based on the use of chemical binders. Greensand moulding, however, remains the single most important method for producing casting. Especially when they are required in large numbers involves the use of mechanized moulding plant. In order to obtain the optimum economic production with green sand plant, it is imperative that foundry managerial and supervisory staffs are familiar with the best method for control and operation.

Moulding sand is commonly used to cast both ferrous and non-ferrous metals because of its ability to withstand the temperature of the molten metal, absorb and transmit heat, and has good permeability to allow gasses generated during casting to escape without causing casting defects (Ademoh and Ahmed, 2008). The use of sand as a moulding medium is determined by the type of metal being cast, economics, casting quality required, and the degree of consistency desired in the final products (Mshelia et al., 2016).

The major constituents of moulding sands include silica sand, clay and moisture. Each of the constituents is important in determining the characteristics of moulding sand (Nigerian Foundries Limited, 1995). Clay is responsible for bonding; moisture content determines the plasticity of the moulding sand (Steve, 1996), while silica sand impacts refractoriness, chemical resistivity and permeability (Scaffer and James, 1995; Sarka, 1967). Silica sand is specified according to its average size and shape (Aribo, 2011). The higher the sand grain fineness, the higher the cohesiveness, and the lower the permeability of the sand (Aribo et al., 2009). Clay is made up of two ingredients: fine silt and true clay. Fine silt is a kind of foreign matter in clay deposit and possesses no bonding power. True clay provides the necessary bonding action which it acquires in the presence of an appropriate amount of moisture (Atanda et al., 2012; Mechanicalinfo, 2019). However, as the quantity of the clay increases, the permeability of the moulding sand decreases (Atanda et al., 2012).

Sand casting which is perhaps the most versatile of the casting methods can be used for casting various articles ranging from very small size to extremely large size (Ibitoye, 2005). It is used to cast several engine components such as engine blocks, machine tool bed, cylinder heads, piston rings, wheels, pump housings, water supply pipes, mill rolls, valves etc. However, in order to produce good quality casting, the properties of the moulding sand must be at the optimum level (Mahesh et al., 2008). Research has shown that the quality of the casting is largely affected by moulding sand properties (Dhruval et al., 2015; Mishra, 2017; Saikaew and Wiengwiset, 2012), such as cohesiveness, green compressive strength, dry strength, permeability, mould hardness, compatibility and shatter index. All these properties invariably depend on such parameters as the quality of binder used, amount of water and sand grain size (AFS, 1963; Loto and Omotoso, 1999; Ayoola et al., 2010).

1.1	Background of the Study

During the past four decades, the industry has undergone a period of remarkable progress and transition. In this brief span, the number of iron foundries has been cut nearly in half, primarily as a result of the increasing capital requirements necessary to remain competitive while maintaining to meet safety and pollution control regulation and increasing customer requirement for quality. Moreso, with the increasing technological development around the world, one would definitely agree that there is need to introduce a new dimension to the quality and standard of the foundry products obtained in the country, given that the economic development in any country is a function of its technological development. However, many researchers had done quite a number of works on how to modify or rather, to improve the quality of the moulding sand employed as moulding materials. The dividend of their research work is what we are enjoying nowadays, that is, development in technology.

Besides, it is obvious that more than 75 percent of the materials employed to achieve the so-called technological advancement is constituted by casting. In other words, technological development that has become an object of concern around the world cannot be treated in isolation without considering the quality and standard of casting. A thorough analysis had revealed that most defects embedded in casting are as a result of sub-standard quality of moulding sand employed during production process. Having considered the fact that the level of technological development obtainable in a country will be drastically affected if the materials employed are characterized by defects so, the need to characterize the silica sands at Oloje, Ajase-Ipo, and Tsaragi in Kwara State to ascertain or rather to establish the various foundry properties contained in the silica sands and to specify whether they are suited for the casting processes with their various mechanical properties and defects after casting is necessary.

1.2	Statement of the Problem

There are many known deposits for silica sand all over the country, which can be employed as a moulding material for casting, but are lying idle or useless. So, there is need to characterize the silica sands at Oloje, Ajase-Ipo, and Tsaragi respectively so that the deposits, will be adequately and effectively utilized for specific applications.

1.3	Significant of the Study

The study will reduce the rigour of up-grading silica sand and it will make the foundry product cost effective. It will enhance to a great extent the technological and economic development of the nation at large when the casting produced is of good standard and quality. The study will also increase the industries in the country because it will afford the industrialist or rather; the investors the opportunity to have a good knowledge of the available raw materials in the country and for what application they can be employed. This will serve as a guide for the investors to make a right choice what types of foundry operation to embark upon in order to maximize profit.

Lastly, the study will also afford scholar in the field of foundry the opportunity to further characterize the silica sand of some other location that are not included in the project.

1.4	Aim and Objectives of the Project

The aim of this project work is to characterize the silica sands at Oloje, Ajase-Ipo, and Tsaragi in Kwara State and to establish the various foundry properties embedded in the sands.

The objectives of the study are as follows:

- To carry out the sieve analysis of the silica sands’ samples

- Use the silica sands for non-ferrous metal casting to ascertain its castability.

- Characterize and determine the mechanical foundry properties (green strength, permeability, clay content and moisture content) of the silica sands at Oloje, Ajase-Ipo, and Tsaragi of Kwara State.

- For the work to serve as a basis for other scholars to know what is to be done in order to increase or reduce the amount of specific foundry properties needed for a particular application.

1.5	Scope of the Study

This study will dwell more on the characterization of the foundry properties of silica sands at Oloje, Ajase-Ipo, and Tsaragi of Kwara State. Various foundry properties such as green strength, permeability, refractoriness, moisture content and clay content shall be carried out on these sands. It is highly imperative to note that there is no available equipment to measure refractoriness directly, so the refractoriness of these sands will be estimated based on the clay content present in the silica sands.

CHAPTER TWO

2.0	LITERATURE REVIEW

The process by which casting are made involves melting of metal by melting furnace appliance, poured the molten metal into a pre-shaped mould cavity created by pattern in conformity with desired components and allowed it to solidify before it’s shake out of the mould and thereafter settling operation is being carried out on the produced cast. The mould reproduces the shape of a pattern and a cheap and reliable material for making the mould is a plastic mixture consisting of bounded with moist clay. The mixture is weak enough to flow and be packed tightly around the pattern, strong enough to retain its shape during withdrawal of the pattern and pouring of the metal, and dry enough to avoid explosive formation of steam. Since the sand is used in this moist form immediately after stripping from the pattern it is termed ‘green’. This sand moulding process is suitable for the production of iron, steel, aluminum and copper based alloy castings.

According to Desai et al., (2016), green sand moulding is still the main moulding process used in more than 80 percent of U.K. foundries despite all the competition from chemical binder such as resin and silicates. Clay bounded sands have been largely replaced by chemical moulding systems for large, heavy casting, where the benefits are:

- High production rate

- Fast turn: round of pattern and moulding boxes

- Elimination of drying stove.

- Reduces handling

- Less floor spaces

- Improved dimensional accuracy

Greensand predominates for smaller castings, and is still widely used for medium - weight castings. Synthetic greensands, made from silica sand with added clay and coal dust, are used in the majority of medium to large foundries. Many small iron foundries and non-ferrous foundries still rely on natural clay bounded sands.

2.1	Moulding Sands

Sand is the principal moulding material in the foundry shop where it is used for all types of casting, irrespective of whether the cast metal is ferrous or non-ferrous, iron or steel. This is because it possesses the properties vital for foundry purposes. The most important characteristics of sand are its refractory nature, it can easily withstand the high temperature of molten metal and loss not get fuse. Secondly, moulding sand has chemical resistivity; it does not chemically react or combine with molten metal and can therefore be used time and again. Thirdly, sand has a high degree of permeability; it allows gases and air to escape from the mould when molten metal is poured on without interfering with the rigidity and strength of the mould. The degree of strength, hardness and permeability can also be adjusted, as desired, by varying the composition or the ingredients of the sand. Such flexibility is extremely difficult to achieve with any other moulding material. But the properties vary from one sand to another, and it should be noted that only those sands characterized by the foregoing features are considered for moulding work.

2.2	Principal Ingredient of Moulding Sand

The principal ingredients of moulding sand are:

- Silica sand grains.

- Clay

- Moisture

2.2.1	Silica sand grains

Sand grains are of paramount importance in moulding sand because they impart refractoriness, chemical resistivity and permeability to the sand. They are specified according to their average size and shape. The finer the grains, the more intimate will be the contact and lower the permeability. However, fine grains tends to fortify the mould and lessen its tendency to get distorted. The shapes or the grains may vary from round to angular. The grains are classified according to their shape.

2.2.1.1 Rounded grains

These grains have the least contact with one another in a rammed structure, thereby making the sand highly permeable to gases. Sand having rounded grains however, lack strength and do not pack up to the optimum extent states (Oke and Omidiji, 2016). The binder requirements are minimum.

2.2.1.2 Sub angular grains

These grains have comparatively lower permeability and greater strength than the rounded ones.

2.2.1.3 Angular grains

These grains have defined edges and the surfaces area nearly flat. They produce higher strength and lower permeability in the mould than sub-angular grains. The binder consumption is likely to be high.

2.2.1.4 Compounded grains

In some cases, the grains are cemented together such that they fail to separate when screened. They consist of rounded, sub-angular or angular grains or a combination of the three. Such grains are called compounded grains and are least desirable due to their tendency to breakdown at high temperature. According to (Oke and Omidiji, 2016), in practice, sand grains contain mixed grain shapes, depending on origin. A sub-angular to rounded grain mixture would be the best combination.

2.2.1.5 Sands

Sands: green sands are based on mineral quartz, which consist of silica (SiO2). According to Dhruval et al., (2015), Nigeria has quarries in many parts of the country e.g. Ife, Osogho, Bacita, lgbokoda etc. In other words, foundries in Nigeria have suitable sand supplies within a radius of 50 – 100 miles. Silica sands at Oloje, Ajase-Ipo, and Tsaragi serve some foundries in Kwara, Oyo and Niger states axis of the country. Sand is formed by the disintegration of granite and other rocks compose of individual mineral grains firmly cemented together. Over million of years, these rocks were broken down into individual grains by the action of frost, heat, water and wind.

Granite is composed of three minerals: Feldspar, Mica and quartz. The quartz is most resistant to weathering and the grains were washed down from mountain and hills and deposited in shallow moving water.

Most foundry sands are found in a considerable distance from the site of parent rock. The original quartz grains were angular but, over long periods, they have become rounded by transport such as wind actions during desert conditions. This action also sort out grains of varying size and tends to produce sand of uniform size.

The feldspar minerals are less resistant to weathering and may be present in the silica sand as clay substance. Other sands contain mica and when much of this mineral is present, the sand become unsuitable for foundry use.

Many sand contain clay, and foundry-men divide sand into two classes:

1.	Silica sands, which are relatively free from clay as quarries. These usually contain more than 95 percent silica.

2.	Natural sands, which contain up to 20 percent clay as quarries and can be used for moulding without the addition of any extra bonding materials.

If the green moulding sand is prepared from clay containing sands, it is called naturally bonded greensand. If a greensand mixture is prepared from relatively clean silica sand by the addition of clay, it is called synthetic greensand.

The majority of naturally bonded sands are fine grained, whereas, the synthetic greensands are normally prepared from coarser silica sands. Most foundries now use synthetic greensand since the physical properties can be adjusted by means of clay and water addition to meet the need of a particular designs and moulding process.

2.2.2	Bonding clay

Clay is natural mineral found in many parts of the world, several different types of clay mineral exist but they are all hydrous alumina silicates. They are very finely grained material, which absorb water and become plastic, but on drying become rigid and strong. Their properties provide cohesion and plasticity in green state and high strength when dried. Clay are resistant to moderate heat, and the plasticity and strength properties can be subsequently restored by the addition of further water. Since clay bonded sands are easily regenerated and recycled, they are economical for foundry use.

Murray (1986), classified clay mineral most widely used as binder as:

- Kaolinites (Al2O3.2SiO2.2H2O)

- Illites [(K2Al4CSi8. Alx). (O2COH)4]

- Montimorillonites (Al2O3.4SiO2.H2O + nH2O).

2.2.3	Moisture

The moisture content of moulding sand is the most important variable, as on this all other properties depend. Temper water act as an activator. Stefanesai (1992), noted that clay however, would not function as a binder unless activated by temporary water, which result in strength development, which is an important property of moulding sand.

According to Asuquo and Bobojama (1991), moisture content of moulding sand is considered as the amount of free or mechanical water available in the sand. The moisture content of moulding sand normally varies between 4 and 8 percent. This is liable to change, and must therefore be checked frequently. It is not practicable to work at peak green strength and the moisture content is normally in a specific range. Atanda et al., (2012), also reported that too much water in green sand can lead to formation of gas cavities in the casting. Grim and Gutherbert (1945), states that, dry strength will continue to increase with water for different bentonite content. This is a result of their research study on clay - water system relationship.

CHAPTER THREE

3.0	MATERIALS AND METHOD

3.1	Collections and Preparation of Materials

3.1.1	Silica Sand

The silica sands used in this project were obtained from the vast deposits at Oloje, Ajase-Ipo, and Tsaragi, Kwara State respectively. The silica sands were washed, scrubbed and sieved through an Endecott sieve to remove exceptionally coarse or fine material and dried under the Sun for 5 days. All calcaceous matters such as crab shells and snail shells were removed.

3.1.2	Preparation of the Standard Test Specimens

The AFS cylindrical test specimens was prepared using the metric standard rammer. The AFS cylindrical test piece of 50.8mm diameter x 2mm is made by dropping 6.356kg weight three times through a height 50.8mm onto the measured quantity of sand. 150g of the prepared sand was weight out and placed in a 127mm height special tube with an internal diameter of 50.8mm, the base of which had been sealed by a suitable metal cup. The weight on the rammer was raised by means of the handle provided on the side of the equipment. The specimen tube and the cup were then placed under the ramming head with the centralizing peg on the metal plug located in the hole of the base plate. The rammer head and weight were then lowered until they were supported by the sand in the container. Rotating handle attached to the apparatus was allowed to fall freely through a 50.8mm height determined by the cam on the equipment raised the rammer weight. This operation was repeated twice to ram three times for all silica sands. The specimen was removed from the rammer by raising the weight.

3.2	Method

3.2.1	Green compressive and green shear strength

The compressive strength was performed on the universal sand strength tester, which first requires shaping the sample in the AFS standard tube. The AFS cylindrical test specimen was stripped from the tube on a suitable striping post. The prepared stripped specimens were carefully set on the universal sand tester. A manually operated rotating device applied to the load to move the components were then operated and the components were moved along the semi-circular graduated scale until they fractured. A small moving magnet placed on the accessory indicated the reading.

The green shear strength was similarly determined by placing the necessary accessories for the shear strength.

3.2.2	Moisture content

The hot air methods were employed to determine the moisture content. The apparatus was switch on and allow to heat up for some minutes. 150g of the prepared sands were measured and placed in the pan provided at the base of the instrument. The thermostat on the equipment was set to 110°C and the drier was set in operation by means of a timer switch. The dried samples of the sands were then allowed to cool and reweighed. So the moisture contents of the sands were then determined.

3.2.3	Sieve analysis

The size and distribution of the sand grains were determined with sieve analysis test. A dried 150 grammes of the silica sands were measured on a weighing balance. The weight sands were then placed on top of a series of sieve that ranges from l400m to 45m or rather a set of sieves of decreasing aperture size contained on a shaker. The shaker was switched on for a period of 15 minutes. Then the sands retained in each sieve and the bottom pan were weighed and recorded against the sieve aperture size and their percentages as a measure of the total samples were determined.

CHAPTER FOUR

4.0	RESULTS AND DISCUSSION

4.1	Data and Results

The results obtained during the sands test were recorded and were as subsequently presented in the tables 4.1, 4.2 and 4.3, which represent the result of the sieve analysis while tables 4.4. 4.5. 4.6, 4.7, 4.8, 4.9 and 4.10, 4.11 and 4.12 reveals the effect of varying additive with constant volume of water on the green compressive strength, green shear strength, and moisture content while figures 4.1 to 4.3 show the variation in moulding properties of Oloje, Ajase-Ipo, and Tsaragi moulding sands with different bentonite and coal dust percentages.

Table 4.1: 	Sieve Analysis of Oloje silica sand

| S/N | Mesh (N) | Sieve diameter (micron) | Wt of sieve pan (g) | Wt of pan and retained sand (g) | Wt of retained sand (g) | % wt of retained sand (g) | Product (g) [% Wt of retained sand x sieve No] | Cumulative |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 12 | 1400 | 312.881 | 313.012 | 0.131 | 0.042 | - | - |
| 2 | 16 | 1000 | 299.931 | 300.003 | 0.072 | 0.024 | 0.288 | 0.066 |
| 3 | 22 | 710 | 287.070 | 287.429 | 0.359 | 0.125 | 2.000 | 0.191 |
| 4 | 30 | 500 | 259.858 | 267.935 | 8.077 | 3.108 | 68.376 | 3.299 |
| 5 | 44 | 355 | 241.321 | 260.277 | 18.956 | 7.855 | 235.650 | 11.154 |
| 6 | 60 | 250 | 233.595 | 253.248 | 19.653 | 8.413 | 358.292 | 19.567 |
| 7 | 85 | 180 | 225.282 | 249.647 | 24.365 | 10.815 | 648.900 | 30.382 |
| 8 | 120 | 125 | 213.470 | 239.823 | 26.353 | 12.345 | 1049.325 | 42.727 |
| 9 | 170 | 90 | 211.693 | 220.345 | 8.652 | 4.087 | 490.440 | 46.814 |
| 10 | 240 | 63 | 208.904 | 211.434 | 2.530 | 1.211 | 205.870 | 48.025 |
| 11 | 350 | 45 | 210.610 | 211.343 | 0.733 | 0.348 | 83.520 | 48.373 |
| 12 | 350 | - | 196.147 | 196.643 | 0.496 | 0.253 | 88.550 | 48.626 |
|  |  |  |  |  |  | 48.626 | 3231.211 |  |

AFS =

AFS = 66.45

AFS grain fineness number is 66.5

Table 4.2: 	Sieve Analysis of Ajase-Ipo silica sand

| S/N | Mesh (N) | Sieve diameter (micron) | Wt of sieve pan (g) | Wt of pan and retained sand (g) | Wt of retained sand (g) | % wt of retained sand (g) | Product (g) [% Wt of retained sand x sieve No] | Cumulative |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 12 | 1400 | 312.881 | 313.028 | 0.147 | 0.047 | - | - |
| 2 | 16 | 1000 | 299.931 | 300.015 | 0.084 | 0.028 | 0.336 | 0.075 |
| 3 | 22 | 710 | 287.070 | 287.443 | 0.373 | 0.130 | 2.080 | 0.205 |
| 4 | 30 | 500 | 259.858 | 266.046 | 6.188 | 2.381 | 52.382 | 2.586 |
| 5 | 44 | 355 | 241.321 | 259.083 | 17.762 | 7.360 | 220.800 | 9.946 |
| 6 | 60 | 250 | 233.595 | 253.175 | 19.580 | 8.382 | 368.808 | 18.328 |
| 7 | 85 | 180 | 225.282 | 249.970 | 24.688 | 10.959 | 657.540 | 29.287 |
| 8 | 120 | 125 | 213.470 | 241.188 | 27.718 | 12.984 | 1103.640 | 42.271 |
| 9 | 170 | 90 | 211.693 | 220.355 | 8.662 | 4.092 | 491.040 | 46.363 |
| 10 | 240 | 63 | 208.904 | 211.446 | 2.542 | 1.217 | 206.890 | 47.580 |
| 11 | 350 | 45 | 210.610 | 211.353 | 0.743 | 0.353 | 84.720 | 47.933 |
| 12 | 350 | - | 196.147 | 196.653 | 0.5061 | 0.258 | 90.300 | 48.191 |
|  |  |  |  |  |  | 48.191 | 3278.536 |  |

AFS =

AFS =

AFS grain fineness number is 68.03

Table 4.3: 	Sieve Analysis of Tsaragi silica sand

| S/N | Mesh (N) | Sieve diameter (micron) | Wt of sieve pan (g) | Wt of pan and retained sand (g) | Wt of retained sand (g) | % wt of retained sand (g) | Product (g) [% Wt of retained sand x sieve No] | Cumulative |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 12 | 1400 | 312.881 | 313.062 | 0.181 | 0.058 | - | - |
| 2 | 16 | 1000 | 299.931 | 300.039 | 0.108 | 0.036 | 0.432 | 0.094 |
| 3 | 22 | 710 | 287.070 | 287.463 | 0.393 | 0.137 | 2.192 | 0.231 |
| 4 | 30 | 500 | 259.858 | 267.347 | 7.489 | 2.882 | 63.404 | 3.113 |
| 5 | 44 | 355 | 241.321 | 259.625 | 18.304 | 7.585 | 227.550 | 10.698 |
| 6 | 60 | 250 | 233.595 | 253.182 | 19.587 | 8.385 | 368.940 | 19.083 |
| 7 | 85 | 180 | 225.282 | 249.601 | 24.319 | 10.795 | 647.700 | 29.878 |
| 8 | 120 | 125 | 213.470 | 240.768 | 27.298 | 12.788 | 1086.980 | 42.666 |
| 9 | 170 | 90 | 211.693 | 220.377 | 8.684 | 4.102 | 492.240 | 46.768 |
| 10 | 240 | 63 | 208.904 | 211.812 | 2.908 | 1.392 | 236.640 | 48.160 |
| 11 | 350 | 45 | 210.610 | 211.370 | 0.7603 | 0.361 | 86.640 | 48.521 |
| 12 | 350 | - | 196.147 | 196.684 | 0.5374 | 0.274 | 95.900 | 48.795 |
|  |  |  |  |  |  | 48.795 | 3308.618 |  |

AFS =

AFS =

AFS grain fineness number is 67.81

Table 4.4:	Moulding properties of prepared Oloje moulding sand

(8% bentonite, 6% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 57.20 | 57.00 | 57.10 | 57.10 |
| Shear strength (KN/M2) | 25.40 | 25.20 | 25.30 | 25.30 |
| Moisture content (%) | 3.30 | 3.10 | 3.20 | 3.20 |

Table 4.5:	Moulding properties of prepared Ajase-Ipo moulding sand (8% bentonite, 6% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 55.60 | 55.40 | 55.50 | 55.50 |
| Shear strength (KN/M2) | 24.20 | 24.40 | 24.30 | 24.30 |
| Moisture content (%) | 3.10 | 2.90 | 3.00 | 3.00 |

Table 4.6:	Moulding properties of prepared Tsaragi moulding sand (8% bentonite, 6% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 55.30 | 55.20 | 55.10 | 55.20 |
| Shear strength (KN/M2) | 23.70 | 23.50 | 23.60 | 23.60 |
| Moisture content (%) | 2.90 | 2.80 | 3.00 | 2.90 |

Table 4.7:	Moulding properties of prepared Oloje moulding sand (8.5% bentonite, 6.5% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 77.50 | 75.50 | 75.00 | 76.00 |
| Shear strength (KN/M2) | 27.10 | 27.00 | 27.50 | 27.20 |
| Moisture content (%) | 2.90 | 3.20 | 3.20 | 3.10 |

Table 4.8:	Moulding properties of prepared Ajase-Ipo moulding sand (8.5% bentonite, 6.5% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 74.00 | 73.50 | 72.70 | 73.40 |
| Shear strength (KN/M2) | 25.00 | 24.50 | 25.50 | 25.00 |
| Moisture content (%) | 2.80 | 2.90 | 2.85 | 2.85 |

Table 4.9:	Moulding properties of prepared Tsaragi moulding sand (8.5% bentonite, 6.5% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 73.50 | 73.00 | 73.25 | 73.25 |
| Shear strength (KN/M2) | 24.50 | 24.10 | 24.30 | 24.30 |
| Moisture content (%) | 2.75 | 2.70 | 2.65 | 2.70 |

Table 4.10:	Moulding properties of prepared Oloje moulding sand (9% bentonite, 7% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 94.50 | 94.10 | 94.60 | 94.40 |
| Shear strength (KN/M2) | 28.50 | 28.70 | 28.60 | 28.60 |
| Moisture content (%) | 2.80 | 3.00 | 2.90 | 2.90 |

Table 4.11:	Moulding properties of prepared Ajase-Ipo moulding sand (9% bentonite, 7% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 93.00 | 92.50 | 93.50 | 93.00 |
| Shear strength (KN/M2) | 26.50 | 26.70 | 26.30 | 26.50 |
| Moisture content (%) | 2.70 | 2.80 | 2.60 | 2.70 |

Table 4.12:	Moulding properties of prepared Tsaragi moulding sand (9% bentonite, 7% coal dust)

| Properties | 1st reading | 2nd readings | 3rd reading | Average |
| --- | --- | --- | --- | --- |
| Green compressive strength (KN/M2) | 92.30 | 91.90 | 92.40 | 92.20 |
| Shear strength (KN/M2) | 25.50 | 25.80 | 25.80 | 25.70 |
| Moisture content (%) | 2.70 | 2.60 | 2.50 | 2.60 |

Figure 4.1: Variation in moulding properties of prepared Oloje, Ajase-Ipo and Tsaragi moulding sand (8% bentonite and 6% coal dust)

Figure 4.2: Variation in moulding properties of prepared Oloje, Ajase-Ipo and Tsaragi moulding sand (8.5% bentonite and 6.5% coal dust)

Figure 4.3: Variation in moulding properties of prepared Oloje, Ajase-Ipo and Tsaragi moulding sand (9% bentonite and 7% coal dust)

4.2	Discussion of Results

4.2.1	Green compressive strength

There was general increase in the green compressive strength with increase in the additive to the silica sand as can be seen from the table 4.4 to 4.12. This increase in green compressive strength was due to the combined bonding and hardening effect offered by the added bentonite and coal dust with the passage of time. It is a known fact that coal dust are used in green sand mould for protecting mould surfaces against the action of molten metal and improve the surface finish of the castings. When the molten metal comes in contact with mould surface containing coal dust, a gaseous envelope is formed which resists the fusion of the sand to metal, the use of coal dust increases green strength, shear green strength and dry strength. reduces tendency to scabbing and metal penetration. Bentonite was used with high silica sand as a green sand additive to increase the bonding action and impart plasticity, so it increases both green compressive strength and green shear strength. The addition of water is what generates the bond. Bentonite resists erosion of moulds and its volumetric contraction helps in compensating the expansion of silica grains.

4.2.2	Green Shear Strength

It was observed from the tables and figures 4.1 to 4.3 that shear strength is in accordance with the one found in the literature review (Hassan, 2001). Due to this, Oloje, Ajase-Ipo and Tsaragi can be effectively used for moulding in foundry work.

4.2.3	Moisture content

It was observed that the moisture content decreases as the added additives increases. This was an indication that so far the temper water is not increased; the additive will definitely reduce the water content, so the moisture content will be lowered. Moisture content in moulding sands is the major requirement for ensuring ease of moulding, good quality mould and good casting. When the moisture content is too much, the particles of the sand will not bind together as expected i.e. the mixture will be water logged and if it is not sufficient, there will be some dried sand embedded in the mould formed.

4.2.4	Grain size

The washed sand grains range from sub-angular to rounded. It has a well-defined grading with 70 percent and above of the sand grains retained by three adjacent sieves. The AFS reveals that the sand grains are relatively fine.

4.2.5	Surface finish of the casting

A properly designed casting, a properly prepared mould, and correctly melted metal should result in a casting having good surface finish and with Little or no defects. Surface finish of the casting is the final assessment on a casting before any operations such as fettling, heat treatment and finishing, inspection and testing are carried out.

4.2.5.1 Surface finish of the casting using Oloje moulding sand

The casting produced by the use of Oloje moulding sand was with fine surface finish with little or no defect. There were little defects of shrinkage cavity or depression caused by a large or small depression on the casting that results from varying rates of contractions while the metal is changing from liquid to solid. This minor depression is known as stress.

4.2.5.2 Surface finish of the casting using Ajase-Ipo moulding sand

The casting produced by the use of Ajase-Ipo moulding sand was with fine surface finish with little or no defect. There were little defect of blow holes or gas holes caused due to entrapped air or gas. They were generally rounded cavities spherical, flattened or elongated air or gas. These were generally found inside the casting.

4.2.5.3 Surface finish of the casting using Tsaragi moulding sand

The casting produced by the use of Tsaragi moulding sand was also with fine surface finish with little or no defect. There were little defect of cold shuts caused due to non- uniform of metal stream resulting in discontinuity due to imperfect fusion where two streams of metal have converged. This defect may appear as a crack or seam with smooth rounded edges.

4.2.5.4 Surface finish of the casting using all the moulding sands in equal                                                  Proportions (mixing of all)

The casting produced by the use of all the moulding sands in equal proportion was of good surface finish with little defect of shrinkage cavity or depression also caused by a large or small depression on the casting that results from varying rates of contractions while the metal is changing from liquid to solid. This minor depression is known as stress.

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATIONS

5.1 	Conclusions

Based on the results obtained from these studies, the following conclusions were deduced:

(i)	The sand mix with 8.5% bentonite and 6.5% coal dust are the best mixtures in all the three sands and their properties compares favourable well with the proportion of the moulding sand currently used in foundries for the production of small and medium size iron castings.

(ii)	Besides, the sieve analysis also reveals that the grains of the sands are sub-angular and their AFS number shows that they are relatively fine sands.

(iii)	However, the cast object of the same component using all the different silica sands and also their mixing in equal proportion to cast a single component by the use of zinc alloy has reveals that all the silica sands tested are suitable for casting.

Conclusively, the silica sands at Oloje, Ajase-Ipo and Tsaragi respectively will be most suitable for zinc casting or any non-ferrous metals. It can also be employed for both small and medium iron castings.

5.2	Recommendations

The following recommendations are thereby tendered for further work on this project:

(i)	The sands can be upgraded by increase the percentage of silica content through thorough washing.

(ii)	The proportions of the temper water should be varied to a fixed proportion of coal dust and bentonite so as to determine the optimal amount of water that will develop great strength and other required properties.

(iii)	In addition, the silica sands should be adequately sieved in a 350cm Endecott sieve before the moulding properties of the sands are determined.

(iv)	Finally, in-depth study of other moulding properties such as refractoriness, collapsibility, permeability, specific gravity, flowability, clay content, bulk density etc should be conducted so as to fully appreciate the service behaviour of the sand mixtures.

REFERENCES

Ademoh, N. A. and Abdullahi, A.T. (2009). Assessment of foundry properties of steel casting moulds bonded with grade 4 acacia species (gum arabic). International Journal of Physical Sciences, 6, pp 238-241.

Ademoh, N. A. and Ahmed, A. T. (2008). Estimation of the effect of kaolin clay addition on the mechanical properties of foundry moulding sand bonded with grades 3 and 4 Nigerian gum arabic (Acacia species), Middle-East Journal of Scientific Research, 3(3), pp 126–133.

Aribo, S. (2011). Effect of varying corn cob and rice husk ashes on properties of the molding sand. Journal of Minerals & Materials Characterization & Engineering,10(15), pp 1449-1455, ASTM D854 – 14: Standard Test Methods for Specific Gravity of Soil Solids by Water Pycnometer, ASTM International, United States of America.

Aribo, S., Folorunso, D.O., Olaniran, O. and Oladele, I.O. (2009). Optimization the green compression strength and permeability of green sand made from Epe silica sand, International Journal of Science and Technology, 11, pp 101-126.

Asuquo. L.O. and Bobo-jarna S.A. (1991), Foundry Technology, Abic Publishers, Enugu, Nigeria. Pp. 23 - 29.

Atanda, P. O., Olorunniwo, O. E., Alonge, K. and Oluwole, O. O. (2012). Comparison of bentonite and cassava starch on the moulding properties of silica sand. International Journal of Materials and Chemistry, 2(4), pp 132-136.

Ayoola, W. A., Adeosun, S. O., Oyetunji, A. and Oladoye, M.A. (2010). Suitability of Oshogbo sand deposit as moulding sand, Kenya Journal of Mechanical Engineering, Volume 6(1), pp 33-41.

Desai, B., Mokashi, P., Anand, R. L., Burli, S. B. and Khandal, S. V. (2016). Effect of additives on green sand moulding properties using design of experiments and Taguchi’s quality loss function - An experimental study, IOP Conference Series: Materials Science and Engineering, 149, pp 1-17.

Dhurval, P. Vivek, D., Ela, J., Viral, P., Snikunj, D., and Jay, P. (2015). Study of sand composition on mould properties and selection of Taguchi orthogonal array for design of experiments, International Journal of Current Engineering and Scientific Research, 2(3), pp 31-34.

Ibitoye, S.A. (2005). Effect of the addition of sodium silicate and bulk density variation on the permeability of potter's clay-bonded moulding sand, Nigerian Society of Engineers Technical Transactions. 40, pp 67-77.

Loto, C. A. and Omotoso, E. O. (1999). Analysis and development of Igbokoda clay as binder for synthetic moulding sand, Applied Clay Science, 5(1), pp 85 – 97.

Mahesh, B. P., Pratihar, D. K. and Datta, G.L. (2008). Forward and reverse mapping in green sand mould system using neutral networks, Applied Soft Computing, 8(1), pp 239-260.

Mikhailov, A.M. (1989). Metal casting, Mir Publisher, Moscow, Pp. 71 – 90.

Morey, R.E. and Ackerlind, C.D. (1947). “Trans American Foundry Men Association”, Pp. 65 and 288.

Mshelia, Z., Abolarin, M., Abubakre, O. and Ademoh, N. A. (2016). Characterisation of natural moulding sands from selected deposits in Maiduguri- Nigeria for casting applications, Arid Zone Journal of Engineering, Technology and Environment, 12, pp110-121.

Murray, H.H. (1986), “Binders; Industrial Mineral in Encyclopedia of Material Science and Engineering”, Vol. 1, Pp. 305 – 306.

Nigerian Foundries Limited (1995). The fundamentals of greensand technology. Foundry Africa Conference, pp 1-7.

Nwajagwu, GO. and Okafor, I.C.I (1987). “Improving the day characteristic of Kaolonitic clay bonded moulding sand” refractory journal, v 62 n2, Pp. 6 – 12.

Oke, A. O. and Omidiji, B .V. (2016). Investigation of some moulding properties of a Nigerian clay-bonded sand. Achieves of Foundry Engineering, 16(3), pp 71- 76.

Scaffer, E. and James, P. (1995). The science and design of engineering materials, 1st Edition, Longman, London.

Stefanesai, O.M. (1992). “Casting Metal Handbook”, Metal Park, Ohio.