EFFECT OF GRAPHITE ADDITIVE ON THE REFRACTORY PROPERTIES OF TSONGA CLAY

BY

BALOGUN FAHEED ADEDAYO

ND/23/MET/FT/070

SUBMITTED TO THE

DEPARTMENT OF METALLURGICAL ENGINEERING,

INSTITUTE OF TECHNOLOGY,

KWARA STATE POLYTECHNIC, ILORIN, NIGERIA.

IN PARTIAL FULFILMENT OF THE REQUIREMENT FOR THE AWARD OF NATIONAL DIPLOMA (ND) IN METALLURGICAL ENGINEERING TECHNOLOGY

JULY, 2025

CERTIFICATION

This is to certify that this project work was carried out by Balogun Faheed Adedayo with Matric Number: ND/23/MET/FT/070 has met the requirement and regulations governing the award of National Diploma (ND) in Metallurgical Engineering, Kwara State Polytechnic, Ilorin and under the supervision of the project supervisor.

________________________				_________________

ENGR. D. A. ADEGBITE 					DATE

Supervisor

______________________					_________________

ENGR. D. A. ADEGBITE					DATE

Head of Department

_______________________				_________________

EXTERNAL EXAMINER 					DATE

DEDICATION

The project work is dedicated to God Almighty, my creator, my strong pillar, my source of inspiration, wisdom, knowledge and understanding. He has been the source of my strength throughout this program.

ACKNOWLEDGEMENT

My outmost gratitude goes to Almighty God, the Alpha and the Omega, who has been the source of my strength and breath throughout the years.

I want to appreciate my supervisor, Engr. D. A. Adegbite for his assistance rendered to me on my project. I want to say a big thanks to you, may God bless you abundantly.

To my beloved parent, I would forever be grateful to you for your love, care, moral and financial support. God bless you, Amen.

My acknowledgement would not be completed without appreciating the effort of lecturers: Engr. A. S. Adesina, Engr. Alagbe, M., Engr. S. A. Babalola, and Engr. F. F. Ihogbetin, for impacting so much in me both in knowledge and characters, I am grateful.

To my families, friends and course-mates, I thank you for your support and prayers.

ABSTRACT

Effect of graphite additive on the refractory properties of Tsonga clay was investigated. The use of graphite for upgrading some refractory properties of Tsonga clay, found abundantly in Edu Local Government of Kwara State, for the production of refractory bricks for furnace lining have been studied. 20 – 40% graphite were used as blend. Refractory properties measured include: permeability, linear shrinkage, apparent porosity, bulk density, thermal shock resistance, cold crushing strength and refractoriness. Linear shrinkage, permeability and apparent porosity of the bricks made from the blend decreased with the percentage graphite addition. The thermal shock resistance of the bricks was increased as percentage graphite addition increased. The cold crushing strength of the bricks also increased as percentage graphite addition increased up to 30% and decreased as the percentage graphite increase to 40%.

TABLE OF CONTENTS

Title page										i

Certification 										ii

Dedication 										iii

Acknowledgement 									iv

Abstract										v

Table of Contents									vi

List of Tables										ix

List of Figures										x

CHAPTER ONE:

1.0	INTRODUCTION

1.1	Background of the Study							1

1.2	Statement of the Problem							2

1.3	Significant of the Study							3

1.4	Aim and Objectives of the Project						3

1.6	Scope of the Study								3

CHAPTER TWO

2.0	LITERATURE REVIEW

2.1	Identification of Clay Materials						4

2.2	Types of Clay									6

2.3	Chemical Composition of Clay						7

2.4	Classification of Refractories							9

2.4.1 	Acid Refractories							9

2.4.2	Basic Refractories 							9

2.4.3	Neutral Refractories 							9

2.4.4	Super Refractories 							10

2.5	Mechanism of Bonding in Refractory Materials 				10

2.5.1	Binding Properties of Clay						10

2.5.2	Mechanism of Bonding						11

2.6	Properties of Refractories							13

2.6.1	Refractoriness 							13

2.6.2	Graphite								15

CHAPTER THREE

3.0	MATERIALS AND METHODS

3.1	Materials									16

3.1.1	Equipment 								16

3.2	Methods									16

3.2.1	Experimental Testing Procedures of the Refractory Bricks		16

3.2.2	Measurement of Linear Shrinkage					17

3.2.3	Determination of Apparent Porosity and Bulk Density		17

3.2.4	Determination of Cold Crushing Strength				18

3.2.5	Determination of Thermal Shock Resistance				18

CHAPTER FOUR

4.0	RESULTS AND DISCUSSION

4.1	Results										19

4.2	Discussion 									25

4.2.1	Thermal Shock Resistance 						25

4.2.2	Permeability								25

4.2.3	Apparent Porosity							25

4.2.4	Bulk Density								26

4.2.5	Linear Shrinkage							26

4.2.6	Cold Crushing Strength (CCS)					26

4.2.7	Refractories								27

4.2.8	The Loss on Ignition							27

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATIONS

5.1	Conclusion 									28

5.2	Recommendations 								28

REFERENCES 								29

LIST OF TABLES

Table 2.1:	Chemical Composition of Clay					8

Table 2.2:	Chemical Composition of a Typical Clay				8

Table 4.1: 	Particle Size Analysis of Tsonga Clay Sample			19

Table 4.2: 	Physical Properties of Clay Sample 					20

Table 4.3: 	Chemical Analysis of the Tsonga Clay Sample			21

Table 4.4: 	Physical Properties of Tsonga Clay + Graphite 			21

LIST OF FIGURES

Fig. 2.1:	Fine (firmly bonded) clay 			Coarse (loosely bonded) clay particles with water binder, 	     particles resulting from small

Resulting from large area of contact 	      area of contact		12

Fig. 4.1:	Effect of Graphite Additive on Thermal Shock Resistance of the Brick									22

Figure 4.2:	Effect of Graphite Additive on Permeability of the Brick		22

Figure 4.3:	Effect of Graphite Additive on Apparent Porosity

of the Brick								23

Figure 4.4:	Effect of Graphite Additive on Bulk Density of the Brick		23

Figure 4.5:	Effect of Graphite Additive on Linear Shrinkage of the Brick	24

Figure 4.6:	Effect of Graphite Additive on Cold Crushing Strength

of the Brick								24

CHAPTER ONE

INTRODUCTION

1.1	Background of the Study

Refractory are high temperature materials necessary for lining furnaces and high temperature reactors (Jourdain, Lapoujade and Le Mat; Boch, 2001; Kolli et al., 2007; Poirier, 2011; Minh et al., 2018; Lopez-Perales et al., 2021; Jan et al., 2022). They are strategic materials because they are essential for the production of steel, glass, cement, non-ferrous metals, which are foundations of our civilisation (Boch, 2001; Rouschka, 2004; Kolli et al., 2007; Amraneet al., 2011; Poirier, 2011; Muhammed et al., 2019; Hossain and Roy, 2021; Lopez-Perales et al., 2021). Historically, clay refractory materials are basic materials obtained from cheap local resources (Rouschka, 2004; Subhojeet et al., 2013; Jan et al., 2022). Today, even they do not correspond to “hightech” materials, they remain useful in many applications requiring high temperature processes like pottery, earthenware, table ware, sanitary ceramic, bricks and tiles production (Jouenne , 1984; Maiti et al., 2004; Poirier, 2011; Chaouki, 2014; Bomeni et al., 2018; David et al., 2021). They were also use as general purpose materials, safe linning in the production of steel, cement etc.

Clay as defined by (Chesti, 1986) are those materials with particle of sand below 20mm in diameter which fill to settle at a rate of 25mm per minute or at one inch per minute when suspended in water. (Hoffman) in its own work defined clay as a hydrated earthly material containing a considerable portion of aluminium and silicon [kaolin (A12 (Si2O7) (OH4)]4.

American Standard of Testing and Materials (ASTM) defines refractories as non-metallic materials having those chemical and physical properties that make them application for structures or as component systems that are expressed to environments above 538oC (811K, 1000oF) (Bhatia, 2012). Refractory materials must be chemically and physically stable at high temperatures. Depending on the operating environment, they need to be resistant to thermal shock, be chemically inert, and have specific ranges coefficient of thermal expansion.

Also (Jam and Jam) defined clay as certain earthy which are highly plastic, when wet and which, when heated to redness, losses their plasticity and are converted into a hard mass, which is unaffected by water. Clays are formed by the weathering (i.e. decomposition) of igneous and feldspar rocks by various agencies through time and are composed essentially of hydrated aluminium silicates such as (Al2.Si2O7.2H2O) together with other substances such as quartz, which were present with the feldspar in the original rock (e.g. granite).

2KAlSiO8 +2H2O +CO2K2CO3+ Al2O3 .2SiO2 .2H2O+4S1O2

The alkali is leached out by water.

1.2	Statement of the Problem

There is availability of refractory clay in Tsonga, Edu Local Government Area, Kwara North of Kwara State which can be used for lining of furnace. So, the study is to evaluate its certain properties with the addition of silicon carbide and graphite so that the refractory can be adequately and effectively utilized for furnace lining.

1.3	Significant of the Study

In Nigeria today, there is need to cultivate the habit of processing our local raw materials into useful form. So, the idea of developing Tsonga refractory clay into useful form for lining of furnace is to save foreign exchange and also create employment opportunity for the people.

1.4	Aim and Objectives of the Project

The aim of this project work is to study the effect of graphite additive on the refractory properties of Tsonga clay.

The objectives of the study are as follows:

- To leach out the detrimental constituents particularly oxides of sodium and potassium, which reduce the refractoriness of the clay;

- To test for the refractory properties of the blended clay.

1.5	Scope of the Study

The study will cover the addition of graphite on Tsonga refractory clay in which the refractory clay will be characterized. The refractory properties such as linear shrinkage, apparent porosity, bulk density, thermal shock resistance and cold crushing strength would be carried out on this refractory clay.

CHAPTER TWO

2.0	LITERATURE REVIEW

2.1	Identification of Clay Materials

(Chester,1973) traced the first refractory used by man to the fireclay, on his work on refractory, fireclay is plastic in nature and when mixed with water become singularly useful for the production of crucible for metal melting and refractories for lining furnaces. Mineral impurities in clays vary considerable and this depends on the different deposits or locations. The amount of particular clay minerals present varies in the crystalline of a particular clay mineral of different sizes. The chemical composition, the mineralogical and the physical characteristics are all varying properties due to different locations or deposit of clays. A common characteristic is their crystalline structure consisting of electrically neutral alumina - silicate layers which lead to a fine particle size and plate-like morphology and allows the particle to such physical properties as soapy feel and easy cleavage.

All clay minerals according to the geologist are of secondary geologic origin that is; they were formed as alteration products of aluminium-silicate rocks in an environment in which water is present. In view of these natural variations, it is important to identify and classify clay mineral from any deposit. The particular properties or class of properties of the clay minerals can be used to group them together. These properties include:

Physical or chemical change

(i)	Those dependents on some physical and chemical within a mineral, which can be measured under, controlled conditions such as in thermal analysis. This method is use to identify and estimate the mineral content of clay materials and in assessing the principal reactions and the temperature at which they occur.

(ii)	Those that depend on the chemical nature of the mineral such as spectrographic analysis, chromatographic analysis and flame photometry. All the elements can be revealed by this chemical method and their proportion in a sample. The analysis results are usually expressed in terms of oxides present such as silica (SiO2), Alumina (A12O3) etc. Therefore the forms in which various elements are combined cannot be indicated by those methods of analysis, this is when sulphides are present, and the result in terms of oxides will introduce error.

(iii)	Those dependent on the external crystallographic features of the mineral, that is, the microscopic properties. The use of optical microscope is employed in this method for examination of thin section in transmitted light which may be ordinary light plane-polarized light under which some minerals like micas, biotitie, display pleochroism, that is, show of colour change when rotated under the plane-polarized light.

(iv)	Those dependent on the inter-atomic or ionic arrangement within the crystal lattice. They include x-ray diffraction, infrared and electron diffraction analysis.

2.2	Types of Clay

In a seminar held at Federal Institute of Industrial Research, Oshodi, Lagos. (Dr. Irabor J.) analyzed the various types of clays that exist on the earth crust. Among these he said, include:

- Kaolin: - These are clay formed by the weathering on site of feldspars and are usually called the primary clays. Kaolin clays are characterized by coarse particle, non-plastic and highly refractory. It has its melting point at l800°C. Because of its coarse particle texture, it possesses low volume shrinkage, and a reduction in the water content of kaolin turns it to montmorillonites which possess a less (or medium) grain size particles, further reduction of water from montmorillonites turns it to illites, a fine particle clay size.

- Ball clay: This type of clay has opposite properties to that of kaolin. It is secondary clay found in stratified layer with alternating layer of coal and other types of clay. It tightens into a dense structure when fixed to about 13°C and burn into light grey or buff colour. They are characterized by excessive shrinkage up to20% when fired because of the presence of carbonaceous materials, which burns off during firing.

- Earthenware clay: - This includes most of the valuable clay found in nature. It may contain iron and other impurities, which cause it to become light and hard-fired at about 950- l000oC. The presence of non-oxide impact the colour of red brown, grey in raw state, and these colours change on firing to pink, tar red, brown or black depending on the condition of firing.

2.3	Chemical Composition of Clay

Clay in its natural states, consist of mineral of primary origin, present in the rock and undergone no significant changes. It also consists of minerals of secondary origin, produced by the action of chemical and physical agents on the primary mineral resulting in breakdown and conversion to secondary minerals. The usual chemical composition of clay is similar to the earth as a whole. Silica and alumina content of clay are usually very similar with every small amount of iron. Clays with better composition contain a relatively more alumina and less iron. In view of this study, blending together of two different clay may result in better composition constituent of these oxides, which possess good refractory properties e.g, MgO, CaO, SiO2, A12O3.

If one sample of clay possesses higher MgO, the second clay may possess higher SiO2 or CaO and this effect results in higher refractoriness.

The results of David and Delman on the analysis of the chemical composition of the different clays are shown in table 2.1 below:

Table 2.1: Chemical Composition of Clay

| Compound | Kaolinite | Fireclay | Earth ware | Stone ware | Brick Clay |
| --- | --- | --- | --- | --- | --- |
| SiO2 | 44-52% | 44-56% | 45-60% | 45-75% | 60-80% |
| A12O3 | 34-39% | 31-38% | 24-38% | 15-37% | 5-20% |
| Fe2O3 | 0.3-1.0% | 0.6-3.0% | 0.8-1.2% | 0.7-4.5% | 3-15% |
| TiO2 | 0.1-1.0% | 0.2-2% | 0.2-2.0% | 0.2-2.0% | - |
| CaO | 0.2-2.0% | 0.1-1.0% | 0.1-1.3% | 0.1-1.0% | 0-0.8% |
| MgO | 0.1-0.7% | 0.1-1.0% | 0.1-1.0% | 0.1-1.0% | 0-0.3% |
| Mg2O + K2O | 0.1-1.5% | 0.1-1.5% | 0.1-2.0% | 0.2-2.0% | 3-15% |

Table 2.2 Chemical Composition of a Typical Clay

| Constituent | Percentage |
| --- | --- |
| SiO2 | 45 |
| A12O3 | 40 |
| Fe2O3 | 0.40 |
| Na2O | 0.15 |
| K2O | 0.10 |
| CaO | 0.05 |
| TiO | 1.15 |

Table 2.2 Shows that silicon and aluminum oxide are the principal ingredients in typical clay, these two constituent elements in clay are the ones that combined with water to produce clay.

Apart from these two elements, all other elements facilitate the formation of fluxes.

2.4	Classification of Refractories

Norton defined refractories as embracing all materials that can withstand high heat effect, chemical and physical effects within the furnace. They are used in processes that involves high temperature such as steel making, cement making, Glass making, etc. On the basis of chemical reactivity and the nature of slay to be generated in furnaces, refractories have been classified as acid, base and neutral.

2.4.1	Acid Refractories

They have silica (SiO2) as their main constituents. However alumina (A12O3) may also be present in substantial amounts. Based on alumina content, acid refractories have been subdivided into siliceous, firebricks and aluminous bricks. Acid refractories are known to react readily with basic clay.

2.4.2	Basic Refractories

These are based on magnesium oxide (MgO). They generally include magnesite, dolomite and chrome magnesite. However, alumina and mullite are classified as basic refractory because of their amphoteric character. Calcining magnesite rock produces the MgO. Basic refractories are usually attacked by acid slag.

2.4.3	Neutral Refractories

This group does not have pronounced acidic or basic properties (Graphite, Chromite). Alternatively, the acidic basic properties are almost equally balanced.

2.4.4	Super Refractories

These are specially developed for use at exceptionally high temperature (above 1800oC) or for contact with very reactive gas, for instance in gas turbines. These include zirconia (ZrO2) Thoria (ThO2), Beryllia (BeO) and various other carbides and borides.

2.5	Mechanism of Bonding in Refractory Materials

2.5.1	Binding Properties of Clay

The bonding action in clays is acquired only in the presence of adequate amount of water. The water added to the clay particles penetrate the mixture and form microfilm which coats the surface force between the clay particles forming a plastic mass that can be moulded to desired shapes and then fire to hard-mass. Plasticity and bond formation are developed by the addition of water. Net attractive force are developed or generated between charged hydrated clay particles or micelles and between these and other particles of the clay type. This effect is more pronounced when two different clays are blended together inverse in the amount of chemical constituents cause increases in the rate of bond formation. The strength of the ionic bond form is a function of the total surface area of the particles and is strongly influenced by the adsorption of exchangeable cation at the free surface, this modify the balance of the local forces between the particles.

2.5.2	Mechanism of Bonding

The bonding mechanism in clay varies with different clay and with the particle size of such clay. Some factors are responsible for these bonding action of clay and these include.

- The base exchange phenomenon

- Surface tension forces and inter-particle friction.

Base exchanges phenomenon

In the base exchange phenomenon, clay crystals become negatively charge either by absorption of anion on its surface (through water molecules) or because of an unsaturated valency bond at the surface of the clay particles, therefore, dissociation of ion occur when clay is suspended in water, this occur to a distant depending on their valency so that each cation of the clay may be exchange for one another. The Base Exchange phenomenon is found to be more pronounced in the fine crystal particles, where there are enough surface area of contact between the clay to clay ions and the water to clay ions. This leads to a strong bond between the clay and water.

Surface tension and inter-particles friction

These are responsible in the coarse particle size of clays, when being compacted, the coarse particle which are basically silica sand are bonded together. The clay form a lens shaped masses at the point of contact of the silica (coarse) grain and with similar clay layer on neighbouring grain bonding the silica grain. Here, there is a small area of contact between the silica and the clay binder. The coarse particles on joining together create some pore spaces within its grains, this pores are filled with water during compaction, hence a weak bond exist between the water molecules and the coarse particle in its vicinity. This weak bond helps to keep the clay particle into solid mass when moulded

Fig. 2.1 Fine (firmly bonded) clay 		Coarse (loosely bonded) clay

Particles with water binder, 			particles resulting from small

Resulting from large area of contact 			area of contact

It is an obvious fact that low contact result in a small bond area, subsequently a weaker bond, while forcing the grains firmly together creates a larger bond and subsequently a strong bond.

On drying, clays losses water absorbed, these loss of water absorbed, produces shrinkage of the lattice and further strength the bond so that clay binders are effective in both the green and dried condition. Hydration is reversible to temperature well above the drying range. This mould may be dried or used directly. Heating clays to oppressively higher temperature however, removes the chemically combined water and causes permanent loss of binding capacity, the temperature by which this occur varies with the particular clay but the loss begin at approximately 400°C and in all cases complete at700°C.

Kaolin, when compacted changes to illite as a result of reduction in its water content. Further losses of water in illite turn it to montmorillite. Kaolin crystals tend to be larger than illite and illite crystals tend to be larger than montmorillitc.

2.6	Other Refractories and Abrasive Materials Used

2.6.1	Silicon Carbide

SiC Molecular weight 40.07; specific Gravity 3.2; disassociates without fusing at about 2250°C, silicon carbide exhibits excellent chemical stability falls between corundum and diamond or 9 and 10 on mohrs hardness scale and because of its high thermal emissivity, conductivity and low thermal expansion has found wide acceptance in high temperature refractory applications.

Electrical resistance of SiC is such that the materials belong in a class known as semiconductors. The resistance varies with decreased and increased temperatures. Products associated with silicon carbide are loose grain or grinding compounds, bounded abrasives, coated abrasives refractories and various engineered ceramic applications such as seals, nozzles, valves from automotive engine component, heat exchangers, solar receivers combustors, suction box covers and various wear applications in the pipe industry.

SiC refractories are classified into types as the basis of the bonds used. Associated type bonds are oxide or silica, clay, silicon oxymtride, siliconmtride as well as self-bonds. The dense silicon carbonate contain 85 to 90% SiC; the clay bonded contain 75 to 80% SiC and the semi silicon carbide are still lower in SiC content.

Properties of these various type of silicon carbide refractories vary according to the type and amounts of bond used. Generally speaking, SiC refractories exhibit properties that warrant its use in kiln furnace applications, structural member chemical and municipal incinerators coal handling equipment, recuperators tubes muffles, retorts crucible and pyrometer projection tubes. Added to plastic, fireclay, silicon carbide imparts its properties of high thermal emissivity and conductivity to the refractory and extends the useful application of this material. Silicon carbide also finds application as refractory cements, laying SiC brick or mortars are sized for each specific application. Bonds generally of phosphate or clay type impart thermal working range to the particular cement and maintained at predetermined temperature.

The electrical properties of silicon carbide have permitted the successful use of this material in applications such as heating elements, lighting arrestor blocks and electronic components. Silicon carbide is used increasingly as wear materials in both its seal bonded and nitride-bonded porous form as well as dense centered shapes of single-phase materials which are useful to extremes of temperature, wear or corrosion. Application such as seals, coal chutes, handling equipment and proper machine components are widely practiced.

Silicon carbide also is used extensively in the production of both bonded and coded abrasives.

2.6.2	Graphite

Graphite is nature best refractory and graphite refractories have many desirable properties such as high thermal conductivity, high electrical conductivity, low thermal expansion, high resistance to molten metal and flux attack, excellent heat shock resistance, increased strength at high temperatures, resistance to wetting by molten substances and also high refractoriness. All types of graphite are used in refractories. Madagascar flake is used almost exclusively in crucibles. Mexican, Ceylon and flake dusts are used in manufacturing of foundry facings.

Their purpose is to prevent sand from adhering to metal castings. Other graphite containing refractories include stopper heads and nozzles, retorts, tubes, rods and stirrers, bricks, slabs and special shapes, refractory cements and plastic linings for cradles, runner e.t.c. Amorphous graphite is used in most ramming mixes which are generally used in the steel industries.

Graphite is mixed with fire clay to produce plastic patch material, unburned brick, proportion of graphite used in various refractories will vary from 10% to 60% except in foundry facing where some grades of pure graphite are used.

CHAPTER THREE

MATERIALS AND METHODS

3.1	Materials

The materials used for this project includes; refractory clay from Tsonga in Kwara State, graphite and water.

3.1.1 	Equipment

The equipment used for this research are compression moulding machine, Muffle Furnace, oven, desiccators and compression testing machine

3.2	Methods

The as-received clay material was soaked in water for three days, decanted to remove the water and then dried in the sun. This treatment was necessary to remove alkalis and some dead organic matters contained in the raw clay samples. The presence of alkalis, containing sodium and potassium is known to retard mullite formation and hence lower the refractory and strength. The dried clay was grounded into powder using a ball mill. The powdered clay was sieved through 860μm mesh. The sieved clay was mixed thoroughly with 30% ground graphite. The drying was first done in open atmosphere for 24hours, after which it was then dried in the oven at a preset temperature of 110oC. The samples was then fired in the muffle furnace at a temperature of 900oC.

3.2.1	Experimental Testing Procedures of the Refractory Bricks

The fired refractory bricks produced were tested for linear shrinkage, apparent porosity, bulk density, cold crushing strength, and thermal shock resistance.

3.2.2	Measurement of Linear Shrinkage

Green bricks were pressed in a box of size 75mm x 75mm x 75mm. The shrinkage properties of the pressed bricks were determined measuring the green dimension of the bricks using a ruler or a vernier caliper. These were then compared with the fired dimension; the linear shrinkage was calculated as a percentage of the original green dimensions (i.e. ∆L/L).

Where ∆L is the change in length of the fired brick and L is the original length of green brick.

3.2.3	Determination of Apparent Porosity and Bulk Density

For each of the samples, six test bricks each of 46mm x 42mm size after firing were tested. The dry weight (W1) of each specimen was measured; after which the specimen was transferred and suspended in a vessel of boiling water for 20 minutes. At this time, the boiling was discontinued and the hot water was replaced by cold water. After 30 minutes in cold water, the weight (W2) was measured. The soaked specimen was weight in air (W3). The apparent porosity of the brick was calculated using the following relations.

Pa= W3- W1W3-W2 ×100%

Where:    Pa is apparent porosity,

W1 is weight of dry sample,

W2 is weight of sample suspended in cold water, and

W3 is weight of soaked sample suspended in air. The bulk density BD was determined from the following relationship.

BD	=

3.2.4	Determination of Cold Crushing Strength

The cylindrical brick measured 49mm in diameter and 75mm in length was subjected to strength test using universal strength-testing machine. The strength values of the brick in the direction of forming were recorded.

3.2.5	Determination of Thermal Shock Resistance

A standard square brick 75mm x 75mm x 75mm was placed in the furnace and this was maintained at 1100°C for 30 minutes. The brick was cooled in air for 10 minutes. The brick was tested for failure using a standard rig. This cycle of heating, cooling and testing was repeated, until fracture occurred. The number of complete cycles required to produce fracture in each specimen was noted and recorded.

CHAPTER FOUR

4.0	RESULTS AND DISCUSSION

4.1	Results

Table 4.1 shows the result of particle size of Tsonga clay analysis using Gaudin Schuhmann’s method. The physical properties of the pure Tsonga clay sample are presented in table 4.2, while chemical compositions of Tsonga clay are presented in table 4.3. Table 4.4 shows the physical properties of Tsonga clay blended with 20% to 40%. Graphite while figures 4.1 to 4.6 show the graphs of the results.

Table 4.1: Particle Size Analysis of Tsonga Clay

| S/N | Sieve size range (μm) | Nominal Aperture (μm) | Weight Retained (g) | % weight Retained (g) | Cumu lative (%) under size | Log of Cumu lative (%) under size |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | +1000 | 1000 | 22.42 | 4.48 | 95.52 | 1.980 |
| 2. | -1000+850 | 850 | 39.08 | 7.82 | 87.70 | 1.943 |
| 3. | -850+500 | 500 | 97.58 | 19.52 | 68.18 | 1.834 |
| 4. | -500+300 | 300 | 105.61 | 21.12 | 47.06 | 1.673 |
| 5. | -300+180 | 180 | 127.92 | 25.58 | 21.48 | 1.332 |
| 6. | -180+125 | 125 | 80.27 | 16.05 | 5.43 | 0.740 |
| 7. | -125+63 | 63 | 18.10 | 3.62 | 1.81 | 0.260 |
| 8. | Pan |  | 5.36 | 1.06 |  |  |

Initial weight of samples = 500g

Table 4.2: Physical Properties of Clay Sample

| Sample Location | Bulk Density (g/cm3) | Apparent Porosity (%) | Permeability | Linear Shrinkage (%) | Thermal Shock Resistance | Cold Crushing Strength (KN/m2) | Refractoriness (oC) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bacita | 2.30 | 22 | 84 | 4 | 30+ | 12000 | 1500 |
| *Fireclay | 2.30 | 20 – 30 | 25 – 90 | 7 – 10 | 20 – 30 | 15000 minimum | 1500 – 1700 |

Table 4.3: Chemical Analysis of the Tsonga Clay Sample

| Parameters | Level Detected (%) |
| --- | --- |
| SiO2 | 47.06 |
| A12O3 | 36.16 |
| Fe2O3 | 0.72 |
| CaO | 0.14 |
| TiO2 | 1.35 |
| MgO | 0.09 |
| K2O | 0.07 |
| Na2O | 0.02 |
| LOI | 12.78 |

Table 4.4: Physical Properties of Tsonga Clay + Graphite

| Silicon carbide addition | 20% | 25% | 30% | 35% | 40% |
| --- | --- | --- | --- | --- | --- |
| Thermal Shock Resistance at 12000C | 28 | 28 | 29 | 30+ | 30+ |
| Permeability (cm/sec) | 70 | 66 | 62 | 57 | 50 |
| Apparent porosity at 12000C (%) | 20.6 | 18.02 | 17.74 | 15.00 | 12.84 |
| Bulk density (g/cm3) | 2.27 | 2.24 | 2.20 | 2.10 | 2.13 |
| Linear Shrinkage (%) | 4.20 | 4.16 | 4.16 | 4.00 | 4.00 |
| Cold Crushing Strength (KN/m2) | 16200 | 18200 | 21200 | 19117 | 17000 |

Refractoriness: Intact at the furnace temperature

Figure 4.1:	Effect of Graphite Additive on Thermal Shock Resistance of the Brick

Figure 4.2:	Effect of Graphite Additive on Permeability of the Brick

Figure 4.3:	Effect of Graphite Additive on Apparent Porosity of the Brick

Figure 4.4:	Effect of Graphite Additive on Bulk Density of the Brick

Figure 4.5:	Effect of Graphite Additive on Linear Shrinkage of the Brick

Figure 4.6: Effect of Graphite Additive on Cold Crushing Strength of the Brick

4.2	DISCUSSION

4.2.1	Thermal Shock Resistance

Figure 4.1 shows that the thermal shock resistance of pure Tsonga clay sample falls within the acceptable values of 25-30 cycles. The TSR of Tsonga clay blended with Graphite blend is found to increase as the percentage of Graphite in the clay sample increase and fall within the recommended values of 25 – 30 cycles (De Bussy, 1972). This result was as a result of uniform heating and cooling. Long soaking refractories at high temperature increases mineral inversion, thereby causing high thermal shock resistance.

4.2.2	Permeability

Figure 4.2 shows that the permeability number of the pure sample is within the internationally accepted range of 25 – 90. The permeability of the blended clay with Graphite fall within the recommended value and reduces as the percentage of Graphite increases. Permeability is a function of gases or liquid passing through the brick. Refractories under the influence of gases and liquid should be impervious, this would help to eliminate leakage of gases and penetration of liquids through the walls of the furnace (Chester, 1973).

4.2.3	Apparent Porosity

Figure 4.3 shows that the value for the pure clay sample falls within the standard values of 20 – 30% (Chester, 1973). The values for the blended clay sample with Graphite reduce as the percentage of graphite increases. The value may be increased by addition of fine grain silica or additives such as sawdust, baggage, and rice husk.

4.2.4	Bulk Density

Figure 4.4 shows that the average bulk density of the pure clay sample was within the range of 1.7 – 2.lg/cm3 for dense firebricks and 2.2 – 2.80g/cm3 for high alumina refractories (Chesti, 1986). Bulk density is an important property of steel - work silica brick. The bulk density values of the brick made from 20 - 40% additions to Tsonga clay with graphite decreases as the percentage of graphite increases.

4.2.5	Linear Shrinkage

Figure 4.5 shows that the average linear shrinkage for the pure clay sample is within the recommended values for fireclay, 2 – 7% (Chester, 1973). The average linear shrinkage for the blended clay sample reduces as the percentage of Graphite increases. Higher shrinkage values may result in warping and cracking of the brick and, this may cause loss of heat in the furnace.

4.2.6	Cold Crushing Strength (CCS)

Figure 4.6 shows that the Tsonga clay sample have value below the recommended value. The Cold Crushing Strength of the blended clay with Graphite increases up to a certain level after which decreases as the addition of Graphite increases. Cold crushing strength shows the effect of firing on ceramic bond and this may be affected by firing, sintering characteristics and pressing method.

4.2.7	Refractories

The refractoriness of the pure clay sample from Tsonga fall within the recommended value of 1500 – 1700°C, the refractoriness of blended clay sample with Graphite and Silicon carbide at the maximum temperature obtainable in the furnace is 1600°C. The sample is still intact. This value showed that the sintering temperature is high in the blended clay, which is an indication of good refractoriness, which falls within the range of 1580-1759°C for fire clay (Grimshaw, 1971).

4.2.8	The Loss on Ignition

The value obtained for 100% Tsonga clay is within the range recommended for Kaolinic clay, which have values in the range of 12 – 15%.

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDAT1ONS

Having gone through the experimentation and the result gotten, necessary conclusion has been arrived at and with this view, recommendations were also presented.

5.1	Conclusions

The investigations on the properties of the blended clay sample show that its values compare favourably with imported fire clay refractories. The result revealed that the addition of 20 – 40% silicon carbide and graphite gave an improvement in the refractoriness, permeability, linear shrinkage, apparent porosity, thermal shock resistance and cold crushing strength properties of Tsonga clay. It can be classified as heavy-duty refractories based on the range of 1600 – 1760°C. The refractory properties showed that the blended clay sample could be used for the production of refractory bricks or ramming mass for furnace lining operating at temperature of about 1700°C.

5.2	Recommendations

These include suggestions for improvement study with related aspect.

The recommendations are as follows:

- Studies should be carried out on other properties such as modulus of rupture, refractory under load and slag resistance.

- Studies should be done on other types of additives and make comparison to determine the most suitable.

REFERENCES

Ajuwa, I. C. and Oakhinan, E.P. (1990), Nigeria: Developing a Domestic Refractory Industry”, Journal of American Ceramic Society. Pp 656-657.

Akinbode, F. O. (1996), “An Investigation on the Properties of Refractory Material for Furnace Lining. Indian Foundry Journal, Pp 10-13.

Aliprandi G. (1979). Matériaux réfractaires et céramique techniques. Septima, Paris.

Amrane B., Ouedraogo E., Mamen B., Djaknoun S. and Mesrati N. (2011). Experimental study of thermo-mechanical behaviour of alumina-silicat refractory materials based on a mixture of Algerian kaolinitic clays. Ceramics International, 37, 3217-3227.

Boch, P. (2001). Matériaux et processus céramiques. Hermès Science Publications, paris.

Boch, P. (2001). Propriétés et applications des céramiques. Hermès Science Publications, paris.

Bomeni I.Y., Njoya A., Ngapgue F., Wouatong A.S.L., Yongue F.R., Kabeyene V.K. and Fagel N. (2018). Ceramic with potential application of ngwenfon alluvial clays (noun, west cameroon) in building construction: Mineralogy, physicochemical composition and thermal behaviour. Construction and Building Materials, 182, 493–503.

Chaouki S. (2014). Recent advances in silica-alumina refractory: A review. Journal of Asian Ceramic Society, 283-96.

Chester, J. H. (1973), Refractories, Production and Properties. The Iron and Steel Institute, London, Pp 4-13,295-315.

Chesti, A. R. (1986), Refractories Manufacture, Properties and Applications. Prentice-Hall of India, New Delhi. Pp 25-27, 60-90.

Chigbo, G. O. (1965), The characteristics of Nigeria Clays (Melewon Clay). Research report No 34, Federal Institute of Industrial research, Oshodi, Lagos. Pp 809.

David Z., Karel L., Lukáš T., Dalibor V., Lenka N., Petr Š., Pavel K., Lucie K. and Karel D. (2021). Development and Properties of New Mullite Based Refractory Grog. Materials, 14, 779.

Day, M. F. (1979), “Materials for High Temperature Use.” Engineering Design Guides, Vol. 28. Oxford University Press. Pp15.

De Bussy, J. H. (1972), “Materials and Technology”. Vol. 2, Non -Metallic Ores, Silicate Industries and Mineral Fuels. Longman Group Limited, Pp 267 - 290.

Grimshaw, R. W. (1971), “The Chemistry and Physics of Clays. Pp 211-327.

Hassan, S. B. (2001), “Effect of Silicon Carbide on some Refractory Properties of Kankara Clay” N. S. E. Technical Transactions, Vol. 28, No 3, Pp 46 - 52.

Hossain S.S. and Roy P.K. (2021). Preparation of multi-layered (dense-porous) lightweight magnesium-aluminum spinel refractory.Ceramics International, 47,13216–13220.

Jam, P. C. (1992), “Engineering Chemistry”. Dhanpat Rai and Sons, Nai Sarak, Delhi. Pp 582-593.

Jan K., Jiří H., Jaroslav K., Jan B. and Tomáš H. (2022). Effect of high-temperature inert gas atmosphere on the thermal stability of advanced refractory materials. Ceramics-Silikáty, 66 (2), 228-235.

Jouenne C.A. (1984). Traité de céramiques et matériaux minéraux. Septima, Paris.

Jourdain, A. (1966). Technologie des produits céramiques réfractaires. Edition, Paris.

Kolli, M., Hamidouche M., Fantozzi G. and Chevalier J. (2007). Elaboration and characterization of a refractory based on Algerian kaolin. Ceramics International, 33, 1435-1443.

Lapoujade, P. & Le Mat, Y. (1986). Traité pratique sur l’utilisation des produits réfractaires.Edition, Dourdan, France.

Lopez-Perales J.F., Jose E. C., Vazquez-Rodríguez F.J., Gomez-Rodríguez C.,Díaz-Tato L., Banda-Munoz F. and Eden A. R. (2021). Partial replacement of a traditional raw material by blast furnace slag in developing a sustainable conventional refractory castable of improved physical-mechanical properties. Journal of Cleaner Production, 306, 127266.

Maiti K.N., Agarwal P. and Savsani R. M. (2004). Use of beneficiated blended clays in traditional ceramics. Transactions of the Indian Ceramic Society, 63(1), 15-19.

Minh T.T., Thanh M.P., Ngoc H.P., Thi Diem N., Thi Xuan Q.N., Minh T.D., Van T. L. and Hoai T.N. (2018). Manufacturing of Chamotte Refractory Brick from Clay Sources in Vietnam. Journal of Engineering Science and Technology Review, 11(4), 25-30.

Muhammed O.H.A., Simon I.I. and Folorunsho T.L. (2019). Refractory Properties of Alumina/Silica Blend. The West Indian Journal of Engineering, 42, (1), 22-32.

Oniya, K (1967), “Brick making Characteristics of some Nigerian Clays. Research Report No 37,Federal Institute of industrial Research, Oshodi, Lagos. Pp 6 – 8.

Poirier, J. (2011). Les céramiques réfractaires, de l’élaboration aux propriétés d’emploi. Verres Ceramiques & Composites, 1 (2), 28-42.

Routschka G. (2004). Refractory materials. 2ndEdition, Vulkan-Verlag, Essen, Germanic.

Subhojeet G., Chirag S., Atul M. and Swapan K.D. (2013). Effect of reactive alumina on the physico-mechanicalproperties of refractorycastable. Transactions of the Indian Ceramic Society, 72(2) 113-118.

Trojan, P. K. (1990), Engineering Materials and their Applications”. Oxford University Press, Fourth edition. Pp 358-362.

Wayne, A. E.(1979), Structural Clay, Refractories and Abrasive Materials, Vol. 183, No l, A Cahner Publication. Pp 23-42.