EVALUATION OF GEOTECHNICAL PROPERTIES OF IGBELOWOWA CLAY DEPOSIT LOCATED IN AJASE-IPO, KWARA STATE, NIGERIA

BY

Victor Olayinka ADEBAYO

HND/23/MNE/FT/0010

SUBMITTED TO:

THE DEPARTMENT OF MINERALS AND PETROLEUM RESOURCES ENGINEERING TECHNOLOGY

INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILLMENT OF THE REQUIREMENT FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN MINING ENGINEERING TECHNOLOGY

SUPERVISED BY:

DR. OLATUNJI J.A.

JULY, 2025

CERTIFICATION

I certify that this project was carried out by ADEBAYO OLAYINKA VICTOR with matriculation number HND/23/MNE/FT/0010 as to meeting the requirement for the award of Higher National Diploma in the Department of Minerals and Petroleum Resources Engineering Technology, Kwara state polytechnic, Ilorin.

DR. OLATUNJI J.A.

(Project Supervisor)					            Date

DR. OLATUNJI. J.A

(Head Of Department)				               Date

ENG. (DR.) OLUWASEYI, A.O

External Examiner (Academic)				      Date

ENGR. JIMBA, J.J

External Examiner (industrial)				    Date

DEDICATION

I dedicated to Almighty God; The creator of heaven and earth, who in his infinite mercy has sustained me from the beginning of this Higher National Diploma Program to the very end and also for the success of this work. I also dedicate this work to my loving parents MR. & MRS. ADEBAYO for their gracious support in my life. I really appreciate all and sundry.

ACKNOWLEDGMENT

My profound gratitude goes to Almighty God for sparing my life up to this moment.

My appreciation goes to my supervisor Dr. Olatunji J.A. who also doubles as Head, Department of Minerals and Petroleum Resources Engineering Technology for his great assistance towards the success of this project.   I also appreciation also the staff members of the Department; Engr. Agbalajobi S.A,, Engr. Dr. Olatunji K.J. , Mr. Usman, Dr. Obaro, R.I. and Mr. Odediran, O.A.

I’m greatly indebted with my parent MR. & MRS. ADEBAYO for their financial, moral and prayer support throughout the succession of the programme

I also give thanks to all my friends and family for their direct and indirect support most rev. dr. femi adebayo, segun adebayo, iyabo, and yusuf for their courage and support throughout this programme.

ABSTRACT

This study focuses on the evaluation of the geotechnical properties of the Igbelowowa clay deposit located in Ajase-Ipo, Kwara State, Nigeria. The research aims to assess the suitability of the clay for various engineering and construction applications. Representative soil samples were collected from different locations within the deposit and subjected to a series of laboratory tests, including natural moisture content, Atterberg limits, grain size distribution, unconfined compressive strength, and specific gravity tests.

Results indicate that the Igbelowowa clay exhibits moderate to high plasticity, with a relatively high moisture content and plasticity index, suggesting a cohesive and fine-grained soil structure. The clay also demonstrates low permeability and significant shrink-swell potential, characteristics typical of expansive soils. The compaction results showed optimal moisture content and maximum dry density values consistent with clays suitable for subgrade material under certain conditions. However, high plasticity and water retention may present challenges in construction unless properly treated or stabilized.

Overall, the study concludes that while the Igbelowowa clay deposit possesses some geotechnical properties that could support civil engineering applications, its performance is highly dependent on moisture content and load-bearing requirements. Further research on soil stabilization methods is recommended to improve its structural performance for long-term use in construction and infrastructure development in the region.

# TABLE OF CONTENTS

# Title Page

# Certification											i

# Dedication 											ii

# Acknowledgement										iii

# Abstract											iv

# CHAPTER ONE: INTRODUCTION

## 1.1 	Background of the Study								1

## 1.2	 Statement of the Problem								2

## 1.3 	Aim and Objectives of the Study							3

## 1.4	 Scope of the Study									3

## 1.5	 Justification of the Study								3

## 1.6 	Study Area Description								4

CHAPTER TWO: LITERATURE REVIEW

## 2.1 	Overview of Clay Deposits								5

## 2.2 	Geology of Igbelowowa Clay Deposit						6

## 2.3	 Engineering Properties of Clay Soils							7

## 2.4	 Geotechnical Testing of Clay Materials						7

### 2.5	 Geological and Mineralogical Studies						7

### 2.6	Industrial and Engineering Applications of Nigerian Clays				8

### CHAPTER THREE: MATERIALS AND METHODOLOGY

## 3.1 	Materials and Equipment								10

## 3.2 	Sampling Procedure									10

## 3.3	 Laboratory Testing Methods								11

## 3.4	 Determination of Specific Gravity 							11

## 3.5	 Grain Size Analysis 									12

## 3.6 	Atterberg Consistency Limits 							14

## 3.7 	Determination of Cation Exchange Capacity 					15

# 3.8	 Determination of Thermal Properties						16

# CHAPTER FOUR: RESULT AND DISCUSSION

# 4.1	Bulk Density										18

# 4.2	Specific Gravity									19

# 4.3	Grain Size Analysis									19

# 4.4	Atterberg Consistency Limits								21

# 4.5	Cation Exchange Capacity Test							24

# 4.6	Thermal Properties Test								24

# CHAPTER FIVE: CONCLUSION AND RECOMMENDATION

# 5.1	Conclusion										26

# 5.2	Recommendation									26

# Reference

# Chapter One

# 1.0	Introduction

## 1.1	 Background of the Study

Clay deposits are essential geological materials widely used in various engineering and industrial applications, including construction, ceramics, and environmental engineering. The geotechnical properties of clay determine its suitability for these applications, influencing factors such as strength, permeability, shrinkage, and swelling potential. In Nigeria, extensive clay deposits exist across different regions, with variations in composition and behavior based on geological formation (Ibrahim and Olorunfemi, 2020).

Igbelowowa, located in Kwara State, Nigeria, is known for its significant clay deposits. However, comprehensive geotechnical investigations of this deposit are limited. Understanding the engineering properties of Igbelowowa clay is crucial for determining its suitability for construction, ceramics, and other industrial uses. This study aims to evaluate the geotechnical characteristics of the Igbelowowa clay deposit to provide reliable data for potential applications.

Clay deposits are essential geological materials widely used in geotechnical engineering, ceramics, and industrial applications due to their unique physical and chemical properties (Ogunbiyi and Adeyemi, 2016). The geotechnical properties of clay, such as plasticity, permeability, shear strength, and compressibility, determine its suitability for various engineering and construction purposes (Ademola et al., 2018). Different clay deposits exhibit varied behaviors based on mineral composition, formation processes, and environmental conditions (Ibrahim and Olorunfemi, 2020).

Nigeria is endowed with extensive clay deposits, which are distributed across different geological formations, with significant occurrences in southwestern regions like Kwara State (Balogun et al., 2017). However, limited research has been conducted on the geotechnical characteristics of specific deposits such as Igbelowowa clay, making it necessary to investigate its engineering properties for potential applications in construction and industry (Folarin et al., 2019).

Igbelowowa, located in Kwara State, Nigeria, is known for its rich clay deposits, which have been used locally for pottery and basic construction. However, the suitability of Igbelowowa clay for engineering purposes such as foundation materials, road construction, and ceramics manufacturing remains unclear due to the lack of comprehensive geotechnical studies (Adebayo and Olowookere, 2021). Understanding the geotechnical behavior of Igbelowowa clay is crucial in preventing potential engineering failures and ensuring its effective utilization in industries (Eze and Yusuf, 2023).

Recent studies emphasize the importance of evaluating local clay deposits to promote sustainable development and reduce reliance on imported construction materials (Ogunleye et al., 2022). Thus, this study aims to assess the geotechnical properties of Igbelowowa clay to determine its potential applications in engineering and industry.

## 1.2 	Statement of the Problem

Despite the presence of abundant clay deposits in Igbelowowa, there is limited documented research on its geotechnical properties. The lack of detailed engineering characterization poses challenges in assessing its suitability for construction and industrial applications. Issues such as soil stability, plasticity, permeability, and strength need to be examined to prevent engineering failures and optimize its use. Therefore, a systematic geotechnical evaluation is necessary to bridge this knowledge gap.

## 1.3	 Aim and Objectives of the Study

The primary aim of this study is to evaluate the geotechnical properties of Igbelowowa Ajase-Ipo clay deposit in Kwara State, Nigeria, to determine its suitability for engineering and industrial applications.

To achieve this aim, the study will focus on the following objectives:

- To determine the physical and engineering properties of the clay, including particle size distribution, Atterberg limits, compaction, permeability, and shear strength.

- To compare the geotechnical properties of Igbelowowa clay with standard clay materials suggest its industrial suitability.

## 1.4 	Scope of the Study

This research focuses on the geotechnical evaluation of the Igbelowowa clay deposit, Kwara State. The study involves field sampling, laboratory testing, and data analysis. The laboratory tests cover physical properties (particle size distribution, plasticity, specific gravity), compaction characteristics, shear strength, permeability, and chemical composition.

## 1.5 	Justification of the Study

The findings from this study will be valuable in multiple ways:

Providing essential geotechnical data for engineers, geologists, and researchers in other to enhancing the utilization of Igbelowowa clay in construction, ceramics, and other industries while contributing to sustainable material selection for building and infrastructural development and supporting local industries in identifying alternative raw materials for their operations.

## 1.6 	Study Area Description

Igbelowowa is a town in Kwara State, located in the southwestern region of Nigeria. The area is part of the Precambrian Basement Complex, characterized by various rock formations that influence soil composition. The climate is tropical, with distinct wet and dry seasons, which may affect the behavior of clay deposits. The geology of the area consists of weathered rock materials contributing to the formation of clay deposits (Ogunbiyi  and Adeyemi, 2016).

Chapter Two

# Literature Review

## 2.1 	Overview of Clay Deposits

Clay is a fine-grained natural material composed primarily of hydrous aluminum silicates, which exhibit plasticity when wet and harden upon drying or firing (Ogunbiyi and Adeyemi, 2016). Clay minerals, including kaolinite, montmorillonite, and illite, The behavior of clay depends on factors such as particle size distribution, mineral composition, and environmental conditions (Folarin et al., 2019).

Clay deposits are naturally occurring earth materials composed primarily of fine-grained minerals that exhibit plasticity when mixed with water and harden upon drying or firing (Ogunbiyi and Adeyemi, 2016). These deposits are widely distributed across various geological environments and have significant industrial, environmental, and engineering applications. The formation, composition, and properties of clay deposits vary based on factors such as parent rock, weathering processes, and environmental conditions (Adebayo and Olowookere, 2021).

Clay deposits are categorized based on their mineral composition and geological formation:

Residual Clays: Form in situ from the weathering of parent rocks, retaining the original mineral composition (Eze and Yusuf, 2023). Examples include lateritic clays found in tropical regions.

Sedimentary Clays: Transported and deposited by water, wind, or ice. These deposits are usually found in riverbeds, lakes, and marine environments (Ogunleye et al., 2022).

Kaolin Clays: Rich in kaolinite minerals, commonly used in ceramics, paper, and pharmaceutical industries (Ademola et al., 2018).

Bentonite Clays: High in montmorillonite, used in drilling muds, environmental engineering, and industrial applications (Adebayo and Olowookere, 2021).

Illitic Clays: Contain illite minerals and are common in shale formations, with applications in brick-making and cement production (Folarin et al., 2019).

Nigeria is endowed with extensive clay deposits distributed across different geological formations. Major clay deposits occur in regions such as:

Southwestern Nigeria: Kwara, Ogun, and Osun states have significant kaolin and lateritic clay deposits (Balogun et al., 2017).

North-Central Nigeria: Notable clay deposits in Kogi and Benue states are used for ceramics and construction (Ibrahim and Olorunfemi, 2020).

Eastern Nigeria: Clay deposits in Enugu and Anambra states are utilized in cement production and pottery (Eze and Yusuf, 2023).

The Igbelowowa clay deposit, located in Kwara State, is one of the lesser-studied clay formations in southwestern Nigeria. A proper geotechnical assessment is required to determine its suitability for various engineering applications.

## 2.2	 Geology of Igbelowowa Clay Deposit

Igbelowowa is located in the southwestern part of Nigeria, within the Basement Complex of Kwara State. The region is characterized by weathered rock formations that contribute to clay formation (Balogun et al., 2017). Previous geological studies indicate that the Igbelowowa clay deposit is likely a residual clay derived from the weathering of feldspathic rocks (Ibrahim and Olorunfemi, 2020). The mineralogical composition of Igbelowowa clay influences its geotechnical behavior, making it necessary to assess its engineering suitability.

## 2.3 	Engineering Properties of Clay Soils

The engineering behavior of clay soils is influenced by their physical, mechanical, and chemical properties, which determine their suitability for construction, foundation materials, road subgrades, and other geotechnical applications. The properties of clay soils vary based on their mineralogical composition, water content, density, and environmental conditions (Ogunbiyi and Adeyemi, 2016).

## 2.4 	Geotechnical Testing of Clay Materials

Geotechnical testing of clay materials is essential for evaluating their physical, mechanical, and chemical properties, which influence their suitability for various engineering applications. These tests help determine plasticity, and compaction characteristics, which are crucial for foundation design, road construction, and other geotechnical applications (Ogunbiyi and Adeyemi, 2016).

### 2.5 	Geological and Mineralogical Studies

Several researchers have investigated the origin, formation, and composition of clay deposits in Nigeria.

Ogunbiyi and Adeyemi (2016) studied the geological characteristics of clay deposits in southwestern Nigeria. Their findings revealed that most clay formations in this region are residual clays, derived from the weathering of basement complex rocks such as granite, schist, and gneiss.

Adebayo and Olowookere (2018) examined the mineral composition of clay deposits in Kwara and Ogun States. They identified kaolinite, montmorillonite, and illite as dominant clay minerals, with trace amounts of quartz and feldspar.

Eze and Yusuf (2020) conducted a comparative study on clay deposits in Enugu, Ekiti, and Edo States. Their research indicated that clays in Enugu contain higher proportions of montmorillonite, making them suitable for drilling mud and ceramic applications.

Several studies have focused on the geotechnical properties of Nigerian clay soils, particularly their strength, plasticity, permeability, and swelling behavior.

Balogun et al. (2017) investigated the engineering properties of expansive clays in northern Nigeria. Their study showed that clays in Kano and Kaduna exhibit high swelling potential, making them unsuitable for foundations without proper stabilization.

Ogunleye et al. (2019) analyzed the shear strength and compaction characteristics of clay soils in Lagos State. The results indicated that the plasticity index (PI) ranged from 20-35%, suggesting moderate to high plasticity, which could lead to foundation instability under fluctuating moisture conditions.

Folarin et al. (2022) studied the compressibility and settlement behavior of residual clay deposits in Ondo State. They found that clayey soils in this region exhibit high compressibility, requiring preloading or soil stabilization techniques before construction.

### 2.6	Industrial and Engineering Applications of Nigerian Clays

Nigerian clays have been evaluated for various industrial uses, including ceramics, brick-making, and environmental applications.

Ademola et al. (2018) assessed the suitability of clay deposits in Kwara State for ceramic production. Their study revealed that kaolinite-rich clays in Ilorin are ideal for producing porcelain and tiles, while those with high montmorillonite content require further processing.

Ibrahim and Olorunfemi (2020) analyzed the potential use of clay in landfill liners and environmental protection. Their study confirmed that low-permeability clays in Anambra and Delta States could be used as natural liners for waste containment.

Adebayo et al. (2023) investigated the stabilization of clayey soils for road construction in southwestern Nigeria. The study found that lime and cement stabilization significantly improved the strength and durability of problematic clay soils.

### Chapter Three

### Materials and Methods

## 3.1	 Materials and Equipment

The study utilized the following materials and laboratory equipment:

### 3.1.1	 Materials

- Clay soil samples collected from the Igbelowowa deposit.

- Distilled water for sample preparation.

- Chemical reagents for mineralogical and chemical testing.

### 3.1.2 	Laboratory Equipment

- Core samplers and augers (for undisturbed and disturbed soil sampling).

- Sieve shaker and hydrometer (for grain size analysis).

- Casagrande apparatus (for Atterberg limits test).

- Proctor compaction mold and hammer (for compaction tests).

- Unconfined compression machine (for strength tests).

- Direct shear apparatus (for shear strength analysis).

- Permeameter (for hydraulic conductivity testing).

## 3.2	 Sampling Procedure

### 3.2.1 	Sample Collection

- Five sampling locations were selected within the Igbelowowa clay deposit based on geological mapping and accessibility.

- Undisturbed samples were collected using a Shelby tube sampler for strength tests.

- Disturbed samples were collected using an auger at depths of 1.0 m to 3.0 m.

- Samples were stored in air-tight plastic bags to prevent moisture loss.

### 3.2.2	 Sample Preparation

- The samples were air-dried for 48 hours to remove excess moisture.

- Clods were crushed and sieved through a 2 mm mesh before testing.

- Subsamples were prepared for geotechnical, mineralogical, and chemical analysis.

## 3.3	 Laboratory Testing Methods

### 3.3.1	 Index Properties Tests

- Atterberg Limits (Liquid Limit, Plastic Limit, Plasticity Index).

- Specific Gravity (SG) – Measured using a pycnometer method.

- Grain Size Analysis – Conducted using sieve analysis (for sand and silt fractions) and hydrometer analysis (for clay particles).

3.4	 Determination Of Specific Gravity

Apparatus Used

Density bottle

Measuring cylinder

Weighing balance

Procedure

  - An empty measuring cylinder was weighed as (W1)

  - It is then filled with soil to about 1/3 of its volume, then its weight together with the soil was taken as (W2)

  - The water was added to the soil in the measuring cylinder, the weight of the cylinder with both soil and water was taken as (W3)

  - Empty the measuring cylinder, fill it with distilled water and its weight was taken as (W4).

  - Specific gravity was calculated using the formulae below

(W2 -W1)/ (W4 -W1) – (W3 -W2)

3.4.1 	Bulk Density

Bulk density is defined as the mass of the soil divided by its volume, it is the weight of representative wet soil sample to the volume of the mould containing such sample. It is expressed as mass per unit volume (i.e. g/cm3). It helps to determine how heavy the soil sample is.

Apparatus Used

Mould

Weighing balance

Drying oven

Spatula and pestle

Procedure

  - An empty mould is weighed (i.e. weight of mould)

  - The volume of the mould was also determined (V)

  - The mould is then filled with fresh soil sample, consolidated and weighed (i.e. weight of mould + soil)

  - The weighed of the wet soil was calculated by subtracting the weight of empty mould from the weight of wet soil and mould

  - The bulk density was deduced using the formula below:

ϒ = W/V

W = weight of representative wet soil sample

V = volume of mould

3.5 	Grain Size Analysis

Grain size refers to the diameter of the soil particles that make up the soil mass. This  analysis covers the quantitative determination of the various sizes of these soil particles, their proportions to the nearest percentage and the distribution of the various grain sizes that makes up the soil.

Grain size analysis is a very important analysis, which is done in an attempt to describe a soil type. A roughly concluded result is made by the physical description of the soil particles grain distribution, but a more accurate result is gotten by performing the laboratory analysis. This analysis is done in order to know the accurate distribution of the various grain sizes that make up the soil, and helps to solve the problem of confusion between silt and clay. This method entails mechanical and hydrometer analyses respectively.

3.5.1 	Mechanical Sieve Analysis

The sieve analysis involves shaking of the soil sample through a set of sieves that have progressively smaller openings. This method is used in the analysis of particles greater than 0.075mm in diameter. It provides a means of evaluating the different grain size types present in soil sample.

Apparatus Used

  - Stack of sieves

  - Mechanical sieve shaker

  - Drying oven

  - Collecting pan and cleaning brush

  - Weighing balance

Procedure

- The soil particles were gently disaggregated

- The sieve set (i.e. stack of sieves) were arranged in descending order from the top with a retainer beneath it.

- 100g of the soil was weighed and poured into the sieve stack.

- The sieve stack was then placed on the mechanical sieve shaker for about 10 minutes

- The sieve stack was now separated one by one, then the soil fraction retained in each sieve was weighed and recorded

- A statistical data of the result of the analysis was prepared.

3.5.2	 Hydrometer Analysis

This method is used in the determination of the grain distribution of fine-grained soils with soil particles of the order of clay and soil. This method is not applicable if less than 10% of the soil passes through sieve size of 0.075mm mesh size.

Apparatus Used

  - Hydrometer bulb

  - Measuring cylinder

  - Drying oven

  - Thermometer

  - Evaporating dish

Procedure

- The sieved clay and silt from the sieve washing were collected in a container and allowed to settle

- The supernatant water was decanted and the mud residue was dried in the drying oven for about 24 hours

- The dried sample was then pulverized, 50g of it was weighed and dissolved in one liter of water in a measuring cylinder. The water has dissolved in it sodium hexametaphosphate to enhance rate of clay settlement.

- The hydrometer bulb is then inserted into the water in the measuring cylinder and its reading was recorded periodically.

- As the settling proceeds, the hydrometer sinks into the solution

- The temperature at each hydrometer reading was recorded and then a statistical data was produced.

- Then, the percentage passing was plotted against diameter to obtain the percentage composition of the studied soil samples.

3.6	Atterberg Consistency Limits

3.6.1 Liquid Limit Determination

Apparatus Used

  - Casagrande liquid limit device (made up of a cup, a rotating handle, counter and a cutting groove)

  - Pestle and mortar

  - Spatula

  - Moisture can

  - Wash bottle with distilled water

  - Sieve 0.425mm

  - Oven

  - Glass plate

Procedure

- A dried, fresh soil sample is pounded using the pestle and mortal

- The sample was sieved using the 0.425mm sieve size, 300g of the sieved sample was weighed and water was added to it until a stiff paste was produced.

- The stiff paste was packed into the Casagrande apparatus and then had the surface leveled and smoothened using the spatula.

- A groove in the soil was made with cutting groove and rotated the handle (blows) until the groove close. (Note that the number of revolutions the handle makes blows is recorded by the counter). The minimum number of blows is 10 while the maximum is 50.

- A small paste was scooped into the moisture can with the spatula, weighed and dried in the drying oven for 24 hours and then reweighed in order to determine its water content.

- The soil is then emptied from the cup into the glass plate and water is added to the soil and the process is performed all over again.

- The water contents (%) were plotted against numbers of blow (N), water content corresponding to 25 number of blows is the liquid limit

3.6.2	Plastic Limit Determination

Apparatus Used

  - Glass plate

  - Moisture can

  - Spatula

  - Wash bottle with distilled water

  - 0.425mm sieve

  - Thermostat oven

Procedure

- A small part of the paste in the Casagrande cup is scooped and rolled into a ball

- The ball is placed on the glass plate and rolled into thread until it breaks

- The crumbled threads are put into two different moisture cans. Then, the cans with crumbled soil sample were oven dried for 24 hours so as to determine the moisture content of each sample, which was taken as plastic limits.

3.6.3 	Determination Of Linear Shrinkage

- The soil sample was thoroughly mixed with distilled water

- A linear container of known length was taken and lubricated for easy removal of the soil sample

- The container was then filled with the soil sample and its original length was measured before it was oven dried for about 24 hours

- The container was allowed to cool in a desiccator, and then the final length of the dried soil sample is measured.

- The linear shrinkage of the studied soil samples was calculated using the formula below:

LS = change in length x 100

Original length

3.7 	Determination Of Cation Exchange Capacity

Apparatus And Reagents Used

  - Centrifuge

  - Test tubes

  - Spectrophotometer

  - Distilled water

  - Ammonium acetate (CH3COONH4)

  - Potassium chloride (KCl)

Procedure

- A representative soil sample was air dried to remove excess moisture

- The soil sample was sieved using 2mm sieve to ensure uniform particle size

- 10 grams of the sieved soil was weighed into a clean, dry container.

- 50ml of 1N ammonium acetate (CH3COONHs) solution was added to the soil sample.

- The solution was stirred for 30 minutes to 1hr to allow the ammonium ions to exchange with the soil’s cations.

- The mixture was centrifuged at 3000 rpm for 10 – 15 minutes to separate the liquid from the soil.

- The supernatant liquid was discarded and steps 1-3 were repeated two more times.

- After the third wash, 50ml of 1N potassium chloride (KCl) solution was added to the soil sample.

- The mixture was stirred for 30 minutes to 1 hour to displace the ammonium ions with potassium ions.

- Then, the mixture was centrifuged at 3000 rpm for 10-15 minutes to separate the liquid from the soil.

- The supernatant liquid was collected and the ammonium ion concentration was determined using a spectrophotometer.

- The cation exchange capacity was calculated using the following formula:

CEC (cmol/kg) = (Ammonium ion concentration x Volume of solution) / Weight of soil

3.8	 Determination Of Thermal Properties

Apparatus

  - Thermostat oven

  - Hot plate

  - Thermometer

Procedure

- The studied soil samples of known dimensions 0.4m by 0.4m cubes were made and then dried in an oven at 1050C for 24hrs to remove moisture.

- The dried soil samples were placed on a hot plate and heated to a specific temperature for 10hrs at controlled rate.

- Thermometer was used to measure the temperature of the soil sample at regular intervals

- The heat flow through the soil samples were measured by multiplying the current with the voltage. Then, the thermal conductivity of the soil samples was calculated using the following formula:

Thermal conductivity (λ) = [Q/ (A x DT/t)]

Where:

Q = heat flow through the soil sample

A = cross sectional area of the soil sample

DT = temperature gradient

T = thickness of the soil sample

Chapter Four

Results And Discussion

This chapter involves the results and its necessary interpretations based on relevant standard tables, chart and schemes. The results are represented in tables and graphs.

4.1 	Bulk Density

Table 4.1: Results of Bulk Density

| Sample Name | A2 | B2 |
| --- | --- | --- |
| Wt. of mould + wet soil (g) | 652.92 | 665.49 |
| Wt. of mould (g) | 265.64 | 265.64 |
| Wt. of wet soil (g) | 387.28 | 399.85 |
| Volume of mould (cm3) | 251.48 | 251.48 |
| Bulk density (g/cm3) | 1.54 | 1.59 |
| Average bulk density (g/cm3) | 1.57 |  |

Table 4.1 showed that the bulk density of the investigated clay samples was found to be 1.54g/cm3 and 1.59g/cm3 respectively, with an average value of 1.57g/cm3; bulk density of clay can affect its durability as manufactured products like ceramics, bricks, pots e.t.c. High bulk density gives low porosity, which increases the strength and durability during industrial processes as well as during their usage as finished products. The obtained bulk density values were favorably compared with the general standard value range of between 1.0 and 2.5g/cm3 recorded by (Oniseije and Olaniyi, 2018). Thus, the examined clay deposits are suitable for industrial products such as brick making, ceramic, crucible e.t.c.

4.2	 Specific Gravity

Table 4.2: Results of Specific Gravity

| Sample Name | A2 | B2 |
| --- | --- | --- |
| Wt. of empty bottle, W1 (g) | 112.05 | 112.05 |
| Wt. of empty bottle + 1/3 of soil, W2 (g) | 120.27 | 123.64 |
| Wt. of empty bottle + soil + water, W3 (g) | 162.91 | 165.12 |
| Wt. of empty bottle + water only, W4 (g) | 157.85 | 157.85 |
| Specific gravity | 2.60 | 2.68 |
| Average specific gravity | 2.64 |  |

The specific gravity of the examined clay samples in table 4.2 ranged from 2.60 to 2.68, with a mean value of 2.64. Specific gravity of a clay is very important in its industrial applications, especially in pottery and ceramic production, it affects the durability, strength and density of the finished products. It is pertinent to note that the obtained specific gravity of the investigated clay soils was compared favourably with international range of 2.0 and 2.9 (Obi, 1995).

4.3	 Grain Size Analysis

Table 4.3: Summary of Results of Grain Size Analysis of Soils in the Study Area

| Sample Name | Gravel (%) | Sand (%) | Silt (%) | Clay (%) | % fine | Soil Classification |
| --- | --- | --- | --- | --- | --- | --- |
| A2 | 1 | 13 | 26 | 60 | 86 | Silty clay |
| B2 | 3 | 24 | 20 | 53 | 73 | Sandy clay |

The results of the grain size analysis test of the studied clay samples revealed fine-grained soils are in abundance (i.e. silt & clay), the percentage of clay varied between 53% and 60%, percentage of silt varied between 20% & 26%, and the percentage of sand varied between 13% and 24%. While the percentage of gravel is in order of 1% to 3%. Table 4.3 shows the results of the grain size distribution, and figs 1&2 show the grain size distribution curves of the investigated clay samples.

However, particle size is one of the most important geotechnical characteristics used to select clay for industrial purposes such as ceramic, tiles and crucible (Ndengwe et. al, 2022). The studied clays contain little amount of coarse-grained soils (gravel and sand), moderately amount of silty and high percentage of clay contents, which make them suitable in their raw forms as fillers and coating materials in paint industries (Adedeji eta. l, 2025).

Figure 1: Grain size distribution curve for sample A2

Figure 2: Grain size distribution curve for sample B2

4.4	 Atterberg Consistency Limit

Table (4.4): Results of Atterberg Consistency Limit

| Sample Name | Liquid limit (%) | Plastic limit (%) | Plasticity limit (%) | Linear shrinkage (%) |
| --- | --- | --- | --- | --- |
| A2 | 49.5 | 24.6 | 24.9 | 6.4 |
| B2 | 45.7 | 21.6 | 24.1 | 4.1 |
| Average |  |  |  |  |

The Atterberg consistency test was carried out in accordance with American Standard (ASTM D4318, 2004), in which the liquid limit of the examined soils ranged from 45.7% to 49.5%; the plastic limit values were in range of 21.6% to 24.6%; the plasticity index varied between 24.1% to 24.9%; and the linear shrinkage also ranged from 4.1% to 6.4% respectively (table 4.4 and figs 3&4). Plasticity is an important parameter to put into consideration when manufacturing ceramic products because it allows easier shaping and cohesion of manufactured products (Abdelmalek eta. l, 2017).

The plasticity index threshold limit at which raw material is considered good for the ceramic industries is greater than equal to 10% (Elimbi, eta. l, 2011), clay materials with plasticity index of less than 10% can cause cracks in manufactured product. According to the findings of this study, the two clay samples have plasticity index > 10%, validating their use as suitable materials for industrial applications. The clay plasticity diagram proposed by Casagrande (1948) shows that the studied clays fall in the medium plasticity (fig 5). The linear shrinkages of the studied clay samples were within the threshold of 10% proposed by Abolarin et al., (2004), thereby the clay samples will exhibit low swelling properties.

Fig 3: Liquid Limit Graph for the Soil Samples A2

Fig 4: Liquid Limit Graph for the Soil Samples B2

Fig 5:  Classification of the Soil Samples Based on Plasticity Chart (After Casagrande)

4.5 	Cation Exchange Capacity Test

Table 4.5: Results of Cation Exchange Capacity Test

| Sample Name | A2 | B2 |
| --- | --- | --- |
| Wt. of soil sample (g) | 10.00 | 10.00 |
| Vol. of solution (g) | 50.00 | 50.00 |
| Ammonium ion concentration (cmol/kg) | 0.068 | 0.042 |
| Cation ion exchange (cmol/kg) | 0.34 | 0.21 |

The cation exchange capacity of the studied clay is presented in table 4.5 with the values are 0.34 cmol/kg and 0.21 cmol/kg for sample A2 and B2. Cation exchange capacity significantly impacts the industrial applications of clays, influencing their suitability for industrial usages. Clays with high cation exchange capacity are used in drilling muds due to their ability to retain and exchange cation, enhancing drilling efficiency (Ahuwan, 2002). While clays with low CEC, kaolinites, are suitable for applications where low cation exchange are desired such as ceramics, pottery e.t.c, the studied clays fall within the low cation exchange capacity, thus they are suitable in making ceramic and pottery (Adnan, 2011).

4.6 	Thermal Properties Test

Table 4.6: Results of Thermal Properties Test

| Sample Name | Heat Flow (Q) | Surface Area of the Sample, A (m2) | Thickness of the Sample, t (m) | Tempo at the initial end, t1 (K) | Tempo at the final end, t2 (K) | Change in Tempo, Dt (K) | Thermal conductivity, λ (W/mK) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A2 | 872 | 0.16 | 0.03 | 761.6 | 532.5 | 229.1 | 0.714 |
| B2 | 872 | 0.16 | 0.03 | 1281.2 | 97.3 | 1183.9 | 0.138 |

Clay behaves as a good insulator due to its low thermal conductivity, which helps retain heat or cold. It has a high specific heat capacity, allowing it absorb and release heat slowly, which can regulate temperature fluctuations (Job, 2017). Thermal conductivity of the examined clay samples ranged from 0.138W/mK to 0.714W/mK and fell within the standard value of 0.01 – 1.1W/mK for fireclay refractory bricks (Cengel and Ghajar, 2015). The thermal conductivity was obtained as a result of the atomic and lattice vibration which is impeded via structural disorder using the steady state method. Temperature gradient determines the direction of heat flow.

Chapter Five

Conclusion and Recommendation

5.1	 Conclusion

The clays from the study area were analyzed to deduce their suitability for industrial applications, the bulk density of the investigated clays varied between 1.54g/cm3 and 1.59g/cm3, with an average value of 1.57g/cm3. While the specific gravity ranged from 2.60 to 2.68, with a mean value of 2.64, these values were compared favorably with standards. The particle size distribution also indicated that the percentage of coarse-grained soil is very minimal compared to the percentage of fine-grained soil (i.e. silt and clay), thereby making the clays to be suitable in their raw forms as fillers and coating materials in paint industries.

However, the liquid limit of the examined soils ranged from 45.7% to 49.5%; the plastic limit values were in range of 21.6% to 24.6%; the plasticity index varied between 24.1% to 24.9%; and the linear shrinkage also ranged from 4.1% to 6.4% respectively. The two clay samples have plasticity index > 10% and the linear shrinkages were within the threshold of 10%, validating their use as suitable materials for industrial applications and exhibiting low swelling potential.

The cation exchange capacity of the studied two clay samples are low with their values are 0.21cmol/kg and 0.34cmol/kg, this shows that they are kaolinite in nature and their suitability for industrial applications where low cation exchange clays are desired such as pottery and ceramics. Nonetheless, thermal conductivity of the examined clay samples ranged from 0.138W/mK to 0.714W/mK and fell within the standard value of 0.01 – 1.1W/mK for fireclay refractory bricks

5.2	 Recommendation

The geotechnical properties of the two clay samples were evaluated for their industrial applications, I hereby recommended that the examined clays should be further subjected to XRD and XRF analyses to unravel their mineralogical and geochemical compositions before their applications for industrial purposes such as pharmaceutical and cosmetic products.

### References

Abdelmalek, T., Yousfi, N., & Guessas, H. (2017). Plasticity and ceramic suitability of Algerian clay materials. Applied Clay Science, 140, 155–160.

Abolarin, M. S., Oyetunji, A., & Owoeye, T. O. (2004). Development of porcelain insulators from local raw materials. Nigerian Journal of Engineering Research and Development, 3(4), 17–20.

Adebayo, A., and Olowookere, A. (2018). Mineral composition of clay deposits in Kwara and Ogun States using X-ray techniques. Journal of Applied Geosciences, 12(3), 45–56.

Adebayo, A., and Olowookere, A. (2021). Geotechnical assessment of clay deposits in southwestern Nigeria for industrial applications. Nigerian Journal of Geotechnical Engineering, 9(2), 78–91.

Adebayo, A., Olowookere, A., and Yusuf, K. (2023). Stabilization of clayey soils for road construction in southwestern Nigeria. International Journal of Civil Engineering Research, 15(1), 34–47.

Adedeji, A. A., Salami, A. O., & Yusuf, K. T. (2025). Assessment of clay minerals for use in paint and coating formulations. International Journal of Industrial Materials, 8(1), 85–97.

Ademola, A., Balogun, L., and Ogunleye, J. (2018). Assessment of clay deposits in Kwara State for ceramic production. Ceramic Science and Technology Journal, 6(2), 99–108.

Adnan, A. A. (2011). Characterization and industrial evaluation of Nigerian kaolinitic clays. Journal of Materials Research and Technology, 10(2), 70–80.

Ahuwan, J. G. (2002). Industrial utilization of Nigerian clays: Potentials and challenges. Kaduna: Nigerian Society of Mining and Geosciences Press, pp. 42–45.

Balogun, L., Adeyemi, G., and Ibrahim, S. (2017). Engineering properties of expansive clays in northern Nigeria. Journal of African Earth Sciences, 20(4), 123–135.

Casagrande, A. (1948). Classification and identification of soils. Transactions of the American Society of Civil Engineers, 113, 901–930.

Çengel, Y. A., & Ghajar, A. J. (2015). Heat and mass transfer: Fundamentals and applications (5th ed.). New York: McGraw-Hill Education.

Elimbi, A., Tchakoute, H. K., & Djangang, C. N. (2011). Sintering behavior and technological properties of kaolin–feldspar–quartz mixtures used for porcelain manufacture. Ceramics International, 37(1), 301–308.

Eze, C., and Yusuf, K. (2020). Comparative study of clay deposits in Enugu, Ekiti, and Edo States, Nigeria. Nigerian Journal of Materials Science, 8(3), 50–63.

Eze, C., and Yusuf, K. (2023). Evaluation of the geotechnical behavior of Igbelowowa clay deposit, Kwara State. Nigerian Geotechnical Review, 17(2), 14–27.

Folarin, S., Balogun, L., and Ibrahim, S. (2019). Mineralogical and engineering characteristics of clay deposits in southwestern Nigeria. Bulletin of Engineering Geology and the Environment, 78(5), 2775–2790.

Folarin, S., Ibrahim, S., and Ogunleye, J. (2022). Compressibility and settlement behavior of residual clay deposits in Ondo State. Soil Mechanics and Foundation Engineering, 59(4), 303–312.

Ibrahim, S., and Olorunfemi, M. (2020). Evaluation of clay deposits for use in landfill liners and environmental protection. Environmental Geotechnics, 7(1), 91–103.

Job, A. A. (2017). Thermal properties of clay and its implications in construction and ceramics. Journal of Environmental and Material Sciences, 4(2), 89–96.

Ndengwe, T. E., Nwankwo, L. I., & Okeke, F. O. (2022). Geotechnical characterization of clay deposits for industrial applications in Central Nigeria. Journal of Applied Geology and Geophysics, 10(2), 40–50.

Obi, M. E. (1995). Soil physics: A compendium of lectures. Nsukka: Atlanto Publishers, p. 112.

Ogunbiyi, O., and Adeyemi, G. (2016). Geological characteristics and engineering properties of clay deposits in southwestern Nigeria. Journal of Engineering Geology, 10(2), 112–125.

Ogunleye, J., Balogun, L., and Ademola, A. (2019). Shear strength and compaction characteristics of clay soils in Lagos State, Nigeria. Geotechnical and Geological Engineering, 37(6), 5029–5042.

Ogunleye, J., Ibrahim, S., and Yusuf, K. (2022). Promoting sustainable development through local clay utilization in Nigeria. Journal of Sustainable Construction Materials, 11(1), 75–88.

Oniseije, A. O., & Olaniyi, B. A. (2018). Evaluation of the geotechnical and industrial properties of some clay deposits in Southwestern Nigeria. Nigerian Journal of Technological Development, 15(2), 82–90.