GEOCHEMICAL AND TRACE ELEMENTAL STUDIES OF QUARRY DUST IN KAM QUARRY, KWARA STATE

By

SALAHUDEEN AFEEZ OPEYEMI

HND/23/MNE/FT/0036

SUBMITTED TO:

THE DEPARTMENT OF MINERALS AND PETROLEUM RESOURCES ENGINEERING TECHNOLOGY INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILLMENT OF THE REQUIREMENT FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN MINING ENGINEERING

JULY, 2025

Certification

This is to certify that this project was carried out and submitted by SALAHUDEEN, of Matric number HND/23/MNE/FT/0036 to the Department of Minerals and Petroleum Resources Engineering, Kwara State Polytechnic, Ilorin in partial fulfilment of the Requirement for the Award of Higher National Diploma in Mining Engineering Technology.

………………………… 	                                                       ……………………………

Dr. Reuben Obaro								Date

Project Supervisor

………………………  	                 	                                      ……………………………

Dr. J. A. Olatunji								Date

Head of Department

….………………………….                                                   …………………………………

Engr. Dr. Oluwaseyi, A.O (Academic)                                                         Date

External Examiner

………………………                                                              …………………………………..

Engr. J.J. Jimba (Industrial)                      					Date

External Examiner

Dedication

I  dedicated  this  project  work  to  Almighty  Allah, the  creator  of  every  creature  , for  his  protection  and  blessings  upon  my  life.  Also to my lovely parents Mr.  and Mrs.  Salahudeen, thank  you  for  your  guidance  and  support  over  me. Thank  you  for  being  amazing  parents, May  Almighty  Allah  spare  your  life  in  good  health  with  abundantly  blessings (Amen)

Acknowledgements

All  thanks  and  praise  be  to  Almighty  Allah  the  merciful  and  most  beneficent  God, for  his  protection, kindness,  love  and  guidance  throughout   my  stay  in  this  great  institution, and  successful  completion  of  this  project.

I  express  my  sincere  gratitude  to  my  supervisor  of  this  project  in  person  of  Dr. Reuben Obaro  for  his  sacrificial  time,  guidance,  support  and  advice  in  the  course  of  executing  this  project .  I pray may Almighty Allah bless you abundantly (Amen).

I would like to extend my heartfelt gratitude fo my parents Mr and Mrs Salahudeen for their unwavering support and encouragement and I also appreciate the assistance and encouragement from my homies which is Ajagbe Toheeb, Babatunde Taofeek and Adebayo Adeshina Adam and my friends and colleagues for their support may almighty Allah bless them all (Amen).

Abstract

Quarrying of rocks has enhanced and develop the economic diversification of Kwara State, Nigeria. However, the entire process has generates particulate pollution in the environment. The high level of particulates generated at the drilling and crushing areas depicts them as hazard zones. Quarry workers and communities living in proximity to these hazard zones are exposed to various health risks. In view of this, this project was carried out to determine the trace element concentration in the dust from Kam quarry in order to establish their extent of contamination and infer their possible human health implications. The results of major oxides suggest that the study area possess high silica along with low Fe2O3, TiO2 Na2O, K2O, MgO which reflects plutonic origin. The trace elemental composition such as As, Cd, Cr, Co, Cu Ni, Pb, Zn and Mo were interpreted based on atomic absorption spectrometry. Geochemical analysis of quarry dust from Kam quarry showed that the concentration of trace elements in the dust exceeds the permissible limit set by WHO. Some of which are very harmful to human health even at very low concentration exposure. It is certain that long exposure of quarry workers and those living in close proximity via Inhalation and ingestion can result to various health challenges. The release of these trace elements in high concentration by quarry companies enriching their concentration in the environment, polluting air, soil and both surface and ground water which variably affects human, animal and plants through this chain causing diseases and eventual death of man.

Table of Contents

Title page											i

Certification											ii

Dedication											iii

Acknowledgement										iv

Abstract											v

Table of content										vi

List of Figures											vii

List of Tables											viii

CHAPTER ONE										1

1.0	INTRODUCTION									1

1.1	Background of the study								1

1.2	Aim of the Study									2

1.3	Objective of the Study								2

1.4	Problem statement									2

1.5	Justification of the Study								2

1.6	Scope of the Study									3

CHAPTER TWO										4

2.0	LITERATURE REVIEW								4

2.1	Review of previous studies								4

2.2	Geology of Nigeria									5

2.3	Geology of the study Area								7

2.4	Composition of Quarry Dust								9

2.5	Chemical Composition of Quarry Dust						9

CHAPTER THREE										10

3.0	MATERIALS AND METHOD							10

3.1	Sample Collection									10

3.2	Atomic Absorption Spectrometry							10

3.3	Procedure for Atomic Absorption Spectrometry					11

CHAPTER FOUR										14

4.0	RESULTS AND DISCUSSION							14

4.1	Results of Major oxides								14

4.2	Discussion of X – Ray Fluorescence							15

4.3	Results of Trace Elemental Constituents						16

4.4	Discussion of Trace Elemental Composition						17

4.5	Discussion on Health Implications							17

CHAPTER FIVE										22

5.0	Conclusion and Recommendations							22

5.1	Conclusion										22

5.2	Recommendations									22

References										23

List of Figures

Figure 2.1.	Geological Map of Nigeria (Modified from Africa Atlases, 2007)		6

Figure 2.2.	Location Map of the Study Area (modified after Olasehinde et al., 1998)	8

List of Tables

Table 4.1.	Concentration of major oxides analyzed in the Quarry dusts			14

Table 4.2.	Results of Trace Element of Quarry Dust					16

Table 4.3.	Measured Concentration of some selected Heavy Metals in Dust from Kam Quarry 		and WHO (2000) maximum permissible limit				21

CHAPTER ONE

INTRODUCTION

1.1	Background of the study

Kwara is one of the major states in Nigerian that have relatively high clusters of quarrying activities. Following the effects of air pollution on general human being and environment. The major interest of people engaged in quarrying activities in Kwara State where Ilorin west and south situated is socio-economic benefits. At the same, the operation of quarrying in the state serves as internal generating fund for the local government and state government, means of business profit to private stakeholder, and it provides employment opportunities to the populace Akanbi et al. (2019). According to Adeyanju and Manohar (2017), different air pollutants are associated with health effects and they are stated as follows; nitrogen oxides (NO2) linked with lung irritation, respiratory illness, premature death, carbon monoxide (CO) associated with headaches and reduces mental alertness, particulate matters and sulphur dioxide related with increase in existing heart disease, breathing difficulties and respiratory illness The large operation of quarrying in Kwara state is not far from the myopic thinking the people have about it as a source of revenue without considering the health impacts of the operation. Therefore, this study aimed to assess the impacts of air pollution on people living in Ilorin south North close to quarry operation sites in Kwara State, Nigeria. The process of extracting quarry materials, which are typically rocks, from the ground or beneath it is known as quarrying (Godwin et al., 2021). Sandstone, limestone, perlite, marble, ironstone, slate, granite, rock salt, and phosphate rock are a few of the stones that are removed. Because the quarrying of stones is motivated by economic concerns, the acceptability of a stone for quarrying depends on its quality, its ability to be quickly and affordably transported to a big market, and its depth and inclination below the surface for easy harvesting. Removal of overburden, rock material drilling, blasting, and crushing are typical quarrying processes. The final effects of these stages of the quarrying process depend on the locations and sizes of the products. The development of dust, noise production, smoke and fumes, vibration of the ground, and production of toxic gases are common concentrated adverse consequences of quarrying. Of all the pollutants from quarrying operational operations, particulate matters are contributed to the environment through quarrying to a significant extent (WHO, 2024). Godwin et al. (2021) reported that any degradation and alteration of environment enhance ambient conditions and they are essential contributor to poor health, a low standard of living, and sustainable development. According to Abdulkarim (2023), air pollution can be defined as the presence of any solid, gaseous, liquid substances, including noise, in the atmosphere in such way its usual/unnatural concentrations could be deleterious to the human health, other living things and climate.

1.2	Aim of the Study

The aim of this project is focus on chemical and trace elemental composition of quarry dust and its health implication.

1.3	Objective of the Study

The objective of this study includes:

i.	to determine the chemical composition of quarry dust.

ii.	to determine the trace elemental constituents of quarry dust and its health implications

iii.	to compare with standard parameters.

1.4	Problem statement

It has been established that particulate concentration constitute hazards to humans that either work at quarry sites or live in proximity to quarry sites are exposed to respiratory and other disease caused by exposure to particulate matter.

1.5	Justification of the Study

This research work is therefore aimed at determining the chemical and trace elemental composition of the dust particulates from Kam quarry with particular reference to determination of the potentially harmful elements in the dust and their possible health implications.

1.6	Scope of the Study

The scope of this project will be restricted to collection of quarry dust from Kam quarry, Kwara State. The project is limited to field work and laboratory analysis. The global positioning system will be used to take the coordinate.

CHAPTER TWO

LITERATURE REVIEW

2.1	Review of previous studies

Several notable authors has reported the effect of quarry dust in Nigeria. Among these researchers is Daspan et al. (2018) that the release of trace elements in high concentration by quarries can enrich their concentration in the environment thereby polluting the air, soil and both surface and ground water which variably affects human, animal and plant lives through food chain which may cause diseases and eventual death of man. According to Adeyanju and Manohar (2017) different air pollutants are associated with health effects and they are stated as follows; nitrogen oxides (NO2 ) linked with lung irritation, respiratory illness, premature death, carbon monoxide (CO) associated with headaches and reduces mental alertness, particulate matters and sulphur dioxide related with increase in existing heart disease, breathing difficulties and respiratory illness. Oguntoke et al. (2009) reported that there are various air pollutants, the emission of particulates is quite outstanding from quarries which have both micro and regional effect. Air pollution and ground vibration arising from blasting, crushing and emission of noxious gasses have negative impacts on human health and well-being. Infantes et al. (2020) opined that when dust from quarrying operations is uncontrolled and allowed to enter the atmosphere, it can cause a variety of unpleasant environmental problems which may include wear and tear on machines, decreased visibility, an increase in the risk of accidents, and pulmonary damage from breathing in minerals like silica, asbestos, and coal dust. WHO (2024) estimates, ischemic heart disease and stroke accounted for about 37% of premature deaths linked to outdoor air pollution. From the statistical report of WHO in 2019, 18% of chronic obstructive pulmonary disease 23% of acute lower respiratory infections linked to deaths of human beings respectively, and respiratory tract cancer accounted for 11% of deaths.

2.2	Geology of Nigeria

Nigeria is classify into three rocks which are basement rock, younger granite, sedimentary rock. (Fig 2.1). It forms the southern part of the trans Saharan mobile belt east of the east Africa Craton and North East of Congo Craton (Caby, 1989) and also explained to be the Tuareg shielding (Black, 1980). This basement complex comprises Archean and Proterozoic rock which is noted to be the result of the three major organ cycle of deformation, metamorphism and remobilization and basement reactivation corresponding to their radiometric ages by Librarian (2700 + 200ma) Eburnean (ca 2000Ma). Pan African (600Ma) which resulted from plate coil is ion between the passive continental margin of the West Africa Carton and the active continental margin (Grant and Dada, 1970). Nigeria is underlain by seven major sedimentary Basin (from the oldest) the Calabar flank, the Benue trough, the Chad, Lullemenden (Sokoto), Dahomey and Niger Delta. Sedimentary succession in this area is of middle Mesozoic to Paleozoic age. Older sedimentary deposit was not preserved, probably because during the Paleozoic (Oyawoye, 1959). Nigeria younger Granite were formed from peralkaline melt by fusion of local basement rocks.it is also suggested that the associated metal aluminous trend is caused simply by more complete melting and that peraluminous granite developed during subsequence cooling. When feldspar normative composition of younger granite is plotted in the quartz saturated, ternary feldspar system, they support a cyclic event of fusion and cooling to account for the variation in the rock type (James and Hanulton, 1969).

Figure 2.1: Geological Map of Nigeria (Modified from Africa Atlases, 2007)

2.3	Geology of the study Area

The study area is located within latitude of N08°27’04.0” and E004°21’25.5” at elevation of 304m (Fig. 2.2) for Kam quarry. Precambrian Basement complex of north central Nigeria and is underlain by rock of metamorphic and igneous type (Figure 2.2). However, migmatite predominantly underlies the rocks in the area while other principal rocks include granites and gneisses which are emplaced by Precambrian time and have overtime subjected to tectonic activities characterized by large changes on temperature and resulting in folding and fractures such as joints, faults and fractures within the basement complex rock. (Ibrahim et al., 2012). The mineralogical composition in these rocks include quartz, feldspar, mica (muscovite and biotite), and hornblende.

Figure 2.2: Location Map of the Study Area (modified after Olasehinde et al., 1998)

2.4	Composition of Quarry Dust

Quarry dust can be described as the residue or tailing material after the extraction and processing of rocks and that forms fine particles less than 4.75mm. As oppose to smooth granular nature of sand, quarry dust has rough surface textures and angular shape due to crush nature of the aggregate. Rough surface texture provide better interlocking and good bond between the cement paste and the aggregate. It constitutes 20% - 25 % of the output of rubble crushing (Information gathered from the quarry owners). Smooth round shape of river sand makes bond between the cement paste and the aggregate relatively weak. However, due to spherical shape of the river sand (surface area to volume of sand is small) and relatively low percentage of voids.

2.5	Chemical Composition of Quarry Dust

The chemical composition of quarry dust is typically 70 - 77% silica, 11 - 13% alumina, 3 - 5% potassium oxide, 3 - 5% soda, 1% lime, 2 - 3% total iron and less than 1% magnesia and titanium. While the main element of sand is silicon dioxide (SiO2), followed by smaller amount of aluminum, iron oxide, and calcium oxide. (Nanda et al., 2010). Silica, SiO2, is a colourless crystalline compound found mainly as sand, quartz, flint, and many other minerals. Silica is an important element to manufacture to enhance the strength property in a wide variety of materials. It is understood that the SiO2 is the main chemical component which possess the strength parameters in cement and sand. Hence, in this regards it is recommended to crusher owners to check chemical property of SiO2 of their quarries shows higher than 80%.

CHAPTER THREE

MATERIALS AND METHOD

3.1	Sample Collection

Fresh representative samples of quarry dust tagged Sample A, Sample B and Sample C were collected on the field using equipment such as hammer, chisel, sample bags and global positioning system among others. The three (3) samples was separated in different sample bags and transported to Nigerian geological Survey agency (NGSA), Kaduna for detailed analysis.

3.2	Atomic Absorption Spectrometry

Atomic Absorption Spectrophotometer (N1100A model) was used to analyze the rock samples. Graphite cuvette was used for electro thermal atomizer; ultra-high purity acetylene was used as the carrier gas. Volumetric measurements were carried out with the analyzer TA-4 with polyethylene impregnated graphite electrode. As a reference electrode, silver/silver chloride electrode was used. Calibration solutions of lead, nickel, and cobalt were obtained by diluting the standard samples obtained from Sigma. Nitric, hydrofluoric and hydrochloric acids were purchased ultrapure quality.

Rocks samples are dried, ground, and homogenized. An aliquot is digested with a combination of nitric, hydrofluoric, and perchloric acids, in Teflon '^' beakers, heated on a hot plate at 200°C. The resulting salts are dissolved in hydrochloric acid and deionized water. The solutions are analyzed by atomic absorption spectroscopy after the addition, in certain cases, of appropriate matrix modifiers. Additional interferences are removed or compensated for through the use of mixed-salt standards and background correction.

3.3	Procedure for Atomic Absorption Spectrometry

All glassware should be cleaned immediately before use by rinsing, first with dilute HCl (1+1) and then with demineralized water. Dry the sample by an appropriate procedure such as freeze-drying, or in an oven at 105°C. If the sample is greater than 100g, split it down to less than 100g by use of a nonmetallic sample splitter (riffle sampler) or by coning and quartering. Grind the sample with a mixer mill or an agate mortar and pestle until all material is finer than 100 mesh. Weigh and transfer 0.5000 g of finely ground sample to a 100 mL Teflon beaker; weigh out appropriate standard materials as well, and use several empty beakers for blanks. Place the hot plate in a perchloric acid hood, turn on the hood and hotplate, and adjust the hot plate to produce a surface temperature of 200°C. To each beaker, add 6 mL HNO3 (SP Sr. 1-41), and place it on the hot plate for approximately 30 minutes.

Remove the beakers from the hot plate and wait 5 minutes. Add 6 mL HF (specific gravity of 1.17) and 2 mL HCl specific gravity of 1.67), and return the beakers to the hot plate. Continue heating until the evolution of white per chloric fumes and the solutions have reached incipient dryness; however, do not bake the residues. Remove the beakers from the hot plate, wait 5 minutes, and repeat the process again. Remove the beakers from the hot plate, wait 5 minutes, and add 2 mL HCl (sp gr 1.67) and return the beakers to the hot plate. Continue heating until the evolution of white per chloric fumes and the solution reaches incipient dryness; however, do not bake the residues. Remove the beakers from the hot plate, lower the hot plate temperature to 100°C, and add 2 mL dilute HCl (1+1) and swirl the beaker; add 10 mL demineralized water and return to the hotplate until the residues dissolve. Cool the beakers, and pour each solution into a 50 mL volumetric flask. Rinse the beaker several times with demineralized water and bring to the mark with demineralized water. Pour the solution into an acid-rinsed plastic bottle for storage. This solution represents a dilution factor of 100X. Remove a 5 mL aliquot from the 100X solution, add 1 mL HCl (Specific gravity 1.19), place in a 50 mL volumetric flask, and bring to the mark with demineralized water. Pour the solution into an acid rinsed plastic bottle for storage. This solution represents a dilution factor of 1000X. Finally, remove a 5 mL aliquot from the 1000X solution, add 1 mL HCl (Specific gravity 1.19) and place in a 50 mL volumetric flask, and bring to the mark with demineralized water. Pour the solution into an acid rinsed plastic bottle for storage. This solution represents a dilution factor of 10000X. Set up the atomic absorption spectrophotometer according to the specifications and analyze the 100X solutions for Cr, Co, Cu, Pb and Ni.

Determine the concentration of each constituent in the 100X solutions (Cr, Co, Cu, Pb and Ni) from the digital display while aspirating each sample and record the results (average of 3 readings once the system has stabilized). The actual concentration of each constituent in the sample, can be obtained by multiplying the concentration in each sample solution by 100, if no further dilutions are made.

Each quarry dust samples were further pulverized and digested in aqua-regia (HNO3/HCl) in the ratio 1:3. The digested samples were analyzed for Zn, Fe, Pb, Cd, Cu, Co, Ni, As, Mn, and Cr. The analysis was done using an Atomic Absorption spectrophotometer (AAS) at the Nigerian Geological Survey Agency (NGSA) Laboratory, Kaduna. Standard stock solutions for all the elements were procured from Merck as well as prepared in the laboratory following the procedures as described in APHA (2012). The glassware used was Pyrex, which was washed several times with soap, distilled water, and diluted nitric acid to remove any impurities. Similarly, water samples were directly aspirated into the Atomic Absorption Spectrometry (A.A.S) and the concentration of each metal (Pb, Zn, Cu, Fe, Co, Ni, As, Mn, Cd and Cr) was determined when extracts were sprayed into the flame, light rays from a hollow cathode lamp is shone through the flame, thereby triggering atoms of the elements to be determined, leading to radiation absorption. The rate of absorption is directly proportional to the concentration of the element. Each element is detected with its cathode lamp, and the concentrations are recorded in mg/L units.

CHAPTER FOUR

RESULTS AND DISCUSSION

4.1	Results of Major oxides

The results of major oxides of quarry dusts for the three samples is shown in table 4.1.

| S/n | Sample Name Chemical Compositions (%) | Sample A (%) | Sample B (%) | Sample C (%) | Range | Mean (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | SiO2 | 65.25 | 64.33 | 61.24 | 61.24 – 65.25 | 63.51 |
| 2. | Al2O3 | 14.25 | 14.83 | 13.88 | 13.88 – 14.83 | 14.32 |
| 3. | Fe2O3 | 8.05 | 8.02 | 7.25 | 7.25 – 8.05 | 7.77 |
| 4. | CaO | 5.25 | 5.23 | 4.32 | 4.32 – 5.25 | 4.93 |
| 5. | MgO | 2.08 | 2.06 | 2.01 | 2.01 – 2.08 | 2.05 |
| 6. | TiO2 | 0.88 | 0.99 | 0.79 | 0.79 – 0.99 | 0.84 |
| 7. | Na2O | 3.82 | 2.88 | 3.11 | 2.88 – 3.82 | 3.27 |
| 8. | K2O | 0.35 | 0.43 | 0.42 | 0.35 – 0.43 | 0.40 |

Table 4.1. Concentration of major oxides analyzed in the Quarry dusts

4.2	Discussion of X – Ray Fluorescence

The major oxides for Sample A, Sample B and Sample C was evaluated for their chemical composition. The major oxide in Table 4.1 indicates that the percentage Silicon oxides for the three samples ranges from 61.24% to 65.25% with an average of 63.51%, Aluminum oxide (Al2O3) ranges from 13.88% to 14.83% with an average of 14.32%, Iron oxide (Fe2O3) ranges from 7.25% to 8.05% with an average of 7.77%. Calcium oxide (CaO) also falls within 4.32% and 5.25% with an average of 4.93%, Magnesium oxide (MgO) ranges from 2.01% to 2.08% with an average of 2.05%, Titanium oxide (TiO2) ranges from 0.79% to 0.99% with an average of 0.84%, Sodium oxide (Na2O) ranges from 2.88% to 3.82% with an average 3.27% while Potassium oxide (K2O) ranges from 0.35% to 0.43% with an average of 0.40%.

Geochemical distribution values generally suggest that the study area possess high silica concentrations and these support the granitic origin of the analyzed rock samples. The high silica content clearly indicate felsic origin and this is supported by the low Fe2O3 content while the mean of Na2O and K2O reflects the abundance of potassium rich rock forming silicate like biotite. Low concentration of MgO and TiO2 values are indicative of plutonic origin. This trend is characteristic of Archean granitic rocks. The relatively low alumina suggest the abundance of biotite and feldspar in the rock. Major minerals that are found includes quartz, orthoclase and plagioclase feldspar, albite, hematite, anorthite, hyperstene and corundum while the minor minerals includes rutile, ilmenite and zircon. The presence of K2O are indicative of calc- alkaline affinity.

4.3	Results of Trace Elemental Constituents

The result for the trace elements (in ppm) for the quarry dust from Kam quarry is given in table 4.2 below.

| S/n | Sample Name Trace Compositions | Sample A (ppm) | Sample B (ppm) | Sample C (ppm) | Range (ppm) | Mean (ppm) |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Arsenic (As) | 0.4 | 1.0 | 1.3 | 0.4 - 1.3 | 0.9 |
| 2. | Cadmium (Cd) | 0.29 | 0.26 | 0.25 | 0.25 - 0.29 | 0.27 |
| 3. | Chromium (Cr) | 4 | 3 | 8 | 3 – 8 | 5.0 |
| 4. | Cobalt (Co) | 0.9 | 0.8 | 1.1 | 0.8 - 1.1 | 0.93 |
| 5. | Nickel (Ni) | <0.001 | <0.001 | <0.001 | <0.001 | <.0.001 |
| 6. | Lead (Pb) | 45.64 | 42.55 | 37.23 | 37.23 - 45.64 | 41.31 |
| 7. | Copper (Cu) | 3.18 | 2.23 | 2.21 | 2.23 - 3.18 | 2.54 |
| 8. | Zinc (Zn) | 129.1 | 128.6 | 133.56 | 129.1 – 133.56 | 130.42 |
| 9. | Molybdenum (Mo) | 500.4 | 540.5 | 570.0 | 500.4 – 570.0 | 536.97 |

Table 4.2. Results of Trace Element of Quarry Dust

4.4	Discussion of Trace Elemental Composition

Trace elements in the quarry dust from Kam quarry includes Arsenic (As) concentration which ranges from 0.4 - 1.3ppm with average concentration of 0.88 ppm. Cadmium (Cd) concentration ranges from 0.25ppm - 0.29ppm with average concentration of 0.27ppm. Chromium (Cr) concentration fall within 3 - 8ppm with average concentration of 5ppm. Cobalt (Co) concentration ranges from 0.8ppm - 1.1ppm with average concentration of 0.95. Nickel (Ni) concentration ranges from 0.6ppm - 0.9ppm and has average concentration 0.7ppm. Lead (Pb) concentration is very high; it ranges from 37.23ppm - 45.64ppm with average concentration of 41.31ppm. The highest concentrations are recorded in dust samples from Kam quarry.

Copper (Cu) concentration in Kam quarry ranges from 2.23ppm - 3.18ppm with average concentration of 2.54ppm. It can be seen that the concentration of Cu in samples from Kam quarry is relatively high and it also showed slight distinct concentration. Zinc (Zn) concentration is very high and maintained almost the same concentration in all the dust samples from Kam quarry. The concentration ranges from 129.1ppm - 133.56ppm and has average concentration of 130.42ppm. Molybdenum concentration in dust samples from Kam quarry ranges from 500.4ppm – 570.0ppm and has average concentration of 536.97ppm (Table 4.2).

4.5	Discussion on Health Implications

Generally, Quarry workers and those close to Kam quarry are at high health risk due to long exposure to these high trace elemental concentration may be through direct ingestion, percutaneous absorption, inhalation or bioaccumulation in the human system through the food chain. Trace elements and their possible health implications are however associated with deficiency that are dangerous to both human and animal environments. The Arsenic concentration in the dust ranges 0.4ppm - 1.3ppm with average concentration of 0.88 ppm exceeds the WHO permissible limit of 0.01ppm (Table 4.3). Generally, Arsenic is regarded as human carcinogen from extremely low levels of exposure, having no possible beneficial metabolic function for human (Daspan et al., 2008). Its low level exposure causes Nausea and vomiting, based on low level of exposures essentially causes abdominal pains while its long term exposure results to darkening of the skin along with appearance of small corns in palm soles. Minor effects that may occur include anorexia, fever, fluid loss, goiter, hair loss, headache, sore throat, weakness and interferes with the uptake of folic acid. The highly toxic non – essential heavy metal, Cadmium does not have a role in biological processes. It ranges from 0.25ppm - 0.29ppm with average concentration of 0.27ppm and it can be lethal even in low concentrations. It is found to exceed the WHO permissible limit of 0.01ppm (Table 4.3). Long term exposure to cadmium can lead to possible lung damage and kidney disease including fragile bones. Cadmium is very toxic, its long- term exposure to lower level leads to build up in the kidney and possible kidney disease, lung damage, and fragile bones. Arthritis, diabetes, Hypertension, anaemia, cancer, cardiovascular disease, cirrhosis, headache and strokes are some it long term effect or diseases associated with Cadmium. Lead is also a toxic metal even at low or minimal concentration levels. The relatively low concentration of lead in the dust ranges from 37.23ppm - 45.64ppm with average concentration of 41.31ppm which essentially exceeds the WHO permissible limit of 0.05ppm (Table 4.3). Diseases associated with deficiency of lead is not recognized but those associated with excess exposure either through ingestion or inhalation can leads to varieties of disorder such as  destruction of red blood cells; liver necrosis, system hypertension; gastro intestinal pains and bleeding, pulmonary edema; anemia, kidney failure and other central and peripheral nervous system disorder including lingering toxicity  which could lead to skin disorder such as eczema, hyperkeratosis, melanosis, ulceration and skin cancers Chromium concentration in the dust ranges from Chromium (Cr) concentration in the dust fall within 3ppm - 8ppm with average concentration of 5ppm. (Table 4.3). Chromium is vital to the maintenance of metabolism in the human body. It is apply in effective in management of diabetic patients and it serves as a cofactor with insulin. Its absence result in defective glucose metabolism, hyperlipidemia, corneal opacity. On health grounds, excess exposures of Chromite dust causes irritation and generation of lesions in skin, respiratory tract, and, pulmonary edema, acute kidney failure, Long-term risk for lung cancer, pneumoconiosis from exposure. Cobalt is vital component of vitamin B12 molecules. It is an essential element needed in human body for normal physiological function. Its concentration in the dust however ranges from 0.8ppm - 1.1ppm with average concentration of 0.95ppm which are above the WHO permissible limit of 0.1ppm (Table 4.3). Health implications of cobalt includes anemia and anorexia. Excess ingestion results to Cardiomyopathy, including cancer. Excess inhalation causes respiratory irritation “Hard metal” pneumoconiosis. Percutaneous exposure also causes allergic dermatitis.

Copper is an essential element for plant and animal health. Its concentration in the dust ranges from 2.23ppm - 3.18ppm with average concentration of 2.54ppm. It all exceeds WHO permissible limit. Copper concentration which falls below the permissible limit (Table 4.3). Its deficiencies is lead to Anemia. Its health effects is associated with excess inhalation and ingestion. Intestinal and liver inflammation, hemolysis (destruction of red blood cells, with diffusion of hemoglobin into surrounding fluids), and hyperglycemia are the deadly illness associated with copper dusts. Zinc is an element that is also crucial for human and animal health. It has an important role in metabolism, growth and general wellbeing. Zinc concentration in the dust ranges from 154.1ppm - 157.6ppm and has average concentration of 156.6ppm exceeding the WHO permissible limit of 5.0ppm (Table 4.3). Diseases associated with Zn deficiency are anorexia, dwarfism, anemia, hypogonadism, hyperkeratosis, acrodermatitis, enteropathica, depressed immune response and teratogenic effects. Health effects associated with excess ingestion is hyperchronic anemia and inhalation is metal fume fever at high doses.

Molybdenum is an important element necessary for human and animal body to perform it normal physiological function. Molybednum concentration in the dust varies from 500.4ppm and 570.0ppm and has average concentration of 536.97ppm. This is exceedingly high in the concentration. Molybdenum dust is commonly associated with Mo deficiencies are growth depression, keratinization effects and hyperurinemia. Exposure to excess of Mo causes high uric acid in serum and urine, loss of appetite, diarrhea, slow growth, anemia, “gout-like lesions and molebdenosis. Nickel plays some roles in body functions including enzyme function. In trace or minute amount, it may be beneficial to activate some systems. It has a concentration of <0.001ppm in the dust. This concentration is found to be much lower and inconsequential than the permissible limit of 0.02ppm by WHO/EPA (Table 4.3). However, the health effect associated deficiency is not recognized but exposure to Nickel inhalation results to chronic bronchitis, emphysema, reduced lung capacity, cancers of the lung and nasal sinus. Ingestion of Ni can also lead to cardiac arrest, which is essentially death. Gastrointestinal effects such as nausea, cramps, diarrhea, including vomiting, along with effect on blood, liver, kidney is also as a result of Nickel ingestion. Also, neurological effects such as giddiness weariness can also be attributed to Nickel inhalation or ingestion.

Table 4.3. Measured Concentration of some selected Heavy Metals in Dust from Kam Quarry and WHO (2000) maximum permissible limit

| Heavy Metals (ppm) | Measured Concentration range in Quarry dust (ppm) | Average Concentration (ppm) | WHO/EPA permissible limit (ppm) |
| --- | --- | --- | --- |
| As | 0.4 - 1.3 | 0.88 | 0.01 |
| Cd | 0.25 - 0.29 | 0.27 | 0.01 |
| Cr | 3.0 - 8.0 | 5.0 | 0.1 |
| Cu | 2.23 - 3.18 | 2.54 | 2.00 |
| Ni | <0.001 | <0.001 | 0.02 |
| Mo | 500.4 – 570.0 | 536.97 | 0.15 |
| Pb | 37.23 - 45.64 | 41.31 | 0.05 |
| Co | 0.8 - 1.1 | 0.95 | 0.10 |
| Zn | 129.1 – 133.56 | 130.42 | 5.00 |

CHAPTER FIVE

Conclusion and Recommendations

5.1	Conclusion

Quarrying of rocks have shown to have contributed to the development of many developed and developing nations. However, it generates and releases particulate pollution in the environment. The high level of particulates generated at the drilling and crushing areas depicts them as hazard zones. Geochemical analysis of quarry dust from Kam quarry suggest that the concentration of trace elements in the dust exceeds the permissible limit set by WHO. Some of which are very harmful to human health even at very low concentration. It is certain that long exposure of quarry worker and those living in close proximity through inhalation, ingestion and percutaneous absorption can result to various health challenges. Trace elemental concentrations are much higher and extensively contaminated. The release of these trace elements in high concentration by this quarry can enrich their concentration in the environment thereby polluting the air, soil and both surface and ground water which variably affects human, animal and plant lives through food chain which may cause diseases and eventual death of man.

5.2	Recommendations

The following recommendation should be carried out:

- It is crucial to give air pollution at the quarrying site prompt attention in order to prevent severe environmental hazards because nobody decides the type of air to breath.

- The air pollution from quarry dust at quarrying site can be tackled through dust suppression techniques and treating quarry pit with water before discharging

References

Abdulkarim, H. R. (2023). The Role of Industrial Sector Pollution Control in the context of 	Sustainable Development Goals. 1-12, 10.5771/intechopen.112671.

Adeyanju, A. A. and Manohar, K. (2017). Biodiesel Production and Exhaust Emission Analysis 	for Environmental Pollution Control in Nigeria. American Journal of Engineering 	Research (AJER), 6(4), 80-94. https://www.ajer.org

Ankley, G. T., Lodge, K., Call, D. J., Balcer, M. D. and Smith, B. J. (1992). Heavy Metal 	Concentrations in Surface Sediments in a Near Shore Environment, Jurujba Sound, 	Southeast Brazil. Environ. Poll. Bull. 48, 405 – 408.

Akanbi, M. O., Ukoli, C. O, and Erhabor,  G. E. (2009). The burden of respiratory disease in 	Nigeria. Afr J Resp Med, 2(3): 10-17. 	https://www.africanjournalofrespiratorymedicine.com

Daspan, R. I., Obadiah, E. G., Lekmang, I. C., Dibal, H. U., Chup, A. S., Daku, S., Wazoh, H., 	Diyelmak, V. B. and Azi, B. (2018). Preliminary Assessment of the Trace Element 	Composition of Dust from Two Granite Quarries from Jos Plateau and Their Possible 	Health Implications. Journal of Environment and Earth Science www.iiste.org 8, 8, 140.

Deborah, S. (1996). Breathtaking: Premature Mortality due to particulate air pollution in 239 	American Cities. Natural Resources Defence Council, New York.14-15

Dockery, D. and Pope, C. (1994). ‘Acute Respiratory Effects of Particulate Air Pollution’. Annual 	Review of Public Health. 15; 107-132Last, J. M (1998).Public Health and Human Ecology 	(2nd) McGraw-Hill Medical Publishing Prentice-Hall Int. Education Canada. P153-200

Godwin, I. I., Alkali, M. Emeodilichi, H. M. and Udofia, U. A. (2021). Assessment of Dust 	Concentration and Compounds at Quarry Sites in Akamkpa Cross River State, Nigeria. 	Asian Journal of Geological Research.  4(1): 40 - 47, http://www.sdiarticle4.com

Islam, M. S., Ahmed, M. K., Raknuzzaman, M., Habibullah – Al – Mamun, M. and Islam, M. K. 	(2015). Heavy Metal Pollution in Surface Water and Sediment: A Preliminary Assessment 	of an Urban River in a Developing Country. Ecological Indicators, 48: 282 - 291

Lee, H., Kabir, M. I., Kwon, P.S., Kim, J. G., Hyun, S. H., Rim, Y. T., Myoung, S. B., Ryu, E. R. 	and Infantes A, Kugel M, Raffelt, K, et al. Side-by-Side Comparison of Clean and 	Biomass-Derived, Impurity-Containing Syngas as Substrate for Acetogenic Fermentation 	with Clostridium Ljungdahlii. Fermentation, 2020, 6, 84. 	https://doi:10.3390/fermentation6030084

Jung, M. S. (2009). Contamination Assessment of Abandoned mines by Integrated pollution Index 	in the Han River Watershed. The open Environmental Pollution and Toxicology Journal, 	1: 27 – 33

National Industrial Sand Association (1997).Respiratory Health Effects of Crystalline Silica. As 	available at www.Riccisand.com/health.

Plumlee, G. S. and Ziegler, T. L (2004). The Medical Geochemistry of Dusts, Soil, and other Earth 	Material.US Geological Survey, Denver, CO. USA.

Shazili, N. A. M., Yunus, K., Ahmad, A. S., Abdullah, N. and Rashid, M. K. A. (2006). Heavy 	Metal Pollution Status in the Malaysian Aquatic Environment. Aquatic Ecosystem Health 	and Management, 9(2): 137 – 145

Sudhere, R. and Rengarajan, A.K, (2012). Atmospheric Mineral Dust and Trace Elements over 	Urban Environment in West India during winter. Aerosol and Air Quality Research, 12: 	923 - 933

Varol, M. (2011). Assessment of Heavy – Metal Contamination in Sediment of Tigris River 	(Turkey) using pollution indices and Multivariate Statistical Techniques. Journal of 	Hazardous Materials, 195: 355 – 364

USEPA. Region 4: Laboratory and field Operations – PM.2.5: Objectives and History. 2008. 	Available at en.wikipedia.org/wiki/particulate.

WHO (2024). Clean air for public health - Assessing population exposure to air pollution. 	https://www.who.int/teams/environment-climate-change-and-health/air-quality-energy-	and health/outreach-advocacy/webinar-series. 2024.