GEOTECHNICAL PROPERTIES OF LATERITIC SOILS WITHIN KWARA STATE POLYTECHNIC CAMPUS

BY

Abdulmuiz Olasheni BABATUNDE

ND/23/MPE/FT/0036

A PROJECT SUBMITTED TO THE DEPARTMENT OF MINERAL AND PETROLEUM RESOURCES, INSTITUTE OF TECHNOLOGY (IOT), KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILMENT OF THE REQUIREMENTS FOR THE AWARD OF NATIONAL DIPLOMA (ND) IN MINERAL AND PETROLEUM RESOURCES, INSTITUTE OF TECHNOLOGY(IOT)KWARA STATE POLYTECHNIC ILORIN

AUGUST, 2025

CERTIFICATION

This research project has been examined and approved as meeting the requirement for the award of National Diploma in the Department of Mineral And Petroleum Resources, Institute of Technology (IOT) Kwara State Polytechnic Ilorin.

DEDICATION

This work is dedicated to Almighty God, the source of my wisdom and strength.

It is also lovingly dedicated to my dear parents, whose sacrifices, encouragement, and prayers have been my pillar of support, and to all my lecturers and colleagues who have contributed to my academic growth.

ACKNOWLEDGEMENTS

First and foremost, I give all glory, honour, and adoration to Almighty God for His grace, guidance, and protection throughout the period of this project and my academic journey.

I sincerely appreciate my supervisor, Mr. Odediran, for his invaluable guidance, constructive criticism, and encouragement throughout the preparation of this work. My heartfelt gratitude also goes to all my lecturers in the Department of Mineral and Petroleum Engineering, Kwara State Polytechnic, for imparting knowledge and providing the foundation upon which this project stands.

I am deeply grateful to my parents and family for their unwavering love, prayers, and financial support. Special thanks to my friends and colleagues in ND Mineral and Petroleum Engineering for their cooperation, motivation, and companionship during the course of this research.

Finally, I acknowledge everyone who, in one way or another, contributed to the success of this work. May God bless you all abundantly

TABLE OF CONTENTS

Title Page								i

Certification								ii

Dedication								iii

Acknowledgements							iv

Table of Contents							v-vi

Abstract 								vii

List of Tables								viii

List of Figures								ix

CHAPTER ONE

- Introduction							1

  - Location And Accessibility					1

  - Relief And Drainage						1

  - Climate And Vegetation					2

  - Aims And Objectives						2

  - Statement of the Problem					3

  - Justification							3

  - Scope and Limitation						3

CHAPTER TWO

- Literature Review						4

### 2.1 	Overview of Lateritic Soils					4

### 2.2 	Formation and Occurrence of Lateritic Soils			5

  - Regional Distribution Of Lateritic				6

  - Characteristics Of Lateritic					6

  - Attending Limits						6

  - Compaction 							7

  - Sieve Analyses						8

CHAPTER THREE

### 3.0 	Research Methodology					9

### 3.1 	Collection of Samples						9

### 3.2 	Preparation of Disturbed Samples				9

### 3.3 	Laboratory Procedures					10

### 3.4 	Grain Size Distribution Test					10

  - Atterberg Limit Tests						11

  - Compaction Test						11

  - Moisture Content Test						12

  - Specific Gravity Test						12

  - Bulk Density Test						13

CHAPTER FOUR

4.0	Results and Discussion					14

4.1	Results of Moisture Content Test				14

4.2	Results of Atterberg Limit Test				14

4.3	Results of Grain Size Analyses				16

CHAPTER FIVE

5.0	Conclusion and Recommendations				19

5.1	Conclusion							19

5.2	Recommendations 						19

References							20

ABSTRACT

This study investigates the geotechnical properties of lateritic soils within Kwara State Polytechnic, Ilorin, to evaluate their suitability for construction purposes. Soil samples were collected from selected locations across the campus and subjected to laboratory tests including natural moisture content, bulk density, dry density, specific gravity, Atterberg limits, grain size distribution, and compaction characteristics, in accordance with BS 1377 and ASTM standards. Results show that the soils are predominantly sandy in nature, with moisture content ranging between 4.1% and 5.2%, bulk density between 1.63 g/cm³ and 1.76 g/cm³, and specific gravity values between 2.68 and 2.83. The Atterberg limits indicate low plasticity, while grain size analysis classifies the soils as clayey sand and silty sand. Compaction results reveal maximum dry density values ranging from 1.81 to 1.95 g/cm³ with optimum moisture contents between 6% and 8%. These findings suggest that the lateritic soils are generally suitable for use as subgrade and fill materials in civil engineering works, though improvement methods such as stabilization may be required for certain applications.

LIST OF TABLES

Table 1:	Details of sample locations					9

Table 2:	Natural Moisture Content Test of Collected Samples	13

Table 3:	Bulk Density of Collected Samples				14

Table 4:	Dry Density Test of collected samples			14

Table 5:	Specific gravity test of collected samples			14

Table 6:	Atterberg Limit Tests of collected samples			15

Table 7:	Summary of result of Grain Size Analysis of soil		16

Table 8:	Compaction Parameters of Maximum Dry Density (MDD) and Optimum Moisture Content (OMC)				16

Table 9:	Compaction and Ratings of Unified Soil Classification for Construction (ASTM 1557-91) 				17

LIST OF FIGURES

Fig.1: 		Graph showing water content			13

Fig 2: 		Graph Showing Plasticity Chart 			15

Fig. 3: 		Grain Size Analysis Graph				16

Fig. 4: 		Graph Showing Compaction Parameters		17

CHAPTER ONE

Introduction

  - Location And Accessibility

Kwara State Polytechnic is located in Ilorin, the capital city of Kwara State, in the North Central region of Nigeria. The institution lies approximately on latitude 8.50°N and longitude 4.55°E. The campus is accessible through major roads such as the Old Jebba Road and the University Road, which link to other parts of the city. Public transportation such as buses, motorcycles, and tricycles are readily available, making the area highly accessible.

The campus consists of several faculties and departments spread over a large area with diverse landforms. The variation in topography and land use within the campus makes it an ideal location for studying lateritic soils in different contexts.

According to Obaje, N. G. (2009) more than 80% of the state consists of crystalline Precambrian basement complex rocks, with the rest being made up of Cretaceous and younger sediments,. The basement complex terrain consists of rocks such as granites, amphibolites, granite gneiss, biotite gneiss, migmatites, quartzites, etc. The younger sediments mainly consist of alternating layers of sandstones, shales, and clays.

Local geology involves categorizing and identifying the various types of rocks found in the area based on their field traits and where they are located. The rock categories consist of crystalline rocks and meta-sediments. The primary rock type found in the region is quartzite, which is accompanied by small intrusions like pegmatites and quartz veins [Reyment, R. A. 1965].

  - Climate and Vegetation

Ilorin experiences a tropical wet and dry climate, characterized by two distinct seasons: the rainy season (April to October) and the dry season (November to March). Average annual rainfall ranges from 1000 mm to 1500 mm, while average temperatures vary between 22°C and 35°C.

The vegetation within the campus is a mix of natural savannah grasses, shrubs, and trees, alongside planted ornamental and economic species. These vegetation types influence soil development and characteristics by contributing organic matter and stabilizing the soil structure.

  - Relief And Drainage

The topography of Kwara State Polytechnic campus is relatively undulating, with elevations ranging between 290 to 320 meters above sea level. The landscape consists of gently sloping surfaces, interspersed with small depressions that serve as water collection points during rainfall.

Drainage within the campus is mainly dendritic and natural, although some areas have been altered by human activities and construction. Seasonal streams and man-made drainage channels help in controlling surface runoff. However, during heavy rainfall, poor drainage in some areas causes waterlogging and erosion, which can affect the stability and properties of lateritic soils.

  - Aim and Objectives

The aim of this project is to determine the geotechnical properties of lateritic soils within Kwara State Polytechnic campus and assess their suitability for construction purposes.

The specific objectives are as follows

- to identify and classify the lateritic soils present within different locations on the campus.

- to determine the physical and engineering properties of the soil, such as grain size distribution, Atterberg limits, compaction characteristics, permeability, and shear strength.

- to provide recommendations for the use of lateritic soils in future engineering projects within the campus.

  - Statement of the Problems

Infrastructural development within Kwara State Polytechnic is expanding rapidly, yet little scientific data exists on the suitability of the local soils for construction. Poor soil conditions can lead to foundation failure, road damage, and increased construction costs. There is a need for detailed geotechnical investigation to assess the properties of lateritic soils within the campus and provide guidance for safe and sustainable engineering design.

  - Justification

This study is justified by the increasing demand for infrastructure development within Kwara State Polytechnic. Understanding the geotechnical properties of the soil will enable engineers, architects, and developers to make informed decisions regarding foundation design, road construction, and other engineering applications. Furthermore, the research will contribute to the body of knowledge in geotechnical engineering and provide a reference point for future investigations.

  - Scope and Limitation

The research covers soil sampling from selected locations within the Kwara State Polytechnic campus. Laboratory tests were conducted to evaluate properties such as moisture content, particle size distribution, Atterberg limits, compaction characteristics, California Bearing Ratio (CBR), and shear strength.

The study is limited to lateritic soils within the campus and does not consider imported soils or other soil types.Time and financial constraints may limit the number of samples tested.Weather conditions during sampling may slightly affect soil properties such as moisture content.

CHAPTER TWO

- Literature Review

### 2.1 	Overview of Lateritic Soils

Lateritic soils are among the most widespread and important soil types in tropical and subtropical regions, including Nigeria. These soils are formed under intense weathering conditions and are characterized by their richness in sesquioxides, especially iron and aluminium oxides, which give them their distinctive reddish, brownish, or yellowish coloration(Abubakar, 2006). The term "laterite" was first used by Francis Buchanan in 1807 to describe a reddish soil in India, and it has since been used globally to refer to similar soils formed under comparable climatic and environmental conditions.

Lateritic soils are residual in nature, meaning they develop in place from the prolonged decomposition of underlying rocks such as granite, basalt, gneiss, or sandstone. This distinguishes them from transported soils, which are carried and deposited by water, wind, or ice. The development of lateritic soils is facilitated by alternating wet and dry seasons, which contribute to the leaching of silica and the accumulation of iron and aluminium compounds.

In geotechnical engineering, lateritic soils hold considerable significance due to their abundance and relatively good properties when dry or properly compacted. These soils are used extensively for building foundations, road subgrades, and embankments, especially in areas where more costly imported materials are not readily available. However, their performance can be unpredictable due to variability in composition, moisture sensitivity, and presence of clay minerals.

Lateritic soils can exhibit a wide range of engineering behaviors depending on their degree of weathering and mineral content. For instance, some lateritic soils are highly stable and make excellent construction materials, while others, especially those with high clay content, may suffer from swelling, shrinkage, or loss of strength when wet. This variability makes it essential to study their geotechnical properties on a site-specific basis (Reyment, 1965).

Moreover, lateritic soils are increasingly being evaluated for sustainable construction practices, including the production of compressed earth blocks, eco-friendly building components, and road pavements. Their natural abundance and relatively low cost make them attractive materials in regions where conventional construction materials are expensive or difficult to access.

### 2.2 	Formation and Occurrence of Lateritic Soils

Lateritic soils are formed through a complex process known as laterization, which occurs in regions with high rainfall, high temperatures, and well-drained topography (Emesiobi, 2000). The laterization process involves intense chemical weathering of silicate rocks, where soluble bases and silica are leached out, while less soluble oxides of iron and aluminium accumulate in the soil profile. This residual accumulation of oxides and hydroxides leads to the development of a distinctive soil horizon rich in ferric and aluminic compounds.

The parent material from which lateritic soils form plays a critical role in determining the final characteristics of the soil. Rocks such as granite, schist, basalt, and gneiss, which are rich in iron-bearing minerals like biotite and hornblende, are particularly susceptible to laterization. The decomposition of these minerals releases iron and aluminium, which subsequently precipitate and become concentrated in the soil under suitable environmental conditions.

Topography also influences the formation and distribution of lateritic soils. Upland or well-drained terrain promotes the efficient removal of silica through leaching, thereby enhancing the concentration of iron oxides. Conversely, in poorly drained lowlands or valleys, the laterization process may be inhibited, leading to the formation of different types of clay-rich soils instead of laterite(Whitlow, 1995). Thus, the best-developed lateritic profiles are often found on hilltops, plateaus, and gently sloping areas.

Lateritic soils are commonly found in large parts of West Africa, Southeast Asia, South America, and Australia. In Nigeria, they are prevalent in the Middle Belt and southern regions, especially in areas like Kwara State, where climatic conditions and geology are favorable for their formation. Their presence in Kwara State Polytechnic is attributed to the area's Basement Complex geology and the associated weathering of crystalline rocks.

It is important to note that lateritic soils may occur at various stages of maturity. Immature lateritic soils may still contain significant amounts of kaolinite and montmorillonite clays, which influence plasticity and strength, while mature laterites may be highly indurated, forming hard pans known as "lateritic crusts." Understanding the formation and degree of weathering of lateritic soils is essential for determining their suitability in engineering applications and for selecting appropriate stabilization methods when needed.

  - Regional Distribution Of Lateritic

The presence and properties of lateritic soils vary regionally depending on the parent rock, climate, vegetation, and topography. In Nigeria, the soils are commonly found in:

- Southwest Nigeria: Oyo, Osun, Ogun, and Lagos States.

- North Central Nigeria: Kwara, Kogi, and Niger States.

- Southeast Nigeria: Enugu, Ebonyi, and Anambra States.

In Kwara State, the geology is dominated by Precambrian Basement Complex rocks such as granite and gneiss, which contribute to the development of lateritic soils through weathering (Ola, 1983). The regional distribution also influences soil color, texture, plasticity, and engineering behavior.

  - Characteristics Of Lateritic

Lateritic soils exhibit a range of physical and engineering characteristics that influence their suitability for construction and other civil works. Some of the notable features include:

Color, typically red, reddish-brown, or yellowish due to iron oxide content.Texture, can range from gravelly to silty or clayey, depending on the degree of weathering.Plasticity varies from low to high depending on the clay content.

Porosity and Permeability, usually moderate to high, affecting drainage and compaction.Cohesion, some lateritic soils have good cohesion, making them stable for use in embankments and slopes.

These properties are site-specific and influenced by depth, drainage, vegetation, and human activity.

  - Attending Limits

The Atterberg limits are used to describe the plasticity and consistency behavior of fine-grained soils, including lateritic soils. The three main limits include:

The moisture content at which soil changes from a plastic to a liquid state.The moisture content at which soil changes from a semi-solid to a plastic state. The range of moisture content over which the soil exhibits plastic behavior, calculated as PI = LL – PL.

Lateritic soils generally have a moderate plasticity index. High PI values may indicate clay-rich soils with poor workability, while low values suggest better load-bearing characteristics. These limits help in classifying the soil and predicting its behavior under various moisture conditions.

  - Compaction

Compaction is a vital geotechnical test used to determine the maximum dry density (MDD) and optimum moisture content (OMC) of soils. These parameters are essential in evaluating the load-bearing capacity of lateritic soils used in embankments, road bases, and building foundations.

Compaction increases soil density by reducing the air voids, thereby improving strength and reducing permeability. For lateritic soils, standard Proctor and modified Proctor tests are commonly used to determine compaction characteristics. Factors affecting compaction include:

- Moisture content

- Soil gradation

- Clay content

- Method and energy of compaction

Well-compacted lateritic soils can withstand higher loads and show improved performance in construction applications.

  - Sieve Analyses

Sieve analysis is a fundamental soil test used to determine the particle size distribution of soil. It involves passing a dry soil sample through a series of sieves arranged in decreasing order of size to separate and quantify the different particle sizesgravel, sand, silt, and clay.

The results of the sieve analysis help in classifying the soil using systems like the Unified Soil Classification System (USCS) and AASHTO. For lateritic soils:

- A well-graded soil has a good range of particle sizes, which enhances compaction and strength.

- Poorly graded soils may have gaps in size distribution, which can lead to reduced stability.

Sieve analysis is particularly useful in evaluating lateritic soils for road construction, as it helps to determine whether the soil meets required specifications for sub-base and base materials.

CHAPTER THREE

### Research Methodology

### 3.1 	Collection of Samples

### The details of the sample locations are presented in table 1

### Table 1: Details of sample locations

| ### S/N | ### Location | ### Latitude | ### Longitude | ### Evaluation | ### DEPTZ |
| --- | --- | --- | --- | --- | --- |
| ### 1 | ### Yankari | ### N080.33.4261 | ### 1E0040.37.881 | ### 336 | ### 0.50m |
| ### 2 | ### Tourism | ### N080.33.4281 | ### E0040.37.881 | ### 309 | ### 0.75m |
| ### 3 | ### IFMS | ### N080.33.4301 | ### E0040.37.8831 | ### 309 | ### 0.79m |

### 3.2 	Preparation of Disturbed Samples

In the laboratory, the disturbed samples were air-dried to a constant weight in a controlled environment away from direct sunlight to avoid altering the natural soil structure. After drying, the samples were gently pulverized using a wooden mallet and passed through a 4.75 mm sieve to remove large particles and foreign materials such as roots or stones.

The processed soil was stored in clean, labelled containers and kept under dry conditions prior to testing. Care was taken to ensure homogeneity of each sample batch to maintain consistency across all laboratory analyses.

### 3.3 	Laboratory Procedures

All tests conducted followed the procedures outlined in relevant British Standards (BS 1377) and ASTM (American Society for Testing and Materials) standards. The tests were designed to measure key geotechnical parameters such as particle size distribution, consistency limits, compaction characteristics, moisture content, specific gravity, and bulk density.

Each test was conducted at least twice to ensure reproducibility and to minimize errors. The results were documented, interpreted, and later presented in graphical or tabular form in Chapter Four.

### 3.4 	Grain Size Distribution Test

The grain size distribution (sieve analysis) test was conducted to determine the proportions of gravel, sand, silt, and clay in the soil samples. The procedure involved oven-drying the soil sample, weighing it, and then passing it through a series of standard sieves arranged in descending order of mesh size.

The retained weight on each sieve was recorded and used to calculate the percentage passing each sieve. A grain size distribution curve was plotted on semi-logarithmic graph paper. The result helps classify the soil and evaluate its gradation and suitability for engineering works, especially in road construction.

  - Atterberg Limit Tests

The Atterberg limits are important measurements that show the critical moisture levels of a fine-textured soil, including the shrinkage limit, plastic limit, and liquid limit. When a dry, clayey soil absorbs more water, it experiences unique transformations in its behavior and texture (Ige, 2009). The soil can be solid, semi-solid, plastic or liquid, depending on its water content. The engineering properties of soil vary from state to state due to differences in consistency and behavior. In thisway, the border of each state can be determined by a shift in the characteristics of the ground. This examination was conducted following BS: 1377(1990) guidelines.

  - Compaction Test

The purpose of the tests was to establish the best moisture content (OMC) and highest dry density (MDD). It includes measuring the mass of dry soil per cubic meter when compacted in a specific way across various moisture levels, including the highest possible mass of dry soil per cubic meter. The sample that successfully passed through the sieve analysis was thoroughly mixed and then 5kg was measured (British Standard Institution, 1990). A precise volume of distilled water was poured into the weighed sample and thoroughly blended. The soil was densely packed into three layers of about the same weight. Following compaction, the molds were taken out and the compacted soils were smoothed with a straight edge. During this process, small soil samples were collected to determine the moisture content. The necessary equipment for this experiment consists of a mold, scoop, rammer, moisture cans, and measuring cylinder, BS test sieve with a 20mm diameter, weighing balance, tray, and oven. This examination was conducted following BS: 1377(1990) guidelines. The dry densities achieved were graphed in relation to the moisture content for every sample. The graph provided the OMC and MDD values for the soil. This exam was conducted following BS: 1377(1990) guidelines.

  - Moisture Content Test

The moisture content percentage was measured according to the ASTM D 2216 guidelines for determining water content in soil, rock, and soil aggregate mixtures in a laboratory setting. This experiment was conducted to ascertain the proportion of moisture contained in the laterite specimen (British Standard Institution, 1990). The water content is a crucial index for many soils to determine the relationship between soil behavior and properties. The moisture content of a fine-textured soil is a key factor in determining its consistency. The moisture content is also utilized to describe the phase interactions of air, water, and solids within a specific soil volume (Gidigasu, 1976). The moisture content test involved recording the number of moisture cans and lids used. The weight of the dry and clean moisture can, along with its lid, was measured and documented. The wet earth was put into the water container, and the cover was fastened. The weight of the damp soil-filled moisture can with the lid was measured and noted. The cover was taken off, and the container holding the damp soil was put in the drying oven set at 105 °C. It was left in the oven overnight before being taken out. The cover on the wet container was gently and firmly put back on with gloves, then left to cool down to the temperature of the room. The weight of the moisture can and lid with the dry soil inside (MCDS) was measured and noted down. The moisture level of the laterite was subsequently determined (Nwankwoala,et al., 2014).

  - Specific Gravity Test

The specific gravity of the soil samples varied between 2.40 and 2.78. According to Wright (1986), the standard range of values of Specific gravity of soils lies between 2.60 and 2.80. Therefore, the obtained values of specific gravity are expected for the tested soils. Que et al. (2008) have shown that specific gravity is closely linked with the mineralogy and/or the chemical composition of soil. It could be concluded that sample S4 (with the highest specific gravity) is the most lateritised sample, while sample S9 (with the lowest specific gravity) is the least lateritised sample (De Graff-Johnson, 1972). Also, lower specific gravity values indicate a coarse soil, while higher values indicate a fine grained soil (Wright, 1986). Therefore, sample S9 is the coarsest, while sample S4 is least coarse.

  - Bulk Density Test

The bulk density test was conducted to determine the mass of soil per unit volume, including pore spaces. This was done by filling a cylindrical container of known volume with soil and weighing it.Bulk density is important in evaluating compaction efficiency and estimating the weight of soil in-situ. It also plays a role in determining other properties such as porosity and bearing capacity. For lateritic soils, bulk density values help in assessing their strength and stability under load-bearing applications.

CHAPTER FOUR

4.0   Results and Discussion

4.1   Results of Natural Moisture Content

The results of natural moisture content test are presented in table 2 the moisture content value range between 4.2% and 5.3%, indicating that the soil are relatively dry. According to Ola (1993), typical moisture content for lateritic soils range between 5% and 20% depending on the season and drainage condition. Therefore the sample fall within the lower end of the standard range implying well drained and stable conditions.

Table2: Natural Moisture Content Test of Collected Samples

| Sample A | Sample B | Sample C |
| --- | --- | --- |
| 5.2% | 4.3% | 4.1% |

Fig.1: graph showing water content

4.2 	Results of bulk Density Test

The results of Bulk Density Test are presented in Table3. The bulk density values range from 1.63 to 1.76g/cm3 Murthy (2002) stated that bulk densities for compacted lateritic soils usually range from 1.6 to 2.0g/cm3. Hence, the values obtained are within the acceptable range, with sample C showing the highest density , indicating better compaction and higher  strength.

Table 3: Bulk Density of Collected Samples.

| Sample A | Sample B | Sample C |
| --- | --- | --- |
| 1.63 | 1.73 | 1.76 |

4.3 	Results of Dry Density Test

Two results of Dry Density value (1.58 - 1.69g/cm3) are also within the expected range for Engineering fill materials. According to Das (2010) dry densities for lateritic soils typically range from 1.5 to 2.0g/cm3, indicating that the test ad soils can offer adequate bearing capacity when properly compacted.

Table 4: Dry Density Test of collected samples

| Sample A | Sample B | Sample C |
| --- | --- | --- |
| 1.58g/cm3 | 1.67g/cm3 | 1.69g/cm3 |

4.4 	Result of Specific Gravity Tests

The specific gravity result are presented in table 5 specific gravity value ranged from 2.68 to 2.83 according to Das (2010), the typical specific gravity of lateritic soil falls between 2.60 and 2.85 which confirm that the soil predominantly mineral based with minimum organic contamination.

Table 5:  Specific gravity test of collected samples

| Sample A | Sample B | Sample C |
| --- | --- | --- |
| 2.68g/cm3 | 2.71g/cm3 | 2.83g/cm3 |

4.5 	Results of Atterberg Limit Tests

Liquid Limit (LL): ranges from 22.3 % to 31.6% According to Das (2010), soil with liquid limit value less than 35% are classified as low plasticity soils. All the three samples fall within this categories, indicating low compressibility and moderate workability.

Plastic Limit (PL): value range from 14.6% to 18.2%, which is also consistent with the range expected for lateritic soil.

Plasticity Index (PI): value, calculated as the difference between LL am PL range from 6.9% to 13.4% Ola (1983) noted that lateritic soil generally have pl value ranging from 5% to 20% depending on the degree of weathering. Hence the PL values obtained fall within the expected range, indicating moderate plasticity with Sample A being more plastic than Sample B and Sample C.

Linear Shrinkage (LS): values range from 3.7% to 6.2% According to Adeyemi (1995), values below 10% suggest that the soils has low shrinks well potential, which is desirable for most construction purpose. Sample C has the lowest shrinkage value, suggesting it will be the most suitable under moisture variation

Table 6: Atterberg Limit Tests of collected samples

| Sample | Liquid Limit % | Plastic Limit % | Plastic index | Linear Shrinkage % |
| --- | --- | --- | --- | --- |
| Sample A | 31.6 % | 18.2% | 13.4% | 6.2% |
| Sample B | 22.3% | 15.4% | 6.9% | 4.8% |
| Sample C | 24.8% | 14.6% | 10.2% | 3.7% |

Fig 2: Graph Showing Plasticity Chart

4.6 	Result of Grain Size Analysis

P1 has higher clay content (21%) hence classified has clayey sand

P2 and P3 have more silt and less clay, Thus, silty sand all sample have sand and dominant particle size making them sand based soils.

Fine (<0.075mm) is highest in P1, which support it’s clayey nature.

Table 7: Summary of result of Grain Size Analysis of soil

| Sample Location | Gravel (%) | Sand (%) | Silt (%) | Clay (%) | Fine (%) | Soil classification |
| --- | --- | --- | --- | --- | --- | --- |
| P1 | 10 | 60 | 9 | 21 | 30 | Clayey sand |
| P2 | 12 | 62 | 15 | 11 | 20 | Silty sand |
| P3 | 13 | 63 | 17 | 7 | 24 | Silty sand |

Fig. 3: Grain Size Analysis Graph

4.7 	Result of Compaction Test

Table 8: Compaction Parameters of Maximum Dry Density (MDD) and Optimum Moisture Content (OMC)

| Sample | MDD | OMC |
| --- | --- | --- |
| A | 1.81 | 8 |
| B | 1.89 | 7.5 |
| C | 1.95 | 6 |

Fig. 4: Graph Showing Compaction Parameters

Table 9: Compaction and Ratings of Unified Soil Classification for Construction (ASTM 1557-91)

| Visual Description | Maximum Dry Density (MDD)(g/cm3) | Optimum Moisture Content (OMC)(g/cm3) | Anticipated embankment performance | Value as Subgrade material | Value as Base Course |
| --- | --- | --- | --- | --- | --- |
| Granular material | 2.00 - 2.27 | 7 – 15 | Good to Excellent | Excellent | Good |
| Granular material with soil | 1.76 - 2.16 | 9 – 18 | Fair to Excellent | Good | Fair to Poor |
| Fine sand and sand | 1.76 - 1.84 | 9 – 15 | Fair to Good | Good to Fair | Poor |
| Sandy silts and silts | 1.36 -1.60 | 10 – 20 | Poor to Good | Fair to Poor | Not suitable |
| Elastic silts and clay | 1.36 - 1.60 | 20 -35 | Unsatisfactory | Poor | Not suitable |
| Silty clay | 1.52 - 1.92 | 10 – 30 | Poor to Good | Fair to Poor | Not suitable |

Table 9: present the compaction parameters of collected samples. The (MDD) Maximum Dry Density for sample A is 1.81 for sample B 1.89 while sample C is 1.95 for Optimum Moisture Content (OMC), sample A is 8, Sample B is 7.5 samples C is 6. The three sample being sandy in nature can be range as range fair to good for embankment performance it is fair to poor for subgrade material are not suitable for base course.

CHAPTER FIVE

5.0	Conclusion and Recommendation

5.1 	Conclusion

The geotechnical investigation of laterite within Kwara State Polytechnic campus revealed that the sampled soils possess engineering properties suitable for various civil engineering applications, especially as subgrade and fill materials. Laboratory tests such as particle size analysis, Atterberg limits, and compaction indicated that the laterite falls within the acceptable range for road construction and foundation works under moderate loading conditions.

The results also show that the laterite exhibits good shear strength, moderate plasticity, and favorable compaction characteristics, making it a dependable material for use in local construction project.

5.2	Recommendation

In the view of the occurrence rampant failure in public civil structures, the suitability of fill materials (which is mostly laterite in Nigeria) must be ascertained before use. Also the improvement of samples other than Sample C should be considered. This should be done by the addition of locally available materials e.g. limestone.

REFERENCES

Gidigasu, M. D. (1976). Laterite soil engineering: Pedogenesis and engineering principle. Development in Geotechnical Engineering, 9,554p.

Ige, O. O., Ogunsanwo, O. & Aweda, K. A.. Geotechnical and mineralogical evaluation of some lateritic soils from Southwestern Nigeria. EJGE, 19B (2014) 301-312.

Khamehchiyan, M., Charkhabi, A. M. & Tajik, M. . Effects of crude contamination on geotechnical properties of clayey and sandy soils. Engineering Geology, 85(2006)114-123.

Ola, S. A. (1983). Geotechnical Properties and behavior of some Nigerian lateritic soils, Sin: Tropical soils of Nigeria in engineering practice, Ed. Ola A. Balkema, Rotterdam.

Malomo, S. & Ogunsanwo, O. The pre-consolidation pressure of a laterite soil. Bulletin I AEG, 28(1983)261 -265.

Abubakar, J.B., (2006). Geotechnical study of lateritic soil in Tipper garage, Katampe Area, Abuja Federal capital territory, pp 4-34.

Oke, S. A., Okeke, O. E., Amadi, A. N. and Onoduku, U. S., Geotechnical Properties of the Subsoil for Designing Shallow Foundation in some selected parts of Chanchaga area, Minna, Nigeria. Journal of Environmental Science, 1 (2009), 45-54.

Amadi A.N., Akande W. G., Okunlola I. A., Jimoh M.O., Francis Deborah G, ‘Assessment of the Geotechnical Properties of Lateritic Soils in Minna, North Central Nigeria for Road design and Construction’, American Journal of Mining and Metallurgy, 3 (2015)15-20

Nwankwoala, H.O., Amadi, A.N., Ushie, F.A. and Warmate, T., Determination of Subsurface Geotechnical Properties for Foundation Design and Construction in Akenfa Community, Bayelsa State, Nigeria. American Journal of Civil Engineering and Architecture, 2 (2014), 130-135.

Oke, S. A., Amadi, A. N., Abalaka, A. E., Nwosu, J. E. and Ajibade, S. A., Index and Compaction Properties of Laterite Deposits for Road Construction in Minna Area, Nigeria. Nigerian Journal of Construction Technology and Management, 10 1&2 (2009)28-35.

Amadi, A. N., Eze, C. J., Igwe, C. O., Okunlola, I.A. and Okoye, N. O., Architect’s and Geologist’s view on the causes of building failures in Nigeria. Modern Applied Science, 6 (2012), 31-38.

Obaje, N. G. (2009). Geology and mineral resources of Nigeria. Berlin Heidelberg: SpringerVerlag, 219p.

Murat, R. A. (1972). Stratigraphy and paleogeography of the cretaceous and lower tertiary in southern Nigeria. University of Ibadan press, Nigeria, 251-266.

Ige, O. O., Ogunsanwo, O. & Inyang, H. I. (2010). Characterization of terrain and biotite gneiss derived lateritic soils in Ilorin, Nigeria, for use in landfill barriers. Global Journal of Geological Sciences, 9(2010), 1 -9.

Reyment, R. A. (1965). Aspects of the geology of Nigeria. Ibadan University Press, 133p.

British Standard Institution (1990). Methods of test for soils for civil engineering Properties (BS 1377). British Standard institution: London, UK. 143p.

British Standard Institution, (1990).BS 1377.Methods of testing Soils for Civil Engineering Purposes. British Standard Institution.

Ige, O. O. & Ogunsanwo, O. Assessment of granite-derived residual soil as mineral seal in sanitary landfills. Researcher, 1(2009) 84-90.

American Society for Material and Testing (2001). Standard test method for direct shear test of soils under consolidated drained conditions (ASTM D3080). ASTM International: PA, USA

Emesiobi, F.C. (2000). Testing and quality control of materials in civil and highway engineering. ISBN 078-2009-36-16 Pp 5-7.

Federal Ministry of Works and Housing (1997). Nigerian General Specification for Roads and Bridges (Revised Edition) 2 137-275.

Whitlow, R. (1995). Basic Soil mechanics. 3rd Ed. Edinburg Gate: Addison Wesley Longman Limited