PHYSICAL AND MECHANICAL EVALUATION OF MARBLE IN ELEBU IN KWARA STATE

By

Balogun, Ayomikun MOHAMMED

ND/23/MPE/FT/0079

SUBMITTED TO:

THE DEPARTMENT OF MINERALS AND PETROLEUM RESOURCES ENGINEERING TECHNOLOGY INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN

IN PARTIAL FULFILLMENT OF THE REQUIREMENT FOR THE AWARD OF NATIONAL DIPLOMA (ND) IN MINERALS AND PETROLEUM RESOURCES ENGINEERING TECHNOLOGY

AUGUST, 2025

Certification

This is to certify that this project was carried out and submitted by Balogun, Ayomikun MOHAMMED of Matric number ND/23/MPE/FT/0079 to the Department of Minerals and Petroleum Resources Engineering, Kwara State Polytechnic, Ilorin in partial fulfilment of the Requirement for the Award of National Diploma in Minerals and Petroleum Resources Engineering Technology.

……………………………..						………………………

Dr. Reuben Obaro								Date

Project Supervisor

……………………………….				           ……………………….

Dr. J. A. Olatunji								Date

Head of Department

….……………………………….		     			 ………………………

Engr. C.T Oluwole

External Examiner								Date

Dedication

I am delighted to dedicate this project to Almighty GOD, the creator of all universe who gave me the grace and opportunity to complete my ND program and this research, may His name be glorified.

Acknowledgements

I give all the glory and adoration to Almighty GOD, the beginning and the End, for his greatest protection and love given to me as a privilege to start and complete this research work.

I wholeheartedly extend my special thanks to my amiable supervisor Dr. Reuben Obaro for his professional guidance and support towards the success of this project.

Abstract

Evaluation and economic potential of marble deposit from Elebu, in Moro Local Government Area of Kwara State were examined for their possible industrial applications. Five (5) samples were taken to laboratory for treatment and standard laboratory preparation prior to physical and mechanical analysis at Civil laboratory, University of Ilorin. The physical and mechanical analysis include specific gravity, bulk density, porosity, compressive strength and aggregate abrasion value. It is evident for all the samples that the specific gravity may be credited to low degree of weathering and are suitable for heavy construction work. The lower density values can be attributed to the presence of impurities, especially in the country rocks. These factor contribute to a decrease in the overall density. Based on porosity, the marble is not prone to dissolubility, acid attacks and are less porous and dense along with the effect of weathering which have been of insignificant implication. The relatively lower values of water absorption can also be attributed to factors such as porosity and weathering or even high percentage of impurities including allied minerals. The UCS of all rock samples are not good in the production of floor tiles and cladding stone based on low Uniaxial Compressive Strength. The abrasion values of Elebu marble are compared to the minimum acceptable value specified in the ASTM C503 (2001) standard which suggest that all the samples are above the minimum required standard. Based on this, Elebu marble is not only suitable for fluxing steel but as chips which are crushed in pieces that are produced according to consumers’ size demand and needs. Chips give gardens or landscapes exquisite cool look. It can also be used as marble fittings of high strength materials that are fitted in places where hard substances impervious to moisture are demanded.

Table of Contents

Title page											i

Certification											ii

Dedication											iii

Acknowledgement										iv

Abstract											v

Table of content										vi

List of Figures											ix

List of Tables											x

CHAPTER ONE										1

1.0	Introduction										1

1.1	Background of the study								1

1.2	Aim of the study									2

1.3	Objectives of the study								2

1.4	Problem Statement									2

1.5	Scope of the study									2

1.6	Justification of the study								2

CHAPTER TWO										4

2.0	LITERATURE REVIEW								4

2.1	Review of Previous work								4

2.2	Geology of Nigeria									5

2.3	Geology of the study area								8

2.4	Strength of Marble									10

2.5	Uses of marble									10

CHAPTER THREE										11

3.0	MATERIALS AND METHOD							11

3.1	Sample collection									11

3.2 	Laboratory analysis									11

3.2.1	Sample preparation									11

3.2.2	Procedures for Specific Gravity							11

3.2.3	Procedures for Density								12

3.2.4	Procedures for Porosity								12

3.2.5	Procedures for Water Absorption Test						12

3.2.6	Procedures for Uniaxial Compressive Strength					13

3.2.7	Procedures for Los Angeles (L.A) Abrasion Test					13

CHAPTER FOUR										14

4.0	RESULTS AND DISCUSSION							14

4.1	Results of specific gravity								14

4.2 	Discussion on Specific Gravity							14

4.3	Results of Density (Kg/m3)								15

4.4	Discussion on Density								15

4.5	Results of Porosity (%)								16

4.6	Discussion of Porosity (%)								16

4.7	Results of Water Absorption Capacity						18

4.8	Discussion on Water Absorption							18

4.9	Results of Compressive Strength							20

4.10	Discussion of Compressive Strength							20

4.11	Results of Los Angeles Abrasion test (%)						23

4.12	Discussion on Los Angeles Abrasion							24

4.13	Economic Importance of Elebu Marble						25

CHAPTER FIVE										26

5.0	Conclusion and Recommendation							26

5.1	Conclusion										26

5.2	Recommendation									26

References										27

List of Figures

Figure 2.1.	Geological Map of Nigeria (Obaje, 2009)					7

Figure 2.2.	Location of the study area							9

List of Tables

Table 4.1.	Result of Specific gravity							14

Table 4.2.	Result of Density (Kg/m3)							15

Table 4.3.	Results of Porosity test (%)							16

Table 4.4.	Classification Scheme for porosity of rocks (Moos and De Quervain, 1948)17

Table 4.5.	Result of Water Absorption Capacity						18

Table 4.6.	Results of Compressive Strength of Marble					20

Table 4.7.	Classification of Unconfined Compressive Strength (Mpa or Nmm2)	22

Table 4.8.	Physico-mechanical Properties of Marble (ASTM C503 2001)		22

Table 4.9.	Results of Los Angeles Abrasion test (%)					23