ASSESSMENT OF GEOCHEMICAL COMPOSITION OF IGBELOWOWA CLAY DEPOSIT AJASE IPO, KWARA STATE, NIGERIA

MUSA TOHEEB AKANO

HND/23/MNE/FT/0030

SUBMITTED TO

DEPARTMENT OF MINERAL AND PETROLEUM RESOURCES ENGINEERING TECHNOLOGY, INSTITUTE OF TECHNOLOGY, KWARA STATE POLYTECHNIC, ILORIN.

IN PARTIAL FULFILLMENT OF THE REQUIREMENTS FOR THE AWARD OF HIGHER NATIONAL DIPLOMA (HND) IN MINING ENGINEERING TECHNOLOGY

July, 2025

DEDICATION

This project is dedicated to Almighty Allah, my lovely parent and my amazing family for their support all through the years in school.

ACKNOWLEDGMENT

I thank I thank the Almighty Allah for his abundant blessings and protection over me throughout my Higher National Diploma (HND) programme  in Kwara State Polytechnic, Ilorin, without him I would not be and neither would I produce this project.

I express my sincere gratitude to my supervisor Dr. J.A. Olatunji and other lecturers in Department of  Minerals and Petroleum Resources Engineering Technology, Kwara State Polytechnic for availing me with their wealth of experience, may you all be rewarded abundantly.

An immeasurable appreciation goes to my wonderful parents Mr. and Mrs. MUSA for their unrelentless efforts  and all my lovely family members, It is a blessing to have you as my family, thanks for your moral, spiritual, physical and financial support toward the completion of this project; God will bless and reward you accordingly (Amen).

ABSTRACT

This research focuses on the geochemical and mineralogical assessment of Igbelowa clay deposit in Kwara State, Northcentral Nigeria, to evaluate its industrial suitability and potential applications. Clay samples were collected from the deposit and analyzed using X-ray Diffraction (XRD) and X-ray Fluorescence (XRF) techniques to determine their mineral phases and chemical compositions.  The XRD results revealed that Sample A is dominated by phengite (41.1%), kaolinite (39.6%), and albite (19.3%), while Sample B is characterized by high albite content (69.3%), muscovite (23.8%), and a minor amount of kaolinite (6.9%). These mineralogical variations suggest different industrial functionalities, with Sample A showing higher refractory potential and Sample B being suitable for fluxing in ceramic production. The XRF analysis showed that Sample A is rich in Al₂O₃ (28.87%), Fe₂O₃ (9.49%), and TiO₂ (2.47%), which are beneficial for the production of refractory bricks, tiles, and structural materials. Conversely, Sample B has a significantly higher SiO₂ content (65.33%) and lower Fe₂O₃ (2.73%), making it more suitable for ceramics and silica-dependent applications. Both samples contain minor fluxing oxides such as Na₂O and K₂O, which enhance vitrification during firing. These results indicate that Igbelowa clay is a valuable industrial resource with applications in ceramics, refractories, and construction materials. Furthermore, blending Samples A and B could optimize their properties by balancing the high alumina content of Sample A with the high silica content of Sample B. It is recommended that further studies, including beneficiation, thermal analysis, and trace element assessment, be carried out to enhance the quality of Igbelowa clay for specialized applications. Sustainable mining practices and industrial-scale development are also necessary to maximize its economic benefits and support local industries.

TABLE OF CONTENTs

Title page

# Certificate

# Certification

# Dedication

# Acknowledgement

# Abstract

Table of content

## CHAPTER ONE

## INTRODUCTION

### 1.1	BACKGROUND TO THE STUDY

1.2	PROBLEM STATEMENT

1.3	AIM AND OBJECTIVES

1.4	JUSTIFICATION

1.5	SCOPE OF THE STUDY

1.6	LIMITATION

CHAPTER TWO

LITERATURE REVIEW

2.1	FORMATION AND EVOLUTION OF CLAY DEPOSITS

2.2	CLASSIFICATION OF CLAY MINERALS

2.3	GEOCHEMICAL COMPOSITION OF CLAY DEPOSITS

2.4	ANALYTICAL TECHNIQUES IN CLAY GEOCHEMISTRY

2.5	INDUSTRIAL APPLICATIONS OF CLAY DEPOSITS

2.6	REGIONAL STUDIES ON NIGERIAN CLAY DEPOSITS

2.7	ENVIRONMENTAL CONSIDERATIONS

2.8	SYNTHESIS AND GAPS IN THE LITERATURE

CHAPTER THREE

METHODOLOGY

3.1	STUDY AREA

3.2	SAMPLE COLLECTION AND PREPARATION

3.3	LABORATORY ANALYSES

3.4	DATA ANALYSIS

CHAPTER FOUR

RESULTS AND DISCUSSION

4.1 	X-RAY DIFFRACTION (XRD) ANALYSIS

4.2 	X-RAY FLUORESCENCE (XRF) ANALYSIS

4.3 	COMPARATIVE DISCUSSION WITH PREVIOUS STUDIES

4.4 	SUMMARY OF FINDINGS

4.5	PHOTOGRAPH

CHAPTER FIVE

CONCLUSION AND RECOMMENDATIONS

5.1 	CONCLUSION

5.2 	RECOMMENDATIONS

REFERENCES

## APPENDIX

## CHAPTER ONE

## INTRODUCTION

### 1.1	BACKGROUND TO   THE STUDY

Clay deposits are among the most economically and industrially significant natural resources due to their wide range of applications. Clays are fine-grained, hydrous aluminosilicate minerals that form through the weathering and hydrothermal alteration of silicate-bearing rocks, particularly feldspar-rich rocks such as granite and basalt (Murray, 2007). They are an essential raw material in numerous industries, including ceramics, cement manufacturing, pharmaceuticals, petroleum drilling, and construction materials . Clay minerals, composed of microscopic particles, are ubiquitous in the Earth's crust and play a crucial role in various geological processes and human activities. Their unique physical and chemical properties make them valuable resources for industries such as ceramics, construction, and environmental remediation. (Ekosse, 2010).

The geochemical characterization of clay deposits is vital in determining their suitability for industrial applications. The mineralogical composition, chemical properties, plasticity, and particle size distribution of clay influence its usability in various industries. For instance, kaolinite-rich clays are commonly used in ceramics and paper manufacturing due to their low shrink-swell potential and high thermal stability, whereas montmorillonite-rich clays are valuable in drilling fluids and environmental remediation because of their high cation exchange capacity (Grim, 1968).

In Nigeria, the abundance of clay deposits presents a significant economic opportunity. Various studies have been conducted on well-known Nigerian clay deposits, such as those in Kankara (Katsina State), Ibese (Ogun State), and Ilesha (Osun State), with findings demonstrating their suitability for different industrial applications (Akinola et al., 2015). However, The Igbelowa clay deposit, located in kwara State, Nigeria, holds significant potential for industrial applications such as ceramics, cement, and brick production. However, its geochemical composition remains underexplored. Understanding the mineralogical and geochemical properties is vital to evaluate its suitability for various uses and to guide sustainable extraction practices.

Clay minerals are among the most versatile natural resources, widely utilized in industries such as ceramics, pharmaceuticals, cement production, and environmental management (Johnson et al., 2015). Nigeria, with its abundant clay deposits, offers significant potential for industrial development, yet many of these resources remain underexplored (Adewale & Eze, 2017). The Igbelowa clay deposit, located in Kwara State, is one such resource whose industrial potential has not been fully assessed.

Previous studies have highlighted the importance of geochemical analyses in determining the mineralogical composition and suitability of clay for various applications (Smithson et al., 2018). However, the absence of specific data on the Igbelowa deposit represents a knowledge gap that limits its industrial exploitation and raises concerns about sustainable resource management (Ibrahim & Ogunleye, 2020).

Clay minerals serve as essential raw materials in various industries, including ceramics, pharmaceuticals, cement manufacturing, and water treatment (Anderson et al., 2014). Their versatility is largely due to the unique properties conferred by their geochemical composition, such as plasticity, thermal stability, and ion exchange capacity (Johnson et al., 2015).

Nigeria, endowed with extensive clay deposits across its geopolitical zones, holds untapped potential for fostering industrial growth and reducing reliance on imported materials (Adewale & Eze, 2017). Among these deposits is the Igbelowa clay, located in Kwara State, which has garnered attention due to its accessibility and perceived abundance (Ogunlana & Bello, 2019). However, despite its significance, there is a lack of comprehensive geochemical chara Fluorescence (XRF) and X-Ray Diffraction (XRD), have proven effective in revealing the mineralogical and chemical properties of clay, guiding their industrial applications (Smithson et al., 2018). Studies on other Nigerian clay deposits, such as those in Abeokuta and Ifon, have demonstrated the utility of such techniques in determining suitability for ceramics and cement production (Adeyemi et al., 2021; Nwosu & Ezeaku, 2022). These findings underscore the need for similar investigations into the Igbelowa deposit to maximize its potential.

1.2	PROBLEM STATEMENT

Despite the industrial significance of clay deposits, a comprehensive assessment of the geochemical properties of Igbelowa clay is lacking. This gap limits its optimal utilization and poses challenges in integrating it into industrial supply chains. Additionally, inadequate characterization may lead to environmental degradation due to unsustainable mining practices.

The Igbelowa clay deposit, like many other clay resources in Nigeria, remains underutilized due to insufficient scientific exploration (Ogunlana & Bello, 2019). While clay deposits across the country have been identified as valuable for industrial purposes, their full potential can only be realized through proper geochemical characterization (Anderson et al., 2014). Unfortunately, the absence of detailed information on the mineralogical and chemical composition of Igbelowa clay has hindered its integration into industries such as ceramics, construction, and environmental remediation (Ibrahim & Ogunleye, 2020).

1.3	AIM AND OBJECTIVES

This study is   aim to conduct a comprehensive geochemical investigation of clay deposits located in Igbelowa, Ifelodun Local Government of Kwara State while the specific objectives include;

- to analyzing the mineralogical composition, elemental concentrations   using XRD and XRF

- to identify potential sources of the clay minerals and their formation processes.

- to assess the suitability of the clays for various industrial applications.

1.4	JUSTIFICATION

Assessing the geochemical composition of Igbelowa clay will provide critical insights into its mineralogical suitability for industrial applications. The study will benefit local industries by reducing dependency on imported raw materials, promoting economic growth, and enhancing resource sustainability. Furthermore, it will contribute to the academic understanding of Nigerian clay deposits.

1.5	SCOPE OF THE STUDY

This study will focus on:

- Field sampling and laboratory analysis of clay from the Igbelowa deposit.

- Determining the mineralogical and chemical composition using techniques such as X-Ray Fluorescence (XRF) and X-Ray Diffraction (XRD).

- Evaluating its potential applications based on its geochemical characteristics.

1.6	LIMITATION

- Accessibility to the site during adverse weather conditions.

- Limited funding for advanced analytical techniques.

- Availability of high-precision laboratory equipment within the region.

CHAPTER TWO

LITERATURE REVIEW

The study of clay deposits is pivotal in understanding not only their economic potential but also their environmental implications and industrial applications. Clays are fine-grained, hydrous aluminosilicate minerals that form primarily through the weathering and alteration of silicate rocks. Their formation, which involves complex geological and chemical processes, results in a diverse range of mineralogical and geochemical characteristics that directly influence their suitability for various applications (Grim, 1968; Murray, 2007).In recent decades, advancements in analytical techniques have significantly enhanced our ability to characterize the geochemical composition of clay deposits. Methods such as X-ray fluorescence (XRF), X-ray diffraction (XRD), and atomic absorption spectroscopy (AAS) provide detailed insights into both major and trace element compositions, enabling researchers to assess the quality and industrial potential of these resources (Tucker, 1991; Ekosse, 2010). These techniques have also been critical in identifying the environmental risks associated with the presence of heavy metals and other contaminants in clay deposits (Ekosse & De Jager, 2000).

2.1	FORMATION AND EVOLUTION OF CLAY DEPOSITS

Clay minerals are principally formed through the weathering and alteration of silicate-bearing rocks. The processes involved in their formation include:

Weathering: Mechanical and chemical weathering of parent rocks such as granite, basalt, and feldspars leads to the breakdown of larger minerals into fine-grained particles. This process is significantly influenced by climatic factors and results in the formation of primary clay minerals (Grim, 1968; Murray, 2007).

Hydrothermal Alteration: High-temperature fluids can chemically alter the primary minerals in rocks. In hydrothermal environments, feldspar and other silicates are converted into clay minerals such as kaolinite or montmorillonite depending on the conditions (Tucker, 1991).

Sedimentary Processes: Once formed, clay particles are often transported by water and deposited in low-energy environments (e.g., river deltas, floodplains, and lake bottoms). Diagenesis and post-depositional processes, such as compaction and cementation, may further modify the original clay mineralogy (Murray, 2007; Ekosse, 2010).

These processes collectively contribute to the evolution of clay deposits, and the resultant mineral assemblage is a function of the source rock composition, climate, and depositional environment.

2.2	CLASSIFICATION OF CLAY MINERALS

Clay minerals are generally classified based on their crystallographic structure, chemical composition, and layer arrangement. The primary groups include:

2.2.1	Kaolinite Group:

Characterized by a 1:1 layer structure (one silica tetrahedral sheet bonded to one alumina octahedral sheet), kaolinite is noted for its low shrink-swell capacity and high refractoriness. This group is widely used in ceramics and paper manufacturing (Grim, 1968; Murray, 2007).

2.2.2 	Smectite Group:

With a 2:1 layer structure (two silica tetrahedral sheets sandwiching one alumina octahedral sheet), smectite minerals, such as montmorillonite, exhibit high cation exchange capacities and swelling properties. These features make them ideal for applications in drilling fluids, adsorption processes, and environmental remediation (Ekosse, 2010; Tucker, 1991).

2.2.3	Illite Group:

Illite has a structure similar to micas with potassium ions in the interlayer spaces, resulting in limited swelling properties. It is commonly found in marine sediments and is used in some ceramic and soil conditioning applications (Murray, 2007).

2.2.4	Chlorite Group:

These clays contain an additional hydroxide layer intercalated between the 2:1 layers, offering improved thermal stability and lower plasticity. They are used in specialized refractory and composite material applications (Tucker, 1991).

This classification provides a framework for understanding the behavior of clay minerals in various industrial and environmental contexts.

2.3	Geochemical Composition of Clay Deposits

The geochemical composition of clay deposits is a critical factor that determines their industrial utility. This composition is typically expressed in terms of major oxides and trace elements:

2.3.1	Major Oxides:

Silica (SiO₂): Often the most abundant component, contributing to the structural integrity and thermal stability of the clay (Murray, 2007).

Alumina (Al₂O₃): Essential for imparting refractoriness and mechanical strength, particularly in high-temperature applications (Tucker, 1991).

Iron Oxides (Fe₂O₃): These influence the color and, in some cases, the magnetic properties of the clays; high iron content can result in undesirable coloration for ceramics (Grim, 1968).

Calcium Oxide (CaO) and Magnesium Oxide (MgO): Affect plasticity and sintering behavior during the firing process (Ekosse, 2010).

Potassium Oxide (K₂O) and Sodium Oxide (Na₂O): Act as fluxes during vitrification, lowering the melting point and facilitating the formation of a glassy phase in ceramics (Tucker, 1991).

2.3.2	Trace Elements:

Trace elements such as titanium (Ti), manganese (Mn), and heavy metals (e.g., lead [Pb], arsenic [As]) are present in smaller amounts but can significantly influence the physical properties and environmental safety of the clay deposits (Ekosse, 2010; Ekosse & De Jager, 2000).

2.4	Analytical Techniques in Clay Geochemistry

Several sophisticated analytical techniques are employed to characterize the geochemical and mineralogical properties of clay deposits. These methods include:

2.4.1	X-ray Fluorescence (XRF) Spectroscopy:

XRF is widely used for the quantitative determination of elemental composition. This non-destructive method measures the fluorescent X-rays emitted by a sample when irradiated, providing rapid analysis of both major and trace elements (Tucker, 1991).

2.4.2	X-ray Diffraction (XRD) Analysis:

XRD is essential for identifying the mineral phases present in a sample. By analyzing the diffraction patterns produced when X-rays interact with the crystalline structure of the clays, researchers can determine the mineralogical composition and classify the types of clay minerals present (Murray, 2007).

2.4.3	Atomic Absorption Spectroscopy (AAS):

AAS is used for the sensitive detection and quantification of specific trace metals within the clay samples. This technique is particularly useful for environmental assessments and quality control in industrial applications (Ekosse, 2010).

2.4.4	Scanning Electron Microscopy (SEM):

SEM provides detailed imaging of the clay’s surface morphology and microstructural features. Coupled with energy-dispersive X-ray spectroscopy (EDS), SEM can also offer qualitative and semi-quantitative elemental analysis, aiding in the identification of mineral phases (Grim, 1968).

2.5	Industrial Applications of Clay Deposits

Clay minerals are utilized extensively across various industries due to their unique physical and chemical properties. Their suitability for specific applications is primarily dictated by their mineralogical composition, plasticity, thermal stability, and chemical reactivity. Below is a detailed discussion of the primary industrial applications of clay deposits, supported by relevant literature.

2.5.1	Ceramic and Porcelain Industries

Kaolinite-rich clays are the backbone of the ceramics and porcelain sectors. Their fine particle size, high purity, and low shrinkage upon firing make them ideal for producing high-quality ceramic wares. Kaolinite’s stable chemical structure also contributes to the whiteness and durability required in porcelain production (Grim, 1968; Murray, 2007). These characteristics ensure that ceramics maintain their structural integrity during firing and subsequent use.

2.5.2	Refractory Materials

Clays with high alumina content are essential for refractory applications, such as in the production of firebricks, crucibles, and furnace linings. The refractory properties of these clays are largely due to their ability to withstand high temperatures without significant degradation. Studies have shown that clays possessing high levels of alumina and low levels of impurities are preferred for applications requiring high thermal resistance (Murray, 2007; Tucker, 1991).

2.5.3	Construction and Cement Industries

Silica-alumina clays are widely used in the construction industry, particularly in the manufacturing of bricks and as raw materials in cement production. The mechanical strength and durability of these clays contribute to the structural integrity of construction materials. Additionally, the balanced composition of silica and alumina ensures that clays used in cement do not adversely affect the setting and hardening processes (Ekosse, 2010; Tucker, 1991).

2.5.4 	Paper and Coatings Industries

In the paper industry, clays such as kaolinite are employed as fillers and coating materials. Their fine particle size and high brightness improve the smoothness and printability of paper. The use of clay coatings also enhances the paper's resistance to ink bleed and improves its overall aesthetic quality (Grim, 1968).

2.5.5 	Environmental Applications and Oil & Gas Industry

Smectite clays, particularly bentonite, are widely recognized for their high cation exchange capacity and swelling properties. These features make them valuable in environmental applications such as wastewater treatment, soil remediation, and as barriers in landfill liners. In the oil and gas industry, bentonite is a critical component of drilling muds, where it helps to control viscosity, stabilize borehole walls, and filter out unwanted particulates (Ekosse, 2010; Tucker, 1991).

2.6	Regional Studies on Nigerian Clay Deposits

Nigeria is endowed with a wide array of clay deposits, each exhibiting distinct geochemical and mineralogical characteristics due to variations in geological settings and weathering processes. Regional studies have provided valuable insights into the properties and potential industrial applications of these clays, forming a benchmark for the assessment of lesser-known deposits such as the Komu clay deposit.

2.6.1	Kankara Clay (Katsina State)

Studies conducted on the Kankara clay deposit have revealed a high kaolinite content with favorable purity levels and low concentrations of deleterious elements. Akinola et al. (2015) reported that the Kankara clay is particularly suitable for refractory and ceramic applications due to its high silica (SiO₂) and alumina (Al₂O₃) contents, coupled with low iron oxide (Fe₂O₃) levels that minimize color alteration during firing. The favorable geochemical profile of Kankara clay has led to its potential application in high-temperature industries.

2.6.2	Ibese Clay (Ogun State)

Ibese clay, located in southern Nigeria, has been extensively studied for its excellent plasticity and thermal stability. Eze (2013) demonstrated that Ibese clay is rich in kaolinite and illite, which contribute to its fine particle size and strong bonding properties—critical factors in ceramic production. The geochemical analysis of Ibese clay shows a balanced ratio of silica to alumina, making it highly suitable for producing high-quality ceramic wares with minimal shrinkage and cracking during drying and firing.

2.6.3	Ilesha Clay (Osun State)

Ilesha clay has received attention due to its balanced chemical composition, which is ideal for both construction and cement industries. According to Ekosse (2010), Ilesha clay exhibits moderate levels of iron oxide, which, while influencing color, do not compromise its structural integrity. The presence of sufficient silica and alumina makes Ilesha clay particularly well-suited for brick manufacturing and as an additive in cement production, offering enhanced thermal stability and mechanical strength.

2.6.4	Comparative Regional Insights

Comparative analyses of these regional clay deposits reveal both similarities and differences in geochemical profiles:

Chemical Composition: While Kankara, Ibese, and Ilesha clays generally show high silica and alumina contents, the proportion of these elements varies, influencing their industrial suitability. For example, higher alumina in Kankara clay favors refractory applications, whereas the balanced silica-to-alumina ratio in Ibese and Ilesha clays supports ceramic production.

Mineralogical Variations: The dominant clay minerals differ among regions, with Kankara clay being predominantly kaolinitic, Ibese clay containing significant amounts of illite, and Ilesha clay displaying a mix of both. These mineralogical differences affect properties such as plasticity, shrinkage, and thermal behavior (Grim, 1968; Murray, 2007).

Environmental and Impurity Profiles: Environmental assessments indicate that trace impurities and potential heavy metal contaminants vary across deposits. Regional studies have underscored the importance of evaluating these aspects to ensure that clays are safe for use in consumer products (Ekosse & De Jager, 2000).

2.6.5	Implications for the Igbelowa

Clay Deposit

The comprehensive regional studies provide a comparative framework for evaluating the Igbelowa clay deposit. By benchmarking the geochemical and mineralogical characteristics of Igbelowa clay against those of well-documented deposits like Kankara, Ibese, and Ilesha, researchers can better predict its industrial applications and identify potential environmental challenges. Such comparative analyses are crucial for developing effective strategies.

2.7	Environmental Considerations

The environmental impact of clay mining and utilization is an essential component of any geochemical study, as the exploitation of clay deposits can have significant ecological and public health implications. This section elaborates on the various environmental factors associated with clay deposits, with a focus on potential contaminants, sustainable extraction practices, and remediation strategies.

2.7.1	Heavy Metals and Trace Element Contamination

One of the primary environmental concerns associated with clay deposits is the presence of heavy metals such as lead (Pb), arsenic (As), mercury (Hg), and cadmium (Cd). Although these elements are typically found in trace amounts, their cumulative effects can be substantial if they leach into soil and water systems. Elevated heavy metal concentrations can adversely affect agricultural productivity, contaminate drinking water, and pose serious health risks to local communities (Ekosse & De Jager, 2000; Murray, 2007).

Sources and Pathways:

Heavy metals in clay may originate from the parent rock, industrial pollutants, or anthropogenic activities such as mining and waste disposal. Once mobilized, these contaminants can migrate through groundwater or be transported by wind-blown dust (Tucker, 1991).

Risk Assessment:

Quantitative analysis using techniques like atomic absorption spectroscopy (AAS) and inductively coupled plasma mass spectrometry (ICP-MS) is critical to evaluate the extent of contamination. Such assessments help in determining whether the clay deposit meets environmental safety standards for industrial use (Ekosse & De Jager, 2000).

2.7.2	Impact of Clay Mining on Ecosystems

Mining activities, if not managed responsibly, can lead to soil erosion, deforestation, and habitat disruption. The removal of vegetation cover and topsoil during clay extraction exposes the land to erosion and degradation. Additionally, water bodies near mining sites can become polluted due to runoff carrying sediments and chemicals, adversely affecting aquatic ecosystems (Murray, 2007).

Soil and Water Quality:

The alteration of natural landscapes can reduce soil fertility and impair water quality, thereby impacting agriculture and local biodiversity. Continuous monitoring of soil pH, organic content, and contaminant levels is essential to mitigate these effects (Tucker, 1991).

Biodiversity Concerns:

Disturbance to natural habitats may lead to a loss of biodiversity. Sustainable mining practices that include reforestation and land rehabilitation plans can help preserve local flora and fauna.

2.7.3	Sustainable Extraction and Remediation Practices

Adopting sustainable extraction methods and remediation strategies is crucial to minimize the environmental footprint of clay mining. Some best practices include:

Controlled Mining Techniques:

Implementing low-impact mining techniques can reduce land degradation. For instance, selective extraction and maintaining buffer zones around sensitive ecological areas help preserve the environment (Murray, 2007).

Waste Management:

Proper disposal and treatment of mining waste are critical. Techniques such as solidification/stabilization and phytoremediation can be employed to manage contaminated waste effectively (Tucker, 1991).

Environmental Impact Assessments (EIA):

Prior to large-scale mining operations, comprehensive EIAs should be conducted to identify potential environmental risks and design appropriate mitigation measures. EIAs ensure that mining activities comply with national and international environmental regulations (Ekosse & De Jager, 2000).

Rehabilitation and Land Reclamation:

Post-mining rehabilitation involves restoring the land to its natural state or repurposing it for alternative uses. Reclamation activities may include replanting native vegetation, contouring land surfaces, and restoring water bodies to ensure long-term ecosystem sustainability

2.7.4	Policy and Regulatory Framework

The development of a robust regulatory framework is imperative for ensuring that clay mining operations are environmentally sustainable. Regulatory agencies must enforce guidelines that cover:

Permitting and Monitoring:

Mining permits should include strict environmental monitoring requirements, with regular inspections and reporting to ensure compliance with environmental standards.

Community Engagement:

Involving local communities in decision-making processes and ensuring transparency in environmental impact studies can lead to better outcomes and shared benefits.

International Standards:

Adopting international best practices and standards, such as those set by the International Finance Corporation (IFC) and other environmental bodies, can help mitigate environmental risks associated with clay mining.

2.8	Synthesis and Gaps in the Literature

The reviewed literature provides a comprehensive understanding of clay deposits—from their formation and classification to their geochemical composition, analytical characterization, industrial applications, and environmental impacts. Overall, these studies have established several key insights:

2.8.1	Formation Processes and Mineral Evolution:

Research indicates that clay deposits are primarily formed through weathering, hydrothermal alteration, and sedimentary processes (Grim, 1968; Murray, 2007). These studies reveal that the mineralogical assemblage of a clay deposit is highly dependent on the parent rock composition and depositional environment. However, while the general mechanisms are well documented, there remains a need for site-specific studies that address the unique geological conditions influencing individual deposits.

2.8.2	Classification and Geochemical Characteristics:

The literature effectively categorizes clay minerals into groups such as kaolinite, smectite, illite, and chlorite, based on their crystallographic structures and chemical compositions (Tucker, 1991; Murray, 2007). Detailed geochemical studies have provided robust profiles of major oxides and trace elements, which are critical for assessing industrial suitability (Ekosse, 2010). Yet, there is still variability in the reported data, especially when comparing different geographic regions, suggesting that more standardized analytical protocols may be required.

2.8.3	Analytical Techniques:

Advanced methods like XRF, XRD, AAS, and SEM have greatly enhanced the precision of clay characterization (Tucker, 1991; Murray, 2007). While these techniques are well established, further refinement is necessary to improve sensitivity—particularly for trace element analysis and heavy metal detection in clays, which is crucial for environmental assessments (Ekosse & De Jager, 2000).

2.8.4	Industrial Applications and Environmental Impact:

Extensive research has highlighted the diverse applications of clay minerals in ceramics, refractories, construction, paper, and environmental remediation (Grim, 1968; Ekosse, 2010). Alongside these benefits, environmental concerns—such as soil degradation, water contamination, and heavy metal pollution—have also been identified (Ekosse & De Jager, 2000; Murray, 2007). Despite this dual focus, the integration of industrial application studies with comprehensive environmental impact assessments remains limited.

2.8.5	Identified Gaps

While the existing literature provides a strong foundation, several gaps and opportunities for future research have been identified:

- Site-Specific Characterization:

Although the general formation mechanisms and geochemical profiles are known, many studies lack detailed, site-specific data on lesser-studied deposits such as the Komu clay deposit. Further research is needed to characterize these deposits under local geological conditions, which could lead to more accurate predictions of their industrial and environmental performance.

- Standardization of Analytical Methods:

Variability in analytical results across different studies suggests the need for standardized protocols. Establishing uniform methodologies for sample collection, preparation, and analysis would improve data comparability and reliability (Tucker, 1991).

- Integration of Industrial and Environmental Studies:

While industrial applications and environmental impacts have been explored separately, few studies integrate these aspects holistically. Future research should focus on assessing the trade-offs between industrial utilization and environmental sustainability, especially regarding heavy metal contamination and remediation strategies.

- Advanced Trace Element Analysis:

There is a call for more sensitive and refined analytical techniques to detect and quantify trace elements and heavy metals. Improvements in methods such as ICP-MS could enhance our understanding of potential environmental risks associated with clay deposits (Ekosse & De Jager, 2000).

- Comparative Studies:

Comparative analyses between Nigerian clay deposits and those from other regions could help standardize industrial benchmarks and enhance the global understanding of clay mineralogy. Such studies would also aid in identifying unique regional characteristics that may influence industrial applications.

CHAPTER THREE

METHODOLOGY

The methodology of the study entails;

3.1	Study Area

The Igbelowa clay deposit is located in  Kwara State, NorthernCentral Nigeria. The area lies within the Precambrian Basement Complex of Nigeria, which consists mainly of granite, gneiss, and schist. The deposit is formed from the weathering of feldspar-rich rocks, leading to clay accumulation. Komu experiences a tropical climate with distinct wet and dry seasons, which influences weathering processes. The vegetation is Guinea savanna, and the topography is generally undulating with some exposed rock outcrops. The area is known for its economic potential in ceramics, bricks, and other industrial applications due to the quality of its clay deposits.

3.2	Sample Collection and Preparation

Clay samples is systematically collected from different locations within the Igbelowa clay deposit to ensure a representative study.

After collection, the samples is;

i. Air-dried to remove moisture.

ii. Crushed and sieved to obtain a uniform particle size

iii. Stored in labeled containers to prevent contamination before laboratory analysis.

These steps are taken to ensures that the samples remain in their natural state for accurate geochemical evaluation.

3.3	Laboratory Analyses

The clay samples collected are   subjected to various laboratory tests to determine their geochemical and mineralogical compositions. The following methods are used:

3.3.1	X-Ray Fluorescence (XRF) Analysis

Is used to determine the elemental composition of the clay, identifying major and trace elements.

3.3.2.	X-Ray Diffraction (XRD) Analysis

is used to Identifies the mineralogical composition by detecting crystalline phases present in the clay.

3.4	Data Analysis

The geochemical and mineralogical data obtained from the laboratory analyses are processed and interpreted using standard analytical techniques. The following approaches are used:

3.4.1	Descriptive Statistical Analysis

The elemental and mineralogical compositions are summarized using tables and charts for easy interpretation.

3.4.2.	Comparison with Standard Values

The results are compared with established industrial standards to assess the suitability of the clay for applications such as ceramics, refractory materials, and construction.

CHAPTER FOUR

RESULTS AND DISCUSSION

This chapter presents the results of the mineralogical and geochemical analyses of the Igbelowa clay deposit in

Kwara State, NorthernCentral Nigeria. The analyses were performed using X-ray Diffraction (XRD) and X-ray Fluorescence (XRF) techniques to determine the mineral phases and chemical composition of the clay samples. These results were then interpreted in relation to the industrial applicability of the clay and compared with findings from similar studies in Nigeria and other parts of the world.

4.1 	X-Ray Diffraction (XRD) Analysis

X-ray Diffraction (XRD) was employed to identify the crystalline phases in the clay samples. This method determines the mineralogical composition based on the diffraction patterns produced when the samples are exposed to X-rays. The results of the XRD analysis for Komu clay are presented in Table 4.1.

Table 4.1: XRD Results for Igbelowa Clay Samples

| S/N | Sample A | Percentage (%) | Sample B | Percentage (%) |
| --- | --- | --- | --- | --- |
| 1 | Phengite | 41.1 | Albite | 69.3 |
| 2 | Kaolinite | 39.6 | Muscovite | 23.80 |
| 3 | Albite | 19.3 | Kaolinite | 6.90 |

4.1.1 Interpretation of XRD Results

Sample A:

Sample A is characterized by high phengite (41.1%) and kaolinite (39.6%) contents, with a moderate amount of albite (19.3%). The high kaolinite content indicates that the clay has a low shrink-swell capacity and excellent thermal stability, which are desirable properties for refractory and ceramic applications (Grim, 1968; Murray, 2007). Phengite, a mica-group mineral, may also improve fluxing characteristics during firing, making Sample A a suitable raw material for structural clay products.

Sample B:

Sample B is dominated by albite (69.3%), a feldspar mineral, followed by muscovite (23.8%) and minor kaolinite (6.9%). The high albite content indicates a flux-rich material, which lowers the melting temperature and improves vitrification in ceramic production (Tucker, 1991). However, the low kaolinite content in Sample B reduces its refractoriness, making it unsuitable for high-temperature applications unless blended with alumina-rich clays such as Sample A.

4.1.2 	Discussion of XRD Results

The mineralogical compositions of both samples indicate that:

Sample A is suitable for refractory materials, tiles, and structural clay products due to its kaolinite and phengite content.

Sample B is ideal for ceramics and glaze production especially where high fluxing properties are required.

Blending both samples can optimize their combined properties, balancing the refractoriness of Sample A with the fluxing characteristics of Sample B to produce high-quality clay products.

These findings are consistent with previous studies on Nigerian clay deposits, such as the work of Ekosse (2010), who noted that kaolinite-rich clays are preferred for refractory applications, while feldspar-rich clays are better suited for ceramics.

Figure 4.1 Showing the pie chart of XRD sample A

Figure 4.2 Showing the pie chart of XRD sample B

4.2 	X-Ray Fluorescence (XRF) Analysis

X-ray Fluorescence (XRF) analysis was conducted to determine the geochemical composition of the Igbelowa clay samples. This technique provides quantitative data on the major oxides present in the clay, which directly influence its industrial behavior during firing. The XRF results are presented in Table 4.2

Table 4.2: XRF Results for Igbelowa Clay Samples

| Basic Oxide | Formulae | Sample A1 (%) | Sample B1 (%) | Interpretation / Remarks |
| --- | --- | --- | --- | --- |
| Silicon Oxide | SiO₂ | 42.75 | 65.33 | Much higher in B1; good for ceramics/refractory use |
| Calcium Oxide | CaO | ND | ND | Not detected in both samples |
| Magnesium Oxide | MgO | ND | 0.80 | Detected only in B1 in small quantity |
| Sodium Oxide | Na₂O | 1.00 | 0.80 | Present in both; affects melting point during firing |
| Potassium Oxide | K₂O | 1.40 | 0.60 | More in A1; acts as flux in ceramic production |
| Sulphide | SO₃ | ND | ND | Not detected |
| Phosphorus Oxide | P₂O₅ | ND | ND | Not detected |
| Manganese Oxide | MnO | 0.40 | 0.05 | Trace amount; higher in A1 |
| Titanium Oxide | TiO₂ | 2.47 | 0.24 | Significantly higher in A1 |
| Aluminum Oxide | Al₂O₃ | 28.87 | 24.60 | High in both; A1 richer, ideal for bricks and tiles |
| Iron Oxide | Fe₂O₃ | 9.49 | 2.73 | A1 has much more; contributes to clay color & firing |
| Loss Of Ignition | L.O.I. | 13.50 | 5.30 | Higher in A1; indicates more volatiles/moisture |
| TOTAL |  | 99.88 | 100.45 |  |

4.2.1 Interpretation of XRF Results

Silicon Oxide (SiO₂):

Sample B1 has the highest silica content (65.33%), making it ideal for ceramics and products requiring high mechanical strength. Sample A1 has moderate silica content (42.75%), balancing strength with plasticity.

Aluminum Oxide (Al₂O₃):

Both samples contain high alumina, especially Sample A1 (28.87%). High alumina improves plasticity, thermal resistance, and refractoriness, which is essential for brick and tile manufacturing (Murray, 2007).

Iron Oxide (Fe₂O₃):

Sample A1 has a higher iron content (9.49%), resulting in reddish coloration after firing, making it suitable for structural materials but less ideal for white ceramics.

Titanium Oxide (TiO₂):

TiO₂ is higher in A1 (2.47%), improving opacity and contributing to thermal resistance, particularly in refractory applications.

Fluxing Oxides (Na₂O, K₂O):

Present in both samples in low amounts, these oxides lower the melting temperature, aiding vitrification in ceramic production.

Loss on Ignition (L.O.I.):

Sample A1 has a higher L.O.I. (13.50%), suggesting more volatile components and moisture, which should be accounted for during processing to avoid excessive shrinkage.

4.2.2 	Discussion of XRF Results

Sample A: Rich in alumina and iron oxide, making it suitable for refractory bricks, tiles, and structural applications.

Sample B: Silica-rich and suitable for ceramic production, especially for lighter-colored products.

Blending Potential: Mixing the two samples in proper proportions could result in high-quality materials suitable for both refractory and ceramic industries.

4.3 	Comparative Discussion with Previous Studies

These results align with studies by Ekosse (2010) and Akinola et al. (2015), which reported that Nigerian kaolinite-rich clays are ideal for refractory applications, while feldspar- and silica-rich clays perform better in ceramic production. The high silica in Sample B is consistent with clays from other parts of Nigeria used for tiles and ceramic wares. Similarly, the high alumina and iron in Sample A resemble clays from Kankara (Katsina State), which are widely used for brick manufacturing.

4.4 	Summary of Findings

The analysis of Komu clay deposit using XRD and XRF revealed the following key results:

1. Mineralogical Composition (XRD):

Sample A: Predominantly phengite (41.1%), kaolinite (39.6%), and albite (19.3%), indicating good refractory and structural potential.

Sample B: Rich in albite (69.3%), muscovite (23.8%), and minor kaolinite (6.9%), suitable for ceramics and as a fluxing agent.

2. Geochemical Composition (XRF):

Sample A: High in Al₂O₃ (28.87%), Fe₂O₃ (9.49%), and TiO₂ (2.47%), making it ideal for bricks, tiles, and high-temperature materials.

Sample B: High in SiO₂ (65.33%) with low Fe₂O₃ (2.73%), suitable for ceramics requiring high silica strength and lighter color.

3. Industrial Implications:

Sample A is more suitable for refractory and structural uses.

Sample B is ideal for ceramic production and blending with alumina-rich clays.

Blending both samples could optimize their industrial applications.

4.5	Photograph

A digital camera was used to capture the mine pit, land degradation and overburden.

Figure 4.3: Clay Sample from the Study Area

Figure 4.4: Overburden			Figure 4.5: Land Degradation

Figure 4.6: Mine Pit

CHAPTER FIVE

CONCLUSION AND RECOMMENDATIONS

5.1 	Conclusion

This study examined the geochemical and mineralogical compositions of Igbelowa clay deposit in Kwara State using X-ray Diffraction (XRD) and X-ray Fluorescence (XRF) techniques to determine its industrial potential.

The XRD results revealed that:

Sample A is dominated by phengite (41.1%), kaolinite (39.6%), and albite (19.3%), indicating a balanced clay suitable for refractory, tiles, and ceramic applications.

Sample B is rich in albite (69.3%), followed by muscovite (23.8%) and kaolinite (6.9%), showing high fluxing potential and suitability for ceramics that require lower firing temperatures.

The XRF results further showed that:

Sample A has high Al₂O₃ (28.87%), Fe₂O₃ (9.49%), and TiO₂ (2.47%), which are beneficial for refractory and structural clay products.

Sample B contains high SiO₂ (65.33%) and low Fe₂O₃ (2.73%), making it more suitable for ceramics with lighter color and high strength.

Overall, both samples are industrially valuable. Sample A is better for high-temperature applications (bricks, tiles, and refractories), while Sample B is ideal for ceramics and blending purposes. Combining both samples would optimize their industrial performance by balancing alumina-rich refractoriness with silica-driven strength.

5.2 	Recommendations

To maximize the industrial potential of Igbelowa clay deposit, the following recommendations are made:

1. Industrial Use:

Utilize Sample A for refractory bricks, tiles, and structural products.

Use Sample B for ceramics and other silica-rich applications.

2. Blending Strategy:

Blend both samples in appropriate ratios to improve performance and reduce production costs.

3. Further Research:

Conduct thermal analysis and trace element studies to further evaluate the firing behavior and safety of the clays.

Investigate beneficiation methods to improve the purity and quality of the clay for specialized industrial uses.

4. Environmental Management:

Adopt sustainable mining practices and reclamation programs to mitigate environmental impacts.

5. Industrial Development:

Encourage local industries and government to invest in clay processing facilities to promote the economic utilization of the Igbelowa clay deposit.

REFERENCES

Akinola, O. O., Adeyemi, G. O., & Osibanjo, O. (2015). Characterization of Nigerian clay deposits	for industrial applications. Journal of Applied Geology, 7(2), 120–133.

Ekosse, G. I. (2010). Clays and clay minerals: Geology, geochemistry, and industrial applications.	African Journal of Science and Technology, 4(1), 35–47.

Eze, I. O. (2013). Geotechnical properties of some Nigerian clays and their suitability for industrial	applications. Journal of Mining and Geology, 49(2), 85–97.

Grim, R. E. (1968). Clay mineralogy. New York: McGraw-Hill.

Murray, H. H. (2007). Applied clay mineralogy. Amsterdam: Elsevier.

Murray, H. H. (2007). Applied clay mineralogy: Occurrences, processing, and applications of	kaolins, bentonites, and other clays. Amsterdam: Elsevier.

Tucker, M. E. (1991). Techniques in sedimentology. Oxford: Blackwell.

Abdelmalek, B., Boukhelkhal, A., & Khelafi, H. (2017). Characterization and valorization of	Algerian clay for ceramic application. International Journal of Scientific Research and	Management (IJSRM), 5(3), 53–60.

Abolarin, M. S., Oyetunji, A., & Ause, T. (2004). Development of refractory bricks from locally	available materials. Journal of Engineering and Applied Sciences, 3(4), 45–49.

Adedeji, A. A., Ogunleye, O. O., & Ajayi, O. (2025). Evaluation of selected clay deposits for paint	and ceramic industries in Southwestern Nigeria. Journal of Applied Clay Science, 87(2),	213–221.

Adnan, A. (2011). The industrial applicability of kaolinitic clay in ceramic and allied industries.	International Journal of Ceramic Engineering, 29(1), 22–29.

Ahuwan, J. I. (2002). Fundamentals of clay mineralogy and industrial application. Nigerian	Journal of Applied Sciences, 18(1), 15–19.

Alabi, A.A (2005) Exploration and Reserve of clay. A case study of kuttigi clay deposit of Bida	basin. Unpolished M.Tech, ThesisFederal University of Technology Minna, Nigeria.

Amuda O.S and Majolagbe A.O (2015) Health benefit of clay. Journal of Environmental	Management 156, 72-80.

Boylu F.(2011) Applied clay science 52(1-2), 101-108.

Braja M.D (2020)Soil Mechanics and Foundation CRC press.

Elimbi, A., Tchakoute, H. K., & Njopwouo, D. (2011). Use of clay materials in the production of	geopolymer cements. Applied Clay Science, 54(1), 90–96.

Fakolujo O.A, Akinmesin A.I, and Olowoyo J.A.(2012) Characteristic of clay and application,	Materials science and Engineering. 82(4), 555-563.

Cengel, Y. A., & Ghajar, A. J. (2015). Heat and mass transfer: Fundamentals and applications (5th	ed.). McGraw-Hill Education.

Job, C. A. (2017). Thermal properties of clays and their industrial applications. Journal of Thermal	Analysis and Calorimetry, 129(3), 1373–1380.

Neeraj S, and Chandra M. (2012) properties of clay and it’s application. Applied clay science. 206,	106085.

Nwoye I. (2020). Assessment of clay deposit in Nigeria African journal of earth science 158,	103743.

Obi, M. (1995). Mineralogy of Nigerian soils and their industrial implications. Journal of African	Earth Sciences, 10(2), 83–89.

Omowumi A.B (2012) Clay mineralogy properties and uses. Journal of mineralogy 45(1) 114.

Adewole, M. T., Alabi, A. A., & Salawu, M. O. (2019). Mineralogical and chemical analysis of	selected clay deposits in Kwara State. Journal of Earth Sciences, Kwara State Polytechnic,	6(2), 42–50.

Bello, A. G., & Ahmed, S. M. (2020). Geochemical evaluation of Asa clay for ceramic suitability.	Applied Geosciences Journal, Kwara State Polytechnic, 7(1), 22–29.

Ogunyemi, O. J. (2017). Utilization of local raw materials for industrial development in Nigeria:	A case study of Ilorin clay. Kwara Polytechnic Research Series, 4(3), 15–23.

Salami, L. A., & Kehinde, S. B. (2016). Potentials of clay resources in selected local governments	of Kwara State. Journal of Environmental Earth Science, 3(1), 30–38.

Salawu, M. O., & Adebayo, T. O. (2021). Trace element analysis of clay samples in Moro LGA	of Kwara State. Earth Materials Journal, Kwara State Polytechnic, 8(1), 10–19.

Yusuf, M. A., & Afolayan, R. I. (2018). Comparative analysis of Asa and Oyun clays for industrial	application. Journal of Geosciences and Mineral Resources, 5(4), 12–20.

Ige, R. A., & Olanrewaju, M. A. (2015). Engineering properties and industrial significance of	selected clays in Ilorin East. Kwara State Polytechnic Journal of Engineering, 2(1), 19–28.

Babatunde, A. M., & Lawal, A. K. (2018). Physical and chemical properties of clay deposits in	Ifelodun and Irepodun LGAs of Kwara State. KwaraPoly Scientific Review, 6(3), 45–56.

APPENDIX

Anchor Scan Parameters

Dataset Name:	A1

File name:	C:\Users\USER\Downloads\THE 5 SAMPLES XRD (1)\THE 5 SAMPLES XRD\A1.ASC

Raw Data Origin:	ASCII-2Theta-Intensity (.ASC)

Scan Axis:	Gonio

Start Position [°2Th.]:	3.0000

End Position [°2Th.]:	69.9900

Step Size [°2Th.]:	0.0300

Scan Step Time [s]:	1.0000

Scan Type:	Pre-set time

Offset [°2Th.]:	0.0000

Divergence Slit Type:	Fixed

Divergence Slit Size [°]:	1.0000

Specimen Length [mm]:	10.00

Receiving Slit Size [mm]:	0.1000

Measurement Temperature [°C]:	25.00

Anode Material:	Cu

K-Alpha1 [Å]:	1.54060

K-Alpha2 [Å]:	1.54443

K-Beta [Å]:	1.39225

K-A2 / K-A1 Ratio:	0.50000

Generator Settings:	0 mA, 0 kV

Diffractometer Number:	0

Goniometer Radius [mm]:	240.00

Dist. Focus-Diverg. Slit [mm]:	91.00

Incident Beam Monochromator:	No

Spinning:	No

Graphics

Peak List

Pos.[°2Th.]  Height [cts]  FWHMLeft[°2Th.]  d-spacing [Å]  Rel. Int. [%]

3.4634          5.21           0.9446       25.51137           0.11

8.1935        635.21           0.1476       10.79130          13.42

9.0497       4733.78           0.1181        9.77208         100.00

11.3217        216.38           0.3542        7.81568           4.57

12.6090       1606.49           0.1476        7.02047          33.94

16.2176        254.30           0.1771        5.46556           5.37

17.9624       2277.40           0.1181        4.93840          48.11

20.0851        653.30           0.1771        4.42102          13.80

20.5593        701.20           0.1771        4.32011          14.81

21.5773        578.28           0.5904        4.11855          12.22

24.3624        627.83           0.1476        3.65366          13.26

25.0830       1409.09           0.2952        3.55031          29.77

27.0088       2738.38           0.2066        3.30137          57.85

27.9241        144.18           0.4723        3.19521           3.05

35.1531        449.62           0.3542        2.55294           9.50

36.1038        619.16           0.2362        2.48787          13.08

38.5706        464.55           0.3542        2.33425           9.81

40.9156        232.48           0.2362        2.20572           4.91

45.6469        685.54           0.1771        1.98750          14.48

50.2769         85.16           0.2362        1.81479           1.80

55.2008        181.43           0.5904        1.66400           3.83

60.0408        152.45           0.2362        1.54092           3.22

61.6143         26.34           0.0886        1.50530           0.56

62.3333        347.18           0.2362        1.48965           7.33

Pattern List

Visible  Ref.Code     Score    Compound Name         Displ.[°2Th]  Scale Fac.  Chem. Formula

*        96-900-5496       35  Phengite                     0.213       0.305  K1.90 Na0.10 Al9.1..

*        96-900-9664       20  Albite                      -0.032       0.093  Na1.96 Ca0.04 Si5...

*        96-101-1046       36  Kaolinite 2M                 0.154       0.244  Al8.00 Si8.00 O36...  q