# KWARASTATEPOLYTECHNIC,ILORIN.

INSTITUTEOFTECHNOLOGY

FLEXTURALSTRENGTHOFBAMBOOREINFORCEDCONCREATESLAB

BY

MUIZ ABDULSALAM OLADIMEJI

ND/23/CEC/PT/0127

SUBMITTEDTO

THEDEPAERTMENT OFCIVILENGINEERING,

INSTITUTIONOFTECHNOLOGY(IOT)KWARASTATEPOLYTECHNIC,PMB 1375ILORIN KWARA STATE.

INPARTIALFULFILMENTOFTHEREQUIREMENTFORTHEAWARDOF NATIONAL DIPLOMA (ND) CERTIFICATE IN CIVIL ENGINEERING DEPARTMENT.

JUNE,2025.

## CERTIFICATION

Thisistocertifythat thisresearchstudywasconducted by MUIZ ABDULSALAM OLADIMEJI

(ND/23/CEC/PT/0127)andhadbeenreadandapprovedasmeetingtherequirement fortheaward of National Diploma (ND) in Civil Engineering, Institute of Technology, Kwara StatePolytechnic, Ilorin.

…………………………………….	………………………….. ENGR.SAHHEDABDULHAMEED

DATE

ProjectSupervisor

…………………………………….	………………………….. ENGR. A. SANNI

DATE

PARTTIME CORDINATOR

…………………………………….	…………………………..

DATE

ExternalExaminer

ENGR.ABDULHAMEEDABDULRASAQADUAGBA

TABLEOF CONTENTS

  - INTRODUCTION

  - BACKGROUND

  - OBJECTIVES

  - SCOPE

  - LITERATUREREVIEW

  - NATUREANDDESCRIPTIONOFWOOD’SSTRUCTURE

2..1.1DIFFERENTTYPESOFWOOD

    - TIMBERANDITSAPPEARANCE

    - STRUCTURALTIMBER

  - BRIEFDESCRIPTIONSOFNIGERIANGROWNTIMBERS

    - BASICCHARACTERISTICSOFBAMBOO

    - DURABILITYOFBAMBOOASANENGINEERING MATERIAL

  - EFFECT OFWATERABSORPTIONOFBAMBOO

  - BONDINGSTRENGTHOF BAMBOO

  - TIMBERASASTRUCTURALMATERIAL

  - COMPOSITEACTIONINTIMBER-CONCRETESYSTEMS

    - STRUCTURALBEHAVIOROFTIMBER-CONCRETE COMPOSITES

  - FLEXURALSTRENGTH

  - METHODOLOGY

  - MATERIALSOURCING

    - SAMPLINGOFSAWNTIMBERLENGTHS

  - METHODOLOGY

  - MATERIALSOURCING

    - SAMPLINGOFSAWNTIMBERLENGTHS

    - PREPARATIONOFTESTSPECIMENS

    - COARSEAGGREGATE

    - FINEAGGREGATE

    - PORTLANDCEMENT

    - WATER

  - FLEXURALSTRENGTHTESTOFTIMBERREINFORCEDCONCRETESLAB

    - REINFORCEMENTPREPARATION

  - RESULTANDDISCUSSIONS

  - FLEXURALTESTSTRENGTH

    - FLEXURALSTRENGTHTEST ONTEAKTIMBERREINFORCEDCONCRETESLAB

  - FLEXURALSTRENGTH(EXPERIMENTALLOAD)RESULTOFTEAKREBARSLAB

  - :FLEXURALSTRENGTHTEST(EXPERIMENTALLOAD)RESULTOFSTEELREINF.SLAB

5.0CONCLUSION

5.1RECCOMMENDATION

REFERENCES

# DEDICATION

IdedicatethisprojecttomyparentsMr&Mrs Abdulsalam and mygaurdiance, Mr Adulsalam and to everyone who has supported and inspired me throughout this journey. To my family and friends, thank you for your unwavering encouragement and belief in me. To my mentors and teachers, your guidance has been invaluable. This work is a reflection of the collective effort and support of all those who have walked alongside me.

ACKNOWLEDGMENT

I would like to express my sincere gratitude to Almighty God & my beloved parents(Mr&MrsAbdulsalam)andto everyone whosupported me throughout the completion of this project.

First and foremost, I thank my project supervisor, [ Engr, Saheed Abdulhameed],forhis valuableguidance,encouragement,andinsightful feedback. His expertise and support were instrumental in shaping this work.

Ialsoappreciatetheassistanceandcooperationofmyteammembersand colleagues, who contributed their time and ideas, making this project a collaborative success.

Finally, Iamgratefultomyfamilyand friendsfortheircontinuous motivation and understanding during this endeavor.

# ABSTRACT

Thisprojectinvestigatestheflexuralstrengthofconcreteslabsreinforced with bamboo as an alternative to conventional steel reinforcement.

Bamboo, being a sustainable and eco-friendly material, offers potential benefits in reducing construction costs and environmental impact. The studyinvolvesdesigningandcastingconcreteslabswith varyingbamboo reinforcement configurations, followed by systematic flexural testing to evaluate their load-bearing capacity and failure modes. Results indicate thatbamboo-reinforcedconcreteslabsexhibitpromisingflexuralstrength characteristics, suggesting their viability for low-cost and sustainable construction applications. This research contributes to expanding the use of renewable materials in structural engineering while promoting green building practices.

CHAPTERONE

  - Introduction

  - Background

Concrete slabs are fundamental components in modern construction, primarily reinforced with steel to handle tensile stresses. However, due to rising costs and environmental concerns associatedwithsteelproduction,alternativereinforcement materialsaregainingattention.Timber, a renewable and lightweight material, presents a potential reinforcement alternative, especially when sustainably sourced and treated for structural applications.Composite structural systems combine two or more materials with different mechanical properties to achieve performance benefits that exceed those of individual components. In structural engineering, the most common composite systems include steel-reinforced concrete and timber-concrete composites (TCC).These systems are designed to exploit the compressive strength of concrete and the tensilestrength of another material — typically steel. However, with rising awareness of environmental sustainability and circular economy principles, alternative composite systems involving timber asa reinforcing or load-sharing component are gaining interest.

Timber has been used as a building material for thousands of years due to its natural abundance, workability, and renewable nature. It possesses a high strength-to-weight ratio and is readily available in many regions of the world. In modern engineering, timber is increasingly used in the form of engineered wood products such Glued Laminated Timber (Glulam), Laminated Veneer Lumber (LVL) and Cross-Laminated Timber (CLT). These engineered products overcome the limitationsofnaturalwood—suchasanisotropy,dimensionalinstability,andstrength

variability—byprovidingconsistentperformanceandimprovedmechanicalproperties.

Reinforced concrete is one of the most widely used construction materials worldwide due to its versatility, strength,andrelativeeconomy.Traditionally,reinforcement isachievedwithsteelbars (rebar), which provide the necessary tensile resistance that concrete lacks. However, steel has several drawbacks such as high carbon footprint due to energy-intensive manufacturing, susceptibility to corrosion in aggressive environments, heavy weight, increasing transportationand structural loads and rising costs of raw materials. These challenges have led researchers and engineers to explore alternative reinforcement materials, including fiber-reinforced polymers (FRPs), bamboo, and timber.

In consequence ofthe consumers choosing industrialized products, among other effects, activities are suppressed in rural areas or even in small towns, and renewable materials are wasted and causing permanentpollution. In this sense, it becomes obvious that ecological materials satisfy such fundamental requirements, making use of agricultural by-products such as ricehusk,coconut fibres, sisaland bamboo and thereforeminimizing energyconsumption, conserving non- renewable natural resources, reducing pollution and maintaining a healthy environment. Bamboo is one material, which will have a tremendous economical advantage, as it reaches its full growth in just a few months and reaches its maximummechanicalresistance in just few years. Moreover, it exists in abundance in tropical andsubtropical regions of the globe.The energy necessary to produce 1m3 per unit stress projected in practice for materials commonly used in civil construction, such as steelor concrete, has been compared with that of bamboo. It was found that for steel it is necessary to spend 50 times more energy than for bamboo . The tensile strength of bamboo is relatively high and can reach 370MPa. This makes bamboo an attractive alternative to steel in tensile loading applications. This is due to the fact that the ratio of tensile strength to specific weight of bamboo is six times greater than that of steel.

The development of timber-reinforced concrete slabs is rooted in the pursuit of sustainable, efficient, and locally adaptable structural systems. Bycombining concrete’s compressive strength withtimber’srenewabletensileperformance, TRC slabsofferacompellingalternative for modern construction. However, successful implementation depends on addressing technical challenges related to bond behavior, durability, moisture effects, and standardization. This background establishes the foundation for further investigation into the performance, feasibility, and application of timber-reinforced concrete slab system.

### Objectives

- Toevaluatethephysicalandmechanicalpropertiesofthebamboomaterialthroughreview.

- Toevaluate the structuralperformanceoftimber-reinforcedconcrete slabs.

- Tocompare mechanicalperformanceagainststeel-reinforcedslabs.

### Scope

The study focuses on slabs using timber as primary reinforcement.Hardwood such as Teak timber is considered as reinforcement in concrete. The specimen preparation were done in accordance with BS 8110 for reinforcement preparation.

## CHAPTERTWO

### LiteratureReview

  - Natureanddescriptionofwood’sstructure

Wood is generallycomposed of cells parallel to each other along the trunk of a tree which is of primary interest to engineers as it is from the trunk that structural timber is manufactured. Wood cells possess cavities inside and are elongated and spindle-shaped. Figure 2.1 shows a cross- section of a trunk pointing out its main features in growing trees. Some basic information and perceptions ofwood are prerequisites to understanding the behavior and the limitations oftimber.

Figure2.1:Cross-sectionofatrunk(Brostowetal.,2010)

In most trunks of trees, the first principal part to notice is the sapwood which is the outer, pale- coloured wood, lighter region close to the cambium that has three main functions in a tree:from the supporttothe conductionand the storage function. Furthermore, whenthe cells are dead, they conveywaterand minerals fromthesoil. Followed bythe heartwoodinthesecond instancewhich

is the inner partofthe woodthat is mostlydarker because ofthe resins and gums contained inside the cells but in contrast with the sapwood, the heartwood provides the main structuralsupport for the trees. Meanwhile, it does not possess any living cells, water conductsorstores andis notessentialinthegrowingprocess andthesurvivalofthetrees (Forest Products Laboratory, 1966). Another important part is the bark which shelters the interior of the trunk of the tree. The wood cells are produced by a layer of cells called the cambium that can onlybe seen using the microscope and inside all the tissues present at the center of the tree are referred to as xylemwhile those outside are the bark including the phloem that transport energy sources made by the plant and the cork layers. The ray and axial parenchyma cells, when initially produced by the cambium, are alive but they lose their cell contents and become hollow, microscopic tubes with lignified walls at the moment they become functioning, water-conducting cells, referred to as tracheids and vessels (Bamber, 1964).

### Differenttypesofwood

In a living tree from which h timber comes, the two main types of tree are softwood andhardwood which should not be mixed up with the hardness or softness of the wood itself but frequently, hardwood trees are denser than softwood ones though (Ragland, 2010).

Softwoods are woods from gymnosperm coniferous trees, evergreen with vertical cells called tracheid of about 3 mm long and roughly 30 μm wide sometimes referred to as non-pored wood such as Scots Pine which is the most world widely used softwood. Generally, softwoods provide longer trunks and grow faster in line with Ragland, (2010). These cells have an open channeland thin cell walls and are used for support and conduction while the storage cells are found in the radial direction. The water-conducting cells known as tracheid in softwood are taper in shape.

Figure2.2:AsectionofSoftwood(Primefacts,2008)

Hardwoods are broad-leaved trees from dicot angiosperm or trees with enclosed seeds containing pores ranging in size and shape allowing water to travel from the roots to nourish the wood (Armstrong, 2017).Theyare madeup oftwo distinct typesofcells: thevesselsthat canusuallybe seenwiththe naked eye and the fiber cells that impart strengthinthe broad-leaved trees. Theyare reproduced by flowers with verticalcells of1 to 2 mm long and 15 μmwide. Thesecells arethick- walledwith a confiningcentralchannel, inappropriate for conduction, used only to support and so, thetreeneedsvesselsforthispurpose.Vesselsareeitheropen-endedxylemorphloemof0.2to

1.2 mm long, stacked verticallyto formtubes of less than 0.5 mm in diameter (Primefacts, 2008). It is allproduced bya fluid movement inside the capillary, reaching thetopsofevenverytalltrees related to the surface tension. The vessels and the fibers in hardwood are tubular.

Figure2.3:Aclose-upsectionofhardwood(Primefacts,2008)

The strength property, shrinkage, and grain pattern properties of timber and other products are affected by the characteristics of the stalky cells and their arrangement. The microscopic cellular structure ofwood including the ring in the cross-section ofthe stemor root ofa temperate woody plant, produced by one year's growth and the ray that stores food in the stem, produces the characteristic grain patterns in different species of the trees. This grain pattern is also determined by the plane in which logs are cut at the sawmill. The ray cells unlike other cells are arranged horizontally, extending radially outwards and towards the bark. The annual rings appear like concentric bands with rays extending outward like each of the bars or wire rods connecting the center of a wheel to its outer edge (spokes) in transverse or cross-sections and can be counted to age-date the tree as shown in Figure 2.4 (Brostow et al., 2010).

Figure2.4:Atreecross-sectionwith24distinctannualrings(Brostowetal.,2010)

### TimberanditsAppearance

Brostow et al. (2010), reported that timber is an organic construction material for most societiesanddescribessawnwoodwithawide rangeofphysicalandmechanical properties for which it is important for the ones selected to have properties suitable for aspired use. The strength, appearance, durability, the moisturecontent (shrinkagerates) arethemainpropertiesaffectingthe choice of timber. But for certain applications, other properties such as density, hardness, fire performance, etc. are also important.

(Trada, 1999) affirmed that most timbers come in a varietyof colors between and within species; timbers exposed to light and those that remain unprotected and exposed to weatherwill change color, especially for the latter once mold growth is developed. To broadly describe timber's appearance and some specific characteristics, the term grain may be used; it refers to thedirection, size, and arrangement of the woodcells and should not be used alone instead forinstance sloppy grain, wavy grain, spiral grain etc. (Forest and Wood Products Research and Development Corporation, 2004).Timbersalso come in varietiesoftextureswhichcanbe coarse, fine, even, or uneven, etc., and based on the size and arrangement of wood cells, difference is made between the different types of texture. (National Association of Forest Industries, 2004). It can	also	divulge	some	other naturalcharacteristicsthatcanaffectthestrengthpropertiesandaestheticslikestains,splits gum veins, and knots which are the part of the branches embedded in the main stem of the tree and sloping grain.

### Structuraltimber

Structural timber or timber machined for structural use has its constituents sawn from the tree trunkinaprismaticshapewitharectangularcross-sectionexcept for someexceptionsintheshape. The size of the trees in the forest is the main factor that determines the maximum possible dimension ofthose constituentsthat areapplied for load-carrying functions in structures. Manyprovisions in the production line to obtain the appropriate structural elements therefore exist; for instance, the longitudinal axis of a structural timber component should synchronize with the wood cells grain direction, (Kohler, 2007). As the outcome of the basic processing steps such as debarking,sawing, planning if necessary, finger-jointing only for some products, and gluing on the broader side, during the production of structural timber, its main characteristic is the anisotropic nature it has where the naturalwood structure will be retained to a high degree (Angst et al., 2008).

### BriefdescriptionsofNigerian grown timbers

2.2.1.Basiccharacteristicsofbamboo

Bamboos are giant grasses and not trees as commonly believed. They belong to the family of the Bambusoideae. The bamboo culm, in general, is a cylindrical shell,which is divided by transversal diaphragms at the nodes. Bamboo shells are orthotropic materials withhigh strength in the direction parallel to the fibres andlow strength perpendicular to the fibres respectively.Bamboo is a composite material, consisting of long and parallel cellulose fibres embedded in a ligneous matrix. The density of the fibres in the cross-section of abamboo shell varies along its thickness. This presents a functionallygradient material, evolved according to the state of stress distribution in its natural environment. the fibres are concentrated in regions closer tothe outer skin. This is consistent withthe stateof stress distributionwhenthe culm is subjected to wind forces. In establishing the mechanicalproperties of bamboo, in the elastic range, the rule of mix for the composite materials is used. The properties of the fibres and matrix with their volumetric fractions are taken into account. Eq. (1) presents the calculation of the elasticity modulus, Ec, of the bamboo as a composite. In this equation Ef and Em are elasticity moduli and VfandVm=(1-Vf)arethevolumetricfractionsofthefibresandmatrixrespectively.Inthe

developmentofEq.(1),long,uniformlyspacedandalignedfibresareassumedinadditiontoa

perfect bondingbetweenfibresand matrix.

Ec=EfVf+Em(1- Vf)	1

In the application of Eq. (1) to the analysis of bamboo, the variation of the volumetric fraction of fibres, Vf(x), with thickness should be taken into account.

Figure 2.5:Bamboo

### 2.2.2DurabilityOfBamboo AsAnEngineeringMaterial

Just like timber, bamboo is vulnerable to environmental degradation and attacks by insects and moulds. Its durability varies with the type of species, age, conservation condition, treatment and curing. Curing should be initiated when bamboo is being cut in the bamboo grove. There is a strong relation between insect attacks and the levels of starch plus humidity content of bamboo culm. In order to reduce the starch content, bamboo receives a variety of treatments including curing on the spot, immersion, heating or smoke. Drying bamboo is fundamental to its conservation for various reasons. Bamboo with low humidity is less prone to mould attacks especially when humidity content is less than 15%. Physical and mechanical properties ofbamboo increase with a decrease in its humidity content. Bamboo to be treated with apreservativeneedstobedrytofacilitatepenetrationandobtainabetterresultandreducing

transport costs. Bamboo can be dried in air, green house, and oven or by fire. The durability of bamboo depends strongly on the preservative treatment methods in accordance with basic requirements: its chemical composition should not have any effect on the bamboo fibre and once injected it must not be washed out by rain or humidity. The preservative can be applied using simple systems such as leave transpiration, immersion, impregnation, Modified Boucherie Method, Boucherie Method to sophisticated modern equipment of cauldrons and specialchambers working with vacuum or pressure. Many steel and concrete structures builtin the past 30 years reveal serious deterioration caused mainly bythe corrosion ofthe steelreinforcement. In Fig. 5 a steel reinforced concrete column after 10 service years and the first bamboo reinforced concrete beam tested at PUCRio in 1979 are presented and compared. The steel reinforcedcolumn is part of the tunnel structure of Rios Metro. The bamboo reinforced beam after testinghas been exposed to open air in the university campus. It can be observed that the bamboo segment ofthebeamreinforcement,treatedagainst insectsaswellas for bondingwithconcrete, is still in satisfactorycondition after 15 years. However, the steelreinforcing bars ofthe column are severely corroded and need to be replaced. The bamboo segments of the beam were taken out of the tested concrete beam to establish its mechanical strength. Compared to the original untreated bamboo a slight deterioration of tensile strength was observed in the weathered samples of bamboo reinforcement.

Figure 2.6: Durability of bamboo and steel reinforcement in concrete elements. (a) Bamboo reinforcement of a tested beam exposed in open air after15 years. (b) Steel reinforcement of a column in the tunnel of metro after 10 years in closed area.

### 2.3.EffectOfWaterAbsorptionof Bamboo

One of the main shortcomings of bamboo is water absorption when it is used as a reinforcement and/or permanent shutter formwithconcrete. Thecapacityofbamboo to absorbwater wasstudied on several species. DG, and Bambusa vulgaris schard, VS, absorbed the least amount of water among all compared species. The dimensional variations of the transversal section of bamboosDG and VS reached up to 6% after 7 days immersion in water. The dimensional variation of untreated bamboo due to water absorption can cause micro or even macro cracks in curedconcrete.

### 2.4.BondingStrengthof Bamboo

A reinforcing bar in concrete is prevented from slipping by adhesion or bond between them. The main factors which affect the bond between the reinforcing bar and concrete are: adhesive properties of the cement matrix, the compression friction forces appearing on the surface of the reinforcing bar dueto shrinkage ofthe concrete andthe shear resistance ofconcretedueto surface form and roughness of the reinforcing bar. The dimensional changes of bamboo due to moisture and temperature variations influence allthe three bond characteristicsseverely. During the casting and curing ofconcrete, reinforcing bamboo absorbs water and expands as shown in Fig. 7(a). The swelling of bamboo pushes the concrete away, shown in Fig. 7(b). Then at the end of the curing period, the bamboo loses the moisture and shrinks back almost to its original dimensions leaving voids around itself, shown inFig. 7(c). The differentialthermalexpansionofbamboo withrespect toconcretemayalsoleadtocrackingoftheconcreteduringservicelife.Theswellingand

shrinkageofbambooinconcretecreateaseriouslimitationintheuseofbambooasasubstitute

for steel in concrete. To improve the bond between bamboo segments and concrete, an effective water-repellenttreatment isnecessary.Varioustypesoftreatment have beenstudiedwithdifferent degrees of success.

Figure 2.6:Behaviour ofuntreated segment bamboo as reinforcement in concrete: (a) bamboo in fresh concrete, (b) bamboo during curing of concrete and (c) bamboo after cured concrete.

### TimberasaStructuralMaterial

Timber is characterized by anisotropic behavior, high strength-to-weight ratio, and excellent workability. Engineered wood products like LVL and glulam offer consistent mechanical properties and dimensional stability. Timber has been used as a structural material for thousandsof years due to its natural abundance, ease of processing, and favorable mechanical properties. In modern structural engineering, timber has evolved from a traditional building material to an engineered product withconsistent and predictable performance characteristics. Withthe growing emphasis on sustainability and carbon reduction in the built environment, timber is experiencing renewed interest as a primary or hybrid structural material. Timber is an orthotropic material, meaning it exhibits different mechanical properties along its three principal axes—longitudinal, radial,andtangential.Itslongitudinal direction,which alignswith thegrain,isthestrongestand

stiffest, making it particularly effective in resisting tensile and compressive forces along the grain.However, timber is relatively weak in tension and compression perpendicular to the grain and in shear, requiring carefuldetailing to avoid splitting and failure (Green & Evans, 2008).To overcome natural limitations of solid timber—such as knots, grain variability, and dimensional instability—engineered wood products (EWPs) have been developed. These are manufactured by bonding wood strands, veneers, or laminations under controlled conditions. Common EWPs include:

- GluedLaminatedTimber(Glulam):Madefrom layersof dimensional lumberbondedwith durable adhesives. Offers high strength and can be curved into custom shapes.

- LaminatedVeneerLumber(LVL):Thinwoodveneersgluedinthesamegraindirection, resulting in high strength and stiffness.

- Cross-LaminatedTimber(CLT):Layersoftimberorientedperpendicularlyandbondedtogether, providing dimensional stability and strength in multiple directions.

- OrientedStrandBoard(OSB):Usedprimarilyinsheathing,itconsistsofwoodstrands bonded in specific orientations.

These products allow timber to compete with steel and concrete in terms of structural performance, especially in mid- and high-rise construction (Mohammad et al., 2012).

### CompositeActioninTimber-ConcreteSystems

Timber-concrete composites (TCCs) have been studied primarily in floor systems where concrete bears compression and timber resists tension. The composite action is often achieved using mechanical fasteners, notches, or adhesive bonding. Composite construction integrates two or more distinct materials to act together structurally, achieving enhanced performance by utilizing the strengths of each. In timber-concrete systems, the goal is to combine timber’s tensile strength

and lightweight characteristics with concrete’s compressive strength, rigidity, and mass. These systems are primarily used in floor construction, where timber beams or slabs are topped with a layer of reinforced concrete. Timber-concrete composites (TCC) are a response to the growing demand for sustainable, efficient, and low-carbon construction systems. By leveraging the complementary behavior of wood and concrete, TCC systems offer improved strength, stiffness, and serviceability compared to traditional timber floors, while being lighter and more sustainable than conventional reinforced concrete slabs (Dias et al., 2007). Composite action refers to the degree of cooperation between two bonded materials to resist loads. In a TCC system, full composite action implies that no slip occurs at the interface between timber and concrete,resulting in maximum structural efficiency. However, due to material differences and practical constraints, partial composite action is usually achieved. The effectiveness of composite action depends on interface connection system, material compatibility, stiffness of connectors, shear transfer capability.According to Lukaszewska (2009), partial interaction affects both flexural stiffness (EI) and load distribution, making accurate modeling and testing essential for design.

### StructuralBehaviorofTimber-ConcreteComposites

In bending, concrete (in compression) and timber (in tension) share the load based on their stiffness and the level of interaction at the interface. The effective bending stiffness of a TCC system lies between that of a non-composite (no-slip) and a fully composite (perfect bond)section. The γ-method, as introduced in Eurocode 5 (EN 1995-1-1), is a widely used design approach to quantify the degree of composite action by using a gamma factor (γ) to modify the stiffness of the system (Lukaszewska, 2009). Key structural benefits includes increased load- bearing capacity, reduced mid-span deflection, improved vibration performance, better sound insulation and fire resistance due to the mass of the concrete. Timber-concrete composite floors are increasingly used in residential and commercial buildings, retrofits ofold timber structures (to

increase capacity without full demolition), sustainable mid-rise and low-rise buildings and modular and prefabricated systems.

Composite action in timber-concrete systems allows for the efficient use of both materials by combining their strengths. While full composite action is rarely achieved due to interface slip, partial interaction—properly designed—can result in structurally sound, cost-effective, and sustainable systems. These hybrid structures hold great promise for both new construction and renovation, particularly in low- to mid-rise applications where lightweight construction and environmental performance are priorities.

### FlexuralStrength

In the flexural test, the theoretical maximum tensile stress reached in the bottom fiber of atest beamorslab is knownasthe modulusofrupture,which is also flexuralstrength, bending strength, or fracture strength. When concrete is subjected to bending, the transverse bending test is most frequently employed, in which a specimen having either a circular or rectangular cross-section is bent until it fractures or yields. The value of flexural strength would be the same as tensile strength if the materials are homogenous. The flexural strength represents the highest stress experienced within the material at its moment of rupture. It is measured interms of stress represented with the symbol sigma. For determining the flexural strength or modulus of rupture, the following two systems of loading of the specimen maybe adopted (Gupta & Gupta, 2004):

#### Central PointLoading

In this system of loading, the load is applied at the mid or central point of the test specimenwhich gives a triangular bending moment distribution. The maximum stress fiber stress will be below the point of loading wherethe bendingmoment is maximum.Thus, the maximum stress occurs atone sectionofthe specimen, not necessarilythe weakest sectionofthe specimen. Figure

2.19 shows the arrangement ofthe apparatus in a one-point test to determine the flexuralstrength of a rectangular beam.

Figure2.1:Flexuraltest(Centralloading).Source:(GuptaandGupta,2004)

Forarectangularsampleunderaloadinatwo-pointbendingsetup(Figure2.1),theflexural strength is calculated with equation (2.1)

𝜎=3𝐹𝐿

2𝑏𝑑2

Where

(2.1)

Fistheload(force)atthefracturepoint(N)Listhe lengthofthesupport span(mm) biswidth(mm)

disthickness(mm)

#### TwoPointsLoading

This systemofloading produces a constant bending moment betweenthe load points so that one- third of the span is subjected to the maximum stress and thus in this region cracking is likely to take place. Nowadays, this system of loading is taken as the standard method of

loading. The systemoftwo points loading isshown inFigure 2.2Forarectangular sample under a load ina four-point bending setup(Figure2.20)wherethe loadingspanisone-thirdofthesupport span, the flexural strength is calculated with equation (2.2)

Figure2.2:Flexuraltest(Twopointsloading).Source:(GuptaandGupta,2004)

𝜎=𝐹𝐿

𝑏𝑑2

(2.2)

Where:

Fistheload(force)atthefracturepoint(N)Listhe lengthofthesupport span(mm) biswidth(mm), disthickness(m)

## CHAPTERTHREE

  - Methodology

  - MaterialSourcing

    - Samplingofsawntimberlengths

  - Methodology

  - MaterialSourcing

    - Samplingofsawntimberlengths

Bamboospecieweresourcedfromtheforestandprocessedtosamplespecimen.

### Preparationoftestspecimens

After conditioning, the solid-sawn woods were cut by the required specimen dimensions given by the Code of Practice BS EN 373:1957. The preparation of test specimens took place in the wood workshopoftheFacultyofEngineering, UniversityofIlorin.The split bamboo culmswere of 30mm wide rectangular sections. The smooth surface of the bamboo splints was cleaned and slightly roughened before being coated with a thin layer of the impermeable product together with sand. The pieces were then wrapped with 1.5mm wire at 10mm distance and once more coated with the same product. Immediately after that, fine sand was manually pressed into the surface and the splints were allowed to dryfor 24hbefore being fixed inside the formwork. The bamboo reinforcing ratio, q, varied between 1% to3%

### CoarseAggregate

Thecoarseaggregateusedforthisexperimentisgranite.Granitesizerangingfrom5mmto10mm fromquarryalongrovalvalleyroadGariki,Ilorin,KwaraState.The coarseaggregateuse

conformedtotherequirementofBSEN12620:2013

### FineAggregate

Thefineaggregateusedforthisexperimentissand.Sandwasgottenfromariveralongoko-olowo area,Ilorin, KwaraState.Thefine aggregateuseconformedtotherequirement ofBSEN 12620:2013

### PortlandCement

Dangote(3X)cementwithstrengthof42.5RisobtainedfromalocalselleralongoldKwara polytechniccampus,Ilorin, KwaraState.Thecement isusedasabinder andconformedto requirement of BS EN 197-1-2000.

### Water

ThewateruseforthisstudyconformstotherequirementofBSEN1008:2002(Mixingwaterfor concrete).

### FlexuralStrengthTestofTimberReinforcedConcreteSlab

This section covers the flexural test on the bamboo reinforced concrete slab to determine the variation of the slab's flexural strength with an increase in the percentage of longitudinal timber reinforcement. The flexural test was carried out by BS EN 12390-5:2009 (Testing hardened concrete: Flexural strength of test specimens) using a universal testometric machine (UTM) at Material Science, Mechanical Department, University of Ilorin, Ilorin, Kwara State.

### ReinforcementPreparation

Design parameters were formulated based on BS 8110-1:1997 to give average initial values for laboratory tests. Longitudinal reinforcements were varied by section of the slab (area) in 1%and 3% concrete slab samples. In this case, the longitudinal squares of two different local timbereach360mmlong,andsquaretransversetimbereach160mmlongwerenailedtogetherata

right angle. The longitudinal timber bars were placed below while the transverse bars were placed above. Also, Steelreinforcementforcontrolslabs was preparedsimilarly. Information on reinforcement sizes and arrangement using timber are shown in Table 3 below.Table 4 also shows the arrangement of steel reinforcement for slab test as control.

### Table1: Description ofTimberRebarArrangementforSlabTest.

| Label | h mm | d mm | LongitudinalBar |  |  |  |  | TransverseBar |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | As mm2 | 100As /bh (%) | 𝜙 mm | No | S mm | As mm2 | 100As /Lh (%) | 𝜙 mm | No | S mm |
| 1CT | 75 | 54 | 150 | 1 | 12 | 2 | 160 | 900 | 3 | 16 | 5 | 72 |
| 2CT | 75 | 53 | 300 | 2 | 12 | 3 | 80 | 900 | 3 | 16 | 5 | 72 |

hdenotesthethickness oftheslab(mm)

TTdenotestreatedtop

ddenotestheeffectivedepth(mm) TB denotes the treated bottom

Asdenotedtheareaofreinforcement(mm2)

      - denotesthebar sizeinsquare(mm).

Sdenotesthespacing (mm).

### Table2:DescriptionofSteelReinforcementArrangementforSlab Test.

| Label | h mm | d mm | LongitudinalSteelbar |  |  |  |  | TransverseSteelBar |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | As mm2 | 100As/bh (%) | 𝜙 mm | No | S mm | As mm2 | 100As/ Lh (%) | 𝜙 mm | No | S mm |
| SS1 | 75 | 54 | 120 | 0.8 | 10 | 2 | 160 | 360 | 1.2 | 10 | 5 | 72 |

Note:

The minimumreinforcement forhigh-yieldsteelin Slabis0.12%bhwhilethe maximumrange is from1to2%bh(BS8110:Part1:1997).Thepercentageto beusedforthis researchischosen as 0.80% for the longitudinal bar and 1.2% for the transverse bar.

### ConcreteSlabPreparation

The preparation of concrete samples was carried out after the arrangement of timber reinforcement. The concrete samples used were cement, fine aggregate (sand), and coarse aggregate (granite).Hand mixing techniques were employed to mix the ingredients of the concrete with a designed trial mix ratio of 1:2:4 with a water/cement ratio of 0.50 on a clean concrete slab. Sample slabs of 75 mmdeep by200 mmwide by400 mm long (Figure 3.1) were cased inside a prepared wooden formwork. Casting started by firstplacing the woodenformwork on the floor. The internal surface of the formwork was oiled to prevent the adhesionof concrete onto the surface of the formwork. A concrete layer of 20 mm was initially poured into the formwork which served as a cover for the reinforcement. The slab reinforcement was then placed in the formwork on the concrete cover and more concrete was poured until the formwork was filled up. The wet concrete in the formwork was then tamped round with a 25mmsquare steeltamping rod. After 60minutes ofsetting the concrete, identification inscriptions were made on the slabs for easy identification. The wooden formwork was then taken off after24 hoursof casting and the concrete slabs were cured for 7,14, and 28 days by wetting the slabs daily and covering the slabs with polythene sheeting to prevent loss of moisture. A total of eighteen (18) slabs consisting of 12 No. of timber reinforced slabs and 6 No. of steel-reinforced slabs were cast on different days.

Figure3.1:ConcreteSlab Section.

PlateV:ArrangementandFailureModeofTimberReinforcedSlab

## CHAPTERFOUR

  - Resultand Discussions

  - FlexuralTestStrength

    - FlexuralStrengthTest onTeakTimberReinforcedConcreteSlab

Table 4.1 shows experimental load resultsofthe centralpoint flexuraltestonthe teakreinforced concrete slabs. The flexural strength of the teak reinforced slabs (CRS) at 28 days strength was from2.20 N/mm2 to 2.43 N/mm2 with increase in the percentage ofteak rebar from1% and3%.

### Table4.1FlexuralStrength(ExperimentalLoad) ResultofTeakRebarSlab

| Label |  | 1stcrack load Pcr(N) | Failure loadPult(N) | Deflection at peak (mm) | Flexural Strength (N/mm2) | Modeoffailure |
| --- | --- | --- | --- | --- | --- | --- |
| 1BRS | Minimum | 3051 | 5502 | 3.13 | 2.74 | Two number of cracksandfailure is in Tension Two number of cracksandfailure is in Tension |
|  | Maximum | 4300 | 7530 | 5.02 | 2.90 |  |
|  | Mean | 3676 | 6516 | 4.08 | 2.82 |  |
| 3BRS | Minimum | 3642 | 5514 | 2.40 | 2.86 |  |
|  | Maximum | 5200 | 8540 | 3.63 | 3.10 |  |
|  | Mean | 3859 | 5954 | 3.38 | 2.98 |  |

  - FlexuralStrengthonSteelReinforcedConcreteSlab

Table4.2 showsexperimentalload resultsofthecentralpoint flexuraltest onthesteelreinforced concrete slabs. The failure stress of the steelreinforce slabs at 28 days strength is 5.28 N/mm2

Table4.2:FlexuralStrengthTest(ExperimentalLoad) ResultofSteelReinf. Slab

| Label | 1stCrack Load | Failure Load (N/mm2) | Deflection at Peak (mm) | Flexural Strength (N/mm2) | Modeof Failure |
| --- | --- | --- | --- | --- | --- |
| SRS | 9647 | 12863 | 4.12 | 5.28 | visiblecracks andfailureis in tension |

## CHAPTERFIVE

### 5.0Conclusion

The study concluded that a slab reinforced with bambooat 3% cross-sectional slab area can achieve up to 56% in terms of flexural strength compared with a steel rebarof 10mm diameter. Teakwoodcaneffectivelybe used asreinforcement inconcreteifa sufficient percentage isused as reinforcement in concrete.

5.1Reccommendation

- More comprehensive research is essential to explore the potential of locally availableNigeria timbers in various types of concrete under different loading conditions and environments.

- More research work should be embarked uponto cover for higher reinforcement percentage (4% and 5% respectively).

## REFERENCES

Aguwa,J.I.(2016)“TheNigerianStructuralTimber”.PublishedandPrintedbyAhmaduBello.

UniversityPressLtd.,Samaru, Zaria.Nigeria.

American	Institute	of	Architects	(AIA),	(2020)	“Building	Codes”,	Retrieved	from https://www.aia.org/resources/18631-building-codes

American	Institute	of	Architects,	(2020)	“Building	Codes”,	Retrieved	from https://www.aia.org/resources/18631-building-codes

Arun,C.,andPriyanranjan,P.(2023)“Studiesonvariouspropertiesofreinforcedconcrete”,

JournalofResearchGate,Pp.193

ASTMD1782-17“StandardTestMethodforOperatingPerformanceofParticularCation-Exchange Materials”.

Bailey,G. (2004)“StructuralFireDesign”,JournalofStructuralEngineer, Vol.8, pp.32-38

BS373(1957)“MethodsofTestingSmallClearSpecimensofTimber”,BritishStandardInstitution, London, United Kingdom.

BSEN1994-1-2(2005)“Eurocode4:Designofcompositesteelandconcretestructures,Part

1.2:”BritishStandardInstitution,London,UnitedKingdom.

BS5950(2003)“Structuraluseofsteelworkinbuilding,Part8:CodeofpracticeforFireResistant design”, British Standard Institution, London, United Kingdom

BSEN1992-1-2 (2004)“Eurocode2:Designofconcretestructures,Part1.2:General rules– Structural fire design”, British Standard Institution, London, U.K

BS EN 1993-1-2 (2005) “Eurocode 3: Design ofsteelstructures. Part 1.2: Structural fire Design, British Standard Institution, London, United Kingdom

Buildings Department (2005) “Code of Practice for the StructuralUse of Steel, Chapter 12: Fire Resistant Design’’ , Hong Kong .