CHARACTERIZATION OF BUDO-EGBA SILICA SAND FOR FOUNDRY APPLICATION

BY

OKPE MATTHEW MARACHUKWU

ND/23/MET/PT/001

SUBMITTED TO THE

DEPARTMENT OF METALLURGICAL ENGINEERING,

INSTITUTE OF TECHNOLOGY,

KWARA STATE POLYTECHNIC, ILORIN, NIGERIA.

IN PARTIAL FULFILLMENT OF THE REQUIREMENT FOR THE AWARD OF NATIONAL DIPLOMA (ND) IN METALLURGICAL ENGINEERING TECHNOLOGY

JULY, 2025

CERTIFICATION

This is to certify that this project work was carried out by Okpe Matthew Marachukwu with Matric Number: ND/23/MET/PT/001 has met the requirement and regulations governing the award of National Diploma (ND) in Metallurgical Engineering, Kwara State Polytechnic, Ilorin and under the supervision of the project supervisor.

________________________				_________________

ENGR. A. S. ADESINA 					DATE

Supervisor

_______________________				_________________

ENGR. D.A. ADEGBITE						DATE

Head of Department

_______________________				_________________

EXTERNAL EXAMINER 					DATE

DEDICATION

The project work is dedicated to God Almighty, my creator, my strong pillar, my source of inspiration, wisdom, knowledge and understanding. He has been the source of my strength throughout this program.

ACKNOWLEDGEMENT

My outmost gratitude goes to Almighty God, the Alpha and the Omega, who has been the source of my strength and breath throughout the years.

I want to appreciate my supervisor, Engr. A. S. Adesina for his assistance rendered to me on my project. I want to say a big thanks to you, may God bless you abundantly.

To my beloved parent, I would forever be grateful to you for your love, care, moral and financial support. God bless you, Amen.

My acknowledgement would not be completed without appreciating the effort of lecturers: Engr. D. A. Adegbite (H.O.D), Engr. Alagbe, M., Engr. S. A. Babalola, and Engr. F. F. Ihogbetin, for impacting so much in me both in knowledge and characters, I am grateful.

To my families, friends and course-mates, I thank you for your support and prayers.

ABSTRACT

There are availability of moulding sands in different locations in Nigeria which have not been utilized for foundry operations. Budo-Egba moulding sand needs to be characterized in order to be useful for productive and profitable foundry practices. In this study, evaluation of chemical and physic-mechanical properties of the natural moulding sand in Budo-Egba, Asa Local Government of Kwara State, Nigeria was carried out to ascertain its suitability for foundry applications. The analysis of the sand samples’ chemical compositions were carried out and different properties were characterized. The results of chemical composition analysis showed that SiO2 have dominance proportion in the sand sample with an average value of 91.80% following by Al2O3 with 5.0% and other compounds were also present within acceptable limits of trace elements. The results showed average physico-mechanical properties of the natural moulding sand sample to include grain finess number (66.5), bulk density (1650.7k/m3), moisture content (7.65%), specific gravity (2.60), permeability (0.11KN/m2), flowability (66.01%), clay content (10.01%), shatter index (21.2%) and refractoriness (>900oC), which were all within the required standards for casting of non-ferrous metals. Therefore, Budo-Egba moulding sand can be used for casting of non-ferrous metals. Though, there may be a need for the use of additives such as starch, bentomite, graphite etc in order to increase the sand potential for foundry applications.

TABLE OF CONTENTS

Title page										i

Certification 										ii

Dedication 										iii

Acknowledgement 									iv

Abstract										v

Table of Contents									vi

List of Tables										x

CHAPTER ONE

INTRODUCTION

1.1	Background of the Study							1

1.2	Statement of the Problem							4

1.3	Significant of the Study							4

1.4	Aim and Objectives of the Project						5

1.5	Scope of the Study								5

CHAPTER TWO

2.0	LITERATURE REVIEW

2.1	Moulding Sands								7

2.2	Principal Ingredient of Moulding Sand					8

2.2.1	Silica sand grains							8

2.2.1.1 Rounded grains						8

2.2.1.2 Sub angular grains						9

2.2.1.3 Angular grains							9

2.2.1.4 Compounded grains						9

2.2.2	Bonding clay								9

2.2.3	Moisture								10

2.3	Additive to Moulding and Core Sand						11

2.4	Classification of Moulding Sands						12

2.4.1	Natural moulding sand						12

2.4.2	High silica sand							13

CHAPTER THREE

3.0	MATERIALS AND METHOD

3.1	Collections and Preparation of Materials					14

3.1.1	Silica Sand								14

3.1.2	Preparation of the Standard Test Specimens				14

3.2 	Methods

3.2.1 	Analysis of the sand chemical compositions 				15

3.2.2 	Physico-mechanical properties					15

3.2.3 	Sieve analysis / Grain fineness number determination 		15

3.2.4 	Moisture content 							16

3.2.5 	Permeability								17

3.2.6 	Specific gravity 							18

3.2.7	Sand strengths 							18

3.2.8	Refractoriness								19

3.2.9 	Shatter index								20

3.2.10 	Clay content								20

CHAPTER FOUR

4.0	RESULTS AND DISCUSSIONS

4.1	Results										21

4.2	Discussions									25

4.2.1 	Chemical Compositions of Budo-Egba Moulding Sand 		25

4.2.2 	Sieve analysis / Grain size distribution and Grain fineness number (GFN) of Budo-Egba Moulding Sand 				25

4.2.3 	Moisture content 							27

4.2.4 	Specific gravity							27

4.2.5 	Bulk density								28

4.2.6 	Permeability								28

4.2.7 	Flowability								28

4.2.8 	Green compressive strength 						29

4.2.9 	Dry compressive strength						29

4.2.10 	Clay content								30

4.2.11 	Shatter index								30

4.2.12 	Refractoriness								31

4.3 	Evaluation of the Selected Budo-Egba Natural Moulding Sand  		31

CHAPTER FIVE

5.0	CONCLUSIONS AND RECOMMENDATIONS

5.1	Conclusions 									33

5.2	Recommendations								34

REFERENCES 								35

LIST OF TABLES

Table 2.1:	Special additions to moulding mixture				11

Table 4.1:	Elemental Composition of Budo-Egba Moulding Sand 		21

Table 4.2: 	Sieve Analysis of Budo-Egba Moulding Sand 			22

Table 4.3: 	Physico-Mechanical Properties of Budo-Egba Moulding Sand 	23

Table 4.4:	Physico-Mechanical Properties of the Sand against recommended/standard values					24

CHAPTER ONE

INTRODUCTION

1.1	Background of the Study

Sand is the principal basic moulding materials used by the foundry-man, whether it is for iron, steel, non-ferrous or light-alloy castings. The study of foundry sand constitutes one of the main section of foundry technology and sand testing has becomes an essential part of the day-to-day control of foundry operation.

Moulding sand is commonly used to cast both ferrous and non-ferrous metals because of its ability to withstand the temperature of the molten metal, absorb and transmit heat, and has good permeability to allow gasses generated during casting to escape without causing casting defects (Ademoh and Ahmed, 2008). The use of sand as a moulding medium is determined by the type of metal being cast, economics, casting quality required, and the degree of consistency desired in the final products (Mshelia et al., 2016). The major constituents of moulding sands include silica sand, clay and moisture. Each of the constituents is important in determining the characteristics of moulding sand (Nigerian Foundries Limited, 1995). Clay is responsible for bonding; moisture content determines the plasticity of the moulding sand (Steve, 1996), while silica sand impacts refractoriness, chemical resistivity and permeability (Scaffer and James, 1995; Sarka, 1967).

Silica sand is specified according to its average size and shape (Aribo, 2011). The higher the sand grain fineness, the higher the cohesiveness, and the lower the permeability of the sand (Aribo et al., 2009). Clay is made up of two ingredients: fine silt and true clay. Fine silt is a kind of foreign matter in clay deposit and possesses no bonding power. True clay provides the necessary bonding action which it acquires in the presence of an appropriate amount of moisture (Atanda et al., 2012; Mechanicalinfo, 2019). However, as the quantity of the clay increases, the permeability of the moulding sand decreases (Atanda et al., 2012).

Moulding sand is classified as natural (green sand) and synthetic sand. Natural moulding sand is taken from the river bed or dug out from pits. Synthetic moulding sand, on the other hand, is made in the foundry by mixing a relatively clay free sand with selected clay binder like bentonite (Atanda et al., 2012). Water and other additives may be added as may be required. Virtually all moulding sand for ferrous castings is of the green sand type (Deepak, 2008). A green sand mould refers to the fact that the mould will contain moisture during the pouring of the molten metal (Desai et al., 2016).

Sand casting which is perhaps the most versatile of the casting methods can be used for casting various articles ranging from very small size to extremely large size (Ibitoye, 2005). It is used to cast several engine components such as engine blocks, machine tool bed, cylinder heads, piston rings, wheels, pump housings, water supply pipes, mill rolls, valves etc. However, in order to produce good quality casting, the properties of the moulding sand must be at the optimum level (Mahesh et al., 2008). Research has shown that the quality of the casting is largely affected by moulding sand properties (Dhruval et al., 2015; Mishra, 2017; Saikaew and Wiengwiset, 2012), such as cohesiveness, green compressive strength, dry strength, permeability, mould hardness, compatibility and shatter index. All these properties invariably depend on such parameters as the quality of binder used, amount of water and sand grain size (AFS, 1963; Loto and Omotoso, 1999; Ayoola et al., 2010).

During the past four decades, the industry has undergone a period of remarkable progress and transition. In this brief span, the number of iron foundries has been cut nearly in half, primarily as a result of the increasing capital requirements necessary to remain competitive while maintaining to meet safety and pollution control regulation and increasing customer requirement for quality. Moreso, with the increasing technological development around the world, one would definitely agree that there is need to introduce a new dimension to the quality and standard of the foundry products obtained in the country, given that the economic development in any country is a function of its technological development. However, many researchers had done quite a number of works on how to modify or rather, to improve the quality of the moulding sand employed as moulding materials. The dividend of their research work is what we are enjoying nowadays, that is, development in technology.

Besides, it is obvious that more than 75 percent of the materials employed to achieve the so-called technological advancement is constituted by casting. In other words, technological development that has become an object of concern around the world cannot be treated in isolation without considering the quality and standard of casting. A thorough analysis had revealed that most defects embedded in casting are as a result of sub-standard quality of moulding sand employed during production process. Having considered the fact that the level of technological development obtainable in a country will be drastically affected if the materials employed are characterized by defects so, the need to evaluate the silica sand at Budo-Egba in Asa Local Government, Kwara State to ascertain or rather to establish the various foundry properties contained in the silica sand and to specify whether they are suited for the casting processes with their various mechanical properties and defects after casting is necessary.

1.2	Statement of the Problem

There are many known silica sand deposits lying un-useful for their purposes, so there is need to characterize the silica sand at Budo-Egba in Asa Local Government, Kwara State to ascertain or rather to establish the various foundry properties contained in the silica sand and to specify whether it’s suited for the casting processes with its various mechanical properties and defects after casting is necessary.

1.3	Significant of the Study

The study will enhance to a great extent the technological and economic development of the nation at large when the casting produced is of good standard and quality. The study will also increase the industries in the country because it will afford the industrialist or rather; the investors the opportunity to have a good knowledge of the available raw materials in the country and for what application they can be employed.

1.4	Aim and Objectives of the Project

The aim of this project work is to characterize the silica sand at Budo-Egba in Asa Local Government in Kwara Central of Kwara State and to establish the various foundry properties embedded in the sand.

The objectives of the study are as follows:

- Analyze the sand chemical compositions

- Carry out the sieve analysis of the silica sand

- Characterize and determine the mechanical foundry properties of the silica sand at Budo-Egba in Asa Local Government Area of Kwara State.

- Compare the values obtained for the mechanical properties with recommended /standard values.

1.5	Scope of the Study

This study will based on the characterization of the foundry properties of silica sand at Budo-Egba in Asa Kwara Central of Kwara State. Various foundry properties such as green strength, permeability, refractoriness, moisture content and clay content shall be carried out on this sand. It is highly imperative to note that there is no available equipment to measure refractoriness directly, so the refractoriness of this sand will be estimated based on the clay content present in the silica sand.

CHAPTER TWO

2.0	LITERATURE REVIEW

The process by which casting are made involves melting of metal by melting furnace appliance, poured the molten metal into a pre-shaped mould cavity created by pattern in conformity with desired components and allowed it to solidify before it’s shake out of the mould and thereafter settling operation is being carried out on the produced cast. The mould reproduces the shape of a pattern and a cheap and reliable material for making the mould is a plastic mixture consisting of bounded with moist clay. The mixture is weak enough to flow and be packed tightly around the pattern, strong enough to retain its shape during withdrawal of the pattern and pouring of the metal, and dry enough to avoid explosive formation of steam. Since the sand is used in this moist form immediately after stripping from the pattern it is termed ‘green’. This sand moulding process is suitable for the production of iron, steel, aluminum and copper based alloy castings.

According to Bcira (1985), green sand moulding is still the main moulding process used in more than 80 percent of U.K. foundries despite all the competition from chemical binder such as resin and silicates. Clay bounded sands have been largely replaced by chemical moulding systems for large, heavy casting, where the benefits are:

- High production rate

- Fast turn: round of pattern and moulding boxes

- Elimination of drying stove.

- Reduces handling

- Less floor spaces

- Improved dimensional accuracy

Greensand predominates for smaller castings, and is still widely used for medium - weight castings. Synthetic greensands, made from silica sand with added clay and coal dust, are used in the majority of medium to large foundries. Many small iron foundries and non-ferrous foundries still rely on natural clay bounded sands.

2.1	Moulding Sands

Sand is the principal moulding material in the foundry shop where it is used for all types of casting, irrespective of whether the cast metal is ferrous or non-ferrous, iron or steel. This is because it possesses the properties vital for foundry purposes. The most important characteristics of sand are its refractory nature, it can easily withstand the high temperature of molten metal and loss not get fuse. Secondly, moulding sand has chemical resistivity; it does not chemically react or combine with molten metal and can therefore be used time and again. Thirdly, sand has a high degree of permeability; it allows gases and air to escape from the mould when molten metal is poured on without interfering with the rigidity and strength of the mould. The degree of strength, hardness and permeability can also be adjusted, as desired, by varying the composition or the ingredients of the sand. Such flexibility is extremely difficult to achieve with any other moulding material. But the properties vary from one sand to another, and it should be noted that only those sands characterized by the foregoing features are considered for moulding work.

2.2	Principal Ingredient of Moulding Sand

The principal ingredients of moulding sand are:

- Silica sand grains.

- Clay

- Moisture

2.2.1	Silica sand grains

Sand grains are of paramount importance in moulding sand because they impart refractoriness, chemical resistivity and permeability to the sand. They are specified according to their average size and shape. The finer the grains, the more intimate will be the contact and lower the permeability. However, fine grains tends to fortify the mould and lessen its tendency to get distorted. The shapes or the grains may vary from round to angular. The grains are classified according to their shape.

2.2.1.1 Rounded grains

These grains have the least contact with one another in a rammed structure, thereby making the sand highly permeable to gases. Sand having rounded grains however, lack strength and do not pack up to the optimum extent states (Jain, 1986). The binder requirements are minimum.

2.2.1.2 Sub angular grains

These grains have comparatively lower permeability and greater strength than the rounded ones.

2.2.1.3 Angular grains

These grains have defined edges and the surfaces area nearly flat. They produce higher strength and lower permeability in the mould than sub-angular grains. The binder consumption is likely to be high.

2.2.1.4 Compounded grains

In some cases, the grains are cemented together such that they fail to separate when screened. They consist of rounded, sub-angular or angular grains or a combination of the three. Such grains are called compounded grains and are least desirable due to their tendency to breakdown at high temperature. According to (Jain, 1986), in practice, sand grains contain mixed grain shapes, depending on origin. A sub-angular to rounded grain mixture would be the best combination.

2.2.2	Bonding clay

Clay is natural mineral found in many parts of the world, several different types of clay mineral exist but they are all hydrous alumina silicates. They are very finely grained material, which absorb water and become plastic, but on drying become rigid and strong. Their properties provide cohesion and plasticity in green state and high strength when dried. Clay are resistant to moderate heat, and the plasticity and strength properties can be subsequently restored by the addition of further water. Since clay bonded sands are easily regenerated and recycled, they are economical for foundry use.

Murray (1986), classified clay mineral most widely used as binder as:

- Kaolinites (Al2O3.2SiO2.2H2O)

- Illites [(K2Al4CSi8. Alx). (O2COH)4]

- Montimorillonites (Al2O3.4SiO2.H2O + nH2O).

2.2.3	Moisture

The moisture content of moulding sand is the most important variable, as on this all other properties depend. Temper water act as an activator. Stefanesai (1992), noted that clay however, would not function as a binder unless activated by temporary water, which result in strength development, which is an important property of moulding sand.

According to Asuquo and Bobojama (1991), moisture content of moulding sand is considered as the amount of free or mechanical water available in the sand. The moisture content of moulding sand normally varies between 4 and 8 percent. This is liable to change, and must therefore be checked frequently. It is not practicable to work at peak green strength and the moisture content is normally in a specific range. Anon (1982), also reported that too much water in green sand can lead to formation of gas cavities in the casting. Grim and Gutherbert (1945), states that, dry strength will continue to increase with water for different bentonite content. This is a result of their research study on clay - water system relationship.

2.3	Additive to Moulding and Core Sand

Materials other than sand, clay and water added to foundry sand are called additives. They are also referred to as auxiliary moulding materials. They are introduced into moulding and core sands to improve their properties such as gas permeability, refractoriness, yield ability, collapsibility etc. (Nwajagwu, 1994). Table 2.1 represent the classification of special addition to moulding mixture. They are usually between 0.5 and 12% by weight of synthetic moulding sands. Modern foundry-men use additive for variety of reasons such as:

a.	Improve sand properties

b.	Improve surface finish of castings

c.	To reduce expansion defects such as scabs and buckles

d.	To make shake-out easier.

Table 2.1: Special additions to moulding mixture

| Purpose of addition | Substance |
| --- | --- |
| Enhance of bench life and resistance to drying out. Hot strength development Surface finish and resistance to metal penetration Inhibition to metal-mould reaction | Molasses, sulphite, cereals, ethylene glycol iron oxide, silica flour sulphur, boric acids, ammonium biflouride cereals, saw dust, wood flour |

(Beeley, 1972).

2.4	Classification of Moulding Sands

Moulding sand according to Jain (1986), can be classified into four different types, these are;

- Natural moulding sands

- High silica sands

- Special sands

- Bonding clays

2.4.1	Natural moulding sand

These sand occurs as deposit in various part of the country, they possess an appreciate amount of clay which acts as bond between the sand grains. The quantity and type of clay mineral present affect the strength, toughness and refractoriness of the sand. The clay may belong to different mineralogical group such as kaolinite, montmorillonite, halloysite, dickite and nacrite. The other minerals present as contain namely; feldspar, Fe2O3 MgO, K2O and Na2O lowers the refractoriness.

Crushing and milling soft yellow sandstone carboniferous rocks e.t.c. during the milling operation obtain natural moulding sand, clay aggregates breakdown and clay particle get uniformly distributed over the sand grains (Jain, 1986). These sand usually have clay bond in excess of the minimum needed for developing necessary strength in the sand mixture. To get desired properties, crude silica sands such as those obtained from river bank and domes, which are relatively free of clay, are mixed with natural sands. By virtue of their ease of availability and low cost, natural moulding sand are used for most of the casting of both ferrous and non-ferrous metals. Table 2.2 represent the various grades of sands that satisfied the requirement for natural moulding sand. The grain shape of these sands is required to be sub-angular to round. Natural moulding sand possess high flexibility of operation unlike synthetic sands, here accurate adjustment of moisture is not required and the range of permissible moisture is high. These sands are therefore suitable for hard moulding, particularly for high casting that use dry sand for moulding.

2.4.2	High silica sand

These sands contain less than 2% of clay, alkalis and mineral. They occur as house or purely consolidated deposits of sedimentary origin dune blown inland from the coast, or accumulated deposits in estuaries and rivers along the coast. They are produced by first crushing quartette sand stones of open texture, and then washing and grading these to yield a sand grade of requisite shape and grain distribution.

Table 2.3 shows the requirement of high silica sand for use in foundries and can be classified into three grades according to the silica content. The clay content of high silica sand should not be more than 2%.

CHAPTER THREE

MATERIALS AND METHOD

3.1	Collections and Preparation of Materials

3.1.1	Silica Sand

The silica sand used in this project was obtained from three different points, tagged A, B, and C (5km apart) within the vast deposit at Budo-Egba in Asa Local Government of Kwara State.

3.1.2	Preparation of the Standard Test Specimens

The AFS cylindrical test specimen was prepared using the metric standard rammer. The AFS cylindrical test piece of 50.8mm diameter x 2mm was made by dropping 6.356kg weight three times through a height 50.8mm onto the measured quantity of sand. 150g of the prepared sand was weight out and placed in a 127mm height special tube with an internal diameter of 50.8mm, the base of which have been sealed by a suitable metal cup. The weight on the rammer was raised by means of the handle provided on the side of the equipment. The specimen tube and the cup were then placed under the ramming head with the centralizing peg on the metal plug located in the hole of the base plate. The rammer head and weight was lowered until they were supported by the sand in the container. Rotating handle attached to the apparatus was allowed to fall freely through a 50.8mm height determined by the cam on the equipment raised the rammer weight. This operation was repeated twice to ram three times for the silica sand. The specimen was removed from the rammer by raising the weight.

3.2 	Methods

3.2.1 	Analysis of the sand chemical compositions

The chemical composition analysis of the silica sand was carried out using the X-Ray Fluorescence (XRF) Analyser at Materials Testing Laboratory, Federal University of Technology, Akure, Nigeria in line with the practice of Patrick et al. (2019). Three (3) grams of the sand sample was measured, put in a sample holder and placed inside the X-ray chamber. The setting of the oxide analyses was carried out. After 100 seconds, the result was displayed on the monitor connected to the XRF.

3.2.2 	Physico-mechanical properties

In order to determine the suitability or otherwise of the silica sand for the casting process, various physico-mechanical properties tests were carried out. The properties that were tested include the grain fineness number, permeability, refractoriness, green compressive strength, bulk density, dry compressive strength, specific gravity, moisture content, clay content and flowability. These tests were carried out at Soil Testing Laboratory, Department of Civil Engineering, Federal University of Technology, Akure, Nigeria. The procedures that were used is in accordance with the American Foundry-men Society (AFS), ASTM and British standards for the determination of these properties as stipulated in technical literatures.

3.2.3 	Sieve analysis / Grain fineness number determination

The silica sands were prepared by washing, drying and picking and sorting processes to remove debris and other unwanted materials from the sand. The weight of the dried cleaned sand sample was determined and recorded. The British standard set of sieves was cleaned, and the weight of each sieve in the set was determined with the use of electronic weighing balance and was recorded along with the bottom pan used. The sieves were then assembled in ascending order of sieve numbers (8, 10, 16, 22, 60, 100, 150 and 200) with the pan placed at the bottom. The sand sample was then carefully poured into the top sieve and covered with the cap. Subsequently, the sieve stack was then placed on the mechanical shaker (Endvolts sieve shaker, volts/220/240, single phase; Ridsdale & Co. Ltd made) and shake for 15 minutes. The stack was removed from the shaker and carefully weighed; the weight of each sieve was recorded with its retained sand. The weight of the bottom pan was also determined and recorded also with its retained fine sand. The grain fineness number was then calculated.

Grain fineness number= Total productTotal % retained by difference sieves

3.2.4 	Moisture content

Three (3) aluminium cans were cleaned, dried and weighed with lid as W1. Silica sand sample was filled into each of the three dried cans. The cans were filled with sand covered with lid, weighed and recorded as W2. Each of the can was then opened with the lid placed beneath them and placed in the oven. The sand was allowed to dry for 24 hours in the oven at 1100C. Each of the cans was brought out from the oven with the dried sand in them, weighed on the electronic weighing balance and recorded as W3. The moisture content was calculated.

Moisture content= W2-W3W3-W1 ×100%

Where	W1 = weight of empty can, W2 = weight of drying can + wet sand and W1 = weight of drying can + dry sand.

3.2.5 	Permeability

The sand sample was filled into a cylindrically shaped mould of 8.50cm diameter and height of 12.73 cm. The filter paper was placed at both ends of the specimen and then centrally placed over the bottom saturated porous stone of the drainage base fixed to the mould. The annular space between the mould and soil specimen was filled with impervious material (gravel) to avoid any leakage from the sides. The drainage cap was then fixed over the top of the mould. The water storage was connected with the outlet of the bottom drainage base plate of the mould and the water was allowed to flow in. The whole water was saturated and 1.00 cm depth of free water was allowed to stand on the top of the sample. The flow was allowed in the specimen for 24 hours. After which the water reservoir was disconnected from the outlet at the bottom and connected to the inlet at the top plate. The stop cock at the top plate was opened and water was allowed to pass through it to remove all the air in the cylinder. The stop clock was closed after all the air has escaped. The outlet at the bottom plate was then opened and the water allowed to flow through the soil in order to establish a steady flow. The water was collected in a graduated measuring flask for 2 minutes time interval. The collection of the water was repeated thrice and the times were noted and recorded.

The permeability was then calculated using the relation below

Permeability K= 2.30 α.LA.tlogh1h2

Where: K = coefficient of permeability at T0C (cm/sec), L = length of soil specimen (cm), h1 = initial head of water at time t1 in the pipe above the outlet (cm), h2 = final head of water at time t2 in the pipe above the outlet (cm), a = cross sectional area of stand pipe (cm2), A = cross sectional area of the soil specimen (cm2) and t = (t1 – t2) time interval (sec) for the head to fall from h1 to h2.

3.2.6 	Specific gravity

The density bottle was washed, dried, cleaned, weighed and recorded as m1. The soil sample was placed in the density bottle with stopper, weighed and recorded as m2. Air free water was added to cover the soil in the bottle. This was placed without the stopper in the vacuum desiccators. The pressure was reduced to about 25 Kilopascals. The bottle was left for 1 hour. The vacuum was released and the desiccator lid was then removed. The soil in the bottle was stirred. The soil particle was washed off before the stirring rod was removed. The lid of the desiccators was replaced and the vacuum procedure was repeated until there was no more air evolved from the soil. The specific gravity was then determined using equation below.

Specific gravity= m2- m1m4-m1- (m4- m2)

Where: m1 = mass of empty bottle; m2 = mass of bottle with sand sample, m3 = mass of sand sample with water and bottle; m4 = mass of bottle filled with water

3.2.7	Sand strengths

(a) 	Green compressive strength

In determining the silica sand green compressive strength, the sand was filled into a standard mould of 50 mm in diameter and 100 mm in length and compacted using sand compaction machine where a 6.6 kg load was dropped 50 times at both ends of the mould. Thereafter the sand in the mould was removed with the use of hydraulic jack placed at the bottom of the mould. This process was repeated nine times to produce nine specimens from the sand sample. Three out of the moulded sand (3 specimens) were placed in the sand compressive strength testing machine, where they were subjected to varying degree of load to determine the maximum amount of load they can withstand before the sand collapsed. The readings on the machine indicator at different load was then recorded to calculate the green compressive strength using equation below.

Green compressive strength= DGR ×0.025Area

Where DGR means ―Dial Gauge Reading

(b) 	Shear strength and dry compressive strength

The shear strength was determined by filling the shear strength machine mould with the sand sample and thereafter the mould was placed in the sand shear strength testing machine and subjected to different loading and the corresponding deflections on the machine scale was recorded for each of the load for the calculation of the shear strength. The shear strength and the dry compressive strength was calculated using equation below.

Shear Strength= DGR ×0.0009Area

Dry compressive strength = Shear strength – Green strength

3.2.8	Refractoriness

Three specimens of the silica sand as described in the green compressive strength procedure was placed in a furnace, the temperature of the furnace was set to 9500C and this temperature was maintained for 3 hours. The silica sands was brought out of the furnace to determine any defect or otherwise in the sand appearances and sizes.

3.2.9 	Shatter index

Three specimens out of the prepared silica sand specimens produced were used for the shatter index test. The shatter index value of the silica sand was determined by allowing the compacted silica sand specimen to fall freely from a height of 1.83 meters unto a steel anvil. The degree of disintegration of each specimen was measured by weighing the specimen before falling (W1) and weighing the bigger piece among the disintegrated specimen after fall (W2), from which the toughness or plasticity of the sand was determined using equation below.

Shatter index= W1-W2W2 ×100%

3.2.10 	Clay content

A measuring cylinder of 1000 ml capacity was filled with an iodine salt of 50g and water was added to fill the cylinder to 300ml. Thereafter, the sand sample of 200g was added into the cylinder. This mixture was left in the cylinder for 2 hours. The mixture was then form three layers in the measuring cylinder. These layers were water which is at the top level (V1), followed by the silt (V2), and the silicate sand at the bottom (V3). Thus, the clay content was calculated between these layers using equation below.

Clay Contents= V3-V2V1

CHAPTER FOUR

RESULTS AND DISCUSSIONS

4.1	Results

The results obtained during the sand test were recorded and were as subsequently presented in the tables 4.1, 4.2, 4.3 and 4.4 in which tables 4.2 and 4.3 represent the result of the elemental composition of Budo-Egba moulding sand and sieve analysis of Budo-Egba natural moulding sand, while tables 4.3 and 4.4 represent physico-mechanical properties of Budo-Egba moulding sand and physico-mechanical properties of Budo-Egba moulding sand against recommended/standard values.

Table 4.1: Elemental Composition of Budo-Egba Moulding Sand

| S/N | Constituents | Weight (%) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | A | B | C | Average Value |
| 1. | SiO2 | 91.80 | 91.70 | 91.90 | 91.80 |
| 2. | Al2O3 | 4.90 | 5.10 | 5.00 | 5.00 |
| 3. | CaO | 0.01 | 0.01 | 0.01 | 0.01 |
| 4. | MgO | 0.065 | 0.067 | 0.066 | 0.066 |
| 5. | Na2O | 0.77 | 0.79 | 0.78 | 0.78 |
| 6. | Fe2O3 | 0.029 | 0.031 | 0.030 | 0.030 |
| 7. | K2O | 0.386 | 0.387 | 0.385 | 0.386 |
| 8. | MnO | 0.005 | 0.005 | 0.005 | 0.005 |
| 9. | ZnO | 0.300 | 0.300 | 0.300 | 0.300 |

Table 4.2: 	Sieve Analysis of Budo-Egba Moulding Sand

| S/N | Mesh (N) | Sieve diameter (micron) | Wt of sieve pan (g) | Wt of pan and retained sand (g) | Wt of retained sand (g) | % wt of retained sand (g) | Product (g) [% Wt of retained sand x sieve No] | Cumulative |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 12 | 1400 | 312.881 | 313.012 | 0.131 | 0.042 | - | - |
| 2 | 16 | 1000 | 299.931 | 300.003 | 0.072 | 0.024 | 0.288 | 0.066 |
| 3 | 22 | 710 | 287.070 | 287.429 | 0.359 | 0.125 | 2.000 | 0.191 |
| 4 | 30 | 500 | 259.858 | 267.935 | 8.077 | 3.108 | 68.376 | 3.299 |
| 5 | 44 | 355 | 241.321 | 260.277 | 18.956 | 7.855 | 235.650 | 11.154 |
| 6 | 60 | 250 | 233.595 | 253.248 | 19.653 | 8.413 | 358.292 | 19.567 |
| 7 | 85 | 180 | 225.282 | 249.647 | 24.365 | 10.815 | 648.900 | 30.382 |
| 8 | 120 | 125 | 213.470 | 239.823 | 26.353 | 12.345 | 1049.325 | 42.727 |
| 9 | 170 | 90 | 211.693 | 220.345 | 8.652 | 4.087 | 490.440 | 46.814 |
| 10 | 240 | 63 | 208.904 | 211.434 | 2.530 | 1.211 | 205.870 | 48.025 |
| 11 | 350 | 45 | 210.610 | 211.343 | 0.733 | 0.348 | 83.520 | 48.373 |
| 12 | 350 | - | 196.147 | 196.643 | 0.496 | 0.253 | 88.550 | 48.626 |
|  |  |  |  |  |  | 48.626 | 3231.211 |  |

AFS =

AFS = 66.45

AFS grain fineness number is 66.5

Table 4.3: Physico-Mechanical Properties of Budo-Egba Moulding Sand

| S/N | Parameters | Sample A | Sample B | Sample C | Average Value |
| --- | --- | --- | --- | --- | --- |
| 1. | Colour | Reddish brown | Reddish brown | Reddish brown | Reddish brown |
| 2. | Moisture content (%) | 7.64 | 7.65 | 7.66 | 7.65 |
| 3. | Specific Gravity | 2.65 | 2.65 | 2.65. | 2.65 |
| 4. | Bulk Density (Kg/m3) | 1650.5 | 1650.7 | 1650.9 | 1650.7 |
| 5. | Permeability (cm/sec) | 0.10 | 0.11 | 0.12 | 0.11 |
| 6. | Flowability (%) | 65.71 | 66.70 | 65.63 | 66.01 |
| 7. | Grain Fineness number | 66.6 | 66.4 | 66.5 | 66.5 |
| 8. | Green Compressive Strength (KN/m2) | 51.3 | 51.4 | 51.5 | 51.4 |
| 9. | Dry Compressive Strength (KN/m2) | 209.9 | 210.1 | 210.0 | 210.0 |
| 10. | Clay Content (%) | 10.2 | 10.1 | 10.0 | 10.1 |
| 11. | Shatter Index (%) | 21.3 | 21.2 | 21.1 | 21.2 |
| 12. | Refractoriness (0C) | >900 | >900 | >900 | >900 |

Table 4.4:	Physico-Mechanical Properties of the Sand against recommended/standard values

| S/N | Parameters | Average obtained Value | Recommended Standard Value |
| --- | --- | --- | --- |
| 1. | Moisture content | 7.65% | 5 – 8% (for the casting of Aluminium, brass and bronze, malleable iron and medium grey iron) (Burns, 1989; Mshelia et al, 2016) |
| 2. | Specific Gravity | 2.65 | 2.6 – 2.8 (Technology, 2016) |
| 3. | Bulk density | 1650.7Kg/m3 | 1100Kg/m3 to 1800Kg/m3 as AFS standard for sand casting process |
| 4. | Permeability | 0.11cm/sec | 0.001cm/sec and above (Technology, 2016) |
| 5. | Flowability | 66.01% | 65% for casting of Aluminum (Burns, 1989) |
| 6. | Grain Fineness Number | 66.5 | 36 – 90 for non-ferrous metals (Burns, 1986; Mshela et al, 2016). |
| 7. | Green Compressive Strength | 51.4KN/m2 | 50-70KN/m2 and above for the casting of Aluminum, brass and bronze, light grey iron and malleable iron (Burns, 1989; Mshelia et al, 2016). |
| 8. | Dry Compressive Strength | 210.0KN/m2 | 200-500KN/m2 for casting of Aluminum, brass and bronze and light grey iron (Burns, 1989; Mshelia et al, 2016) |
| 9. | Clay Content | 10.1% | 10 – 12% for the casting of Aluminum, brass and bronze, light grey iron, malleable iron, heavy steel, light steel and heavy grey steel (Burns, 1989; Mshelia et al, 2016) |
| 10. | Shatter Index | 21.2% | 12% and above (Mshelia et al, 2016) |
| 11. | Refracttoriness | >9000C | 11000C and above (Mshelia et al, 2016) |

4.2	Discussions

4.2.1 	Chemical Compositions of Budo-Egba Moulding Sand

The chemical constituents of the sand samples are as presented in Table 4.1, Silica (SiO2) constitutes the main element in the sand, with an average value of 91.80% by weight, followed by Alumina (Al2O3) which constituted 5.00% on average value. Thus, the sand belongs to Alumina-silicate group of sand. Most foundry sands for metal casting are highly quality silica with physical characteristics (Shuaib-Babata et al., 2017c). Other elements present in the sand include CaO, MgO, Na2O, Fe2O3, K2O, MnO, and ZnO in smaller proportions as recommended (Jimoh et al., 2015). The sand contained no amount of CaO and ZnO which are one of the significant constituents of the clay content in the sand (Jimoh et al., 2015). However, this may have little effect on the strength of the sand because clay serves as a binder which holds the grains of the sand together. This deficiency can be eliminated through the addition of a binder (Mshelia et al., 2016). Information on the sand chemical composition is important as it relates directly to the metal moulded at the foundry (Akinyele and Oyeyemi, 2014).

4.2.2 	Sieve analysis / Grain size distribution and Grain fineness number (GFN) of Budo-Egba Moulding Sand

The average results of the moulding sand’s grain size distributions and AFN grain fineness number are as shown in Table 4.2. In sand, the characteristics shape of a sand grain is an important factor (Shuaib-Babata and Olumodeji, 2014). Many of the sand’s properties are affected by the grain size distribution (Richard, 2003).

The results in Table 4.2 revealed high concentrated grain retained of the sand (88.6%) between sieve size BS No.100 and 150 (0.15 and 0.075 mm). This shows that the sand had a high concentration of fine structure. Fine surface finish casting is enhanced by highly concentrated small grain structure of sand (Mikhailov, 1989; Adesina, 2010). In natural sand, particle distribution and the sand’s shape allow good permeability and strength (Ihom et al., 2011; Turkeli, 2017). The sand’s GFN was averagely 66.5 which fell within the specified standard values (36 – 90) for non-ferrous metals (Burns, 1986; Mshela et al., 2016). The sand’s average grain size will be approximately 195 μm, which are useful parameters with AFN, as the choice of sand should be based on particle size distribution (Burns, 2000). The size distribution has effects on the quality of the castings. However, the sand has higher compatibility level, since the finer the grains of sand, the higher its level of compatibility and vice-versa (Donald, 2010), which results to good surface finishing.

Sand with higher grains fineness number has the tendency to produce a very good surface finish cast product, with low binders (Tuncer, 2017). GFN serves as a guide to determine the quantity of binding materials required to produce desirable properties in new foundry sand (Shuaib-Babata and Olumodeji, 2014). The grain fineness number also affects the permeability of the sand (Mshela et al., 2016). Fine-grained sands yield better surface finish but need higher binder content (Burns, 2000).

4.2.3 	Moisture content

The importance of moisture content on the moulding sand and subsequently on the casting quality cannot be underestimated. Moisture test determined the dampness of the mould. The sand has an average moisture content of 7.65%, this falls in the range of (4 – 8%) which is the recommended standard suitable for casting of light steel, heavy grey steel and medium grey iron (Burns, 1989; Mikhailov, 1989). By establishing the percentage of moisture content of the natural moulding sand, it will help in controlling the amount of water that can be added during the process of mould making (Oke and Omidiji, 2016). If the proper amount of moisture in the sand is not achieved, it can lead to some defects such as scabs and blow holes and it will also affect the strength properties of the moulding sand (Mshelia et al., 2016).

4.2.4 	Specific gravity

The average specific gravity of the sand was discovered to be 2.65 which fall between the 2.5 – 2.8 acceptable ASTM standard (D854) for foundry sand with clay (5%) and foundry sand without clay. Foundry sand with lower specific gravity has been discovered to contain more impurities and inorganic materials that could fuse during molten metal pouring process which might lead to casting defect (Bala and Olabisi, 2017). The sand has a high specific gravity which signifies that the level of impurities in the sand is quite low and thus will not fuse with the cast at a higher temperature (Jimoh et al., 2015).

4.2.5 	Bulk density

The average bulk density was found to be approximately 1650.7Kg/m3 which fall within the AFS standard of 1100 Kg/m3 to 1800 Kg/m3 for sand casting process (Bala and Olabisi, 2017). The bulk density has been discovered to be increasing with increasing moisture content. At very high moisture content, the highest bulk density can be obtained when the sand is adequately rammed to drive off all the air in the mould (Mshelia et al., 2016).

4.2.6 	Permeability

The sand has a permeability of approximately 0.11 cm/sec which is within the standard of 10-3cm/sec and above for foundry sand (Technology, 2016). Although the sand has fine grains low clay content in the sand can also be attributed to high permeability exhibited by the sand (Mshelia et al., 2016). However, it has been established that the finer the sand grains, the lower the permeability and vice versa. Lower permeability can be attributed to one of the major cause of porosity defect in the casting process. Hence it is an important factor that can influence the property of moulding sand and the property of the cast (Jimoh et al., 2015).

4.2.7 	Flowability

The average flowability of the sand is 66.01%. The value is within the standard value of flowability for moulding sand by AFS which is 65% and above (Burns, 1989; Shuaib-Babata et al., 2017c). This can be attributed to higher SiO2 in the sand. Flowability of the sand increases with a decrease in the green strength and vice versa. It also increases with the decrease in grain size of sand (ME Mechanical Team, 2016). This also corresponds to the sand has a higher grain fineness number which shows a decrease in the grain size particles. Flowability is also influenced by clay content and moisture content (Desai et al., 2016).

4.2.8 	Green compressive strength

The average Green compressive strength of the sand was 51.4KN/m2 which is within the recommended standard (50–70 KN/m2) for non-ferrous metals (Mshelia et al., 2016). However, this strength can be improved upon with the addition of binders and some other additives such as clay, bentonite, corn flour and others so that its strength and toughness can be increased and thus enhanced the handling and making of the mould (ME Mechanical Team, 2016). The strength of the sand is also the compression strength that allows it to hold geometric shapes and grains together under the conditions of stresses that will be imposed on it during the sand casting process. Thus, this result shows that the sand is suitable for casting aluminium and other non-ferrous metals.

4.2.9 	Dry compressive strength

The average dry compressive strength of the sand was found to be 210KN/m2. This is quite lower in comparison with the standard value (200-550 KN/m2) (Mshelia et al., 2016). Thus, the sand does not have sufficient strength in its dry form i.e. it will lack appropriate strength in its dry form. The low dry compressive strength is due to the low clay content in the sand as the clay content was found to be 10%. However, this value can be improved with the addition of binder and some other additives such as clay, bentonite, corn flour and others.

4.2.10 	Clay content

The average clay content of the sand was found to be 10.1% which is in agreement with the standard recommended value (10-12%) (Mshelia et al., 2016). The low clay content in the sand has both advantages and disadvantages. Part of the advantages is that it gives the sand high permeability and thus, minimise the probability of porosity defect in the final cast. On the other hand, the moulding sand will have low compaction strength, which has reflected in the sand’s strength (51.4KN/m2). Another disadvantage is that the sand may not be used for casting of objects with intricate shapes but for simple objects such as round bar, rectangular bar and so on (Mshelia et al., 2016). However, these disadvantages can be adequately taken care of by simple addition of binder which includes natural clay, bentonite and other additives to impart adequate compaction strength to the sand (ME Mechanical Team, 2016).

4.2.11 	Shatter index

The average shatter index of the sand was found to be 21.2% which is within the AFS standard requirement (Mshelia et al, 2016). This indicated that the sand sample after compaction lacks sufficient toughness to help satisfactory lift during the withdrawal of the pattern (Jimoh et al., 2015). This high shatter index also indicates that the sand has high collapsibility which is more desired after the withdrawal of the cast from the mould (Sheidi and Ajuwa, 2008). However, high shatter index can be attributed to the low clay content in the sand which will bond the sand grains together and prevent them from easily broken into pieces (ME Mechanical Team, 2016). The shatter index can be improved with the addition of a binder.

4.2.12 	Refractoriness

After the sand was subjected to a temperature above 9000C inside the furnace and removed, the sand retained its shape, size and colour. However, there was a decrease in the compaction strength of the sand physically. This can be attributed to the low clay content in the sand which should have sufficiently bonded the sand grains together and prevent them from separating from each other easily by impacting sufficient strength in the sand grains (ME Mechanical Team, 2016). However, this can also be improved with the addition of a binder to impart sufficient strength in the sand both at low and high temperature (ME Mechanical Team).

4.3 	Evaluation of the Selected Budo-Egba Natural Moulding Sand

The chemical composition and physico-mechanical properties of the natural moulding sand from Budo-Egba community were compared with the AFS standard recommended values as shown in table 4.4. On this basis, the potentials of the Budo-Egba natural moulding sand for foundry application were evaluated. Similarly, the physico-mechanical properties of the sand were tabulated against recommended/standard values from literature in Table 4.4, which reveals the suitability of Budo-Egba moulding sand for various castings of metals, most especially non-ferrous metals.

CHAPTER FIVE

CONCLUSIONS AND RECOMMENDATIONS

5.1	Conclusions

From this research work, the following conclusions were drawn:

1. 	Budo-Egba moulding sand belongs to high-quality silica sand; having SiO2 has its dominance element (91.80%) with other trace elements like Al2O3, CaO, Fe2O3, MgO, ZnO, MnO, K2O and Na2O. The sand chemical compositions determined when compared with the standard recommended properties of natural moulding sands showed that the sand sample characterised does not possess the right properties for sound sand castings in its natural form. This does not, however, make it totally unsuitable for non-ferrous applications but it implies that its reusability has to be closely monitored to ensure timely reconditioning to guard against the production of defective castings.

2. 	The Budo-Egba natural moulding sand has very fine grains and considerably sufficient clay content (10.1%) but only suitable for the casting of non-ferrous metals such as aluminium, brass and bronze in its natural form.

3. 	The sand has considerably low dry strength for the casting of ferrous metals and thus requires the addition of clay or binders but however, it is sufficient for casting object with no intricate shape in its natural form.

5.2	Recommendations

The following recommendations are thereby tendered for further work on this research work:

1.	The sands can be upgraded by increase the percentage of silica content through thorough washing.

2.	In addition, the silica sands should be adequately sieved in a 350cm Endecott sieve before the moulding properties of the sands are determined.

3.	Finally, in-depth study of other moulding property like collapsibility should be conducted so as to fully appreciate the service behaviour of the sand mixtures.

REFERENCES

Ademoh, N. A. and Abdullahi, A.T. (2009). Assessment of foundry properties of steel casting moulds bonded with grade 4 acacia species (gum arabic). International Journal of Physical Sciences, 6, pp 238-241.

Ademoh, N. A. and Ahmed, A. T. (2008). Estimation of the effect of kaolin clay addition on the mechanical properties of foundry moulding sand bonded with grades 3 and 4 Nigerian gum arabic (Acacia species), Middle-East Journal of Scientific Research, 3(3), pp 126–133.

AFS (1963). Foundry handbook, Seventh Edition, American Foundrymen’s Society, Des Plaines, III.

Akintunde, M.A. and S.O. Omole, (2008). Physico-chemical assessment of Ijapo clay deposit as binder for moulding in foundry. The Pacific Journal of Science and Technology, 9(2), pp 572-582.

Akinyele, J. O. and Oyeyemi, K. S. (2014). Strength behaviour of concrete using foundry sand as aggregate, Journal of Natural Science, Engineering and Technology, 13, pp 99-108.

Aribo, S. (2011). Effect of varying corn cob and rice husk ashes on properties of the molding sand. Journal of Minerals & Materials Characterization & Engineering,10(15), pp 1449-1455, ASTM D854 – 14: Standard Test Methods for Specific Gravity of Soil Solids by Water Pycnometer, ASTM International, United States of America.

Aribo, S., Folorunso, D.O., Olaniran, O. and Oladele, I.O. (2009). Optimization the green compression strength and permeability of green sand made from Epe silica sand, International Journal of Science and Technology, 11, pp 101-126.

Asuquo. L.O. and Bobo-jarna S.A. (1991), Foundry Technology, Abic Publishers, Enugu, Nigeria. Pp. 23 - 29.

Atanda, P. O., Olorunniwo, O. E., Alonge, K. and Oluwole, O. O. (2012). Comparison of bentonite and cassava starch on the moulding properties of silica sand. International Journal of Materials and Chemistry, 2(4), pp 132-136.

Ayoola, W. A., Adeosun, S. O., Oyetunji, A. and Oladoye, M.A. (2010). Suitability of Oshogbo sand deposit as moulding sand, Kenya Journal of Mechanical Engineering, Volume 6(1), pp 33-41.

Bala, K. C. and Olabisi, B. A. (2017). Deterioration of moulding sand properties with number of castings. Leonardo Electronic Journal of Practices and Technology, 30, pp 209-220.

Burns, J. R. (2000). Foseco ferrous foundry man’s handbook, Replica Press Ltd., India. Shuaib-Babata USEP: Journal of Research Information in Civil Engineering, Vol.16, No.2.

Deepak, C. (2008). Green sand management—role & application of carbonaceous additives and concept of total carbon in a green sand system, 68th World Foundry Congress, India, pp 127-132.

Desai, B., Mokashi, P., Anand, R. L., Burli, S. B. and Khandal, S. V. (2016). Effect of additives on green sand moulding properties using design of experiments and Taguchi’s quality loss function - An experimental study, IOP Conference Series: Materials Science and Engineering, 149, pp 1-17.

Dhurval, P. Vivek, D., Ela, J., Viral, P., Snikunj, D., and Jay, P. (2015). Study of sand composition on mould properties and selection of Taguchi orthogonal array for design of experiments, International Journal of Current Engineering and Scientific Research, 2(3), pp 31-34.

Donald, R. A. (2010). Essentials of materials science and engineering (6 Edition), Global Engineering, Stamford, United States of America.

Ibitoye, S.A. (2005). Effect of the addition of sodium silicate and bulk density variation on the permeability of potter's clay-bonded moulding sand, Nigerian Society of Engineers Technical Transactions. 40, pp 67-77.

Ihom, A. P., Agunsoye, J., Anbua, E. E. and Ogbodo, J. (2011). Effects of Moisture contents on the foundry properties of Yola natural sand, Leonardo Electronic Journal of Practices and Technologies, 9, pp 85-96.

Jimoh, B. O., Ajibola, O .O. and Borisade, S .G. (2015). Suitability of selected sand mine in Akure, Nigeria for use as foundry sands in aluminium alloy casting, International Journal of Engineering and Technology, 5 (8), pp 485-495.

Loto, C. A. and Omotoso, E. O. (1999). Analysis and development of Igbokoda clay as binder for synthetic moulding sand, Applied Clay Science, 5(1), pp 85 – 97.

Mahesh, B. P., Pratihar, D. K. and Datta, G.L. (2008). Forward and reverse mapping in green sand mould system using neutral networks, Applied Soft Computing, 8(1), pp 239-260.

Mikhailov, A.M. (1989). Metal casting, Mir Publisher, Moscow, Pp. 71 – 90.

Morey, R.E. and Ackerlind, C.D. (1947). “Trans American Foundry Men Association”, Pp. 65 and 288.

Mshelia, Z., Abolarin, M., Abubakre, O. and Ademoh, N. A. (2016). Characterisation of natural moulding sands from selected deposits in Maiduguri- Nigeria for casting applications, Arid Zone Journal of Engineering, Technology and Environment, 12, pp110-121.

Murray, H.H. (1986), “Binders; Industrial Mineral in Encyclopedia of Material Science and Engineering”, Vol. 1, Pp. 305 – 306.

Nigerian Foundries Limited (1995). The fundamentals of greensand technology. Foundry Africa Conference, pp 1-7.

Nwajagwu, GO. and Okafor, I.C.I (1987). “Improving the day characteristic of Kaolonitic clay bonded moulding sand” refractory journal, v 62 n2, Pp. 6 – 12.

Oke, A. O. and Omidiji, B .V. (2016). Investigation of some moulding properties of a Nigerian clay-bonded sand. Achieves of Foundry Engineering, 16(3), pp 71- 76.

Scaffer, E. and James, P. (1995). The science and design of engineering materials, 1st Edition, Longman, London.

Shuaib-Babata, Y. L. and Olumodeji, J. (2014). Analysis of Ilorin sand moulding properties for foundry application. International Journal of Engineering Research and Technology, 3(1), pp 1-8.

Shuaib-Babata, Y. L., Ibrahim, H. K., Ajao, K. S., Ambali, I. O. and Bello, M. O. (2019). Evaluation of the foundry properties of Oyun river (Ilorin) moulding sand, Adeleke University Journal of Engineering and Technology, 2 (1), pp 12-24.

Stefanesai, O.M. (1992). “Casting Metal Handbook”, Metal Park, Ohio.

Steve, H. (1996). Metal Casting: Appropriate technology in the small foundry. Intermediate Technology Publications, London, UK.